Synergistic Bone Regeneration Through Sequential Dual-drug Delivery

Jae Won Jang1,2,†, Hyunji Kim1,2,†, Joon Seok Oh3,†, Dongtak Lee4, Hye-Jung Choi5, Hyunjung Shin6, Chang-Nam Son7, Xian Jin8, Hyo Gi Jung1,2, Yonghwan Kim1,2, Jisung Yoon1,2, Seung-Hyun Kim9, Hak Chang3,*, and Dae Sung Yoon1,2,*

1School of Biomedical Engineering, Korea University, Seoul, 02841, Republic of Korea

2Interdisciplinary Program in Precision Public Health, Korea University, Seoul, 02841, South Korea

3Department of Plastic and Reconstructive Surgery, Seoul National University Hospital, Seoul National University College of Medicine, Seoul 03080, Republic of Korea

4Division of Bioengineering, Incheon National University, Incheon, 22012, Republic of Korea

5Department of Emergency Medical Technology, Gyeongbuk Provincial College, Yecheon, 36830,  Republic of Korea

6Department of Energy Science, Nature Inspired Materials Processing Research Center, Sungkyunkwan University, Suwon, 16419, Republic of Korea

7Department of Rheumatology, Uijeongbu Eulji Medical Center, Eulji University School of Medicine, Uijeongbu, Korea

8Department of Plastic Surgery, The Second Affiliated Hospital of Zhejiang University School of Medicine, Hangzhou, China

9School of Engineering, Brown University, Providence, RI 02912, USA

†These authors contributed equally to this work.

*E-mail addresses: hchang@snu.ac.kr (Hak Chang); dsyoon@korea.ac.kr (Dae Sung Yoon)

Keywords: bone regeneration, sequential drug delivery, bioinspired scaffold, BMP-2, OPG-Fc

Supplementary Material

Figure S1. SEM image of hydroxyapatite (left) and collagen gel scaffold (right).

Figure S2. Compressive stress-strain curve of PBS-rehydrated COHASs (n=3).

Figure S3. (a) The cell viability and (b) ALP activity assay of MC3T3-E1 with various concentrations of BMP-2 and OPG-Fc. Every individual data point represents a set of triplicate measurements.

Figure S4. Incision made down to periosteal level (left). 8 mm-sized cranial defect made by trephination (middle). Insertion of COHAS into the defect site (right).

Table S1. Porosity of COHASs measured from eight samples.

| Diameter (mm) | Height (mm) | Mass (g) | Volume (mm3) | Measured density (g/mm3) | Measured density (g/cm3) | Theoretical density (g/cm3) | Porosity (%) | Average porosity (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 8.44 | 3.14 | 0.022 | 175.67 | 1.25×10-4 | 0.12 | 2.83 | 95.59 | 95.82 |
| 8.8 | 3.82 | 0.024 | 232.34 | 1.02×10-4 | 0.10 | 2.83 | 96.40 |  |
| 8.73 | 3.7 | 0.027 | 221.47 | 1.22×10-4 | 0.12 | 2.83 | 95.69 |  |
| 8.13 | 3.13 | 0.020 | 162.49 | 1.23×10-4 | 0.12 | 2.83 | 95.65 |  |
| 8.25 | 2.9 | 0.015 | 155.02 | 9.68×10-4 | 0.10 | 2.83 | 96.58 |  |
| 8.07 | 3 | 0.018 | 153.45 | 1.17×10-4 | 0.12 | 2.83 | 95.85 |  |
| 8.23 | 2.9 | 0.022 | 154.27 | 1.43×10-4 | 0.14 | 2.83 | 94.96 |  |
| 8.31 | 1.95 | 0.014 | 105.76 | 1.32×10-4 | 0.13 | 2.83 | 95.32 |  |

Table S2. Bone area and volume estimate from micro CT analysis.

| Time | Week 2 | Week 4 | Week 8 |
| --- | --- | --- | --- |
| Group |  |  |  |
| Area |  |  |  |
| COHAS | 91.71±35.60 | 267.54±109.41 | 355.74±140.30 |
| COHAS_B | 94.85±8.78 | 255.69±30.47 | 464.96±99.73 |
| COHAS_O | 120.26±43.60 | 203.57±42.55 | 329.76±90.75 |
| COHAS_B_O | 108.69±16.42 | 218.67±33.82 | 331.59±101.38 |
| COHAS_P@B_O | 100.52±9.38 | 250.45±13.35 | 433.74±16.28 |
| COHAS_B_P@O | 225.39±35.87 | 318.80±18.12 | 547.85±62.20 |
| Volume |  |  |  |
| COHAS | 11.92±6.52 | 20.75±7.76 | 28.68±10.09 |
| COHAS_B | 13.66±1.26 | 23.01±2.74 | 44.13±11.74 |
| COHAS_O | 13.99±2.27 | 21.65±4.57 | 33.01±2.49 |
| COHAS_B_O | 15.65±2.37 | 19.68±3.04 | 29.84±9.12 |
| COHAS_P@B_O | 15.99±3.02 | 26.21±7.35 | 42.70±5.49 |
| COHAS_B_P@O | 21.34±2.18 | 30.36±1.35 | 52.17±4.13 |

Table S3. Bone regeneration area from micro CT analysis with reference to COHAS group

|  | Estimate | 95% Confidence Interval | p-value1) | p-value2) |
| --- | --- | --- | --- | --- |
| COHAS | Reference |  |  | 0.0262 |
| COHAS_B | 33.501 | (-52.1,119.103) | 0.4105 |  |
| COHAS_O | -20.47 | (-106.072,65.132) | 0.6118 |  |
| COHAS_B_O | -18.681 | (-104.283,66.92) | 0.643 |  |
| COHAS_P@B_O | 23.239 | (-62.363,108.84) | 0.5652 |  |
| COHAS_B_P@O | 125.68 | (40.08,211.283) | 0.0076 |  |
| Week 2 | Reference |  |  | <0.0001 |
| Week 4 | 128.88 | (90.659,167.101) | <0.0001 |  |
| Week 8 | 287.04 | (248.816,325.257) | <0.0001 |  |

- P-value whether each group has a statistically different area compared to reference

- P- value whether the difference in bone area is statistically significant

Table S4. Bone regeneration volume from micro CT analysis with reference to COHAS group

|  | Estimate | 95% Confidence Interval | p-value1) | p-value2) |
| --- | --- | --- | --- | --- |
| COHAS | Reference |  |  | 0.0170 |
| COHAS_B | 6.483 | (-1.297,14.263) | 0.0945 |  |
| COHAS_O | 2.434 | (-5.346,10.214) | 0.5083 |  |
| COHAS_B_O | 1.276 | (-6.504,9.056) | 0.7271 |  |
| COHAS_P@B_O | 7.85 | (0.07,15.63) | 0.0483 |  |
| COHAS_B_P@O | 14.176 | (6.396,21.956) | 0.0019 |  |
| Week 2 | Reference |  |  | <0.0001 |
| Week 4 | 8.187 | (4.572,11.802) | <0.0001 |  |
| Week 8 | 23.001 | (19.385,26.616) | <0.0001 |  |

- P-value whether each group has a statistically different volume compared to reference

- P- value whether the difference in bone volume is statistically significant

Table S5. At the 8-week time point, a mixed model analysis including the group-time interaction term was conducted to examine bone regeneration area

|  | Estimate | p-value1) |
| --- | --- | --- |
| COHAS vs COHAS_B_P@O | -192.11 | 0.0012 |
| COHAS_B_O vs COHAS_B_P@O | -216.26 | 0.0004 |

Table S6. At the 8-week time point, a mixed model analysis including the group-time interaction term was conducted to examine bone regeneration volume

|  | Estimate | p-value1) |
| --- | --- | --- |
| COHAS vs COHAS_B_P@O | -23.49 | <0.0001 |
| COHAS_B_O vs COHAS_B_P@O | -22.33 | <0.0001 |