Graphical Abstract Summary:

This study demonstrates the synthesis of sodium silicate from Malaysian rice husk ash (RHA), employed directly as an untreated biochar-type residue, under controlled hydrothermal conditions for use in alkali-activated slag mortars. Using NaOH solutions of 10 M, 12 M, and 14 M at moderate temperatures (40–100 °C), sodium silicate was successfully produced and applied as a single-step activator for ground granulated blast furnace slag. The resulting mortars were benchmarked against OPC and commercial sodium silicate systems and comprehensively evaluated for mechanical and durability performance. Mortars synthesised at 12 M and 14 M under 40–80 °C achieved superior compressive strength (up to 76.8 MPa), reduced porosity, lower water absorption, and enhanced microstructural integrity. These findings highlight the dual significance of RHA as both a silica-rich precursor and a biochar-type material, reinforcing its role in waste-to-resource strategies and validating RHA-derived activators as a technically feasible, low-carbon alternative for sustainable construction.

Table of Contents

1.0	Introduction	4

2.0	Materials and Methodology	7

2.1	Materials	7

2.2	Methodology	9

2.2.1	Rha-Synthesised Na2SiO3	9

Method for Development of Mixes	10

2.2.2	Nomenclature	10

2.2.3 Mix Design	10

2.2.4 Mixing  Procedures	11

2.2.5	Casting, Compaction, Demoulding and Curing of Specimens	12

3.0 Testing Procedures	12

3.1 Compressive and flexural Strength Test	13

3.2 Water Absorption Test	13

3.3 Porosity	14

3.4 Air Permeability	14

3.5 Ultrasonic Pulse Velocity (UPV)	14

3.6 Testing Methods Summary	15

4.0 Results and Discussion	15

4.1 Ultrasonic Pulse Velocity	16

4.2 Mechanical Properties	17

4.2.1 Compressive Strength	17

4.2.2 Flexural Strength	19

4.3 Transport Mechanism	20

4.3.1 Porosity	20

4.3.2 Water Absorption	22

4.3.3 Air Permeability	23

4.4	Characterisation of Na2SiO3-SiO2/Na2O ratio	25

4.4.1 Effect of Synthesis Conditions on Oxide Content	26

4.4.2 Correlation Between SiO₂ Content and Compressive Strength	27

4.4.3 Optimal Na₂O/SiO₂ Ratio for Mechanical Properties	29

4.5 Statistical Analysis (ANOVA)	30

4.5.1 Effect of Synthesis Temperature on the Compressive Strength of Mortar	30

4.5.2 Effect of NaOH Concentration on the Compressive Strength of Mortar	31

4.5.3 Effect of Synthesis Temperature on the Flexural Strength of Mortar	33

4.5.4 Effect of NaOH Concentration on the Flexural Strength of Mortar	35

5.0 Conclusion	36