Supplementary Information

Femtosecond signatures of optically induced magnons before ultrafast demagnetization

Reza Rouzegar1, Oliver Franke1, Gal Lemut1, Oliver Gueckstock1, Junwei Tong1, Dieter Engel2, Xianmin Zhang3, Georg Woltersdorf4, Piet W. Brouwer1, Tobias Kampfrath1, Quentin Remy1

1Department of Physics, Freie Universität Berlin, 14195 Berlin, Germany
2Max-Born-Institut für nichtlineare Optik und Kurzzeitspektroskopie, 12489 Berlin, Germany
3Key Laboratory for Anisotropy and Texture of Materials (Ministry of Education), School of Material Science and Engineering, Northeastern University, Shenyang 110819, China
4Institut für Physik, Martin-Luther-Universität Halle, 06120 Halle, Germany

# S1 All the fits

Figure S1: Comparison of the Stoner model (bi-exponential) and electron-magnon model (tri-exponential) fit for Co. The blue line shows the experimental data. (a) and (b) show the electron-magnon model fit while (c) and (d) show the Stoner model fit. (b) and (d) show the same results as (a) and (c) respectively but for a shorter time range.

Figure S2: Comparison of the Stoner model (bi-exponential) and electron-magnon model (tri-exponential) fit for Fe. The blue line shows the experimental data. (a) and (b) show the electron-magnon model fit while (c) and (d) show the Stoner model fit. (b) and (d) show the same results as (a) and (c) respectively but for a shorter time range.

Figure S3: Comparison of the Stoner model (bi-exponential) and electron-magnon model (tri-exponential) fit for CoFe. The blue line shows the experimental data. (a) and (b) show the electron-magnon model fit while (c) and (d) show the Stoner model fit. (b) and (d) show the same results as (a) and (c) respectively but for a shorter time range.

Figure S4: Comparison of the Stoner model (bi-exponential) and electron-magnon model (tri-exponential) fit for CoFeB. The blue line shows the experimental data. (a) and (b) show the electron-magnon model fit while (c) and (d) show the Stoner model fit. (b) and (d) show the same results as (a) and (c) respectively but for a shorter time range.

Figure S5: Comparison of the Stoner model (bi-exponential) and electron-magnon model (tri-exponential) fit for NiFe. The blue line shows the experimental data. (a) and (b) show the electron-magnon model fit while (c) and (d) show the Stoner model fit. (b) and (d) show the same results as (a) and (c) respectively but for a shorter time range.

Figure S6: Comparison of the Stoner model (bi-exponential) and electron-magnon model (tri-exponential) fit for Py. The blue line shows the experimental data. (a) and (b) show the electron-magnon model fit while (c) and (d) show the Stoner model fit. (b) and (d) show the same results as (a) and (c) respectively but for a shorter time range.

# S2 Model solution

The reason why, as we noted several times in the Methods section, the variation of parameters does not impact much the extracted dynamical parameters is because the Ξ matrix essentially serves to change the relative influence of the different interactions between the subsystems. We discuss this in details below, together with other important features of the model. We postpone the discussion of all interactions and alternative mechanisms to the next section and focus our attention here only on em, ml, sl and el scattering. The general solution of our model involves the inversion and diagonalization of 6×6 matrices and therefore does not provide a helpful intuitive picture of the dynamics, despite its simplicity compared to fully microscopic models. Therefore, we derive an approximate solution based on the concept of partial equilibrium: for each interaction, the system is said to be in partial equilibrium with respect to that interaction if the time elapsed after some perturbation is much larger than the interaction characteristic time. The partial equilibrium is characterized by the interaction specific equilibrium conditions specified in the Methods section. In our materials, the system is actually never in a state of partial equilibrium with any interaction unless a complete equilibrium is reached, since all the important characteristic times to describe the dynamics are fairly close to each other. The analytical formulae that we present below can therefore only provide an estimate of the order of magnitude of each term in the solution.

Before we derive these formulae, we briefly discuss the general form of this solution. To obtain it numerically, one needs first to diagonalize the total scattering matrix α​Γα in equation (11). In the basis that diagonalizes this matrix, the solutions are single exponentials with inverse characteristic times 1/τi given by its eigenvalues. Going back to the original basis, it is found that every thermodynamic variable ξ is a linear combination of such exponentials:

ξt= iAie-tτi,  t>0#S1

Where Ai are some constants given by the matrix elements of Ξ only. This equation is valid after the laser pulse arrives at t=0. At this instant, the electronic temperature rises instantaneously (before convolution by our time resolution function). Because we explicitly keep track of energy and particle number (while the lattice is assumed to be a perfect spin sink where angular momentum can be lost), the corresponding conservation laws always lead to two zero eigenvalues i.e. infinite characteristic times. Thus, the solution is characterized by 4 characteristic times and the 4 corresponding amplitudes. Additionally, the (spin averaged) conduction electrons chemical potential (in general) and temperatures contain a non-zero offset corresponding to the infinite characteristic times. Physically, this corresponds to the fact that a finite amount of energy is permanently (in this model) deposited in the system. The offset is absent for the spin voltage and magnon chemical potential because of the (complete) equilibrium conditions pertaining to these quantities.

First, we assume the system is at some time t such that τem≪t≪τml or τsl implying that it is in partial equilibrium with respect to the em interaction. Since the other interactions do not influence the dynamics at this timescale, the corresponding eigenvalue 1/τ0 of the α​Γα matrix will be 1/τ0≈1/τem. Because em scattering corresponds to a transfer of both energy and angular momentum, it turns out that the corresponding eigenvalue is doubly degenerate. The presence of the other interactions (in the main text, ml and el scattering) lifts this degeneracy. For iron, denoting the other eigenvalue 1/τ0', we find from the exact solution τ0= 9.6 fs and τ0'= 9.4 fs while τem= 9.6 fs. Thus, the partial equilibrium assumption leads to a very good estimate of the initial -∂tM dynamics. Because both eigenvalues are almost degenerate, it is not possible to distinguish them experimentally. From the conservation laws and equilibrium conditions of em scattering, one can easily derive the amplitude of the generated spin voltage and magnon chemical potential, in the absence of other interactions:

μe,speq=-μmpeq=-Ξ45Ξ22-Ξ21Ξ12Ξ11-Ξ44×SΞ33+Ξ55+Ξ54Ξ45Ξ22-Ξ21Ξ12Ξ11-Ξ44. #S2

Here, the superscript ‘peq’ indicates that this value is only true for partial equilibrium (of em scattering) and Ξij denotes the matrix elements of Ξ. This equation can be understood by noting that a diagonal element of Ξ corresponds to a heat capacity c (ΔE=cΔT) or a (spin) susceptibility χ (ΔM=χΔμ), while the off-diagonal elements correspond to conversion elements. For instance, Ξ45 converts a change of magnon temperature into angular momentum. The second factor in equation (S2) describes the total temperature increase of the system in partial equilibrium after it has absorbed the energy density S. The denominator of this term is the relevant heat capacity (i.e. how energy is converted into temperature) containing the heat capacities of the conduction electrons and the magnons plus a third term. The third term describes a process where an increase in temperature is first converted into angular momentum (Ξ45), this angular momentum giving rise to a certain change of spin voltage (or magnon chemical potential) through a corresponding total spin susceptibility Ξ22-Ξ21Ξ12/Ξ11-Ξ44 before being finally converted back into energy (Ξ54). The temperature rise of the second factor is then converted into angular momentum due to the numerator of the first factor (Ξ45) and finally into spin voltage and magnon chemical potential via the total spin susceptibility. The latter consists in the conduction electron (Ξ22) and magnon (Ξ44) spin susceptibilities together with -Ξ21Ξ12/Ξ11 which describes an additional (not negligible) contribution to the conduction electron spin susceptibility due to a change of (spin averaged) chemical potential. In simpler terms, Ξ22 is the spin susceptibility at constant chemical potential while Ξ22-Ξ21Ξ12/Ξ11 is the spin susceptibility at constant number of electrons. For iron (parameters of Extended data Table 1) and an absorbed fluence of 0.03 mJ/cm2 corresponding to our experiments, we find μe,speq= 1.5 meV while the exact calculation leads to a maximum amplitude μe,smax= 1.12 meV i.e. a 25% difference. Equation (S2) still gives a good estimate for the amplitude of the spin voltage provided that em scattering is the fastest scattering mechanism. In this case, the estimated amplitude mostly depends on Ξ44=-Dm0 because it is the largest term of the first denominator while the second denominator is dominated by the electron heat capacity which is a rather well-known quantity, up to some factor of order unity. Ξ45=-Dm1/(kBT0) is not so sensitive on the details of the magnon DOS (see below) and is therefore not expected to determine the amplitude of the spin voltage, also up to some factor of order unity. Ξ44, on the other hand, depends on the magnon gap which is not well-known for our samples. Measurements of the magnon gap for our samples, via for instance all optical ferromagnetic resonance measurements1, is beyond the scope of this paper and will be the topic of future works. Most likely2, the gap is well below 1 meV which will strongly suppress the amplitude of the spin voltage. For a magnon gap of around 40 µeV,3 Ξ44 is around 20 times larger than what is given in Extended data Table 1 and the spin voltage is reduced accordingly with μe,smax= 58 µeV. We note that with our numerical parameters to compute the magnon DOS, including such a small gap has a negligible influence on the calculated values of all Dmn. If the amplitude of the spin voltage matters, one should thus use equation (38) for Dm0 while the other ones always have to be computed numerically.

In a second time, we assume τem≪t ~ τsl or τml≪τep. If the spin dissipation in the lattice happens only through the spin stored in conduction electrons (i.e. sl scattering), we can estimate the spin dissipation time via the following reasoning. Because τem≪t, μe,s(t)=-μm(t). Let us assume that for an infinitesimally short amount of time dt, em scattering is turned off. Then, we get μe,st+dt=μe,st×(1-dt/τsl) and δμet+dt= -Ξ12/Ξ11×μe,st×(1-dt/τsl). Then we turn em scattering back on and let the system reach partial equilibrium instantaneously with respect to em scattering. We now find that

μe,st+dt=μe,st1-dtτslΞ22-Ξ21Ξ12Ξ11Ξ22-Ξ21Ξ12Ξ11-Ξ44-Ξ45Ξ54Ξ33+Ξ55= μe,st1-dtτ1'. #S3

The second equality serves to define 1/τ1' which is an estimate for the next largest eigenvalue 1/τ1 (in the absence of electron-lattice scattering) of Ξ. We also define α≡τsl/τ1'. Because Ξ44 is dominating the denominator of α for all the studied materials, α≪1 and the effect of spin flip scattering in the conduction electrons is very small at the subpicosecond timescale. Physically, the spin susceptibility of the magnons is very large, thus em scattering always forces the spin voltage to remain close to the magnon chemical potential. In other words, the conduction electrons prefer to satisfy the partial equilibrium condition of em scattering μe,s=-μm rather than the one of spin flip scattering for conduction electrons μe,s=0. For iron, α= 5.8 10-3. We thus always neglect this type of spin dissipation.

If instead the spin dissipation happens only through ml scattering, a similar reasoning leads to

μmt+dt=μmt1+dtτmlΞ44-Ξ45Ξ54Ξ55Ξ22-Ξ21Ξ12Ξ11-Ξ44+Ξ45Ξ54Ξ33+Ξ55= μmt1-dtτ1''. #S4

The second equality serves to define 1/τ1'' which is the new estimate for the next largest eigenvalue 1/τ1 of Ξ. We also define β≡τml/τ1''. The sign difference in the denominator of β compared to α comes from the convention for the sign of the magnon chemical potential. The absence of Ξ33 in the numerator of β comes from conservation of energy during ml scattering. In this case, the numerator of β contains Ξ44 and thus β ~1 for all materials. For example, for iron, β= 0.97 leading to τ1''= 55.6 fs which is almost identical to the exact value 55.7 fs. The terms in both α and β can be understood in a similar way as what was done for equation (S2). A similar analysis can be done for the other amplitudes and characteristic times in equation (S1) but we do not need it here.

The previous calculations show that as long as Ξ44 is the dominant term of

χtot=Ξ22-Ξ21Ξ12Ξ11-Ξ44-Ξ45Ξ54Ξ33+Ξ55 #S5

Changes in the values of the Ξ matrix will not change the extracted values of τem and τml when the fit is performed, but it will change the amplitude of the spin voltage. Note that the relevant “total” spin susceptibility depends on the initial conditions and relaxation mechanisms considered.

Below, we state a few other important points about our model.

- Rise time of -∂tM and example of a full solution

In Extended data Fig. 5a and b, we show the full solution of our model for Fe. It is more instructive however to look directly at the numerical values of Ai and τi. These values are shown in Table S1. Because τ0 and τ0' are almost equal, we indeed see that the dynamics of the ferromagnet happens in three temporally distinct steps (Fig. 2). Since -∂tM∝μm∝μe,s (see below), we see that this model gives a finite rise time of -∂tM. We also note that a significant part of the conduction electron temperature dynamics is governed by em scattering (τ0') on top of the well-known effect of electron-lattice scattering (~ τ2). The former effect has already been discussed in previous works4–6. In particular, this bi-exponential decay of the electron temperature seems to be observable in Figure 3 of the work of Tengdin et al.4. Finally, we also see, as one would expect, that the amplitudes for the lattice temperature dynamics are only sizeable for τ2.

- Proportionality between μe,s, μm and -∂tM

In Extended data Fig. 5c, we show that μe,s, μm and -∂tM are indeed approximately proportional in our model, as demonstrated experimentally by the equality between the signals in F/Pt and F samples (see Methods). -∂tM is directly obtained from the sum of the second and fourth line of the matrix product Ξ(α​Γα)ξ, see Methods. This proportionality comes from the fact that the spin dissipation, which gives rise to -∂tM is directly proportional to μm by definition of ml scattering, and μe,s is almost proportional to μm due to the strong em scattering. The difference between these two quantities comes exactly from the fact that we neglected spin flip scattering of the conduction electrons. Even though the influence of the latter scattering mechanism on the magnetization dynamics is very small (see below), including it (with a similar scattering time as for ml scattering) exactly accounts for the tiny difference observable in Extended data Fig. 5c.

- The case of no magnon dispersion

The magnon dispersion relation comes from the transverse part of the Heisenberg Hamiltonian7. In the mean field approximation, the latter is neglected and every spin excitation has the same energy. We discuss this case in detail in section S4 and show that the only difference compared to our model, in the linear regime, is a different magnon DOS and thus different values of Dmn. For iron, calculating Dmn in the case of no dispersion, we obtain α= 0.34 and β= -1.2 10-2. This drastic change in the magnon DOS mostly affects Dm0 as Dm1 is reduced by 40% while Dm0 is reduced by 99.3% i.e. more than two orders of magnitude. Thus, ml scattering is inefficient in this case as conduction electrons then prefer the partial equilibrium with respect to spin flip scattering of conduction electrons. Taking the same value of τsl as for ml scattering in iron (54.2 fs), we find τ1'= 160 fs. The exact value is τ1= 74 fs. This shows (i) that the validity of equations (S3) and (S4) depends on Ξ and (ii) there can be a lot of mixing between the eigenvalues of α​Γα i.e. the characteristic times τi are not necessarily equal to the scattering times for each interaction.

- Mixing of the eigenvalues

The latter fact is obvious since there can be many interactions existing in the system while only four characteristic times can be non-zero. This mixing depends both on Ξ, as we just showed through an example, but also on the values of the scattering times of each interaction. In Extended data Fig. 5d, we show this effect when the value of the em scattering time is varied. As τem increases, an anticrossing like behavior is observed. In particular, for sufficiently large τem, the smallest eigenvalue is almost equal to τml. For the values of τem in our samples, we find that this mixing is rather small for τ0 and τ1. It becomes much larger however for τ2 (see Table S2) and in general, much more complex mixing curves exist as a function of the other scattering times or at higher values of those scattering times.

|  | 0' | 0 | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- | --- | --- |
| τi(fs) | 9.4 | 9.6 | 55.7 | 380.9 | ∞ | ∞ |
| μ | 1 | -1.20 | 0.23 | -0.025 | 0 | 0 |
| μs | 1 | -1.20 | 0.23 | -0.025 | 0 | 0 |
| Ts | 1 | 0.0087 | 0.035 | 0.88 | 0.11 | 0 |
| μm | 1 | -0.043 | -1.08 | 0.12 | 0 | 0 |
| Tm | -1.14 | -0.0071 | 0.028 | 1 | 0.11 | 0 |
| Tl | -0.024 | -2 10-4 | -0.0052 | -0.97 | 1 | 0 |
| Table S1: Characteristic times and amplitudes in front of each corresponding exponential, for each thermodynamic quantity. These amplitudes have been normalized such that, for each thermodynamic quantity, the largest amplitude is one. |  |  |  |  |  |  |

| FM | τ0 (fs) | τ1 (fs) | τ2 (fs) | τem (fs) | τml (fs) | τel (fs) |
| --- | --- | --- | --- | --- | --- | --- |
| Co | 4.5 | 62.7 | 354.8 | 4.5 | 60.2 | 300 |
| CoFe | 6.3 | 71.0 | 346.8 | 6.3 | 66.2 | 300 |
| CoFeB | 7.4 | 66.4 | 347.0 | 7.4 | 61.8 | 300 |
| Fe | 9.4 | 55.7 | 380.9 | 9.6 | 54.2 | 200 |
| NiFe | 17.1 | 102.3 | 438.2 | 17.5 | 98.9 | 300 |
| Py | 13.9 | 179.6 | 438.3 | 14.1 | 175.0 | 300 |
| Table S2 Characteristic times τ0, τ1, τ2 and the extracted scattering times τem, τml and τel for each material. |  |  |  |  |  |  |

# S3 Alternate mechanisms

In this section, we discuss the effect of other interactions and additional effects that can influence the dynamics of the system. Overall, even though all these effects are most likely present in our systems, we find that they are not sufficient to explain our results on their own and their effect on the (normalized!) spin voltage and magnetization dynamics is small. In particular, only em scattering can explain the rise time of the spin voltage. This can be intuitively understood from the fact that magnons hold most of the angular momentum, and therefore a progressive increase of electronic angular momentum must come from the magnon subsystem.

- Spin flip scattering of conduction electrons

Although we have already partially discussed this interaction in the precedent section, we still need to discuss one last scenario with this interaction. When τsl is shorter than τem, the spin voltage rise time τ0 is mostly determined by τsl, just like τ0' is dominated by τml when the latter is much shorter than τem (Extended data Fig. 5d). In order to fit the data however, one needs in this case to also consider ml scattering because of an effect similar to was discussed in the context of equation (S3), i.e. em and sl scattering alone are insufficient to describe spin dissipation in the lattice.

However, with this assumption of a short τsl, we find that μe,s and -∂tM  are no longer proportional, contrary to what our experiments show (see Extended data Fig. 2). This lack of proportionality is because the dynamics of μe,s, now mostly governed by spin flip scattering, is much faster than the dynamics of μm governed by e-m scattering and ml scattering. This scenario can thus be discarded.

- Spin conserving electron-magnon scattering

From a microscopic point of view, spin conserving em scattering is a second order effect where an electron and a magnon interact to exchange energy (the electron absorbs the magnon before emitting another one with a different energy) while the em scattering we talked about so far is usually seen as a first order process (an electron absorbing or emitting a magnon)8, see however section S6 below. If we include this interaction, following the Methods, its main effect is to change τ0'. In the case of iron, if we assume that the spin conserving em scattering time is equal to τem, we get τ0'= 4.7 fs. The second effect is to change the relative weight for the exponentials with characteristic times τ0 and τ0'. Typically, the spin voltage is now mostly determined by τ0 while the electron and magnon temperatures, as well as the magnon chemical potential, are given by τ0'. This means that the proportionality relationship between μe,s and -∂tM is less verified than without this extra interaction. We note however that the spin conserving em scattering time τem is not in general a simple function of τem, and corresponds to a second order effect8. It is therefore likely that τem>τem by a factor of order unity or more, in which case the proportionality between μe,s and -∂tM is verified.

- Magnon-phonon scattering

We can also consider magnon-phonon scattering (which we defined in the Methods as a scattering process that exchanges energy between magnons and the lattice, contrary to magnon-lattice scattering which exchanges angular momentum). This scattering is theoretically predicted to have a negligible impact on the magnetization dynamics below 1 ps and the corresponding scattering times are estimated to reach up to 100 ps or more6,9–11. First, we note that this interaction cannot lead to a rise time of the spin voltage since it does not transfer anything to the electrons. Second, assuming a rather short magnon-phonon scattering time of 1 ps, we find that its main effect is to reduce τ2 from 380.9 fs to 319.1 fs. Thus, we can safely neglect this interaction altogether.

- The slope of the electronic DOS

The slope of the DOS leads to non-zero values of Ξ13, Ξ23, Ξ31 and Ξ32. By definition of these matrix elements, we see that they allow a mixing between energy (temperature) and angular momentum (chemical potential). In particular, an increase in temperature (due to the laser pulse) will generate a finite spin voltage. This effect, combined with electron-lattice and spin-flip scattering of the conduction electrons, allows us to recover the Stoner model as derived in our previous work12. The spin voltage and -∂tM in this case rise instantaneously.

With em, el and ml scattering as the only interactions, the effect of the slope of the electronic DOS on the characteristic times is negligible. For iron, the same characteristic times are obtained up to the precision given in Table 1. The slope of the DOS will however change the values of the amplitudes in Table S1 by around 10% for iron. This does not impact the proportionality between μe,s and -∂tM (up to an unmeasurable time shift less than 10 fs).

- Spin heat accumulation

The slope of the electronic DOS can actually lead to a rise time τ0≠0 even in the absence of em scattering if the laser pulse generates spin heat accumulation in the system i.e., if the temperatures T↑ and T↓ for both spin species of the conduction electrons are different after optical excitation. This can happen because each spin species can absorb a different amount of energy and because for a given amount of energy, a different temperature is obtained due to different heat capacities. Both effects are a consequence of the spin dependent DOS.

In this case, one then needs to include electron-electron (e-e) scattering to allow both temperatures to become equal in partial equilibrium. Following the procedure of the Methods, with now two electronic temperatures T↑ and T↓ and two electronic energies E↑ and E↓, one can show that for each thermodynamic quantity pertaining to the electrons, there will be, in the rate equations, an extra term of the form η(T↑-T↓)/τee with τee the e-e scattering time. In particular, the coefficient η is non-zero for the chemical potentials only if the DOS has a non-zero slope, and is different for different thermodynamic quantities. Because η is different for μ↑ and μ↓, this will lead to a gradual increase of the spin voltage (in absolute value) with a characteristic time τee. Because τee may be estimated to be similar to the Drude scattering time13,14, which are comparable with our experimental values for τ0, this mechanism could a priori explain the observed dynamics of the spin voltage.

We can however discard this effect for two reasons: (i) this effect is neither accompanied with a change in the total angular momentum in the system nor a change in the magnon reservoir, thus μe,s and -∂tM would no longer be proportional anymore (ii) the sign of η depends on the sign of the slope of the electronic DOS which is different for different materials, and so the sign of the measured spin voltage should change for different materials, which we do not observe.

# S4 Results from the s-d model of Beens et al.19

The main equation of the s-d model in the mean field approximation as derived by Beens et al.19 is an equation giving the change of the reduced magnetization md (i.e. normalized to its value at zero Kelvin) of “d” electrons as a function of the spin voltage and the electronic (“s” electrons) temperature. We write it as follows (for a spin ½ associated with each localized “d” electron):

dmddt= πj22ℏD↑D↓Δd-Δμs1-mdcothΔd-Δμs2kBTs, #S9

where j is the s-d coupling constant of the model, Dσ is the electronic DOS per atom for the spin species σ, and Δd is the spin splitting of the “d” electrons. When Δd is dominated by the d-d exchange interaction, the mean field approximation leads to Δd=2mdkBTC with TC the material Curie temperature. Consistently with our model, the relevant characteristic time, which we call τsd, obtained from this equation is the one such that this equation can be written in the linear regime as

dmddt= -md-mdτsd. #S10

Linearizing equation (S9) such that md=tanh(Δd-Δμs/(2kBTs))20, we obtain, consistently with the definition of Beens et al.19

1τsd= πj22ℏmd0D↑D↓Δd0. #S11

Where the 0 superscript indicates that the value of the respective quantity must be taken as the equilibrium room temperature value. This leads to19 τsd-1 = πj2D↑D↓kBTC/ℏ. This is indeed independent of room temperature and scales with the inverse of the Curie temperature, consistently with our measurements shown in Fig. 4. Experimentally, we observe a small change of the characteristic time for em scattering as a function of temperature, of around 1 fs. Such a small temperature variation is also a feature of this model if one considers that the electronic DOS is not constant at the Fermi level but has a non-zero slope. Repeating the calculations of Beens et al.19 to consider such possibility modifies the first bracket of equation (S9) and leads to

1τsd= πj22ℏmd0D↑D↓+D↑'D↓'π2kB2T023Δd0+ D↑'D↓-D↑D↓'2Δd02-D↑'D↓'6Δd03 #S12

where Dσ' is the slope of the electronic DOS per atom for the spin species σ. Note that τsd now depends on temperature explicitly as well as implicitly through md0 which does not cancel out anymore. If the exchange splitting contains a contribution due to s-d exchange, one should use Δd0=Jmd0-js0 where J is the d-d exchange and s0 is the equilibrium spin density of the “s” electrons. To estimate the order of magnitude of this effect, we choose J=0.19 eV (which leads to a Curie temperature of 1100 K for CoFeB), s0= -0.014 (estimated from our ab initio calculation) and j=1.1 eV (which leads to τsd ≈6 fs similar to the em scattering time of our experiments for CoFeB). We find that across the range from 100 to 400 K, τsd varies by around 0.2 fs. Although this model is very simplistic (it fails to quantitatively predict the temperature dependence of magnetization), it can qualitatively explain the weak temperature dependence of the em characteristic scattering time.

Finally, we briefly discuss how this model compares to our model with magnons. In the mean field approximation s-d model (for d electrons with spin ½), the spin excitations of the “d” electrons correspond to promoting an electron with spin (say) up to the energy level with spin down. Because the effect of the transverse part of the Heisenberg Hamiltonian is neglected in this approximation, all the spin excitations have the same energy. Thus, in the mean field approximation, the spin excitations may be seen as Einstein/optical magnons i.e. magnons with a flat dispersion relation. The similarity can also be seen more mathematically by defining the number of “magnons” as the number density n↓ of spins excited to the spin down energy level. The identity Sz=12-n↓ (with md= -Sz/S=n↓-n↑, S=1/2 and n↑+n↓=1) is similar to one of the defining equations of the Holstein-Primakoff approximation Sqz=S-ηq with ηq the magnon number operator in wavevector space and the dynamics equation for n↓ obtained from equation (S9) is

dn↓dt= πj22ℏD↑D↓Δd-Δμs1expβΔd-Δμs-1-n↓1-2n↓,#S13

with β=1/(kBTs), which becomes

dn↓dt= πj22ℏD↑D↓Δd-Δμs1expβΔd-Δμs-1-n↓,#S14

at low temperature where n↓ is small and where the Holstein-Primakoff approximation is valid. This equation is essentially the dynamic equation for a single magnon mode with energy Δd and scattering rate πj2D↑D↓/2 as defined by Tveten et al.21. Thus, in our model, we can recover the low temperature mean field approximation s-d model in the linear regime by using for the magnon dispersion relation a constant given by Δd.

This analogy can be highlighted even further by noting that one can define for those spin excitations a chemical potential from μd=∂F/∂n↓T, with F=U-TS is the free energy, U being the internal energy and S the entropy. From the mean field Hamiltonian, one gets ∂U/∂n↓T=Δd, when the double counting of terms is properly corrected. Overall:

μd=Δd+kBT lnn↓n↑, #S15

Which gives the right equilibrium condition μd=0 ⇔n↓/n↑ =exp(-Δd/(kBT)). Out of equilibrium, this chemical potential is not zero but directly given by the other thermodynamic quantities describing the system.

# S5 Electron-magnon scattering in the model of Manchon et al.22

The model of Manchon et al.22 is another microscopic model of UDM, valid for all temperatures and going beyond the mean-field and Holstein-Primakoff approximations, but only accounting for energy transfers between electrons, magnons and the lattice. Nevertheless, we can use it to estimate the temperature and Curie temperature dependence of em scattering times. Linearizing equation (28) of Ref. 22 for small temperature changes, we get

1τem∝mT2TC, #S16

Where m(T) is the total magnetization of the ferromagnet as a function of room temperature and the proportionality factor is temperature independent. Thus, in this model also, the em scattering time also scales with the inverse of the Curie temperature. It gives however a temperature dependence of the scattering time. For our temperature range and a typical magnetization curve23, the magnetization varies by around 10 % which leads to a variation of the em scattering time of around 1 fs consistent with our measurements.

# S6 Additivity of electron and magnon energies

An important assumption in the phenomenological theory is the additivity of electron and magnon energies. At first sight, this additivity seems to be at odds with the presence of a large exchange interaction Jsd between conduction electrons and magnons/local magnetic moments. It is a natural consequence, however, of the “fluctuating-local-band theory” of itinerant ferromagnetism of Korenman, Murray, and Prange24, which considers the itinerant majority and minority bands with respect to the local magnetization direction mr, instead of the global equilibrium magnetization direction meq. Below, we briefly recall the essence of the arguments of Ref. 24.

We consider a simple model Hamiltonian describing free electrons coupled to a classical magnetic moment mr with mr=1. The first-quantized Hamiltonian for the electrons, which also includes the coupling to the magnetic subsystem, is

H=-ℏ22m∇2-Jsdσ⋅mr#S17

with the spin of the free electrons σ. If the exchange Jsd is small, spin flip scattering can be treated as a change in the occupation number of electrons or magnons, where the probability of a scattering event is given by Fermi’s golden rule (see Refs. 8,25 for a recent application in the context of electron-magnon scattering). However, if Jsd is large and if the magnetization varies sufficiently slowly in space, we expect the s electron spins to locally follow the spatial magnetization profile mr. Both conditions are met in typical itinerant ferromagnets at temperatures well below the Curie temperature26. The spin-flip scattering of electron spins to the magnetic moments is then not determined by Jsd but by the wavelength of magnons. (This becomes obvious in the hypothetical limit of infinite exchange interaction so that electron spin and magnetic moment are always aligned. In this scenario, the adiabatic theorem rules out spin flips, in contradiction to a diverging scattering rate from the naive Jsd2 of Fermi’s golden rule.)

In a more formal way, we write

mr=mzrez+mxrex+myrey  #S18

and assume that mx/yr are small everywhere in the system. We then apply the unitary transformation

H'=UHU† # SEQ eq \* MERGEFORMAT S19

with

U=ei2mxσy-myσx=e12m⊥σ+-m⊥*σ-,  # SEQ eq \* MERGEFORMAT S20

where m⊥=mx-imy and σ±=1/2σx±iσy. We consider small deviations from equilibrium and expand H' to second order in m⊥. This gives (cf. Ref. 24)

H'=He'0+H'em,  # SEQ eq \* MERGEFORMAT S21

where

He'0=-ℏ22m∇2-Jsdσz,H'em=-ℏ24m{∇,∇m⊥σ+-∇m⊥*σ-}+ℏ216m{∇,(∇m⊥r2}  # SEQ eq \* MERGEFORMAT S22

with the anticommutator {A,B}. The large exchange interaction in He'0 causes a splitting of the electronic bands, but is otherwise independent of the local magnon density. Coupling between conduction electrons and magnons is described by H'em, which depends on mr only through its spatial gradient. The first term of H'em describes electron-magnon scattering. It is accounted for via the collision integral in the Boltzmann theory and scales not with Jsd but the wavelength of magnons. The second term describes a dependence of electron energies on the magnon density and, alternatively, of the magnon stiffness on the electronic density. Since this term involves the gradient of the magnetization, its effect is small as long as most magnons have a sufficiently long wavelength.

# References

1.	van Kampen, M. et al. All-Optical Probe of Coherent Spin Waves. Phys. Rev. Lett. 88, 227201 (2002).

2.	Raquet, B., Viret, M., Sondergard, E., Cespedes, O. & Mamy, R. Electron-magnon scattering and magnetic resistivity in 3d ferromagnets. doi:10.1103/PhysRevB.66.024433.

3.	Razdolski, I. et al. Nanoscale interface confinement of ultrafast spin transfer torque driving non-uniform spin dynamics. Nat. Commun. 8, 15007 (2017).

4.	Tengdin, P. et al. Critical behavior within 20 fs drives the out-of-equilibrium laser-induced magnetic phase transition in nickel. Sci. Adv. 4, eaap9744 (2018).

5.	Zahn, D. et al. Lattice dynamics and ultrafast energy flow between electrons, spins, and phonons in a 3d ferromagnet. Phys. Rev. Res. 3, 023032 (2021).

6.	Pankratova, M. et al. Heat-conserving three-temperature model for ultrafast demagnetization in nickel. Phys. Rev. B 106, 174407 (2022).

7.	Nolting, W. & Ramakanth, A. Quantum Theory of Magnetism. (Springer Berlin Heidelberg, Berlin, Heidelberg, 2009). doi:10.1007/978-3-540-85416-6.

8.	Weißenhofer, M. & Oppeneer, P. M. Ultrafast Demagnetization Through Femtosecond Generation of Non‐Thermal Magnons. Adv. Phys. Res. (2024) doi:10.1002/apxr.202300103.

9.	Ma, P.-W., Dudarev, S. L. & Woo, C. H. Spin-lattice-electron dynamics simulations of magnetic materials. Phys. Rev. B 85, 184301 (2012).

10.	Pankratova, M. et al. Coupled atomistic spin-lattice simulations of ultrafast demagnetization in 3d ferromagnets. Sci. Rep. 14, 8138 (2024).

11.	Strungaru, M. et al. Spin-lattice dynamics model with angular momentum transfer for canonical and microcanonical ensembles. Phys. Rev. B 103, 024429 (2021).

12.	Rouzegar, R. et al. Laser-induced terahertz spin transport in magnetic nanostructures arises from the same force as ultrafast demagnetization. Phys. Rev. B 106, 144427 (2022).

13.	Seifert, T. S. et al. Terahertz spectroscopy for all-optical spintronic characterization of the spin-Hall-effect metals Pt, W and Cu 80 Ir 20. J. Phys. D. Appl. Phys. 51, 364003 (2018).

14.	Nádvorník, L. et al. Broadband Terahertz Probes of Anisotropic Magnetoresistance Disentangle Extrinsic and Intrinsic Contributions. Phys. Rev. X 11, 021030 (2021).

15.	Reiss, D. A. & Brouwer, P. W. Finite-frequency spin conductance of the interface between a ferro- or ferrimagnetic insulator and a normal metal. Phys. Rev. B 106, 144423 (2022).

16.	Brataas, A., Nazarov, Y. V. & Bauer, G. E. W. Finite-Element Theory of Transport in Ferromagnet–Normal Metal Systems. Phys. Rev. Lett. 84, 2481–2484 (2000).

17.	Reiss, D. A., Kampfrath, T. & Brouwer, P. W. Theory of spin-Hall magnetoresistance in the ac terahertz regime. Phys. Rev. B 104, 024415 (2021).

18.	Zwierzycki, M., Tserkovnyak, Y., Kelly, P. J., Brataas, A. & Bauer, G. E. W. First-principles study of magnetization relaxation enhancement and spin transfer in thin magnetic films. Phys. Rev. B 71, 064420 (2005).

19.	Beens, M., Duine, R. A. & Koopmans, B. S-d model for local and nonlocal spin dynamics in laser-excited magnetic heterostructures. Phys. Rev. B 102, 054442 (2020).

20.	Remy, Q. Ultrafast magnetization reversal in ferromagnetic spin valves: An s−d model perspective. Phys. Rev. B 107, 174431 (2023).

21.	Tveten, E. G., Brataas, A. & Tserkovnyak, Y. Electron-magnon scattering in magnetic heterostructures far out of equilibrium. Phys. Rev. B 92, 180412 (2015).

22.	Manchon, A., Li, Q., Xu, L. & Zhang, S. Theory of laser-induced demagnetization at high temperatures. Phys. Rev. B 85, 064408 (2012).

23.	Potter, H. H. The magneto-caloric effect and other magnetic phenomena in iron. Proc. R. Soc. London. Ser. A, Contain. Pap. a Math. Phys. Character 146, 362–387 (1934).

24.	Korenman, V., Murray, J. L. & Prange, R. E. Local-band theory of itinerant ferromagnetism. I. Fermi-liquid theory. Phys. Rev. B 16, 4032–4047 (1977).

25.	Dusabirane, F., Leckron, K., Rethfeld, B. & Schneider, H. C. Interplay of Electron-Magnon Scattering and Spin-Orbit Induced Electronic Spin-Flip Scattering in a two-band Stoner model.

26.	Kübler, J. Theory of Itinerant Electron Magnetism. (Oxford University Press, 2009).