Table 1  CO2 Laser Model & Test Range

| Model: MS640D 100W Laser type: CO2 sealed glass tube laser, wavelength 10.64um Laser max power: 100W Resolution: 1000dpi Working area: 600 × 400mm Engraving speed: 0-30000mm / min | CO2 sealed glass tube laser |
| --- | --- |

| Test Range | Power w | Speed mm/sec | spacing | Over focus |
| --- | --- | --- | --- | --- |
| Ceramics (Tiles); Clay; Glass | 5~50w | 0.2~300 | 0.5~0.2mm | 0~40mm |

Table 2 The Orton Cone data with kiln firing

| Temperature measuring cone (sintering →melt) Orton Cone 014. Heating rate(℃/hour); 15; 60; 150. Bending temperature; 757; 807; 838. | Feldspar 1200°C(melt) China clay 1310°C(sintering) Quartz floor tiles 1260°C(sintering) Clay 1230°C(sintering) |
| --- | --- |

( wiki glazy.org, 2020)

Table 3  The test result of laser speed effect on ceramic surface.

| Materials’ class | Speed mm/sec | Result & Ceramic sample firing energy |
| --- | --- | --- |
| Blanks (body 1230°C sintering) | 3~5 mm/sec | Start Obvious wavy or Melt & flow 53.05152364~31.83091418 |
| Glazes (1230°C melting) | 8~10 mm/sec | Start Obvious wavy or Melt & flow 19.89432136~15.91545709 |
| laser power 20w |  |  |

Table 4 The test pictures of laser-firing on the ceramic surfaces with different speeds.

| Feldspar( Room temperature) Laser Power: 20W , speed:1~25 mm/sec. melting at 8 mm/sec. |  |
| --- | --- |
| ( Room temperature)Wet sample Laser Power: 20W , speed:1~25 mm/sec, melting at 10 mm/sec. Transparent glaze and its components K2O 50g CaCO3 10g KL 10g SiO2 30g |  |
| ( Room temperature) Dry sample Laser Power: 20W , speed:1~25 mm/sec, melting at 14 mm/sec. Transparent glaze K2O 50g CaCO3 10g KL 10g SiO2 30g |  |
| Feldspar (fired at 1230 °C) Laser Power: 20W , speed:1~20 mm/sec, melting at 8 mm/sec. |  |
| China clay (fired at 800 °C) Laser power: 20W, speed 1~20 mm/sec, spacing 0.5mm, melting at 8 mm/sec. |  |
| Quartz floor tiles (fired at 1240 °C) speed 1~20 mm/sec , Power 20W, melting at 4 mm/sec. |  |
| Orton Cone 014 (room temperature) Laser power: 20W, speed:4~11, melting at 9 mm/sec. |  |
| Clay, unfired (room temperature) Laser power 20W, speed 1~20mm/sec, melting at 5 mm/sec. |  |
| Clay (fired at 800°C) Laser power 20W, speed 1~20 mm/sec , melting at 5 mm/sec. |  |
| Clay(fired at 1230°C) Laser power 20W, speed 1~20 mm/sec , melting at 5 mm/sec. |  |

Table 5 The relationship between laser energy and kiln firing temperature

| Laser firing energy value | 53.05152364 | 45.62525325 | 30.76996576 | 15.91545709 | 0.08488243782 |
| --- | --- | --- | --- | --- | --- |
| Kiln firing temperature (speculation) | 1250°C | 1240°C~ 1200°C | 1100°C | 1000°C | 1°C(1250~1000°C) |
| speed(mm/sec) | 3 | 3.4883 | 5.1724 | 10 | (3~5mm/sec) |

Table 6 Comparing clay in different firing methods.

A) Clay with 2.33% Fe2O3 → displays green color when laser fired.

B) Left: laser firing clay with 2.33% Fe2O3. Middle: laser firing glaze with 0% Fe2O3. Left: kiln firing clay with 2.33% Fe2O3.

C) Clay with 2.33% Fe2O3 →kiln firing→laser firing displays a green color.

D) Clay with 2.33% Fe2O3 →laser firing→kiln firing displays a brown color.

E) Laser firing 70% Kamado Feldspar  +  30% Kaolin glaze with 0% Fe2O3 displays a transparent color. F) Laser firing 70% Kamado Feldspar  +  30% Kaolin glaze with 2% Fe2O3 displays a green color.

G) Laser firing 70% Kamado Feldspar  +  30% Kaolin glaze  +  3% CuCO3 displays a red color.

H) 70% Kamado Feldspar  +  30% Kaolin glaze  +  3% CuCO3 → oxidation from kiln firing at 1265°C displays a green color→laser firing→displays a red color.

I) After laser firing the CuCO3 and the Fe2O3 on a transparent ceramic surface, the CuCO3 displays a red color and  the CuCO3 displays a light green color.

J) Taiwan, Patent Number I687394.

A.B.

C.D.

E.F.

G.H

I J

Table 7 Test images of laser firing  Fe2O3 and the CuCO3 on a ceramic surface.[A]The Fe2O3 and the CuCO3 are non-conductive. [B] The Fe2O3 and CuCO3 are placed on a ceramic surface and laser-fired without an airflow tube. [C] Cleaning the ceramic surface.[D] CuCO3 with 42Ω; Fe2O3 with 120Ω.

[A] [B]

[C] [D]

https://twpat-simple.tipo.gov.tw/tipotwoc/tipotwkm?.c3d9003AA000100000001000001000001^0000000001000010107703eca