Supplementary Material

Influence of the defect of activated carbon surface on cigarette smoke components adsorption: A DFT study

Xinxin Li1,2, Lu Ning1,2, Jiangfei Yin3, Jing Che1,2, Congxin Chen1,2, Qiang Liu1,2, Hongyun Hu4*

1 China Tobacco Hubei Industrial Co., Ltd., Wuhan 430070, P. R. China;

2 China Tobacco Hubei Industrial of Cigarette Material Co., Ltd., Wuhan 430040,P. R. China;

3 Future-Tech Innovation Institute, Wuhan 430058,P. R. China;

4 State key Laboratory of Coal Combustion, School of Energy and Power Engineering, Huazhong University of Science and Technology, Wuhan, 430074, China

Total number of pages: 8

Total number of table and figures: 12

Figure and Table captions

Fig. S1. Adsorption structures of CO on activated carbon (AC).

Table S1 Adsorption energy of CO on activated carbon (AC).

Fig. S2. Adsorption structures of nicotine on activated carbon (AC).

Table S2 Adsorption energy of nicotine on activated carbon (AC).

Fig. S3. Adsorption structures of phenol on activated carbon (AC).

Table S3 Adsorption energy of phenol on activated carbon (AC).

Fig. S4. Adsorption structures of CO on defective activated carbon (AC1).

Table S4 Adsorption energy of CO on defective activated carbon (AC1).

Fig. S5. Adsorption structures of nicotine on defective activated carbon (AC1).

Table S5 Adsorption energy of nicotine on defective activated carbon (AC1).

Fig. S6. Adsorption structures of phenol on defective activated carbon (AC1).

Table S6 Adsorption energy of phenol on defective activated carbon (AC1).

S1-1. AC-CO                       S1-2. AC-N2O

Fig. S1. Adsorption structures of CO on activated carbon (AC).

Table S1 Adsorption energy of CO on activated carbon (AC)

| Structure | Eads (kJ/mol) |
| --- | --- |
| S1-1. AC-CO | -161.16 |
| S1-2. AC-CO | -159.72 |

S2-1. AC-nicotine                       S2-2. AC-nicotine

S2-3. AC-nicotine                       S2-4. AC-nicotine

Fig. S2. Adsorption structures of nicotine on activated carbon (AC).

Table S2 Adsorption energy of nicotine on activated carbon (AC)

| Structure | Eads (kJ/mol) |
| --- | --- |
| S2-1. AC-nicotine | -85.07 |
| S2-2. AC-nicotine | -90.77 |
| S2-3. AC-nicotine | -4.36 |
| S2-4. AC-nicotine | -112.38 |

S3-1. AC-phenol                       S3-2. AC-phenol

S3-3. AC-phenol

Fig. S3. Adsorption structures of phenol on activated carbon (AC).

Table S3 Adsorption energy of phenol on activated carbon (AC)

| Structure | Eads (kJ/mol) |
| --- | --- |
| S3-1. AC-phenol | -186.95 |
| S3-2. AC-phenol | -13.13 |
| S3-3. AC-phenol | -13.32 |

S4-1. AC1-CO                       S4-2. AC1-N2O

Fig. S4. Adsorption structures of CO on defective activated carbon (AC1).

Table S4 Adsorption energy of CO on defective activated carbon (AC1)

| Structure | Eads (kJ/mol) |
| --- | --- |
| S4-1. AC1-CO | -359.98 |
| S4-2. AC1-CO | -160.04 |

S5-1. AC1-nicotine                       S5-2. AC1-nicotine

S5-3. AC1-nicotine                       S5-4. AC1-nicotine

Fig. S5. Adsorption structures of nicotine on defective activated carbon (AC1).

Table S5 Adsorption energy of nicotine on defective activated carbon (AC1)

| Structure | Eads (kJ/mol) |
| --- | --- |
| S5-1. AC1-nicotine | -320.18 |
| S5-2. AC1-nicotine | -109.90 |
| S5-3. AC1-nicotine | -111.89 |
| S5-4. AC1-nicotine | -165.87 |

S6-1. AC1-phenol                     S6-2. AC1-phenol

S6-3. AC1-phenol                       S6-4. AC1-phenol

Fig. S6. Adsorption structures of phenol on defective activated carbon (AC1).

Table S6 Adsorption energy of phenol on defective activated carbon (AC1)

| Structure | Eads (kJ/mol) |
| --- | --- |
| S6-1. AC1-phenol | -259.84 |
| S6-2. AC1-phenol | -12.83 |
| S6-3. AC1-phenol | -176.08 |
| S6-4. AC1-phenol | -204.49 |