## Slide 1
Microenvironment-Regulating and Self-Decontaminating (MRSD) Meta-Membranes
Hierarchically heterogeneous structured interfaces
Permeability
Hydrophobicity
Purification
Breathable
Decontaminating
Multifunctional integration
Electrical signal transmission
Multiple mechanisms
Multifunctional protection
Nanocrystals
Antibacterial
Waterproof
MRSD-PLA
PLA
Blood splash protection
Water vapor transmission
Nanoblocks
Electrospinning
Electrospray
Isolation protection
Charge redistribution
Electron migration
Mechanical energy
Electrical energy
a
b
Figure 1

## Slide 2
500 nm
Transmittance (a.u.)
Transmittance (a.u.)
Transmittance (a.u.)
Transmittance (a.u.)
Wavenumber (cm‒1)
Wavenumber (cm‒1)
Wavenumber (cm‒1)
Wavenumber (cm‒1)
Intensity (a.u.)
2 Theta (Degree)
Quantity Adsorbed (cm3/g)
Relative Pressure (P/P0)
Stress (MPa)
P-PLA
MRSD-PLA2
MRSD-PLA4
MRSD-PLA6
Tensile Strength (MPa)
Strain (%)
C=O
C=N
−CH3/O−O
C−O
−CH3
1454
1453
1452
1452
1380
1382
1383
1383
O−O
1186
1185
1184
1184
C−O
1090
1089
1089
1088
C−O
（011）
（002）
（112）
（110）
11.1
14.5
16.0
12.8
a
b
High porosity, High electrochemical activity
ZIF-8 nanocrystals
Low surface energy, High electronegativity
200 nm
F-TiO2 nanoblocks
5 μm
5 μm
5 μm
5 μm
1 μm
1 μm
1 μm
1 μm
ZIF-8
ZIF-8
ZIF-8
F-TiO2
F-TiO2
F-TiO2
c
d
e
f
MRSD-PLA6
MRSD-PLA4
MRSD-PLA2
P-PLA
MRSD-PLA6
MRSD-PLA4
MRSD-PLA2
P-PLA
g
h
i
j
k
l
m
n
Figure 2

## Slide 3
WCA (°)
Sand
3 cm
2 cm
Water
Coffee
Cola
Milk
Tea
1 min
2 min
3 min
4 min
5 min
0 s
137.4
125.1
119.1
112.6
Condensed Water Vapor
MRSD-PLA6
Hot Water
MRSD-PLA6
Water
Self-cleaning
Tumble
MRSD-PLA6
MRSD-PLA4
MRSD-PLA2
P-PLA
MRSD-PLA6
MRSD-PLA4
MRSD-PLA2
P-PLA
Air Permeability (mm·s-1)
68.9
69.5
74.9
46.8
WVTR (g·m-2·d-1)
MRSD-PLA6
Cotton
P-PLA
PP
Mask
a
b
c
d
e
f
g
h
i
j
4018
3997
3976
3731
3697
Injection
Hydrophobic
Detached
Suction
Stable
MRSD-PLA meta-membranes
Multifunctional protection
Interconnected network
Microenvironment regulation
Heterogeneous interface
Charge redistribution
Selective transmembrane transport
Fiber
Heterogeneous structure
Rich pores
(Breathable)
e⁻
e⁻
e⁻
e⁻
e⁻
Breathable
Waterproof
Inter-fiber
Rich pores
(Breathable)
Surface
Micropore
ZIF-8
Transmission pathway
Figure 3

## Slide 4
Ⅲ
Day 0
Surface Potential (kV)
MRSD-PLA6
MRSD-PLA4
MRSD-PLA2
P-PLA
5.8
5.5
5.3
3.3
2.6
5.2
4.9
4.5
Dielectric Constant
Frequency (Hz)
Relative Dielectric Constant
Surface Potential (kV)
MRSD-PLA6
Dust particles
Charge capture and storage
High electronegativity
-9.000e-2
9.000e-2
Before polarization
Ⅱ
-3
-2
-1
0
1
2
3
3×105
-3×105
Time (s)
Output Voltage (V)
Output Current (nA)
Output Charge (nC)
Time (s)
Time (s)
Time (s)
Output Voltage (V)
Output Voltage (V)
Time (s)
Time (s)
Output Voltage (V)
Output Voltage (V)
Time (s)
Time (s)
Time (s)
6.4
14.9
19.4
22.3
MRSD-PLA6
MRSD-PLA4
MRSD-PLA2
P-PLA
20.8
28.3
41.5
67.5
MRSD-PLA6
MRSD-PLA4
MRSD-PLA2
P-PLA
0.8
2.0
8.2
MRSD-PLA6
MRSD-PLA4
MRSD-PLA2
P-PLA
5.5
60% RH
80% RH
95% RH
20.0
22.3
22.1
Day 90
Day 0
Day 90
Day 0
Day 90
Day 0
Day 90
After polarization
Deep trap
Charge
l1
l2
l3
l4
a
b
c
d
e
f
h
i
j
k
l
l1
l2
l3
l4
g
Electron migration
Heterogeneous interfaces
e⁻
Charge redistribution
1.72-MRSD-PLA6
1.50-MRSD-PLA4
1.43-MRSD-PLA2
1.39-P-PLA
Ⅳ
Ⅰ
Figure 4

## Slide 5
P-PLA
Filtration Efficiency (%)
Airflow Capacity (L/min)
Pressure Drop (Pa)
10 L/min
85 L/min
MRSD-PLA2
MRSD-PLA4
MRSD-PLA6
99.3
82.4
59.1
142.8
419.2
280.0
234.0
163.7
P-PLA
Quality Factor (Pa-1)
Filtration Efficiency (%)
Airflow Capacity (L/min)
97.5
90.8
91.6
90.7
88.2
95.6
97.0
96.1
Filtration Efficiency (%)
Airflow Capacity (L/min)
Filtration Efficiency (%)
Time (min)
2 μm
PM-filtered
MRSD-PLA6
98.6
94.1
86.4
74.5
65.4
97.0
92.9
89.1
Time (min)
Filtration Efficiency (%)
98.4
93.2
89.5
76.4
Pressure Drop (Pa)
Time (min)
Time (min)
59 Pa
263 Pa
Pore Size (μm)
Percentage (%)
Porosity (%)
83.0
84.0
88.7
77.7
a
b
c
d
e
f
i
g
h
j
0.0067
0.0081
0.0147
0.0029
0.0157
0.0302
0.0430
0.0699
MRSD-PLA6
MRSD-PLA6
P-PLA
MRSD-PLA6
632 Pa
222 Pa
MRSD-PLA6
P-PLA
MRSD-PLA2
MRSD-PLA4
MRSD-PLA6
P-PLA
P-PLA
32 L/min
65 L/min
MRSD-PLA2
MRSD-PLA4
MRSD-PLA6
P-PLA
PM
Capture–storage–regeneration cycle
ZIF-8
F-TiO2
Closed-loop
k
Heterogeneous structured interface
Dynamic charge equilibrium
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
l
Figure 5
P-PLA
Filtration Efficiency (%)
Airflow Capacity (L/min)
Pressure Drop (Pa)
10 L/min
85 L/min
MRSD-PLA2
MRSD-PLA4
MRSD-PLA6
99.3
82.4
59.1
142.8
419.2
280.0
234.0
163.7
P-PLA
Quality Factor (Pa-1)
Filtration Efficiency (%)
Airflow Capacity (L/min)
97.5
90.8
91.6
90.7
88.2
95.6
97.0
96.1
Filtration Efficiency (%)
Airflow Capacity (L/min)
Filtration Efficiency (%)
Time (min)
2 μm
PM-filtered
MRSD-PLA6
98.6
94.1
86.4
74.5
65.4
97.0
92.9
89.1
Time (min)
Filtration Efficiency (%)
98.4
93.2
89.5
76.4
Pressure Drop (Pa)
Time (min)
Time (min)
59 Pa
263 Pa
Pore Size (μm)
Percentage (%)
Porosity (%)
83.0
84.0
88.7
77.7
a
b
c
d
e
f
i
g
h
j
0.0067
0.0081
0.0147
0.0029
0.0157
0.0302
0.0430
0.0699
MRSD-PLA6
MRSD-PLA6
P-PLA
MRSD-PLA6
632 Pa
222 Pa
MRSD-PLA6
P-PLA
MRSD-PLA2
MRSD-PLA4
MRSD-PLA6
P-PLA
P-PLA
32 L/min
65 L/min
MRSD-PLA2
MRSD-PLA4
MRSD-PLA6
P-PLA
PM
Capture–storage–regeneration cycle
ZIF-8
F-TiO2
Closed-loop
k
Heterogeneous structured interface
Dynamic charge equilibrium
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
e⁻
l
Figure 5

## Slide 6
2 cm
2 cm
2 cm
2 cm
2 cm
0 days
14 days
28 days
0 days
14 days
28 days
42 days
42 days
56 days
56 days
70 days
70 days
84 days
84 days
5 cm
MRSD-PLA6
MRSD-PLA4
MRSD-PLA2
P-PLA
Blank
MRSD-PLA6
P-PLA
e-
e-
e-
Q
Q
Ubiquinate
Visible light
NADH
NAD++H+
2H++1/2 O2
H2O
2H++1/2 O2
H2O
Electron transport chain
O2
O2-
O2-
H2O2
SOD
POD CAT
×
H2O+O2
Aggregated proteins
Permeability changed
Binding with protein
Collapsing cell wall
DNA
DNA fragment
Inhibit respiration chain
ROS
CydB
5 cm
Multi-mechanism antibacterial
Antibacterial Efficiency (%)
MRSD-PLA2
MRSD-PLA4
MRSD-PLA6
P-PLA
Antibacterial
a
b
c
d
e
90.3
61.6
37.3
25.5
Meta-membranes
Zn2+
Zn2+
ROS
ROS
Mesosome
Protein
DNA, RNA
Photocatalytic activity
Electrostatic interference
Figure 6

## Slide 7
Energy (keV)
Element
Atomic wt %
Ti
O
21.13
75.25
F
3.62
Counts
200 nm
Hydrophobic process
F-TiO2
TiO2
PFOTES
a
b
c
(c)
200 nm
200 nm
200 nm
200 nm
F-TiO2
Ti
O
F
d
Figure S1

## Slide 8
20 μm
5 μm
ZIF-8
ZIF-8
e
PLA@ZIF-8
f
EDS mapping
C
Zn
O
N
EDS mapping
4.2
4.0
Surface Potential (kV)
PLA@ZIF-8
Day 0
Day 30
Dielectric Constant
Frequency (Hz)
1.40 PLA@ZIF-8
WVTR (g·m-2·d-1)
1st
2nd
3rd
3981
3983
3984
Filtration Efficiency (%)
Airflow Capacity (L/min)
Pressure Drop (Pa)
g
h
i
j
PLA@ZIF-8 PM0.3
Figure S2

## Slide 9
=37 nm
Relative Frequency (%)
Diameter (nm)
Diameter (nm)
Diameter (nm)
Diameter (nm)
Diameter (nm)
Diameter (nm)
=110 nm
=531 nm
=476 nm
=434 nm
=326 nm
a
b
c
d
e
f
Relative Frequency (%)
F-TiO2
ZIF-8
P-PLA
MRSD-PLA2
MRSD-PLA4
MRSD-PLA6
Figure S3

## Slide 10
Temperature (°C)
Residual Weight (%)
a
b
2 μm
C
O
F
Zn
Figure S4

## Slide 11
Water
Coffee
Cola
Milk
Tea
MRSD-PLA6
MRSD-PLA6
Nonwoven material
Different types of liquids
Dye droplets
Dye droplets
Figure S5

## Slide 12
Water Vapor
High RH
Low RH
Fick’s Law:J =－D
Water Vapor
Pores
Water Droplet
Nanofiber
a
b
Figure S6

## Slide 13
e-
I
Electrode Membrane
MRSD-PLA Meta-membrane
Fully Pressed
Releasing
Fully Released
Pressing
Working mechanism
3×105
-3
-2
-1
0
1
2
3
-3×105
COMSOL simulation
Ⅰ
Ⅱ
Ⅲ
Ⅳ
a
b
Figure S7

## Slide 14
MRSD-PLA4
PM Concentration (N/cm3)
MRSD-PLA6
PM Concentration (N/cm3)
MRSD-PLA2
PM Concentration (N/cm3)
10 L/min
32 L/min
65 L/min
85 L/min
P-PLA
PM Concentration (N/cm3)
Upstream
Downstream
Particle size (nm)
Particle size (nm)
Particle size (nm)
Particle size (nm)
Figure S8

## Slide 15
PM Concentration (N/cm3)
PM Concentration (N/cm3)
PM Concentration (N/cm3)
10 L/min
32 L/min
65 L/min
85 L/min
PM Concentration (N/cm3)
Particle size (μm)
Particle size (μm)
Particle size (μm)
Particle size (μm)
MRSD-PLA4
MRSD-PLA6
MRSD-PLA2
P-PLA
Upstream
Downstream
Figure S9

## Slide 16
5 μm
2 μm
P-PLA
5 μm
MRSD-PLA2
2 μm
5 μm
MRSD-PLA4
2 μm
5 μm
MRSD-PLA6
2 μm
Figure S10

## Slide 17
1 μm
1 μm
5 μm
5 μm
F-TiO2
ZIF-8
F-TiO2
ZIF-8
After regeneration
After washing
1 μm
1 μm
F
C
Zn
N
F
C
Zn
N
a
b
c
Figure S11

## Slide 18
MRSD-PLA6
2 μm
After washing
Hot Air
Charge Migration
Charge Loss
a
b
2 μm
MRSD-PLA6
Figure S12

## Slide 19
5.8
5.6
5.8
MRSD-PLA6
After washing
After regeneration
Surface Potential (kV)
0.62
0.08
Capture barrier (eV)
Saturated Zn2+
Unsaturated Zn2+
Density-of-states
Energy (eV)
a
b
c
d
18.8
ESP (kcal/mol)
-18.8
18.8
-18.8
Charge density distribution
MRSD-PLA6
MRSD-PLA6 with H2O
Figure S13

## Slide 20
H2O
CO2
MRSD-PLA
O2
Bacterial community
Photosynthesis
Figure S14

## Slide 21
10 μm
5 μm
microorganisms
MRSD-PLA6
10 μm
5 μm
P-PLA
Figure S15

## Slide 22
14 days
28 days
42 days
56 days
0 days
MRSD-PLA6
14 days
28 days
42 days
56 days
0 days
P-PLA
Time (d)
Mass retention ratio (%)
Time (d)
Mass retention ratio (%)
a
b
c
~25%
~19%
MRSD-PLA6
P-PLA
~5%
~10%
MRSD-PLA6
P-PLA
40 °C, moist soil
Aqueous degradation
Figure S16