Tetrahedral Frameworks and Helical Chains: oP32– CaC2O5 and mP80– CaCO3 Calcium Carbonates above 100 GPa

Apostolos Pantousas* [a], [b], Georgios Aprilis [a], Alena Aslandukova [d], Ilya Kupenko [a], Xiang Li [a][c], Susanne Müller [a], [c], W. Zhou[d], P. Leveque[e], Michael Hanfland [a], Leonid Dubrovinsky [b] and Anna Pakhomova* [a]

[a] European Synchrotron Radiation Facility

Grenoble Cedex F-38043, France

E-mail: apostolos.pantousas@esrf.fr

[b] Bayerisches Geoinstitut,

Universität Bayreuth,

Bayreuth 95440, Germany

[c] University of Institut für Mineralogie,

University of Münster,

Corrensstraße 24, D-48149, Münster, Germany

[d] Material Physics and Technology at Extreme Conditions,

Laboratory of Crystallography,

Universität Bayreuth,

Bayreuth 95440, Germany

[e] Nantes Université, Univ Angers, Le Mans Université,

CNRS, Laboratoire de Planétologie et Géosciences,

LPG UMR 6112, 44000 Nantes, France

[f] Institute of Geosciences,

Goethe University Frankfurt

60438 Frankfurt, Germany

Contents

Section A: Previous knowledge	3

Section B: Methods	5

Section C: CaC2O5	7

Section D: CaCO3	15

Section E: References	22

# Section A: Previous knowledge

Table S1: Previously studied members of the Ca-C-O system at various pressures. Results from calculations, single-crystal X-ray diffraction (SC-XRD) and Powder X-ray diffraction (P-XRD).

(sp2 carbonates, mixed sp2 & sp3 carbonate)

| Phase | Space Group | Pearson Symbol | Pressure range (GPa) | Method | Study |
| --- | --- | --- | --- | --- | --- |
| CaC2O5 | Fdd2 | oF64 | 38 - 72 | Calculations | Yao 2018[1], Wang 2024[2] |
|  |  | oF64 | 58 - 76 | Calculations | Sagatova 2022[3] |
|  | Pc | mP16 | 72 - 82 | Calculations | Yao 2018, Wang 2024 |
|  |  | mP16 | 76 - 85 | Calculations | Sagatova 2022 |
|  | C2 | mC16 | 82 - 160 | Calculations | Yao 2018, Wang 2024 |
|  |  | mC16 | 85 - 100 | Calculations | Sagatova 2022 |
|  | Cmcm | oC36 | 11 - 55 | Calculations | Yao 2018 |
|  | I4/mcm | oI36 | 55 - 160 | Calculations | Yao 2018 |
|  | Cc | mC32 | 9 - 22 | Calculations | Sagatova 2022[3] , Wang 2024 |
|  | C2 | mC60 | 22 - 58 | Calculations | Sagatova 2022, Wang 2024 |
|  | Fd3m | cF128 | 25 - 50 | Calculations | Sagatova 2022 |
|  | I42d | tI64 | 21 - 59 | Calculations | Sagatova 2022, Wang 2024 |
|  |  | tI64 | 18 - 50 | SC-XRD | König 2022[4] |
| Calcite | R3c | hR30 | ambient | Calculations | Yao 2018 |
|  |  | hR30 | ambient | SC-XRD | Wyckoff1920[5], Maslen 1993[6] |
| CaCO3 II | P21/c | mP20 | 1.5 - 2.5 | SC-XRD | Merrill 1975[7] |
| CaCO3 III | P1 | aP25 | 2.5 - 15 | SC-XRD | Merlini 2012[8] |
| CaCO3 IIIb | P1 | aP10 | 1.5 - 11.3 | SC-XRD | Merlini 2012 |
| CaCO3 IV | R3m | hR48 | 2 - 4.5 | SC-XRD | Ishizawa[9] |
| CaCO3 V | R3m | hR24 | 1 - 29 | SC-XRD | Ishizawa[9], Druzhbin[10] |
| CaCO3 Vb | P21/m | mP10 | 3.4 - 29 | SC-XRD | Druzhbin[10] |
| CaCO3 VI | P1 | aP5 | 20 - 40.3 | SC-XRD | Merlini 2012 |
| CaCO3 VII | P21/c | mP20 | 35 - 50 | P-XRD | Gavryushkin 2017[11] |
| Aragonite | Pnma | oP20 | 4 - 32 | Calculations | Yao 2018 |
|  |  | oP20 | 0 - 50 | P-XRD | Santillán 2004[12] |
|  |  | oP20 | 0 - 40 | SC-XRD | Palaich 2016[13] |
| Post aragonite | Pmmn | oP12 | 47 - 75 | Calculations | Yao 2018 |
|  |  | oP12 | 30 - 50 | SC-XRD | Gavryushkin 2017 |
| Aragonite-II | P21/c C2221 | mP20 | 76 - 137 | Calculations | Oganov 2006[14] |
|  |  | oC20 | 137 - 200 | Calculations | Pickard 2015[15] |
|  |  | mP20 | 105 | P-XRD | Lobanov 2017[16] |
| Ca2CO4 | P21/m | mP14 | 76 - 160 | Calculations | Yao 2018 |
|  | Pnma | oP28 | 20 - 89 | SC-XRD | Binck 2022[17] |
| Ca3CO5 | Cmcm | oC | 11 – 55 | Calculations | Yao 2018 |
|  | I4/mcm | tI | 55 - 160 | Calculations | Yao 2018 |
| Ca3[C2O5]2[CO3] | P21/n | mP168 | 20 | SC-XRD | Spahr 2024[18] |

Table S2: Previously reported sp3-carbonates with their CO44-  groups isolated or arranged in groups, chains, rings, or pyramidal configurations (calcium compounds excluded).

| CO4 configuration | Phase | Space Group | Pearson Symbol | Pressure range (GPa) | Method | Study |
| --- | --- | --- | --- | --- | --- | --- |
| Isolated | Li4CO4 | C2/c | mC36 | 25 – 50 | Calculations | Sagatova 2020[19] |
|  | Na4CO4 | C2/c | mC36 | 23 – 50 | Calculations | Sagatova 2020 |
|  | K4CO4 | P21/c | mP36 | 21 - 50 | Calculations | Sagatova 2020 |
|  | Sr3[CO4]O | I4/mcm | oI36 | 20 - 30 | SC-XRD | Spahr 2021[20] |
|  | Sr3[CO4]O | Pnma | oP36 | ambient | SC-XRD | Spahr 2021[20] |
|  | Sr2CO4 | Pnma | oP28 | 20 | SC-XRD | Spahr 2021[21] |
| Framework | SrC2O5 | Fdd2 | oF64 | 32 - 90 | Calculations | Sagatova 2023[22] |
|  | PbC2O5 | Fdd2 | oF64 | 35 - 60 | Calculations | Banaev 2022[23] |
| Rings | Fe2.25Mg0.75C3O9 | C2/m | mC60 | 80 - 103 | Calculations | Boulard 2015[24] |
| Pyramidal | C4Fe2O10 | Fd3m | cF128 | 25 - 65 | SC-XRD | Kovalev 2025[25] |
|  | Ba[H4C4O10][H3C4O10] [H2CO3][HCO3] | P1 | aP48 | 0 - 40 | SC-XRD | Spahr 2025[26] |
|  | CaC2O5 | I42d | tI64 | 18 - 50 | SC-XRD | König 2022[4] |
| Layered | SrC2O5 | C2 | mC16 | 90 - 100 | Calculations | Sagatova 2023 |
| Groups | Mg2Fe2C4O13 | C2/c | mC84 | 141 | SC-XRD | Merlini 2015[27] |
|  | Fe4C3O12 | R3c | hR114 | 74 | SC-XRD | Cerantola 2017[28] |
|  | Mn4C4O13 | C2/c | mC84 | 88 - 130 | SC-XRD | Chariton 2020[29] |
| Chains | CaCO3 | P21/c | mP20 | 76 - 137 | Calculations | Oganov 2006[14] |
|  | CaCO3 | C2221 | oC20 | 137 - 200 | Calculations | Pickard 2015[15] |

# Section B: Methods

Sample preparation

A BX90-type diamond anvil cell (DAC) equipped with synthetic diamond anvils with a culet size of 150  μm was prepared[30]. The rhenium gasket used was indented from an initial thickness of 220 μm down to 20 μm and laser-drilled to create a circular pressure chamber of 80 μm in diameter. A natural sample of CaSiO3 (wollastonite) was grinded to a fine powder using an agate mortar and loaded to the pressure chamber. A crystal of Fe0.94O of a few μm, synthesized as described by Kantor et al.[31] was also loaded to the pressure chamber. The DAC was then compressed to 122 GPa as determined by the pressure-induced shift of the Raman spectrum of the diamonds at the culets. The sample was then heated from both sides of the DAC to 2800(200) K using a custom-made, double-sided Nd-YAG laser system at the ID-18 nuclear resonance beamline of the European Synchrotron Radiation Facility (ESRF) using the sample’s black-body radiation spectrum as a source of temperature information[32].

In situ single crystal X-Ray diffraction

In situ X-ray diffraction measurements were performed at the High-Pressure Diffraction Beamline ID15B[32] (ESRF, Grenoble). An EIGER2 X CdTe 9M detector was used and a monochromatic X-ray beam (λ = 0. 0.41505 Å) was focused on the sample with a spot area of approximately 1.5 × 1.5 μm2. An X-ray map of the laser-heated spot was obtained by scanning the sample chamber by a 15x15 position grid with a step of 5 μm at ω = 0o. The resulting map was analyzed using the XDI software suite in order to identify positions with interesting diffraction data. At each position of interest, scans of a continuous exposure with an exposure time of 2 s per frame were collected during ω rotations of ±35° of the DAC with a step of 0.5°. The resulting diffraction images experiments were analyzed using the CrysAlisPro[33] software suite. The Domain Auto Finder (DAFi) program was used for the search of reflection’s groups belonging to the individual single crystal domains[34]. This approach allowed to identify several products of chemical reactions between the CaSiO3, FeO and diamond, including two new calcium carbonates discussed here, mP32 CaC2O5 and mP80 CaCO3. The data were processed using the Jana2006[35] structural refinement software and successful resolution of the crystal structures of the new compounds was achieved. Crystallographic Information Files (CIF) for mP32 CaC2O5 and mP80 CaCO3 are deposited as Supporting Information as well as in the Cambridge Structural Database (CSD) under deposition numbers CSD 2430600 and 2393144, respectively.

Computational Details.

The first-principles calculations were done using the framework of density functional theory (DFT) as implemented in the Vienna Ab initio Simulation Package (VASP)[36]. To expand the electronic wave function in plane waves we used The Projector-Augmented-Wave (PAW) method[37]. The Generalized Gradient Approximation (GGA) functional was used for calculating the exchange-correlation energies, as proposed by Perdew–Burke–Ernzerhof (PBE)[38]. The PAW potentials with the following valence configurations of 3s23p64s2 for Ca (“Ca_sv”), 3s23p2 for Si (“Si”), 2s22p2 for C (“C”) and 2s22p4 for O (“O”) were used. Convergence tests with a threshold of 2 meV per atom in energy led to a Monkhorst-Pack[39] k-point grid of 11x7x5 and an energy cutoff for the plane wave expansion of 750 eV. The phonon frequencies and phonon band structure calculations were performed in the harmonic approximation with non-analytical term correction with the help of PHONOPY software[40] using the finite displacement method for 3x3x2 supercell (made for the primitive cell (PPOSCAR)) with respectively adjusted k-points: 4x4x2. For Brillouin zone integrations, a mesh of 8x8x4 k-points was used within the tetrahedron method[41]. Equation of state and static enthalpy calculations were performed via variable-cell structural relaxations between 1 bar and 160 GPa. In our static calculations of equation of state, the effect of zero-point motion and temperature was neglected.

# Section C: oP32 CaC2O5

Figure S1: Comparative diagram of Ca-O bond of the compounds presented in this study and previously predicted phases at the experimental pressure (122 GPa). The oP32 CaC2O5 has shorter Ca-O bonds with a smaller deviation of the minimum and maximum bond lengths from the average. The new mP80 CaCO3 phase has Ca-O bonds that are in between the extremes of the two previously reported phases.

Figure S2: Comparative diagram of C-O bond of the compounds presented in this study and previously predicted phases at the experimental pressure (122 GPa). The oP32 CaC2O5 has shorter C-O bonds with a smaller deviation of the minimum and maximum bond lengths from the average. The new mP80 CaCO3 phase has C-O bonds that are in between the extremes of the two previously reported phases, but with a much larger deviation of the minimum and maximum bond lengths from the average.

Figure S3: Comparative diagram of Ca-O bond of the compounds presented in this study and previously predicted phases at the experimental pressure (122 GPa). While the average O-C-O angle remains the same for all compounds, the minimum and maximum angles deviate differently from the average of each phase. For the oP32 CaC2O5 phase, they deviate less than previously predicted phases, while for the mP80 CaCO3 phase, the deviation is far more pronounced.

Figure S4. Geometry of a CaO12 anticuboctahedron in the crystal structure of oP32 CaC2O5 at 122 GPa, resolved from the single-crystal X-ray diffraction data.

Figure S5. In the crystal structure of oP32 CaC2O5, layers of Ca and O atoms are stacking normal to the a axis in ABAB manner with formation of distorted hexagonal-close packing (hcp) arrangement.

Figure S6. Phonon dispersion curves along high-symmetry directions in the Brillouin zone for oP32 CaC2O5 calculated at the experimental volume of ~ 189.68 Å3 (corresponds to theoretical pressure of ~126.9 GPa)[42].

Figure S7: Results of DFT calculated enthalpy difference between novel oP32 CaC2O5 and previously reported phases: a) tI64 CaC2O5[4], b) oF64 CaC2O5[1] and c) mC16 CaC2O5[1]. The calculations were performed in the pressure range of 20GPa – 160GPa with the step of 10GPa and indicate a higher stability of the experimental phase than all previously reported models.

Table S3. Crystal data and structure refinement for oP32 CaC2O5 at 293 K and 122 GPa.

|  | Experimental | Calculated |
| --- | --- | --- |
| Empirical formula | Ca C2 O5 | Ca C2 O5 |
| Formula weight | 144.1 g/mol | 144.1 g/mol |
| Temperature | 293 K | - |
| Wavelength | 0.41 Å | - |
| Crystal system | orthorhombic | orthorhombic |
| Space group | P n a 21 | P 21 c n |
| Unit cell dimensions | a = 3.8651(18) Å, α = 90° b = 13.334(5) Å, β = 90° c = 3.6804(13) Å, γ = 90° | a = 3.8684 Å, α = 90° b = 13.4135 Å, β = 90° c = 3.6945 Å, γ = 90° |
| Volume | 189.68(13) Å3 | 191.7016 Å3 |
| Z | 4 | 4 |
| Density (calculated) | 5.046 g/cm3 | 4.9927 g/cm3 |
| Absorption coefficient | 0.673 mm-1 | - |
| Crystal size | 0.03 x 0.02 x 0.01 mm3 | - |
| θ range for data collection | 3.31 to 21° | - |
| Index ranges | -4<=h<=4, -17<=k<=19, -4<=l<=5 | - |
| Reflections collected | 356 | - |
| Independent reflections | 304 [Rint = 0.0742] | - |
| Completeness to θ = 15.5° | 57% | - |
| Data / restraints / parameters | 304 / 0 / 38 | - |
| Goodness-of-fit | 1.3005 | - |
| Final R indices [I>3σ(I)] | Robs = 0.0567, wRobs = 0.0750 | - |
| R indices [all data] | Rall = 0.1290, wRall = 0.0828 | - |
| Largest diff. peak and hole | 1.42 and -1.66 e·Å-3 | - |

Table S4. Results of ab initio calculations of oP32 CaC2O5.

| Phase | Pressure (GPa) | Lattice parameters (Å, deg) |  |  | Atom | Coordinates |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | x | y | z |
| oP32 CaC2O5 | 126 | a = 3.85589 | b = 13.36968 | c = 3.67939 | Ca1 | 0.06629 | 0.37465 | 0.22065 |
|  |  | α = 90 | β = 90 | γ = 90 | Ca2 | 0.93371 | 0.62535 | 0.72065 |
|  |  |  |  |  | Ca3 | 0.56629 | 0.12535 | 0.22065 |
|  |  |  |  |  | Ca4 | 0.43371 | 0.87465 | 0.72065 |
|  |  |  |  |  | C1 | 0.60235 | 0.45749 | 0.64736 |
|  |  |  |  |  | C2 | 0.39765 | 0.54251 | 0.14736 |
|  |  |  |  |  | C3 | 0.10235 | 0.04251 | 0.64736 |
|  |  |  |  |  | C4 | 0.89765 | 0.95749 | 0.14736 |
|  |  |  |  |  | C5 | 0.57149 | 0.29227 | 0.61505 |
|  |  |  |  |  | C6 | 0.42851 | 0.70773 | 0.11505 |
|  |  |  |  |  | C7 | 0.07149 | 0.20773 | 0.61505 |
|  |  |  |  |  | C8 | 0.92851 | 0.79227 | 0.11505 |
|  |  |  |  |  | O1 | 0.91608 | 0.45469 | 0.72926 |
|  |  |  |  |  | O2 | 0.08392 | 0.54531 | 0.22926 |
|  |  |  |  |  | O3 | 0.41608 | 0.04531 | 0.72926 |
|  |  |  |  |  | O4 | 0.58392 | 0.95469 | 0.22926 |
|  |  |  |  |  | O5 | 0.41694 | 0.37525 | 0.754 |
|  |  |  |  |  | O6 | 0.58306 | 0.62475 | 0.254 |
|  |  |  |  |  | O7 | 0.91694 | 0.12475 | 0.754 |
|  |  |  |  |  | O8 | 0.08306 | 0.87525 | 0.254 |
|  |  |  |  |  | O9 | 0.57124 | 0.29417 | 0.27344 |
|  |  |  |  |  | O10 | 0.42876 | 0.70583 | 0.77344 |
|  |  |  |  |  | O11 | 0.07124 | 0.20583 | 0.27344 |
|  |  |  |  |  | O12 | 0.92876 | 0.79417 | 0.77344 |
|  |  |  |  |  | O13 | 0.89718 | 0.28635 | 0.75937 |
|  |  |  |  |  | O14 | 0.10282 | 0.71365 | 0.25937 |
|  |  |  |  |  | O15 | 0.39718 | 0.21365 | 0.75937 |
|  |  |  |  |  | O16 | 0.60282 | 0.78635 | 0.25937 |
|  |  |  |  |  | O17 | 0.4336 | 0.53817 | 0.77367 |
|  |  |  |  |  | O18 | 0.5664 | 0.46183 | 0.27367 |
|  |  |  |  |  | O19 | 0.9336 | 0.96183 | 0.77367 |
|  |  |  |  |  | O20 | 0.0664 | 0.03817 | 0.27367 |
| mP32 CaC2O5 | 20 | a = 4.50919 | b = 14.13241 | c = 5.11895 | Ca1 | 0.98911 | 0.37284 | 0.20173 |
|  |  | α = 90 | β = 90 | γ = 90 | Ca2 | 0.01089 | 0.62716 | 0.70173 |
|  |  |  |  |  | Ca3 | 0.48911 | 0.12716 | 0.20173 |
|  |  |  |  |  | Ca4 | 0.51089 | 0.87284 | 0.70173 |
|  |  |  |  |  | C1 | 0.62986 | 0.46138 | 0.67569 |
|  |  |  |  |  | C2 | 0.37015 | 0.53862 | 0.17569 |
|  |  |  |  |  | C3 | 0.12986 | 0.03862 | 0.67569 |
|  |  |  |  |  | C4 | 0.87015 | 0.96138 | 0.17569 |
|  |  |  |  |  | C5 | 0.54844 | 0.28986 | 0.64805 |
|  |  |  |  |  | C6 | 0.45156 | 0.71014 | 0.14805 |
|  |  |  |  |  | C7 | 0.04844 | 0.21014 | 0.64805 |
|  |  |  |  |  | C8 | 0.95156 | 0.78986 | 0.14805 |
|  |  |  |  |  | O1 | 0.90059 | 0.45014 | 0.61225 |
|  |  |  |  |  | O2 | 0.0994 | 0.54986 | 0.11225 |
|  |  |  |  |  | O3 | 0.40059 | 0.04986 | 0.61225 |
|  |  |  |  |  | O4 | 0.5994 | 0.95014 | 0.11225 |
|  |  |  |  |  | O5 | 0.45719 | 0.38465 | 0.73648 |
|  |  |  |  |  | O6 | 0.54281 | 0.61535 | 0.23648 |
|  |  |  |  |  | O7 | 0.95719 | 0.11535 | 0.73648 |
|  |  |  |  |  | O8 | 0.04281 | 0.88465 | 0.23648 |
|  |  |  |  |  | O9 | 0.56008 | 0.28345 | 0.39937 |
|  |  |  |  |  | O10 | 0.43992 | 0.71655 | 0.89938 |
|  |  |  |  |  | O11 | 0.06008 | 0.21655 | 0.39937 |
|  |  |  |  |  | O12 | 0.93992 | 0.78345 | 0.89937 |
|  |  |  |  |  | O13 | 0.82229 | 0.26879 | 0.78989 |
|  |  |  |  |  | O14 | 0.17771 | 0.73121 | 0.28989 |
|  |  |  |  |  | O15 | 0.32229 | 0.23121 | 0.78989 |
|  |  |  |  |  | O16 | 0.67771 | 0.76879 | 0.28989 |
|  |  |  |  |  | O17 | 0.51269 | 0.5414 | 0.70932 |
|  |  |  |  |  | O18 | 0.48731 | 0.4586 | 0.20932 |
|  |  |  |  |  | O19 | 0.01269 | 0.9586 | 0.70932 |
|  |  |  |  |  | O20 | 0.98731 | 0.0414 | 0.20932 |

# Section D: mP80 CaCO3

Supplementary Text S1: Analysis of the experimentally obtained diffraction images was performed using the CrysAlisPro software suite and the Jana 2020 software. For the mP80 CaCO3 phase, analyzing the crystal structure in the lower symmetry, chiral space group P21, parameter refinement yields a flack parameter of 0.5. This points to a racemic configuration, as is also suggested by the improved refinement statistics that the racemic configuration boasts over the models with fully Δ- or Λ- helicity. This led us to exclude an orthorhombic unit cell, though systematic extinctions pointed to a C-centered space group. This was done because all C-centered, as well as all primitive, orthorhombic space groups fail to appropriately describe the chirality of the tetrahedral chains, as they have a ratio of either 1:0 or 2:3 between chains of tetrahedra of Δ and Λ helicity. We attribute this mismatch to the dynamic disorder of the carbon atoms within the structure, which we were unable to refine reliably, due to the limitations of the opening of the diamond anvil cell used in the experiment. The resulting monoclinic, racemic model lies in agreement both with the previously reported model[16] and the model produced by the ab initio calculations performed in this work, both of which suggest the P21/c space group (albeit for different unit cells), widely used to describe racemic compounds. Taking all this information into account, the P21/c space group was chosen as the most accurate description of the crystal structure of the new CaCO3 phase.

Figure S8. Geometry of a CaO10 hendecahedron in the crystal structure of mP80 CaCO3 at 122 GPa, resolved from the single-crystal X-ray diffraction data.

Figure S9. In the crystal structure of mP80 CaCO3, layers of Ca and O atoms are stacking normal to the c axis in ABAB manner with formation of distorted hexagonal-close packing (hcp) arrangement.

Figure S10: Comparison of chirality of the CO44- chains between the different models. a) The previously calculated oC20 CaCO3 model (unit cell parameters a = 5.5057 (4) Å, b = 7.2389(3) Å, c = 3.3425(2) Å, V = 133.2161(2) Å3)[16] displays only one chirality for all chains. b) The previously calculated mP20 CaCO3 (unit cell parameters a = 4.5288(13) Å, b = 3.3345(3) Å, c = 9.0927(24) Å, β = 105.57(9)°, V = 132.27256(2) Å3)[16] features a racemic mixture of chains of both Δ and Λ helicity, in agreement to the c) mP80 CaCO3 structure (unit cell parameters a = 3.2989(4) Å, b = 10.877(4) Å, c = 14.224(4) Å, β = 90.162(16)°, V = 510.4(2) Å3) determined by our experimental data.

Figure S11: Le bail profile fitting of data for CaCO3 at 105 GPa published by Lobanov et al.[16]. The goodness of fit parameters are (a) 1.47 for the mP80 CaCO3 that we determined in this work, (b) 1.70 for the mP20 CaCO3 model[15], and (c) 2.11 for the oC20 CaCO3 model[15]. While all reflection observed by Lobanov et al.[16]  can be described by our structural model, some reflections not as well accounted by models proposed before[15-16]. Thus we conclude that the mP20 CaCO3-phase could be the same described by Lobanov et al.[16]. Original diffraction data were provided by Dr S. Lobanov.

Figure S12: Results of ab initio calculations on the new mP80 CaCO3 phase. a) Enthalpy difference as a function of pressure between the mP80 CaCO3 phase and previously calculated oC20 and mP20 models. The relaxed structure of the experimentally determined model demonstrates higher stability than previously calculated models. b) The pressure dependence of the mP80 CaCO3 unit cell volume. The red and black solid circle represents experimental and theoretical data, respectively. The black dashed line shows the fit of the calculated P-V data using the third-order Birch-Murnaghan equation of state.

Table S5. Crystal data and structure refinement for mP80 CaCO3 at 293 K and 122 GPa.

|  | Experimental | Calculated |
| --- | --- | --- |
| Empirical formula | Ca C O3 | Ca C O3 |
| Formula weight | 100.1 g/mol | 100.1 g/mol |
| Temperature | 293 K | - |
| Wavelength | 0.41 Å | - |
| Crystal system | monoclinic | monoclinic |
| Space group | P 21/c 1 1 | P 21/c 1 1 |
| Unit cell dimensions | a = 3.2989(4) Å, α = 90° b = 10.877(4) Å, β = 90.162(16)° c = 14.224(4) Å, γ = 90° | a = 10.872 Å, α = 90° b = 3.298 Å, β = 90° c = 14.217 Å, γ = 90° |
| Volume | 510.4(2) Å3 | 509.7627 Å3 |
| Z | 16 | 16 |
| Density (calculated) | 5.2102 g/cm3 | 5.2165 g/cm3 |
| Absorption coefficient | 0.922 mm-1 | - |
| Crystal size | 0.03 x 0.015 x 0.01 mm3 | - |
| θ range for data collection | 3.66 to 20.89° | - |
| Index ranges | -4<=h<=4, -11<=k<=13, -15<=l<=18 | - |
| Reflections collected | 1399 | - |
| Independent reflections | 787 [Rint = 0.0108] | - |
| Completeness to θ = 13.48° | 45% | - |
| Data / restraints / parameters | 787 / 0 / 101 | - |
| Goodness-of-fit | 1.51 | - |
| Final R indices [I>3σ(I)] | Robs = 0.0391, wRobs = 0.0501 | - |
| R indices [all data] | Rall = 0.1014, wRall = 0.0536 | - |
| Largest diff. peak and hole | 0.64 and -0.59 e·Å-3 | - |

Table S6. Results of ab initio calculations in this study.

| Phase | Pressure (GPa) | Lattice parameters (Å, deg) |  |  | Atom | Coordinates |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | x | y | z |
| mP80 CaCO3 | 128 | a = 10.87200 | b = 3.29800 | c = 14.21700 | Ca1 | 0.750063 | 0.288630 | 0.164228 |
|  |  | α = 90 | β = 90 | γ = 90 | Ca2 | 0.250063 | 0.288629 | 0.664228 |
|  |  |  |  |  | Ca3 | 0.999934 | 0.711372 | 0.085772 |
|  |  |  |  |  | Ca4 | 0.499935 | 0.711371 | 0.585772 |
|  |  |  |  |  | O1 | 0.637780 | 0.790127 | 0.193534 |
|  |  |  |  |  | O2 | 0.137781 | 0.790127 | 0.693534 |
|  |  |  |  |  | O3 | 0.612219 | 0.290130 | 0.056467 |
|  |  |  |  |  | O4 | 0.112219 | 0.290130 | 0.556466 |
|  |  |  |  |  | O5 | 0.861460 | 0.777023 | 0.193239 |
|  |  |  |  |  | O6 | 0.361460 | 0.777022 | 0.693239 |
|  |  |  |  |  | O7 | 0.888539 | 0.222981 | 0.056761 |
|  |  |  |  |  | O8 | 0.388539 | 0.222981 | 0.556761 |
|  |  |  |  |  | O9 | 0.500518 | 0.260739 | 0.195565 |
|  |  |  |  |  | O10 | 0.000518 | 0.260739 | 0.695565 |
|  |  |  |  |  | O11 | 0.749483 | 0.760743 | 0.054435 |
|  |  |  |  |  | O12 | 0.249483 | 0.760743 | 0.554435 |
|  |  |  |  |  | C13 | 0.572875 | 0.007557 | 0.250405 |
|  |  |  |  |  | C14 | 0.072875 | 0.007556 | 0.750404 |
|  |  |  |  |  | C15 | 0.322875 | 0.492439 | 0.000404 |
|  |  |  |  |  | C16 | 0.822875 | 0.492439 | 0.500404 |

# Section E: References

[1]	X. Yao, C. Xie, X. Dong, A. R. Oganov, Q. Zeng, Physical Review B 2018, 98, 014108.

[2]	H. Wang, L. Liu, Z. Gao, L. Yang, G. Naren, S. Mao, Nature Communications 2024, 15, 755.

[3]	D. N. Sagatova, P. N. Gavryushkin, N. E. Sagatov, M. V. Banaev, Physical Chemistry Chemical Physics 2022, 24, 23578-23586.

[4]	J. König, D. Spahr, L. Bayarjargal, P. N. Gavryushkin, D. Sagatova, N. Sagatov, V. Milman, H.-P. Liermann, B. Winkler, ACS Earth and Space Chemistry 2022, 6, 73-80.

[5]	R. W. G. Wyckoff, American journal of science 1920, 4, 317-360.

[6]	E. N. Maslen, V. A. Streltsov, N. R. Streltsova, Acta Crystallographica Section B 1993, 49, 636-641.

[7]	L. Merrill, W. A. Bassett, Acta Crystallographica Section B 1975, 31, 343-349.

[8]	M. Merlini, M. Hanfland, W. Crichton, Earth and planetary science letters 2012, 333, 265-271.

[9]	aN. Ishizawa, Powder Diffraction 2014, 29, S19-S23; bN. Ishizawa, H. Setoguchi, K. Yanagisawa, Scientific Reports 2013, 3, 2832.

[10]	D. Druzhbin, S. V. Rashchenko, A. Shatskiy, W. A. Crichton, ACS Earth and Space Chemistry 2022, 6, 1506-1513.

[11]	P. N. Gavryushkin, N. S. Martirosyan, T. M. Inerbaev, Z. I. Popov, S. V. Rashchenko, A. Y. Likhacheva, S. S. Lobanov, A. F. Goncharov, V. B. Prakapenka, K. D. Litasov, Crystal Growth & Design 2017, 17, 6291-6296.

[12]	J. Santillán, Q. Williams, American mineralogist 2004, 89, 1348-1352.

[13]	S. E. Palaich, R. A. Heffern, M. Hanfland, A. Lausi, A. Kavner, C. E. Manning, M. Merlini, American Mineralogist 2016, 101, 1651-1658.

[14]	A. R. Oganov, C. W. Glass, S. Ono, Earth and Planetary Science Letters 2006, 241, 95-103.

[15]	C. J. Pickard, R. J. Needs, Physical Review B 2015, 91, 104101.

[16]	S. S. Lobanov, X. Dong, N. S. Martirosyan, A. I. Samtsevich, V. Stevanovic, P. N. Gavryushkin, K. D. Litasov, E. Greenberg, V. B. Prakapenka, A. R. Oganov, A. F. Goncharov, Physical Review B 2017, 96, 104101.

[17]	J. Binck, D. Laniel, L. Bayarjargal, S. Khandarkhaeva, T. Fedotenko, A. Aslandukov, K. Glazyrin, V. Milman, S. Chariton, V. B. Prakapenka, American Mineralogist 2022, 107, 336-342.

[18]	D. Spahr, L. Bayarjargal, M. Bykov, L. Brüning, P. L. Jurzick, Y. Wang, V. Milman, K. Refson, M. Mezouar, B. Winkler, Communications Chemistry 2024, 7, 238.

[19]	D. Sagatova, A. Shatskiy, N. Sagatov, P. N. Gavryushkin, K. D. Litasov, Lithos 2020, 370-371, 105637.

[20]	D. Spahr, J. König, L. Bayarjargal, P. N. Gavryushkin, V. Milman, H.-P. Liermann, B. Winkler, Inorganic Chemistry 2021, 60, 14504-14508.

[21]	D. Spahr, J. Binck, L. Bayarjargal, R. Luchitskaia, W. Morgenroth, D. Comboni, V. Milman, B. Winkler, Inorganic Chemistry 2021, 60, 5419-5422.

[22]	D. N. Sagatova, P. N. Gavryushkin, N. E. Sagatov, M. V. Banaev, Journal of Computational Chemistry 2023, 44, 2453-2460.

[23]	M. V. Banaev, N. E. Sagatov, D. N. Sagatova, P. N. Gavryushkin, ChemistrySelect 2022, 7, e202201940.

[24]	E. Boulard, D. Pan, G. Galli, Z. Liu, W. L. Mao, Nature Communications 2015, 6, 6311.

[25]	V. Kovalev, D. Spahr, B. Winkler, L. Bayarjargal, L. Wedek, A. Aslandukova, A. Pakhomova, G. Garbarino, E. Bykova, Communications Chemistry 2025, 8, 66.

[26]	D. Spahr, E. Bykova, L. Bayarjargal, V. Milman, H.-P. Liermann, B. Winkler, Chemical Communications 2025, 61, 161-164.

[27]	M. Merlini, M. Hanfland, A. Salamat, S. Petitgirard, H. Müller, American Mineralogist 2015, 100, 2001-2004.

[28]	V. Cerantola, E. Bykova, I. Kupenko, M. Merlini, L. Ismailova, C. McCammon, M. Bykov, A. I. Chumakov, S. Petitgirard, I. Kantor, Nature Communications 2017, 8, 15960.

[29]	aS. Chariton, (Bayreuth), 2020; bS. Chariton, M. Bykov, E. Bykova, E. Koemets, T. Fedotenko, B. Winkler, M. Hanfland, V. B. Prakapenka, E. Greenberg, C. McCammon, L. Dubrovinsky, Acta Crystallogr E Crystallogr Commun 2020, 76, 715-719.

[30]	I. Kantor, V. Prakapenka, A. Kantor, P. Dera, A. Kurnosov, S. Sinogeikin, N. Dubrovinskaia, L. Dubrovinsky, Rev Sci Instrum 2012, 83, 125102.

[31]	I. Y. Kantor, C. A. McCammon, L. S. Dubrovinsky, Journal of Alloys and Compounds 2004, 376, 5-8.

[32]	I. Kupenko, X. Li, S. C. Müller, D. Bessas, S. Yaroslavtsev, G. Aprilis, A. I. Chumakov, J. P. Celse, R. Rüffer, High Pressure Research 2024, 44, 310-336.

[33]	Y. Agilent Technologies Ltd, Oxfordshire, England, 2014.

[34]	A. Aslandukov, M. Aslandukov, N. Dubrovinskaia, L. Dubrovinsky, Journal of Applied Crystallography 2022, 55, 1383-1391.

[35]	aV. D. Petricek, M., 2000; bL. Palatinus, G. Chapuis, Journal of Applied Crystallography 2007, 40, 786-790.

[36]	G. Kresse, J. Furthmüller, Computational Materials Science 1996, 6, 15-50.

[37]	aP. E. Blöchl, Physical Review B 1994, 50, 17953-17979; bG. Kresse, D. Joubert, Physical Review B 1999, 59, 1758-1775.

[38]	J. P. Perdew, K. Burke, M. Ernzerhof, Physical Review Letters 1996, 77, 3865-3868.

[39]	H. J. Monkhorst, J. D. Pack, Physical Review B 1976, 13, 5188-5192.

[40]	A. Togo, I. Tanaka, Scripta Materialia 2015, 108, 1-5.

[41]	P. E. Blöchl, O. Jepsen, O. K. Andersen, Physical Review B 1994, 49, 16223-16233.

[42]	aA. Togo, Journal of the Physical Society of Japan 2022, 92, 012001; bA. Togo, L. Chaput, T. Tadano, I. Tanaka, Journal of Physics: Condensed Matter 2023, 35, 353001.