# Supplementary Information for

# Extraordinary Hall Effect in Freestanding Oxide Heterostructures

Z. S. Lim†, Z. Zhou†, K. Han, G. J. Omar, Z. Huang, S.W. Zeng, A. Ariando*

Department of Physics, National University of Singapore, Singapore 117551.

†These two authors contributed equally.

*Correspondence to: ariando@nus.edu.sg

In Fig. S1a, we illustrate a plausible scenario with an MTJ. Both ferromagnetic layers FM1,2 are assumed to have PMA, and the bottom FM1 has larger HC due to exchange enhancement by the adjacent antiferromagnetic (AFM) layer. Besides that, FM1,2 also have opposite signs of PS – the majority-spin carriers in FM1 (FM2) are antiparallel (parallel) to the local magnetization (M). Hence, in the Fig. S1a, right panel, the mechanism of AHE is illustrated from an “imbalanced spin-polarization” analogue of the Spin Hall Effect (SHE)54, following a simple Hamiltonian, H=-αsocv×E∙σ where αsoc is the spin-orbit coupling coefficient, v is the electron’s velocity, E is the electric field from the cations, and σ is the free electron spin. This way, using the standard Hall bar connection, FM1 would produce a negative-sign ρAHE loop, where net negative charges are deflected towards the positive-lead of Hall voltage at +MZ (magnetization up) but towards the negative-lead at -MZ (magnetization down). Vice versa, FM2 produces a positive-sign ρAHE loop, where negative charges are deflected towards negative-lead at +MZ but towards positive-lead at +MZ. At the antiparallel (high resistance) state between FM1,2 (Fig. S1b, left panel), it is possible to observe hump features in Hall Effect (Fig. S1b, right panel) that also vanish at a large field, yet do not involve non-collinear magnetic textures.

In Fig. S1c, structure B indeed has more severe carrier localization compared to structure A, as evidenced by the slightly higher (overall) resistivity and low-temperature upturn. The ferromagnetic TC indicated by a transition from linear (ρxx∝T) to Fermi-liquid (ρxx∝T2) is also evident in structure A, but blurred in structure B. As shown in Fig. S1d left panel, reducing the SRO thickness (compared to structure A) would lead to an obvious positive AHE (instead of negative). Likewise, in Fig. S1d right panel, increasing SRO thickness (compared to structure B) would cause the expected positive AHE to be diminished by a competing negative AHE component at ~10 K.

To take a glimpse of the intermediate state prior to epitaxial lift-off, the structure “Cf–intermediate” is grown onto an STO(001) substrate pre-patterned with hall bar bordered by AlN (see methods), and is measured immediately after film growth to minimize the deterioration of SAO by atmospheric moisture’s attack. As seen in Fig. S3a-b and similar to the data of structure Cf in main text Fig. S3c, the Hall Effect humps also exist in structure Cf–intermediate up to 80 K together with dominant-negative AHE, but the humps are weirdly symmetrical at +/- magnetic fields, and are not understood at present.

In Fig. S5, the hysteretic behavior of topological charge density, TCD=m∙∂m∂x×∂m∂y is simulated via MUMAX3, using logical magnetic parameters of SRO at 80 K. These parameters are not extracted from the magnetometry of freestanding trilayer structure Cf due to extra signal from the proximity induced magnetism of iridate and oxygen vacancies. Instead, we use Jex=3kBTc2j(j+1) to estimate the exchange constant, where j is the total angular momentum quantum number. 4d4 electronic configuration is arguably lying between the weak SOC (l-s coupling) and strong SOC (j-j coupling) regimes, with S=1, L=1, and J=L+S=1 because the two vectors are neither parallel nor antiparallel. Using bulk values, Msat ~1.6 µB/Ru, j=1, Tc=160 K, Jex = 3kBTC/4, hence Aex = Jex/a = 4.22 x 10-12 J/m where a is the pseudocubic lattice parameter 3.93 Å. To account for weakened magnetism in the ultrathin regime, we assume TC = 100 K and Msat=1.0 µB/Ru at 0 K. Knowing that temperature-dependent magnetization usually takes the form of M/Mmax=tanh⁡M/MmaxT/Tc from the mean-field generalization to the Langevin’s paramagnetism, at 80 K, T/Tc=M/Mmaxtanh-1M/Mmax=0.8 can be obtained when M/Mmax=0.710412, hence Msat = 0.71 µB/Ru = 1.09x105 A/m at 80 K, where Mmax refers to Msat at 0 K. Noting exchange length lex=2AexµoMsat2=23.86 nm, hence we use a cell size of 4 nm < lex. The uniaxial magnetic anisotropy, Ku is arbitrarily scaled down to 3.08x104 J/m3. Gilbert damping constant is set to 0.1, while the backward/forward field sweep calculations are always initialized with m=Uniform(0,0,±1), so that the emergence of Skyrmions and TCD  are always hysteretic. Combining with DMI Dind = 4.5x10-4 J/m2 induced at the SRO/SIO interface, we obtain a TCD variation within a field range that matches well with the observed Hall Effect hump features, i.e. it reaches the peak at µoH~±0.14 T and vanishes at µoH~±0.3 T. Subsequently the same parameters are used to generate the θ-dependent trend as shown in the main text Fig. 4c, at µoHpeak,TCD = 0.14 T, corresponding to Neel-type Skyrmions’ diameter of ~100 nm.

Supplementary Figures:

Supplementary Figure S1: (a) Left: structure of the conceptual MTJ, where “NMI” denotes the non-magnetic insulating tunneling barrier. Right: the mechanism of AHE, with symbols ⊗, ⦿ and ⨁ representing “into-plane (-MZ)”, “out-from-plane” (+MZ) and positively-charged ions. (b) Sketches of expected data for linear resistivity (top left), magnetic moment (bottom left) and extraordinary Hall resistivity (right). (c) ρxx-T curves for structure A and B. (d) Extraordinary Hall Effect data from the modified structure A and B.

Supplementary Figure S2: (a) A large continuous flake floated with LSMO sacrificial layer and etched by an HCl+KI+H2O solution, without any tape support. (b) No significant ferromagnetic moment can be measured from the large flake in (a).

Supplementary Figure S3: (a) Schematic of structure Cf-Intermediate and the optical microscopy image of its Hall bar. (b) Extraordinary Hall Effect measured from structure Cf-Intermediate, with data shifted vertically for clarity. Ordinary Hall Effect high-field gradient extracted from (c) the epitaxial structures A, B and C and (d) their freestanding counterparts Af, Bf and Cf.

Supplementary Figure S4: The series of Extraordinary Hall Effect data of the structure Cf with a gradual increase of θ, measured at 80 K. The maximum field applied is gradually increased to account for the increasing HC, AHE or HC1. Humps (grey shading in Fig. 4) are not shown here. Data at θ=70o and 80o become too difficult to analyze.

Supplementary Figure S5: Simulated field-sweep result of the TCD showing hysteretic behavior, overlapped with the experimental Hall Effect for comparison. The surrounding snapshots show the corresponding magnetic textures at various magnetic fields.

Supplementary Figure S6: Sketches of Hall Effects illustrating our understanding and expectation on the θ-dependent results, using arbitrary parameters. Left panels are the θ-dependent Hall Effect loops and their deconvolutions, while the right panels show the full trends of the θ- dependent absolute magnitudes and characteristic fields. The scenario in (a) corresponds to our observed trends as well as simulated Neel-type Skymions behavior, while the scenario in (b) corresponds to the description in Fig. S1a. Hence, we believe that Skyrmions exist in our samples (in favor of the AHE+THE interpretation), rather than two decoupled collinear ferromagnetic domains.