# Appendix

Table 3: Fatigue test results as built- and machined specimens

| Specimen-ID | R | Frequency [Hz] | Stress range [MPa] | Number of cycles [-] | Failure location |
| --- | --- | --- | --- | --- | --- |
| T1V1 | 0.1 | 50 | 249.12 | 125.389 | slightly beyond parallel length |
| T1V2 | 0.1 | 50 | 223.43 | 122.543 | slightly beyond parallel length |
| T1V3 | 0.1 | 50 | 191.59 | 201.870 | Parallel length, middle |
| T1V4 | 0.1 | 50 | 159.97 | 436.857 | Parallel length, near end |
| T1V5 | 0.1 | 50 | 147.82 | 339.874 | slightly beyond parallel length |
| T1V6 | 0.1 | 50 | 133.55 | 1.865.055 | slightly beyond parallel length |
| T2V1 | 0.1 | 30 | 314.69 | 68.433 | Parallel length, middle |
| T2V2 | 0.1 | 30 | 346.15 | 32.440 | Parallel length, near end |
| T2V3 | 0.1 | 50 | 151.05 | 415.590 | Parallel length, near end |
| T2V4 | 0.1 | 50 | 138.46 | 609.658 | Parallel length, middle |
| T2V5 | 0.1 | 50 | 135.31 | 686.734 | Parallel length, near end |
| T2V6 | 0.1 | 50 | 129.02 | 1.079.585 | Parallel length, near end |
| T3V1 | 0.1 | 50 | 576.92 | 5.000.000 | Run-out |
| T3V2 | 0.1 | 50 | 692.31 | 9.537 | slightly beyond parallel length |
| T3V3 | 0.1 | 50 | 634.62 | 47.280 | Parallel length, near end |
| T3V4 | 0.1 | 50 | 605.77 | 81.949 | slightly beyond parallel length |
| T3V5 | 0.1 | 50 | 600.00 | 374.265 | slightly beyond parallel length |
| T4V1 | 0.1 | 50 | 611.54 | 5.000.000 | Run-out |
| T4V2 | 0.1 | 50 | 657.69 | 45.933 | Parallel length, near end |
| T4V3 | 0.1 | 50 | 646.15 | 108.889 | Parallel length, middle |
| T4V4 | 0.1 | 50 | 623.08 | 197.398 | Parallel length, middle |
| T4V5 | 0.1 | 50 | 617.31 | 20.401 | Parallel length, near end |
| T4V6 | 0.1 | 50 | 588.46 | 210.635 | Parallel length, middle |

Table 4: Numerical concentrations factors Kt and Kf for as-built specimens

| Specimen ID | Stress concentration factor (Kt) | Notch radius [mm] | Fatigue concentration factor (Kf) | Identification of failure (1 = Yes, 0 = No) |
| --- | --- | --- | --- | --- |
| T1V3 | 4.20 | 0.15 | 3.08 | 1 |
| T1V4 | 4.16 | 0.33 | 3.26 | 1 |
| T2V1 | 3.87 | 0.32 | 3.04 | 0 |
| T2V2 | 3.06 | 0.38 | 2.50 | 1 |
| T2V3 | 4.53 | 0.27 | 3.44 | 1 |
| T2V4 | 4.10 | 0.18 | 3.01 | 1 |
| T2V5 | 2.35 | 0.40 | 1.99 | 0 |
| T2V6 | 3.50 | 0.38 | 2.82 | 1 |

Table 5: Surface parameters as-built specimens

| Specimen ID | Sz frontside [mm] | Sz backside [mm] | Mean thickness [mm] | Standard deviation [-] |
| --- | --- | --- | --- | --- |
| T1V1 | 1.84 | 1.54 | 5.58 | 0.34 |
| T1V2 | 1.32 | 1.46 | 5.43 | 0.39 |
| T1V3 | 1.94 | 1.65 | 5.43 | 0.41 |
| T1V4 | 2.05 | 1.84 | 5.42 | 0.41 |
| T1V5 | 1.36 | 1.66 | 5.39 | 0.39 |
| T1V6 | 1.66 | 1.89 | 5.45 | 0.46 |
| T2V1 | 1.09 | 1.80 | 5.46 | 0.36 |
| T2V2 | 1.59 | 1.38 | 5.40 | 0.32 |
| T2V3 | 1.52 | 1.81 | 5.40 | 0.38 |
| T2V4 | 1.63 | 1.76 | 5.32 | 0.43 |
| T2V5 | 1.33 | 1.43 | 5.44 | 0.35 |
| T2V6 | 1.44 | 1.43 | 5.49 | 0.37 |