Supporting Information

Synthesis of aromatic and citrate-based quaternary ammonium salts for application as thermolatent bases

Matthias Udo Mayer-Kriehuber1,2 ● Evelyn Sattler1 ● Johannes Krämer2 ● David Reisinger1,2 ● Daniel Bautista-Anguís1,2 ● Johanna Uher1,3 ● Elvira Vidovic4 ● Sandra Schlögl1,2

____

Sandra Schlögl

sandra.schloegl@pccl.at; sandra.schloegl@unileoben.ac.at

1	Polymer Competence Center Leoben GmbH, Leoben, Austria

2	Institute of Chemistry of Polymeric Materials, Technical University of Leoben, Leoben, Austria

3	Institute of Chemistry and Technology of Materials, Graz University of Technology, Graz, Austria

4	University of Zagreb Faculty of Chemical Engineering and Technology, Zagreb, Croatia

# Results

Figure S1: (a) 1H NMR, (b) 13C NMR (600 MHz, DMSO-d6) and (c) FTIR spectrum of 1-a.

Figure S2: DSC curve of 1-a.

Figure S3: (a) 1H NMR, (b) 13C NMR (600 MHz, DMSO-d6) and (c) FTIR spectrum of 1-b.

Figure S4: DSC curve of 1-b.

Figure S5: (a) 1H NMR, (b) 13C NMR (600 MHz, DMSO-d6) and (c) FTIR spectrum of 1-c.

Figure S6: DSC curve of 1-c.

Figure S7: (a) 1H NMR, (b) 13C NMR (600 MHz, DMSO-d6) and (c) FTIR spectrum of 1-d.

Figure S8: DSC curve of 1-d.

Figure S9: TGA curve of the pure base TBD.

Figure S10: FTIR spectrum of the pure base TBD.

Figure S11: EGA analysis of the pure base TBD.

Figure S12: (a) 1H NMR, (b) 13C NMR (600 MHz, DMSO-d6) and (c) FTIR spectrum of 2-a.

Figure S13: DSC curve of 2-a.

Figure S14: (a) 1H NMR, (b) 13C NMR (600 MHz, DMSO-d6) and (c) FTIR spectrum of 2-b.

Figure S15: DSC curve of 2-b.

Figure S16: (a) 1H NMR, (b) 13C NMR (600 MHz, DMSO-d6) and (c) FTIR spectrum of 2-c.

Figure S17: DSC curve of 2-c.

Table S1: pH Measurements of activated and not-activated 1-a.

| Mass | Time | Temperature | pHNOT-ACT | pHACT | pH |
| --- | --- | --- | --- | --- | --- |
| mg | min | °C | 1 | 1 | 1 |
| 5.84 | 60.00 | 200.00 | 7.83 | 9.81 | 1.98 |
| 5.84 | 180.00 | 200.00 | 7.83 | 9.56 | 1.73 |
| 5.84 | 60.00 | 180.00 | 7.83 | 10.04 | 2.21 |
| 5.84 | 60.00 | 160.00 | 7.83 | 10.09 | 2.26 |
| 5.84 | 60.00 | 140.00 | 7.83 | 9.22 | 1.39 |
| 5.84 | 60.00 | 120.00 | 7.83 | 8.44 | 0.61 |
| 5.84 | 60.00 | 100.00 | 7.83 | 7.83 | 0.00 |
| 5.84 | 30.00 | 160.00 | 7.83 | 9.95 | 2.12 |
| 5.84 | 90.00 | 160.00 | 7.83 | 10.01 | 2.18 |

Highlighted row indicates the condition at which the highest ΔpH (2.26) was observed for 1-a at 160 °C after 60 min.

Table S2: pH Measurements of activated and not-activated 1-b.

| Mass | Time | Temperature | pHNOT-ACT | pHACT | pH |
| --- | --- | --- | --- | --- | --- |
| mg | min | °C | 1 | 1 | 1 |
| 5.27 | 60.00 | 200.00 | 7.47 | 7.04 | -0.20 |
| 5.27 | 180.00 | 200.00 | 7.47 | 4.59 | -2.65 |
| 5.27 | 60.00 | 180.00 | 7.47 | 8.46 | 1.22 |
| 5.27 | 60.00 | 160.00 | 7.47 | 8.28 | 1.04 |
| 5.27 | 120.00 | 180.00 | 7.47 | 8.81 | 1.57 |
| 5.27 | 180.00 | 180.00 | 7.47 | 7.26 | 0.02 |

Highlighted row indicates the condition at which the highest ΔpH (1.57) was observed for 1-b at 180 °C after 120 min.

Table S3: pH Measurements of activated and not-activated 1-c.

| Mass | Time | Temperature | pHNOT-ACT | pHACT | pH |
| --- | --- | --- | --- | --- | --- |
| mg | min | °C | 1 | 1 | 1 |
| 5.23 | 60.00 | 200.00 | 7.61 | 6.49 | -1.12 |
| 5.23 | 180.00 | 200.00 | 7.61 | 4.95 | -2.66 |
| 5.23 | 60.00 | 180.00 | 7.61 | 8.38 | 0.77 |
| 5.23 | 60.00 | 160.00 | 7.61 | 7.61 | 0.00 |
| 5.23 | 120.00 | 180.00 | 7.61 | 5.55 | -2.06 |
| 5.23 | 30.00 | 180.00 | 7.61 | 8.01 | 0.40 |

Highlighted row indicates the condition at which the highest ΔpH (0.77) was observed for 1-c at 180 °C after 60 min.

Table S4: pH Measurements of activated and not-activated 1-d.

| Mass | Time | Temperature | pHNOT-ACT | pHACT | pH |
| --- | --- | --- | --- | --- | --- |
| mg | min | °C | 1 | 1 | 1 |
| 5.27 | 60.00 | 200.00 | 7.09 | 6.41 | -0.68 |
| 5.27 | 180.00 | 200.00 | 7.09 | 6.31 | -0.78 |
| 5.27 | 60.00 | 180.00 | 7.09 | 6.67 | -0.42 |
| 5.27 | 60.00 | 160.00 | 7.09 | 6.66 | -0.43 |
| 5.27 | 60.00 | 140.00 | 7.09 | 7.20 | 0.11 |
| 5.27 | 60.00 | 120.00 | 7.09 | 7.61 | 0.52 |
| 5.27 | 60.00 | 100.00 | 7.09 | 7.12 | 0.03 |
| 5.27 | 30.00 | 120.00 | 7.09 | 7.41 | 0.32 |
| 5.27 | 120.00 | 120.00 | 7.09 | 7.52 | 0.43 |

Highlighted row indicates the condition at which the highest ΔpH (0.52) was observed for 1-d at 120 °C after 60 min.

Table S5: pH Measurements of activated and not-activated 2-a.

| Mass | Time | Temperature | pHNOT-ACT | pHACT | pH |
| --- | --- | --- | --- | --- | --- |
| mg | min | °C | 1 | 1 | 1 |
| 6.30 | 60.00 | 200.00 | 4.14 | 4.65 | 0.51 |
| 6.30 | 120.00 | 200.00 | 4.14 | 4.93 | 0.79 |
| 6.30 | 180.00 | 200.00 | 4.14 | 4.57 | 0.43 |
| 6.30 | 120.00 | 180.00 | 4.14 | 4.87 | 0.73 |

Highlighted row indicates the condition at which the highest ΔpH (0.79) was observed for 2-a at 200 °C after 120 min.

Table S6: pH Measurements of activated and not-activated 2-b.

| Mass | Time | Temperature | pHNOT-ACT | pHACT | pH |
| --- | --- | --- | --- | --- | --- |
| mg | min | °C | 1 | 1 | 1 |
| 8.94 | 60.00 | 200.00 | 4.80 | 5.50 | 0.70 |
| 8.94 | 120.00 | 200.00 | 4.80 | 6.59 | 1.79 |
| 8.94 | 180.00 | 200.00 | 4.80 | 5.62 | 0.82 |
| 8.94 | 120.00 | 180.00 | 4.80 | 5.63 | 0.83 |

Highlighted row indicates the condition at which the highest ΔpH (1.79) was observed for 2-b at 200 °C after 120 min.

Table S7: pH Measurements of activated and notactivated 2-c.

| Mass | Time | Temperature | pHNOT-ACT | pHACT | pH |
| --- | --- | --- | --- | --- | --- |
| mg | min | °C | 1 | 1 | 1 |
| 11.59 | 60.00 | 200.00 | 7.39 | 8.30 | 0.91 |
| 11.59 | 120.00 | 200.00 | 7.39 | 10.14 | 2.75 |
| 11.59 | 180.00 | 200.00 | 7.39 | 9.66 | 2.27 |
| 11.59 | 120.00 | 180.00 | 7.39 | 7.40 | 0.01 |

Highlighted row indicates the condition at which the highest ΔpH (2.75) was observed for 2-c at 200 °C after 120 min.