Supporting information

Multiple Color Emission of Mechanoluminescence and Photoluminescence from SrZnSO: Bi3+ for multi-mode anti-counterfeiting

Yun-Ling Yang,a Ting Li,c Jia-Yong Yuan,a Yu Zhou,a Qian-Li Li,a Dong-Yun Wan,a Jing-Tai Zhao b and Zhi-Jun Zhang a, *

a School of Materials Science and Engineering, Shanghai University, Shanghai, 200444, P. R. China.

b School of Materials Science and Engineering, Guilin University of Electronic Technology, Guilin, 541004, P. R. China.

c School of Materials Science and Engineering, Guilin University of Technology, Guilin, 541000, P. R. China.

E-mail addresses: zhangzhijun@shu.edu.cn

Fig. S1 (a-f) show XRD Rietveld refinement of Sr1-xBixZnSO (0 ≤ x ≤ 0.1), respectively.

Fig. S2 (a-c) SEM images of Sr1-xBixZnSO. EDS mapping pictures of Sr0.99Bi0.01ZnSO for (d) overlap elements, independent element mapping of (e) Sr, (f) Bi, (g) Zn, (h) S, (i) O.

Fig. S3 (a) Photoluminescence excitation (PLE) spectra of SrZnSO for monitoring emission (613 nm). (b) Photoluminescence emission (PL) spectra of SrZnSO under excitation wavelength of 297 nm.

Fig. S4 (a-d) 3D thermoluminescence spectra of Sr1-xBixZnSO (x = 0.005, 0.02, 0.04 and 0.06 ) after excitation with X-ray for 15 min.

Table S1 ThL peak positions, trap depth, frequency factor and kinetic order of Sr0.999Bi0.001ZnSO.

| Peak | Peak position (°C) | Trap depth (eV) | Frequency factor | Kinetic order |
| --- | --- | --- | --- | --- |
| Fit peak 1 | 81 | 0.72 | 109 | 1.4 |
| Fit peak 2 | 160 | 0.97 | 1010 | 1.3 |
| Fit peak 3 | 229 | 1.02 | 109 | 1.2 |
| Fit peak 4 | 285 | 1.13 | 108 | 2 |