2

2



Two birds, one stone:  long-wavelength carbon dots enables ratiometric detection of ciprofloxacin and Co2+ for smartphone, logic gate, and imaging applications

Yanan Yan a, Hongping Zhang b, Youhong Tang c, Shengmei Song a, Shaomin Shuang a, Chuan Dong a, *

Institute of Environmental Science and College of Chemistry and Chemical Engineering, Shanxi University, Taiyuan 030006, China.   

School of Mechanical Engineering, Institute for Advanced Study, Chengdu University, Chengdu 610106, China

Institute for NanoScale Science and Technology, College of Science and Engineering, Flinders University, South Australia 5042, Australia 

*Corresponding author. E-mail address dc@sxu.edu.cn (C Dong)
Material

Methylene Blue was procured through Aladdin Ltd (Shanghai, China). Antibiotics of Penicillin (PG), Thiamphenicol (THI), Kanamycin (KAN), Clindamycin (CLI), Gentamicin (GEN), Oxytetracycline (OXY), Erythromycin (ERY), Azithromycin (AZM), Clarithromycin (CLR), Ofloxacin (OFL), Difloxacin (DIF), Fleroxacin (FLE), Pefloxacin (PEF), Enoxacin (ENO), levofloxacin (LEV), norfloxacin (NOR) and Ciprofloxacin (CIP) were concocted in the concentration of 0.01 M. Cationic solutions of K+, Ca2+, Na+, Mg2+, Al3+, Zn2+, Cu2+, Hg2+, Ba2+, Cd2+ and Co2+ were formulated in the concentration of 0.1 M. Distilled de-ionized (DDI) water with resistivity higher than 18.25 MΩ/cm was used. 
Quantum yield (Φ) measurements
The Φx of the D-CDs were determined by a comparative method as follows: 

Φx=Φst(Kx/Kst) (ηx/ηst)2 where, the subscripts X and ST denote D-CDs and the reference (Rhodamine B in ethanol). Grad is the gradient from the plot of integrated fluorescence intensity against absorbance and η is the refractive index of the solvent. To prevent the re-absorption effect, a series of solutions of D-CDs and referenced fluorescence dyes were prepared with concentrations adjusted such that the optical absorbance values were between 0-0.1 at 365 nm. The integrated fluorescence intensity was the area under the PL curve in the wavelength range 515-800 nm.

Table S1 Integrated fluorescence intensity against absorbance of Rhodamine B and D-CDs.

	D-CDs
	Rhodamine B

	Abs
	Integrated PL
	Abs
	Integrated PL

	0.0178

	2215.6
	0.0156
	3604.5

	0.0394
	3819.7
	0.0402
	10794

	0.0687
	5892.8
	0.0641
	18421

	0.0801
	7897.5
	0.0817
	26482

	0.0908
	8862.4
	0.0926
	30489


[image: image26.emf]0 100 200 300 400 500 600

0

20

40

60

80

100

Cell Viability(%)

Concentration of CDs(μg/mL)


Figure S1. Plots of integrated fluorescence intensity against absorbance of (a) D-CDs and (b) Rhodamine B at excitation and absorption wavelengths of 365 nm. 

[image: image1.png]@ =

Intergrated fluorescence intensitu (

9000 -
8000
7000 -
6000 -
5000
4000 -
3000 4
2000 4

(b)

Gradient=90298

OAE)Z 063 OAE)4 OAE)S OAE)G 02)7 OAE)S 02)9 0.10
Absorbance

)
w
W
(=3
(=3
(=]

~

30000 4

y (a.u.

25000 4

20000 4

15000 4

10000

5000 -

Intergrated fluorescence intensit

Gradient=351798

0.02 0.04 0.06
Absorbance

0.08

0.10




Figure S2. Effect of continuous irradiation with a xenon arc lamp for 3600 s on fluorescence intensity of D-CDs.

[image: image14]Figure S3. Effect of ionic strength on fluorescence intensity of D-CDs.
[image: image2.jpg]PL Intensity (a.u.)

400

500 600
Wavelength (nm)

700




Figure S4. Effect of different pH on fluorescence intensity of D-CDs.

[image: image3.jpg]P Y
= =& <=

¥ Aa5nm/6620m





Figure S5. The ion selectivity of D-CDs. Comparison of fluorescence intensity of 20 μL, 4.5 mg/mL D-CDs after the addition of 0.1 mol/L metal ions.


[image: image4.emf]OFL DIF FLE PET ENOLEVNOR CIP 

0

1

2

3

4

5

F

445nm/662nm


Figure S6. The fluorescence enhancement effect of different FQs towards D-CDs.
[image: image5.png]



Figure S7 The ratio value F445nm/F662nm of D-CDs (0.45 mg/mL) in the existence of distinct antibiotic (10 mM) before and after the addition of CIP (1 mM).

	Sensing probe 
	Response time
	LOD
	Reference

	CDs/SiDs–BPMA–Cu2+ 
	-
	2 nM
	  [1]

	CDs@Cu2+
	1.5 h
	0.6 M
	[2]

	CD/riboflavin
	1 min
	1.3 μM
	[3]

	CDs/Tb-AMP CPs
	20 min
	7.4 nM
	[4]

	D-CDs
	10 s
	16.8 pM
	This Work


Table S2 Comparison of the ratiometric detection CIP performance of D-CDs prepared in this work with other CDs sensors in the literature.

[image: image15]Figure S8. FTIR spectrum of CIP, D-CDs and CDs/CIP.
[image: image16]
[image: image17]Figure S9. (a) Zeta potential distributions and (b) Zeta potential values of the D-CDs, CDs/CIP and CDs/CIP /Co2+.
Figure S10. UV−vis spectrum of D-CDs (4.5mg/mL) with the addition of various concentrations of CIP. 

Table S3. Comparison of the molecular structures of fluoroquinolones.

	Ofloxacin (OFL)
	
[image: image6.emf]N

O

N

N

H

3

C

F

O

CH

3

OH

O


	Weak hydrogen bond interaction

	Difloxacin (DIF)
	
[image: image7.emf]N

N

N

H

3

C

F

O OH

O

F


	Weak hydrogen bond interaction

	Fleroxacin (FLE)
	
[image: image8.emf]N

N

N

H

3

C

F

O OH

O

F

F


	Weak hydrogen bond interaction

	Pefloxacin (PEF)
	
[image: image9.emf]N

N

N

H

3

C

F

O OH

O


	Weak hydrogen bond interaction

	Enoxacin (ENO)
	
[image: image10.emf]N N

HN

N

F

O OH

O

CH

3


	Weak conjugation system

	Levofloxacin (LEV)
	
[image: image11.emf]N

N

N

OH

O

O

H

3

C

F

O


	Weak hydrogen bond interaction

	Norfloxacin (NOR)
	    [image: image12.emf]N

F

N

HN

O

OH

O

CH

3


	Weak hydrogen bond interaction

	Ciprofloxacin (CIP)
	
[image: image13.emf]N

HN

N

F

O OH

O


	Strong hydrogen bond interaction


Table S4. Calculated adsorption energy (Eads)

	D-CDs/M
	Eads

	D-CDs/OFL
	0.026

	D-CDs/DIF
	0.044

	D-CDs/FLE
	0.038

	D-CDs/PEF
	0.025

	D-CDs/ENO
	0.029

	D-CDs/LEV
	0.032

	D-CDs/NOR
	0.046

	D-CDs/CIP
	0.057


[image: image18]           Figure S11. FTIR spectra of CDs/CIP and CDs/CIP/Co2+
Table S5. Detection of CIP and Co2+ in real samples with fluorescence method. 

	
	Sample
	Added

(nM)
	Found

(nM)
	Recovery

(%)
	RSD

(%)

	CIP detection
	Lake

water
	0.1
	0.102
	102.0
	4.2

	
	
	1
	1.04
	104.2
	3.4

	
	
	2
	2.01
	100.6
	3.8

	
	Milk
	0.1
	0.0970
	97.0
	3.1

	
	
	1
	1.03
	103.2
	4.5

	
	
	2
	2.09
	104.9
	2.8

	Co2+ detection
	Lake

water
	50
	49.9
	99.9
	2.4

	
	
	60
	59.0
	98.4
	1.7

	
	
	70
	69.1
	98.8
	3.0


Table S6. Detection of CIP and Co2+ in real samples with smartphone sensing platform. 
	
	Sample
	Added

(μM)
	Founded

(μM)
	Recovery

(%)
	RSD

(%)

	CIP detection
	Tap
water
	5
	5.2
	104.0
	2.1

	
	
	57
	59.8
	103.5
	2.4

	
	
	208
	218
	104.8
	1.7

	Co2+ detection
	Tap
water
	0.5
	0.48
	96
	2.2

	
	
	13.4
	12.9
	96.2
	2.7

	
	
	22.4
	21.8
	97.3
	3.2


[image: image19]Figure S12. Cytotoxicity test of D-CDs on HeLa cells viability.

Reference
1. 
Gui R, Bu X, He W, Jin H (2018) Ratiometric fluorescence, solution-phase and filter-paper visualization detection of ciprofloxacin based on dual-emitting carbon dot/silicon dot hybrids. New J Chem 42:16217–16225. https://doi.org/10.1039/C8NJ03788D

2. 
Gao X, Sun M, Liu X, et al (2022) A ratiometric fluorescence platform based on carbon dots for visual and rapid detection of copper(II) and fluoroquinolones. Microchim Acta 189:144. https://doi.org/10.1007/s00604-022-05243-3

3. 
Lu C, Liu G, Yang Z, et al (2020) A ratiometric fluorometric ciprofloxacin assay based on the use of riboflavin and carbon dots. Microchim Acta 187:37. https://doi.org/10.1007/s00604-019-3888-5

4. 
Hu Y, Chen X, Wang K, et al (2024) Fluorescent responsive membrane based on terbium coordination polymer and carbon dots with AIE effect for rapid and visual detection of fluoroquinolone. Biosens Bioelectron 254:116205. https://doi.org/10.1016/j.bios.2024.116205


� EMBED Origin95.Graph \* MERGEFORMAT ���





� EMBED Origin95.Graph \* MERGEFORMAT ���





� EMBED Origin95.Graph \* MERGEFORMAT ���





� EMBED Origin95.Graph \* MERGEFORMAT ���





� EMBED Origin95.Graph \* MERGEFORMAT ���





� EMBED Origin95.Graph \* MERGEFORMAT ���









[image: image20.emf]0 500 1000 1500 2000 2500 3000 3500

0

200

400

600

800

1000

1200

1400

1600

1800

FL Intensity (a.u.)

Time (s)

[image: image21.emf]0.0 0.5 1.0 1.5 2.0

0.6

0.7

0.8

0.9

1.0

1.1

1.2

F

445nm/662nm

Concentration of KCl (M)

[image: image22.emf]4000 3500 3000 2500 2000 1500 1000 500

Transmittance (%)

Wavenumber 

(

cm

-1

)

 CIP

 CDs

CDs/CIP

[image: image23.png]Zeta Potential (eV)

14

1

14
24
34
44
.54

64

74

CDs

CDs/CIP

CDs/CIP/Co?*




[image: image24.emf]260 280 300 320 340 360 380 400

0.0

0.1

0.2

0.3

0.4

0.5

Absorbance

Wavenumber (cm

-1

)

 D-CDs

 CDs + 1 μL 1 μM CIP

 CDs + 2 μL 1μM CIP

 CDs + 3 μL 1μM CIP

 CDs + 5 μL 1 μM CIP

 CDs + 7 μL  1 μM CIP

[image: image25.emf]4000 3500 3000 2500 2000 1500 1000 500

Transmittance (%)

Wavenumber (cm

-1

)

 

CDs/CIP/Co

2+

 CDs/CIP

Co-O

Co-N

_1234567893.bin

_1234567897.cdx

_1234567899.cdx

_1234567901.cdx

_1234567902.bin

_1234567903.bin

_1234567900.cdx

_1234567898.cdx

_1234567895.cdx

_1234567896.cdx

_1234567894.bin

_1234567891.bin

_1234567892.bin

_1234567890.bin

