Table 3. Glass transition temperature, melting temperature, and degree of crystallinity (heating rate: 10°C min−1) of P3HB extracted from Bacillus cereus and Azotobacter vinelandii OP under various conditions.

| P3HB sample description | Melting temperature (◦C) |  | Heat melting (J g− 1) |  | Maximum degradation temperature (◦C) |  | Transition enthalpy ΔH (J g− 1) |  | Crystallinity (%) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bacillus cereus |  |  |  |  |  |  |  |  |  |  |
| 100 rpm – 24 h | 163.08 |  | 63.82 |  | 253.19 |  | 464.55 |  | 43.7 |  |
| 100 rpm – 48 h | 162.58 |  | 107.50 |  | 253.43 |  | 454.14 |  | 73.6 |  |
| 250 rpm – 24 h | 149.92 |  | 81.02 |  | 248.84 |  | 483.46 |  | 55.4 |  |
| 250 rpm – 48 h | 154.89 |  | 63.97 |  | 251.37 |  | 520.54 |  | 43.8 |  |
| Azotobacter vinelandii OP |  |  |  |  |  |  |  |  |  |  |  |
| 100 rpm – 48 h |  | 178.79 |  | 97.36 |  | 279.59 |  | 512.80 |  | 66.6 |  |
| 100 rpm – 72 h |  | 177.07 |  | 87.43 |  | 274.73 |  | 541.65 |  | 59.8 |  |
| 250 rpm – 48 h |  | 176.52 |  | 85.16 |  | 263.29 |  | 486.55 |  | 58.3 |  |
| 250 rpm – 72 h |  | 178.02 |  | 59.25 |  | 262.72 |  | 491.29 |  | 40.6 |  |