Electronic Supplementary Material

Compatibilization and toughening of biodegradable poly (lactic acid) / cellulose acetate films by polyamide amine dendrimers

Yansong Huanga,b, Yujuan Jina,b,*, Bo Wanga,b, Huafeng Tiana,b,**, Yunxuan Wengb, Shuang Mena,b

a College of chemistry and materials Engineering, Beijing Technology and Business University, Beijing, P. R. China, 100048.

b Beijing Key Laboratory of Quality Evaluation Technology for Hygiene and Safety of Plastics, Beijing Technology and Business University, Beijing, P. R. China, 100048

* Corresponding author:

Email address: tianhuafeng@th.btbu.edu.cn (H, Tian), jinyujuan@th.btbu.edu.cn (Y, Jin)

Tab.S1 The characteristic group peaks in the PLA/CA blends.

|  | v(C-H) /cm-1 | v(-C=O) /cm-1 | v(C-O-C) /cm-1 |  | v(N-H) /cm-1 |
| --- | --- | --- | --- | --- | --- |
| PLA | 2947 | 1747 | 1180,1128 | 1078,1041 |  |
| CA | 2949 | 1754 | 1237,1161 | 1047 |  |
| PAMAM | 2949 | 1737 | 1177 | 1043 | 1650,1545 |
| PAMAM content (phr) |  |  |  |  |  |
| 0 | 2919 | 1747 | 1180,1128 | 1080,1041 |  |
| 1 | 2925 | 1735 | 1213 | 1028 |  |
| 2 | 2925 | 1735 | 1212 | 1028 |  |
| 3 | 2919 | 1735 | 1213 | 1029 |  |
| 4 | 2949 | 1752 | 1180,1128 | 1080,1042 |  |
| 5 | 2947 | 1747 | 1180,1128 | 1081,1042 |  |

Fig. S1 Statistics of CA particle size in SEM image of PLA/CA blend film with different PAMAM content, (a) 0phr, (b) 1phr, (c) 2phr, (d) 3phr, (e) 4phr, (f) 5phr.

Fig.S2 Statistics of spherulite size of PLA/CA blend systems after isothermal crystallization at 120°C for 30 minutes, (a) 0phr, (b) 1phr, (c) 2phr, (d) 3phr, (e) 4phr, (f) 5phr.

Fig.S3 DSC curves of the rest of the PLA/CA blend system before and after degradation, (a) 0phr, (b) 1phr, (c) 2phr, (d) 3phr, (e) 4phr, (f) 5phr.

Fig.S4 TGA curves of the rest of the PLA/CA blend system before and after degradation, (a) 2phr, (b) 4phr, (c) 5phr.