TGFβ1-Loaded Extracellular Matrix Hydrogels Promote Skeletal Muscle Stem Cell Regeneration via m6A-Mediated Integrin–ERK Signaling

1，2Menghai Zhu, 3Peng Zou, 3Gang Chen,3Chong Lian, 3Benggang Qin

1Department of Foot and Ankle surgery, Center for Orthopaedic Surgery, The Third Affiliated Hospital of Southern Medical University, Guangzhou, Guangdong, PR China.

2 The Central Laboratory, Guangdong Orthopaedic Academy.

3the First Affiliated Hospital of Sun Yat-sen University, Guangzhou, Guangdong, China

Correspondence to: Menghai Zhu, 1248226709@qq.com

Sup Fig. 1. Evaluation of decellularized skeletal muscle ECM hydrogels. (A) Fresh skeletal muscle, decellularized skeletal muscle ECM and hydrogel were stained with Masson’s trichrome. (B) Scanning electron microscopy of cross-sections of fresh skeletal muscle tissue, decellularized skeletal muscle ECM and hydrogel. (C) Quantification of the s-GAG content in fresh skeletal muscle tissue, decellularized skeletal muscle ECM and hydrogel. (D) Quantification of proteins in fresh skeletal muscle tissue, decellularized skeletal muscle ECM and hydrogel.

Sup Fig2 (A) Quantification of bFGF in fresh skeletal muscle tissue, decellularized skeletal muscle ECM and hydrogel. (B) Quantification of bFGF normalized to the protein content in fresh skeletal muscle tissue, decellularized skeletal muscle ECM and hydrogel. (C) Cell viability was determined by an MTT assay.

Sup Fig. 3. (A) Double-sorted SkMSCs were positively stained with antibodies against CD34 and integrin β1 and negatively stained for CD11b and CD45 in freshly sorted SkMSCs.

Sup Fig. 4 (A) Immunofluorescence staining images for antibodies against Pax7 (red) and MyoD (green). Cell nuclei were stained with DAPI (blue). (B) After culture in DMEM with 2% heat-inactivated horse serum, the cells showed more robust expression of MyoD over time, while PAX7 showed the opposite expression pattern. GAPDH was used as an internal control. (C) Quantification of Pax7 and MyoD normalized to GAPDH. (D) Quantitation of Pax7-, MyoD-, desmin-, and MyHC-positive cells. Marker-positive cells are presented as the percentage of the total cell number using triplicate samples. Each bar represents the mean ± standard error of the mean (SEM). *P < 0.05, **P < 0.01, and NS = nonsignificant difference.

Sup Fig. 5. Effects of ECM hydrogels with TGFβ1 treatment on animals. (A) In situ running distance, (B)In situ absolute and (C) specific maximal force. Data are presented as mean ± SEM. *p < 0.05 and **p < 0.01.

Sup Fig. 6 TGFβ1-enhanced ECM hydrogel modulates in vivo outcomes (A) Twitch duration. (B) Half relaxation time. (C) Fatigue resistance. Data are presented as mean ± SEM.  *p < 0.05 and **p < 0.01.