Supplementary Table 2. Method and outcomes characteristics of included studies

| Author/ Year/ Country | Used FFR | Models | Method of decontamination | Decontamination system | Experimental systems | Used organism | Outcomes |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Fisher/2011/US (24) | N95 FFR models | Cardinal N95-ML (Model A) | UVGI | 4, 8, 15, 38 J/m2 | Aerosol application for virus load (medium: 1% ATCC) | MS2 | Biocidal efficacy (Log reduction) |
|  |  | Wilson SAF-T-FIT Plus (Model B) |  | 300, 1000, 3000 J/m2 |  |  |  |
|  |  | 8210 (Model C) |  | 92, 183, 367, 917 J/m2 |  |  |  |
|  |  | 1860 (Model D) |  | 300, 1000, 3000 J/m2 |  |  |  |
|  |  | 1870 (Model F) |  | 471, 941, 1883, 4707 J/m2 |  |  |  |
|  |  | Kimberly-Clark PFR95-174 (Model E) |  | 300, 1000, 3000 J/m2 |  |  |  |
| Lindsley/2015/US (25) | N95 FFR models | 1860, 9210, 1730, Kimberly-Clark 46727 | UVGI | 0, 120, 240, 470, 710 or 950 J/cm2 | Aerosol application (sodium hydrochloride, 200 – 400 nm) | N/A | Filtration performance: + Filter aerosol penetration (%) + Filter airflow resistance (mm H2O) |
| Woo/2012/US (26) | N95 FFR models | 1870 | UVGI | 1.8, 3.6 J/cm2 | Aerosol application and droplet application for virus load (Medium: 100% ATCC) Spraying media: deionized water, beef extract, saliva | MS2 | Inactivation efficiency: IE (PFU control/PFU exposed) |
| Mills/2018/US (27) | N95 FFR models | 1860, 1870, VFlex 1805, Alpha Protech 695, Gerson 1730, Kimberly-Clark PFR, Moldex 1512, Moldex 1712, Moldex EZ-22, Precept 65-3395, Prestige Ameritech RP88020, Sperian HC-NB095, Sperian HC-NB295F, Sperian HC-NB095, Sperian HC-NB295F, U.S. Safety AD2N95A, U.S. Safety AD4N95 | UVGI | 1 J/cm2 | Mucin-soiled droplet application for virus load (Medium: serum-free Eagle’s minimum essential) Sebum-soiled dropket application for virus load (Medium: serum-free Eagle’s minimum essential) | H1N1 | Biocidal efficacy: Log reduction |
| Fisher/2010/US (28) | N95 FFR models | 1860 | UVGI | 3 J/cm2 | Aerosol application (medium: 1% ATCC and 100% ATCC) | MS2 | Biocidal efficacy: Log reduction |
|  |  |  | MGS | 40 seconds |  |  |  |
| Battelle Memorial Institute/2020/US (40) | Surgical N95 | 1860 | VHP | 35%, 120 minutes (10 – 50 cycles) | Droplet and Aerosol application for virus load Aerosol application (sodium hydrochloride) Aerosol application for biological penetration | G. stearothermophilus (For biocidal efficacy) Bacillus atrophaeus (for biological penetration) | Biocidal efficacy: Log reduction Filtration efficacy: + Inert collection efficiency (%) + Biological collection efficiency (%) Inhalation resistance (mm H2O) Fit factor |
| Kenney/2020/US (44) | N95 | 1870 | VHP | 35%, 25 minutes, 1 – 5 cycles |  | Pseudomonas phage phi 6 phage T7 phage T1 | Biocidal efficacy: TCID50 |
|  |  |  | VHP + steam sterilization | 35%, 25 minutes, 1 – 5 cycles; steam sterilization at 275oF (5 minutes) |  |  |  |
| Fisher/2009/US (45) | N95 FFR models | N/A | Sodium hypochlorite (bleach) | 0.0006, 0.006, 0.06 and 0.6%; 10 minutes | Aerosol application (medium: 1% ATCC and 100% ATCC) | MS2 | Biocidal efficacy: Log reduction |
|  |  |  | MGS | 750W; 15s, 30s, 45s, 60s, 75s |  |  |  |
| Vo/2009/US (29) | N95 FFR models | N1105 | Sodium hypochlorite (bleach) | 0.005%, 0.01%, 0.05%, 0.1%, 0.25%, 0.5%, 0.75%; 10 minutes | Droplet application (medium: 100% ATCC) | MS2 | Biocidal efficacy: Log reduction |
|  |  |  | UVGI | 1.44, 2.88, 4.32, 5.76, 7.2 J/cm2 |  |  |  |
| Fischer/2020/US (33) | N95 Particulate models | 9211+/37193 | UVGI | 0.33, 0.99, 1.98 J/cm2 |  | HCoV-19 nCoV-WA1-2020 | TCID50 Half-life of virus |
|  |  |  | Dry heat | 70oC; 10, 20, 30, 60 minutes |  |  |  |
|  |  |  | Ethanol | 70%, 10 minutes |  |  |  |
|  |  |  | VHP | 7 minutes |  |  |  |
| Lin/2018/ Taiwan (30) | N95 FFR models | 8210 | Ethanol | 95%, 80%, 70%, 50% | N/A | Bacillus subtilis | Biocidal efficacy: + Relative survival (%) |
|  |  |  | Sodium hypochlorite (bleach) | 0.54% |  |  |  |
|  |  |  | UVGI | UVA: 1.134, 2.268, 5.67, 11.34, 22.68 J/cm2 UVC: 1.872, 3.744, 9.36, 18.72, 37.44 J/cm2 |  |  |  |
|  |  |  | Autoclave | 121°C, 15 minutes |  |  |  |
|  |  |  | Rice cooker | 149-164°C, 3 minutes |  |  |  |
| Heimbuch/2011/US (31) | N95 Particulate models | P1, P2, P3 | UVGI | 1.44 – 1.8 J/cm2 | Aerosol application and droplet application for virus load (Medium: serum-free Eagle’s minimum essential) | H1N1 | Biocidal efficacy: + Log reduction Physical appearance |
|  |  |  | MGS | 1250 W, 2 minutes |  |  |  |
|  |  |  | WMH | 65 ± 5°C, 85% ± 5% RH, 30 minutes |  |  |  |
| Kumar/2020/Canada (43) | N95 | VFlex 1804, Aura 1870, 1860, 8210, 9210, AO Safety 1054S | Autoclave | 121oC, 15-minute, 1 cycle |  | Vesicular stomatitis SARS CoV-2 | Biocidal efficacy: TCID50 Fit test |
|  |  |  | EtO | 100%, 1 hour |  |  |  |
|  |  |  | LT-HPGP | 59%, 47 min |  |  |  |
|  |  |  | VHP | 35%, 30 minutes, |  |  |  |
|  |  |  | Peracetic acid fogging | 10%, 1 hour |  |  |  |
| Bergman/2010/US (10) | N95 FFR models | N95-A, N95-B, N95-C | UVGI | 4.86 J/cm2 | Aerosol application (sodium hydrochloride, 200 – 400 nm) | N/A | Filtration performance: + Filter aerosol penetration (%) + Filter airflow resistance (mm H2O) Physical appearances |
|  |  |  | Ethylene oxide | 736.4 mg/L, 55°C, 60 minutes |  |  |  |
|  |  |  | HPGP | 59%, 45 - 50°C, 55 minutes |  |  |  |
|  |  |  | VHP | 30%, 125 minutes |  |  |  |
|  | Surgical N95 respirator models | SN95-D, SN95-E, SN95-F | MGS | 2450 MHz, 2 minutes |  |  |  |
|  |  |  | Sodium hypochlorite (bleach) | 0.6%, 30 minutes |  |  |  |
|  |  |  | Liquid hydrogen peroxide | 6%, 30 minutes |  |  |  |
|  |  |  | MHI | 60°C, 80% RH, 30 minutes |  |  |  |
| Viscusi/2007/US (17) | N95 models and P100 models | N/A | Autoclave | 121°C (15 psi), 15 minutes and 30 minutes | Aerosol application (sodium chloride) | NR | Filter performance: + Filter aerosol penetration (%) Physical appearance |
|  |  |  | Isopropanol | 70%, 1 second and 1 minutes |  |  |  |
|  |  |  | Sodium hypochlorite (bleach) | 0.525% and 5.25%, 30 minutes |  |  |  |
|  |  |  | UVGI | 0.432 J/cm2 or 6.912 J/cm2 |  |  |  |
|  |  |  | Liquid hydrogen peroxide | 3% and 6%, 30 minutes |  |  |  |
|  |  |  | Soap and water | 1 g/L, 2 minutes and 20 minutes |  |  |  |
|  |  |  | Ethylene oxide | 725 mg/L or 883 mg/L, 55°C, 60 minutes |  |  |  |
|  |  |  | VHP | 100% |  |  |  |
|  |  |  | Dry heat (Oven) | 80°C and 160°C, 60 minutes |  |  |  |
|  |  |  | Microwave oven irradiation | 2450 MHz, 2 minutes or 4 minutes |  |  |  |
| Visculi/2009/US (16) | N95 models | N95-A, N95-B, N95-C | UVGI | 0.162 – 0.18 J/cm2 | Aerosol application (sodium chloride) | NR | Filtration performance: + Filter aerosol penetration (%) + Filter airflow resistance (mm H2O) Physical appearances |
|  | Surgical N95 respirator models | SN95-D, SN95-E, SN95-F | Ethylene oxide | 55°C and 725 mg/l, 1 hour |  |  |  |
|  | P100 models | P100-G, P100-H, P100-I | VHP | 100%, 55 minutes |  |  |  |
|  |  |  | Microwave oven irradiation | 2450 MHz, 2 minutes |  |  |  |
|  |  |  | Sodium hypochlorite (bleach) | 0.6%, 30 minutes |  |  |  |
| Lin/2017/Taiwan (20) | Electret masks | N95 Gauze Spunlace | Rice cooker | 149 - 164°C, 3 minutes | Droplet application (potassium sodium tartrate tetrahydrate, 14.6nm to 594 nm) | N/A | Filtration performance: + Filter aerosol penetration (%) + Most penetrating particle size (MPS) (nm) + Pressure drop (mmHg) + Filter quality (qf) |
|  |  |  | Autoclave | 121°C, 15 minutes |  |  |  |
|  |  |  | Ethanol | 70%, 10 minutes |  |  |  |
|  |  |  | Isopropanol | 100%, 10 minutes |  |  |  |
|  |  |  | Sodium hypochlorite (bleach) | 0.5%, 10 minutes |  |  |  |
| Fisher/2011/US (18) | Surgical FFR | 1870, 1860, KC PFR95 | Microwave steam bag | MSB X bags, MSB Y bags; 30 min | Droplet application for virus load (medium: 100% ATCC) Aerosol application (sodium chloride) | MS2 | Filtration efficiency (%) Biocidal efficacy: Log reduction Water absorbency (g) |
|  | Particulate FFR | 3M 8210 Cardinal Health Moldex 2200 |  |  |  |  |  |
| Lore/2012/US (32) | N95 FFR models | 1870, 1860 | UVGI | 1.8 J/cm2 | Aerosol application (sodium chloride) | H5N1 | Filter performance: Filter aerosol penetration (%) Biocidal efficacy: Log reduction |
|  |  |  | MGS | 2450 MHz, 2 minutes |  |  |  |
|  |  |  | MHI | 65 ± 5 °C, 3 hours |  |  |  |
| Bergman/2011/US (15) | Surgical N95 respirator models | 1870, 1860, KC PFR95 | UVGI | 1.62 J/cm2 | N/A | N/A | Fit test (FF) Faceseal leakage (FSL) Physical degradation |
|  |  |  | MHI | 60°C, 15 minutes |  |  |  |
|  |  |  | MGS | 2450 MHz, 2 minutes |  |  |  |
| Viscusi/2011/US (11) | N95 | 8210, 8000, Moldex 2200 | UVGI | 3.24 J/cm2 |  | NR | Fit factor Physical appearance |
|  |  |  | MHI | 60°C, 30 minutes |  |  |  |
|  | Surgical N95 respirators | KC PFR95–270, 1870, 1860 | MGS | 2450 MHz, 2 minutes |  |  |  |
| Salter/ 2010/US (19) | Surgical masks | S1, S2, S3 | Ethylene oxide | 54°C, 3 hours | N/A | N/A | Chemical residual: oxidant remaining (mg) |
|  |  |  | VHP | 45 – 55 °C, 55 minutes |  |  |  |
|  |  |  | UVGI | 12.24 or 14.4 J/cm2 |  |  |  |
|  |  |  | Liquid hydrogen peroxide | 3%, 30 minutes |  |  |  |
|  | Particulate masks | P1, P2, P3 | Sodium hypochlorite (bleach) | 0.6%, 30 minutes |  |  |  |
|  |  |  | Mixed oxidants | 10% oxone, 6% NaOCl, 5% Na2CO3; 30 minutes |  |  |  |
|  |  |  | Dimethyl dioxirane | 10% oxone, 10% acetone, 5% Na2CO3; 30 minutes |  |  |  |
| Subhash /2014/US (21) | Elastomeric respirators | 7500 | 2–2-p-diisobutylphenoxyethoxyethyldimethyl ammonium chloride plus 17.2% isopropyl alcohol | 0.28% | NR | H1N1 | Virus recovery by culture and PCR |
|  |  |  | Isopropyl alcohol | 70% |  |  |  |
|  |  |  | Sodium hypochlorite (bleach) | 10% |  |  |  |
| Heimbuch/2014/US (46) | N95 models | 1870, 1860, KC PFR95 | Pamper wipes | 30 seconds | Mucin-soiled aerosol application for virus load (trypticase soy aga) Aerosol application (sodium chloride) | Staphylococcus aureus | Filtration performance: Filter Aerosol Penetration (%) Biocidal efficacy: Log reduction Physical appearance |
|  |  |  | Respirator Cleaning wipes | Benzalkonium chloride, 30 seconds |  |  |  |
|  |  |  | Hype-wipes | 0.9% sodium hypochlorite, 30 seconds |  |  |  |
| Lawrence/2017/US (22) | Half-mask elastomeric respirator models | 6200, 7502, Scott Xcel, Sperian by Honeywell Survivair Blue, North by Honeywell 7700 | Clean with Neutrawash detergent solution. Nonsterile water | 0.5% Potassium polyacrylate in EDTA; 2-3 min | Sebum-soiled droplet application (medium: serum-free Eagle’s minimum essential medium) | H1N1 | Biocidal efficacy: Log reduction |
|  | Powered air-purifying respirator models | Air-Mate, Breathe Easy Turbo, Syntech Maxair 78SP series | Cleaning and disinfection | 0.5% Potassium polyacrylate in EDTA + 0.1% sodium hypochlorite; 21 min |  |  |  |
| Zhang/2013/China (23) | Used simple respirators | N/A | Chlorine | 500 mg/L | N/A |  | Quality rate (%) |
|  |  |  | Machine washing | Cold water (1 min) → Water at 60°C and multi-enzyme cleaner (10 min) → water at 60°C (1 min) → Water at 93°C, 10 minutes → Dry (temperature 90°C, 60 min). |  |  |  |
| Li/2020/US (56) | Surgical facemask; N95 respirator; Cotton cloth mask; Quilted cloth mask | Precept | Steam sterilization | 13-15 min (8-10 minutes of heating and 5 minutes of steam) | Droplet application (phosphate-buffered saline) | MRSA, MS2 phage | Biocidal efficacy (Log reduction) Physical appearance |
|  |  | 1860 | Dry heat | 100°C,15 min |  |  |  |
| Zulauf/2020/US (47) | N95 respirator | 1860 | MGS | 1100w or 1150W, 1 or 3 min | Aerosol application (sodium chloride) | MS2 phage | Biocidal efficacy (Log reduction) Fit test. Physical appearance |
|  |  |  | Dry heat | 105°C, 60 min |  |  |  |
| Wigginton/2020/US (35) | N95 respirator | 1860 | Dry heat | 80-82°C, <10% RH, 30 min | Droplet application | 4 viruses (MS2, phi6, influenza A virus, murine hepatitis virus), 3 bacteria (Escherichia coli, Staphylococcus aureus, Geobacillus stearothermophilus), Fungus (Aspergillus niger) | Biocidal efficacy: + Log reduction. Filtration efficacy Fit test Pressure drop |
|  |  |  | MHI | 80-82°C, 62-66% RH, 30 min |  |  |  |
|  |  |  | EtO | 100%, 1 hour |  |  |  |
|  |  |  | UVGI | 3.8-15.3 µW/cm2, 5 min |  |  |  |
|  |  |  | HPGP | 59%, 24 min |  |  |  |
|  |  |  | VHP | Condition 1: 446-495 ppm, 20 min; Condition 2: 647-659 ppm, 135-150 min |  |  |  |
| Smith/2020/US (34) | N95 | 1860 3M Aura 1870+ industrial 8511 | Ethanol | 70% | Droplet application | SARS-CoV-2 | Biocidal efficacy: + Virus recovery by culture and PCR + Log reduction Fit test |
|  |  |  | UVGI | 0.5, 3.6, 14.3 J/cm2 |  |  |  |
|  |  |  | VHP | 30%, 420 ppm, 60 min |  |  |  |
| Nazeeri/2020/US (61) | N95 FFR models | 3M 8200, 3M 8210 and 3M 8511 | Ethanol-Vacuum | 70% ethanol, followed by vacuum drying to pressures below 6 mBar |  |  | Filtration performance: + Filtration Efficiency (%) |
| Loh/2020/UK (59) | FFP2 and FFP3 respirators models | Honeywell 5321 M/L, 3M Aura 9332+ Gen3, 3M Aura 9320+, 3M 8833, 3M 1873V+, 3M 1863+, 3M 8835, 3M 8810, Alpha Solway S-3V | Dry heat | 85°C, 1 hour |  |  | Fit test Physical appearance |
| Liao/2020/US (37) | N95 FFR models | 8210, 4℃ Air, ESound Onnuriplan | Dry heat | 75℃, 30 min |  |  | Filtration performance + Filtration efficiency (%) + Filter airflow resistance (Pa) Pressure drop (Pa) |
|  |  |  | Steam sterilization | 100℃, 10 min |  |  |  |
|  |  |  | Ethanol | 75% |  |  |  |
|  |  |  | Sodium hypochlorite (bleach) | 2%, 5 min |  |  |  |
|  |  |  | UVGI | 254 nm, 8 W, 30 min |  |  |  |
| Lee/2020/Korea (48) | Face masks | Kleenguard | Ozone gas | 120 ppm, 1 or 5 min | Aerosol Application | HCoV-229E (human coronavirus) | Filtration performance + Filtration efficiency (%) Biocidal efficacy (Log reduction) Physical appearance |
| Cadnum/2020/US (38) | N95 FFR models | 1860S, Moldex 1517, and Kimberly-Clark 46727 | UVGI | Dose: N/A, 1 minute | Droplet application | Methicillin‐resistant S. aureus (MRSA), Bacteriophages MS2 and Phi6, C. difficile | Biocidal efficacy (Log reduction) Physical appearance |
|  |  |  | High-level disinfection cabinet that generates aerosolized peracetic acid and hydrogen peroxide | 21-31 minutes, 1, 2, 3 cycles |  |  |  |
|  |  |  | Dry heat | 70°C, 30 minutes |  |  |  |
| Gil/2020/US (50) | N95 respirator | 3M 1860S | MHI | 60°C, RH 80%, 30 minutes | Droplet application | Methicillin‐sensitive S. aureus (MSSA) | Biocidal efficacy (Log reduction) |
| Schwartz/2020/US (41) | N95 respirator | 3M 1860 | VHP | 35%, 480 ppm, 25 minutes, 30 cycles |  | Geobacillus stearothermophilus spores | Fit test Physical appearance |
| Dennis/2020/US (49) | N95 masks and surgical masks | N/A | Ozone gas | 10 ppm, 20 ppm for 60 minutes each; 20 ppm for 30 min, 3 hours, and 36 hours; 200 ppm for 15, 90, and 720 minutes; 72 - 74 °F; RH 45% – 55% |  |  | Filtration performance: + Filter aerosol penetration (%) Tensile testing (mechanical integrity) |
| Oral/2020/US (42) | N95 respirators | 3M 1860s | VHP | 410 ± 83 ppm, 3 hours |  | SARS‐CoV‐2 | Biocidal efficacy (Log reduction) Filtration performance: + Filter aerosol penetration (%) + Filter airflow resistance (mmH2O Fit test |
| Hossain/2020/India (58) | N95 | Halyard, Peimeware Magnum, Venus-V4420, Venus-V4400 | Ethanol/steam sterilization + recharging | 1000V, 5-60 minutes |  |  | Filtration efficiency (%) |
| Cramer/2020/US (63) | N95 models | 3M 1860, KimberlyClark/Halyard 46767, Gerson 2130, 3M 8210, 3M 9210/37021 | Ionized Hydrogen Peroxide | 7.8%, 15 minutes |  | Geobacillus stearothermophilus spores | Biocidal efficacy: bacterial growth Filtration performance: + Filter aerosol penetration (%) + Filter airflow resistance (mmH2O) Fit test |
| Lin/2020/Taiwan (54) | N95 FFR models | 8210, 1860, SH-2950, 8511 and UVEX-3200 models | Autoclave | 15 min at 121°C under 1.06 kg/cm2 |  |  | Filtration performance: + Filter aerosol penetration (%) + Pressure drop (mmHg) |
|  |  |  | Gamma-radiation | 10, 25 or 30 kGy |  |  |  |
| Price/2020/US (36) | N95 models | 8200, 8210 Plus, 8511, 4C AIR | Dry heat | 75°C, 30 minutes, 5 cycles |  |  | Fit test |
|  |  |  | UVGI | 30 minutes, 8W, 324 nm wavelength, 10 cycles |  |  |  |
| John/2020/US (65) | N95 FFR models | 3M 1860 | Peracetic acid (PAA) | Peracetic acid (0.18%), hydrogen peroxide (0.88%), 12 - 19 minutes, 3 cycles | Droplet application | Bacteriophage MS2, G. stearothermophilus spores | Biocidal efficacy (Log reduction) Filtration performance: + Filter aerosol penetration (%) + Filter airflow resistance (mm H2O) Physical appearance |
| Harskamp/2020/Netherlands (52) | FFP2 and FFP3 respirators | 3M Aura1862+, Maco Pharma ZZM002, 3M Aura 9322, San Huei 2920V, Safe Worker 1016 | Autoclave | 121°C, 17 minutes, 3 cycles |  |  | Filtration performance: + Filter aerosol penetration (%) + Filter airflow resistance (mmH2O) Physical appearance |
| Derr/2020/US (60) | N95 FFR models | 8511, 1860, 1870+, 9211+, Honeywell Sperian N11125 | Aerosolized hydrogen peroxide | 7%, 10 cycles | Droplet application | Geobacillus stearothermophilus spore, SARS-CoV-2, HSV-1, Coxsackie virus B3, Pseudomonas Phi6 Bacteriophage | Biocidal efficacy: growth of virus Fit test result Physical appearance |
| Cramer/2020/US (62) | N95 FFR models | 9105, 8210 | 60Cobalt Gamma Irradiation | 10 kGy, 50 kGy |  |  | Filtration efficiency (%) Fit test |
| Bopp/2020//US (53) | N95 FFR models | 3M 1860, 3M 1805, and 3M 1870/1870+ | Autoclave | 115°C for 1 hour, 121.1°C for 30 minutes, 130°C for 2 minutes, and 130°C for 4 minutes |  | SARS-CoV-2 | Filtration performance: + Filter aerosol penetration (%) + Filtration efficiency Fit test |
| Chen/2020/Canada (39) | N95 FFR models | 1860S, 8210, 9210 | Autoclave | 30 min |  |  | Filtration performance: + Filter aerosol penetration (%) + Filter airflow resistance (mmH2O) Physical appearance |
|  |  |  | Ethanol | 70% |  |  |  |
|  |  |  | Dry heat | 100°C, 30 minutes |  |  |  |
|  |  |  | Humid heat | 75% RH, 75°C, 1 hour |  |  |  |
|  |  |  | HPGP | 59%, 72 min per cycle |  |  |  |
|  |  |  | VHP | 59%, 28 min per cycle |  |  |  |
|  |  |  | UVGI | ~1 J/cm2 |  |  |  |
| Cheng/2020/China (64) | N95 FFR models | 1870+, 1860s | Ionized hydrogen peroxide | 7.8%, 6 seconds |  | H1N1 | Biocidal efficacy (virus recovery) |
| Carrillo/2020/US (55) | N95 | 1870, 1870+ | Immediate-use steam sterilization (IUSS) | N/A |  |  | Fit test Physical appearance |
| Anderegg/2020/US (51) | N95 FFR models | 3M 1860 surgical N95, 3M 1870 surgical N95, 3M 8210 Plus N95, Chen Heng V9501 KN95, HKYQ N95 | Heat and humidity | 85°C, RH 60-85% |  |  | Filtration efficiency Pressure drop Fit test Physical appearance |
| Ma/2020/China (57) | Medical masks and N95 | N/A | Steam sterilization | 100°C | Aerosol application | Avian coronavirus | Filtration efficiency (%) Biocidal efficacy: virus recovery by RT-PCR |
| ATCC: American Type Culture Collection; EDTA: Ethylene diamine tetraacetic acid; EtO: Ethylene oxide; FFP: filtering facepiece; FFR: filtering facepiece respirator; IUSS: Immediate-use steam sterilization; LT-HPGP: Low temperature hydrogen peroxide gas plasma; MGS: Microwave Generated Steam; MHI: Moist heat incubation; MPS: Most penetrating particle size; MRSA: Methicillin-resistant Staphylococcus aureus; MSSA: Methicillin-susceptible Staphylococcus aureus; HPGP: Hydrogen Peroxide Gas Plasma; N/A: not available; NR: not report; PAA: Peracetic acid; PCR: Polymerase Chain Reaction; PFU: plaque forming units; RH: relative humidity; SARS CoV-2: Severe acute respiratory syndrome coronavirus 2; TCID50: 50% Tissue Culture Infective Dose; UV: Ultraviolet; UVGI: Ultraviolet Germicidal Irradiation; VHP: Hydrogen Peroxide Vapor; WMH: warm moist heat |  |  |  |  |  |  |  |