Table 1. Biocidal efficacy, filtration performance and physical appearances of masks after treatments

| Methods | Biocidal efficacy | Filtration performance |  | Physical appearance | Safety concerns |
| --- | --- | --- | --- | --- | --- |
|  | Reduction of survival (organism) | Filter aerosol penetration (%) (mask)* | Filter air flow resistance (mm H2O) (mask) |  |  |
| Gaseous |  |  |  |  |  |
| HPGP (59%, 24– 72 min, 3 cycles) (10, 35, 39, 43) | No recovery (V. stomatitis) > 7.9 log reduction (Phi6) > 3.8 log reduction (influenza) 5.6 log reduction (MS2) | 1.71 - 7.3 (N95) 2.5 - 8.76 (SN95) 0.029 – 14.274 (1860S) < 26 (1860) 0.013 – 42 (8210) 0.027 – 10.108 (9210) | 7.7 - 11.5 (N95) 9 - 14.4 (SN95) Little changes after treatment (1860S, 8210, 9210) |  |  |
| VHP (30%, 125 min, 3 cycles) (10) |  | 0.5 – 1.18 (N95); 0.44 – 2.35 (SN95) | 7.5 – 11.8 (N95); 8.2 – 16.4 (SN95) |  | 0.04-1.77 mg of oxidant residuals |
| VHP (58 – 59%, 25 min, 1 cycle) (17, 39, 43) |  | 0.004 - 0.01 (P100) 0.287 - 0.916 (N95) 0.118 – 0.887 (1860S) 0.109 – 0.277 (8210) 0.098 – 0.541 (9210) | Little changes after treatment (1860S, 8210, 9210) |  |  |
| VHP (100%, 55 min, 1 cycle) (16, 19) |  | 0.071 - 1.47 (N95); 0.542 - 0.727 (SN95); 0.006 - 0.1 (P100) | 6.5 - 9.6 (N95) 6.5 - 8.6 (SN95) 13.4 - 16.2 (P100) | Less shiny and light tarnish nosebands | Trace of oxidant residuals but not significant |
| VHP (35%, 120 min, 10 – 50 cycles) (40) | > 6 log reduction (Geobacillus stearothermophius) |  | 9 - 10 | Made elastic straps stiffer after 30, 40, 50 cycles |  |
| VHP (35%, 20-180 min × 1 cycle OR 120 min 10 – 50 cycles, 3 hours × 1 cycle) (35, 41-44) | No recovery (T1 bacteriophage, T7 Bacteriophage, Pseudomonas phage phi-6, V. stomatitis and SARS-CoV-2, Geobacillus spores) > 6 log reduction (G. stearothermophius) ≥ 2 log reduction (MS2, Bacteriophage phi6, influenza A virus, MHV, E. coli, A. niger) > 1.0 log reduction (S. aureus) | < 1 (1860, 8210, Moldex 1511) 0.99 – 1.50 (1860S) | 17.5 (1860, 8210, Moldex 1511) 9.4 – 10.6 (1860S) | Made elastic straps stiffer after 30, 40, 50 cycles but no physical degradation or odour observed | No residual hydrogen peroxide |
| EtO (725 - 883 mg/L, 1 hour, 1 – 3 cycles) (10, 16, 17, 19, 43) | No recovery (V. stomatitis) >5.8 log reduction (MS2) | 0.101 - 1.77 (N95) 0.003 - 0.008 (P100) 0.25 - 2.55 (SN95) < 1 (1860) | 6.9 - 12 (N95) 12.8 - 15.9 ̣(P100) 6.3 - 16.9 (SN95) | Made P100 straps light dark, no affection for N95 and SN95 | No EtO detected; diacetone alcohol, 2-hydroxyethyl acetate, cyclohexanone found as traces |
| Vapor EtOH (70%, 1-3 cycle) (39) |  | 0.972 – 1.246 (1860S) 0.633 – 1.424 (8210) 1.014 – 2.228 (9210) | Little changes after treatment (1860S, 8210, 9210) |  |  |
| Ozone gas (120 ppm × 1-5 min, 10 – 200 ppm × 60 min) (48, 49) | No recovery (HCoV-229E-influenza A – H1N1 and S. aureus) | 0.7 – 1.4 (KF94) >5 (9210) |  | No visible discoloration or loss of fibres integrity. No affection of mechanical integrity. |  |
| iHP generated by (7.8%, 90 min, 1 – 5 cycles) (63, 64) | 9-log reduction (G. stearothermophilus spores) No recovery H1N1 | 0.53 – 0.67 (1860) 0.11 – 0.22 (KC/Halyard 46767) 1.31 – 2.57 (Gerson 2130) 0.18 – 0.24 (8210) 0.23 – 1.32 (9210/37021) | 9.10 – 10.35 (1860) 14.10 – 15.2 (KC/Halyard 46767) 7.90 – 9.3 (Gerson 2130) 8.85 – 8.95 (8210) | No colour change following seven days of incubation in Releasat medium | H2O2 residual lower than the safety limit |
| Heat and Humidity |  |  |  |  |  |
| MHI (60 - 82oC, 60 - 85% RH, 20 - 30 min × 1 cycle or 15 min × 3 cycles or 1 hour × 1 – 10 cycles) (11, 15, 32, 35, 39, 50) | > 3.4 - 6.8 log reduction (H1N1, H5N1, MS2, phi6, influenza virus) > 2.9 log reduction (S. aureus oxacillin-sensitive strain) > 5.3 log reduction (MRSA) >1.4 log reduction (MHV) <0.3 log reduction (G. stearotherophilus) | 0.43 - 1.04 (N95) 0.58 - 2.16 (SN95) 0.43 - 1.04 (N95) 0.58 - 2.16 (SN95) 0.151 – 0.584 (1860S) 0.231 – 0.7 (8210) 0.945 – 3.239 (9210) | 7.5 - 10.7 (N95) 7.9 - 15.0 (SN95) | A detachment of the inner foam nose cushion on varied models, Stronger odour for N95 model 1860 |  |
| MHI (80-82oC, <10% RH, 30 min × 10 cycles) (35) | 0.05 – 2.3 (MS2) 0.8 – 3.3 (phi6) < 1.0 log reduction (S. aureus, Geobaccilus) | 0.43 - 1.04 (N95) 0.58 - 2.16 (SN95) 0.151 – 0.584 (1860S) 0.231 – 0.7 (8210) 0.945 – 3.239 (9210) 2.1 - 2.27 (Chen Heng V9501 KN95) .02 – 1.12 (HKYQ N95) .37- 1.09 (3M 8210 Plus) .03 - .16 (3M 1870) | 7.5 - 10.7 (N95) 7.9 - 15.0 (SN95) | A detachment of the inner foam nose cushion on varied models, Stronger odour for N95 model 1860 |  |
| Autoclave (121°C, 103 kPa, 15 - 60 min, 1 – 10 cycles) (17, 20, 39, 43, 52-54) | No recovery (V. stomatitis, B. subtilis and SARS-CoV-2) | 2.4 (1 cycle), 18.7 - 34.4 (2 cycles) (N95) 0.059 - 1.426 (P100) 0.195 – 0.315 (1860S) 0.488 – 0.057 (8210) 0.789 – 0.071 (9210) 0.04 (SH-2950) 3 (8511) 5.6 (Aura1862) 10 (San Huei 2920V) 19 (UVEX-3200) 39.7 (Safe Worker 1016) 49.8 (GAUZE) 81.6 (SPUNLACE) | 11 (SH-2950) 7 (8511) 12 (UVEX-3200) Little changes after treatment (Aura1862, San Huei 2920V, Safe Worker 1016, 1860S, 8210, 9210) | No remarkable visual changes were observed in the P100 respirators, though the respirator media itself felt softer. Degraded appearances were observed for N95 masks |  |
| Dry heat (80-85°C, 30 – 60 min) (17, 37, 38) | < 1 log reduction (MS2, Phi6, S. aureus and G. stearothermophillus) > 4 log reduction (MRSA) | 0.008 ± 0.001 (P100) 0.84 ± 0.258 (N95) |  |  |  |
| Dry heat (100°C , 15-30 min × 1 – 3 cycles) (39, 56) | < 3 log reduction (MRSA, MS2) | 0.029 – 0.310 (1860S) 0.010 – 0.156 (8210) 0.036 – 0.024 (9210) | Little changes after treatment (1860S, 8210, 9210) |  |  |
| Dry heat (100°C , 15-30 min × 5 – 10 cycles) (39) | < 3 log reduction (MRSA, MS2) | 0.562 – 9.259 (1860S) 6.638 – 8.107 (8210) 0.046 – 0.265 (9210) | Little changes after treatment (1860S, 8210, 9210) |  |  |
| MGS (1100 – 1150 W, 2 - 75 min) (11, 15, 28, 30-32, 45, 47) | > 4 log reduction (H5N1) 4.23 - 5.94 (H1N1) 4.1 - 6 (MS2) | 0.08 - 1.77 (N95) 0.52 - 2.14 (SN95) 0.006 - 0.009 (P100) | 9.5 - 11.1 (N95) 8.8 - 14.4 (SN95) | A detachment of the inner foam nose cushion on varied models, sometimes caused melting |  |
| MGS (1100 W, 0 – 40 seconds) (28, 45) | < 3 log reduction (MS2) | < 4.5 |  |  |  |
| Microwave steam bag (18) | > 99.86% reduction (MS2) | 0.33 - 0.38 (2810) 0.38 - 0.72 (1860) 1.4 - 4.23 (Moldex 2200) 0.12 - 4.5 (KCPFR95) 0.3 - 1.48 (1870) |  | Not significantly change the filtration performance |  |
| Boiling water steam decontamination (20 – 120 min) (57) | No detection of H120 | 0.046 – 3.627 (MM) 0.018 – 0.038 (N95) |  |  |  |
| Rice cooker steamer (13-15 min) (56) | >5 log reduction (MRSA, MS2) |  |  | No visible changes after 5 cycles |  |
| Rice cooker (149 – 164˚C, 3 min) (20, 30) | > 99.7% reduction (B. subtilis) | 2.5 (N95) 24.9 (GAUZE) 77.1 (Spunlace) 23(Venus 4420) |  |  |  |
| Liquid/chemicals |  |  |  |  |  |
| Liquid hydroperoxide (3 - 6%, 30 min) (17) |  | 0.49 - 1.52 (N95) 0.005 - 0.006 (P100) 0.12 - 3.35 (SN95) | 6.2 - 11.0 (N95) 9.0 - 11.7 (SN95) | No affection if treating with 3% and ink faded if treating with 6% | Trace of oxidant residuals |
| Dimethyl-dioxirane (19) |  |  |  | Metal oxidized and strong odour | 4.53 - 7.72 mg of oxidant residuals |
| Ethanol (70%, 10 min) (20, 30, 34) | 22.3 ± 8% of survival (B. subtilis) No detection of SAR-CoV-2 after treatment | 39 for particle size 445 nm (N95) 61.4 for particle size 496 nm (GAUZE) 80.7 for particles size 400 (Spunlace) |  |  | Impaired mask integrity |
| Ethanol 70% followed by vacuum drying (5 cycles) (61) |  | 4.8 (8200) 3 (8210) 2.8 (8511) |  |  |  |
| Isopropanol (70 - 100%, 10 - 30 min) (17, 20) |  | 17.8 - 21.6 (N95) 0.412 - 0.805 (P100) 71.1 for particle size 414 nm (GAUZE) |  | Ink faded |  |
| Mixed oxidants (19) |  |  |  | Metal oxidized and strong odour | 0.08 - 8.1 mg of oxidant residuals |
| Soap and water (1 g/l, 2 - 20 min) (17) |  | 34.9 - 38.8 (N95) 0.014 - 0.147 (P100) |  | No affection |  |
| 0.5% Neutrawash detergent solution (Potassium polyacrylate and EDTA) (22) | Below detection limit (H1N1) for varied models. |  |  |  |  |
| Chlorine-based (2%, 5 min) (37) |  | 26.9 (N95) | 9 |  |  |
| Sodium hypochlorite 5-10% (19) |  |  |  |  | 0.32 - 1.66 mg of oxidant residuals |
| Sodium hypochlorite 0.25 - 5.25 % , 10 - 30 min (10, 16, 17, 20, 29, 45) | > 3.13 log of reductions (MS2) No survival (B. subtilis) | 0.262 – 18.3 (N95) 0.233 – 4.01 (SN95) 0.004 – 0.027 (P100) 89 for particle size 429 (Spunlace) | 0.68 – 11.4 (N95) 5.9 – 12.1 (SN95) 13.6 – 17 (P100) | Made nosebands tarnished and less shiny, remained bleach smell. Sometimes discoloured and dissolve nose pad, ink faded Strongly damage the structure of Gauze leading to unavailable test for penetration |  |
| Sodium hypochlorite 0.005 - 0.1%, 10 - 30 min (45) | 0.66 - 2.8 log reduction (MS2) | 0.262 - 18.3 (N95) 5.9 - 12.1 (SN95) 0.009 - 0.01 (P100) | 6.9 - 11.4 (N95) 5.9 - 12.1 (SN95) 13.6 - 17 (P100) |  |  |
| Peratic acid (10%), 1 h / cycle (45) | No growth of V. stomatitis and SARS-CoV-2 | No affection of function (N95) |  |  |  |
| Aerosolized hydrogen peroxide 7%, 21 min | Inactivation of HSV-1, CVB3, Phi6. Greater loss of infectiousness with HSV1 and CVB3 |  |  |  |  |
| Aerosolized containing 0.18% peracetic acid, 0.88% hydrogen peroxide, 98.58% water (76 – 87 min) (65) | > 6 log reduction (G. stearothermophilus spores, MS2) . | ≤ 5.0 % |  | Preserved structural integrity, strap elasticity. Bubbles on the surface increase with cycles No change contact angle | No detectable off-gassing of peracetic acid |
| High-level disinfection cabinet 1-3 cycles (40) | 6 log reduction (MRSA) 2-6 log reduction (Bacteriophage MS2) |  |  |  |  |
| Energy |  |  |  |  |  |
| UVGI (120 - 950 J/cm2) (25) |  | Increased ≤ 1.25% (1860, 9210, GE 1730) | Less changed |  |  |
| UV (18.4 J/cm2) (34) |  |  |  | Impaired mask integrity and straps |  |
| UVGI (4.32 - 14.4 J/cm2) (10, 11, 15, 17, 19, 26, 29) | > 3 log (MS2) | 0.072 - 1.77 (N95) 0.34 - 1.86 (SN95) 0.005 - 0.012 (P100) | 7.1 - 11.1 (N95) 6.6 - 17.6 (SN95) 13.1 - 16.5 (P100) | No affection except randomly leading to intolerant odour in N95 MOLDEX 2200 |  |
| UVGI (1.44 - 3 J/cm2) (28, 29) | 0.9 - 2.8 log (MS2) |  |  |  |  |
| UVGI (1 - 1.8 J/cm2) (27, 31) | > 3 - 5.75 log (H1N1) < 1% of relative survival (B. subtilis) |  |  | Photochemical damages on model 8210 |  |
| UV 0.024 J/cm2 (37) | < 3 log reduction (H3N2, phi6, MHV) < 1 S. aureus, G. stearothermophilus |  |  |  |  |
| UV 0.18 J/cm2 (34) | > 4.65 log reduction (H5N1) |  |  |  |  |
| UVGI (30.32 J/cm2, 1 cycle) |  | < 5 (N95) |  |  |  |
| UVGI (30.32 J/cm2, > 20 cycle) |  | 7 (N95) |  |  |  |
| UV (0.63 J/cm2) (34) | Positive detection of SAR-CoV-2 (mask 1860, 8511) No detection of SAR-CoV-2 (1870) |  |  |  |  |
| UV irradiation (0.024 J/cm2) + dry heat (82°C) (10 cycles) + VHP (37) | 2.5-5 log inactivation (MS2) 2.7-3.9 log inactivation (phi6) 2.3-3.1 log inactivation (Influenza) 1-2.1 (MHV) | < 2.5 |  |  |  |
| Gamma irradiation (10, 25, 30, 50 kGy) (54, 62) |  | 14.1 – 75.2 (9105) 20 (UVEX-3200) 30 (SH-2950) 50 (8511) 11.9 – 64.8 (8210) 52 (1860) | 13 (UVEX-3200) 11 (SH-2950) 9 (8511) 11 (8210) 10 (1860) | Taste the saccharin mist Slight unrecognizable odour |  |
| UV-C box (Advanced Ultraviolet Systems, South Hill, VA) (15 min) (38) | 1.12 – 2.16 (MRSA) (1860s) 3.0 – 4.0 (MRSA) (Moldex 1517) 1.3 – 3.7 (MRSA) (Kimberly-Clark 46727) 0.4 – 1.8 (Phi6) (1860s, Moldex 1517) 0.5 – 3.4 (Phi6), (Kimberly-Clark 46727) 0.15 – 3.0 (MS2) (1860s, Moldex 1517, Kimberly-Clark 46727) |  |  | No visible changes were observed |  |
| UV-C box (Advanced Ultraviolet Systems, South Hill, VA) (38) | ≥ 3 log10 reduction (MRSA) (Moldex 1517) | 2.5% |  | No visible changes were observed |  |
| UV-C (2 cycles) 15 min/ cycle using the pulsed-xenon device device (35, 38) | < 3 log10 reduction for (MSRA, Phi6 & MS2) (Moldex 1517) | 2.5% |  | No visible changes were observed |  |
| Microwave oven irradiation (1100 W, 2 min × 1 cycle) (16, 17) |  | 0.105 - 1.460 (N95) 0.652 - 0.711 (SN95) 0 - 0.002 (P100) | 6.2 - 9 (N95) 5.4 - 8.7 (SN95) 13.1 - 15.8 (P100) | No affection on N95, some SN95s and P100s melted during treatment |  |
| Cleaning Wipes |  |  |  |  |  |
| 504/07065 Respirator Cleaning Wipes containing benzalkonium chloride (30 seconds) (46) | Exterior: > 99.72% reduction Interior > 68.92% reduction Fabric > 95.37 (S. aureus) | 1.9 – 4.1 (N95) |  | No affection |  |
| Hype-Wipes containing 0.9% sodium hypochlorite (OCL wipes) (30 seconds) (46) | Exterior: > 99.99% reduction Interior > 98.98% reduction Fabric > 99.99% (S. aureus) | 0.4 – 1.6 (N95) |  | No affection |  |
| Pampers wipes with no active antimicrobial ingredients (INERT) (30 seconds) (46) | Exterior: 59.37 - 98.5% reduction Interior: 69.28 - 90.95 % reduction Fabric: 90.01 - 96.53% reduction (S. aureus) | 0.1 – 2.4 (N95 Kimberly-clark) |  | No affection |  |
| Wipes containing 70% isopropanol (21) | 75% survival (H1N1) |  |  |  |  |
| Wipes containing 0.28% QAC and 17.2% isopropanol (21) | No survival (H1N1) |  |  |  |  |
| Wipes containing 10% sodium hypochlorite and detergent (21) | No survival (H1N1) |  |  |  |  |
| Combinations of methods |  |  |  |  |  |
| UV irradiation (0.024 J/cm2) + dry heat (82oC) (10 cycles) (35) | 0.06 – 1.2 log reduction (S. aureus, G. stearothermophilus) | < 2.5 (1860) | 17.5 (1860) |  |  |
| UV irradiation (0.024 J/cm2) + dry heat (82oC) + low humidity (8% RH) (10 cycles) (35) | 0.3 – 2.1 log reduction (MS2, Phi6) > 3.8 log reduction (influenza) 1.1 (MHV) | < 2.5 (1860) | 17.5 (1860) |  |  |
| UV irradiation (0.024 J/cm2) + moist heat (82 oC, 60 – 66% RH) (35) | > 6.8 log reduction (MS2, Phi6) > 3.3 log reduction (influenza) > 1.4 log reduction (MHV) > 2.7 log reduction (S. aureus) | 2.5 (1860) | 17.5 (1860) |  |  |
| * Measured with particle size 300 nm EDTA: Ethylenediaminetetraacetic acid; EtO: Ethylene oxide; HPGP: Hydrogen peroxide gas plasma; VHP: Hydrogen Peroxide Vapor; MGS: Microwave-generated steam; MHI: Moist heat incubation; QAC: 2–2-pdiisobutylphenoxyethoxyethyldimethyl ammonium chloride (a quaternary ammonium chloride) |  |  |  |  |  |