Explainable GNN Framework Guided by Local Chemical Features to Predict Binding Energies in Bimetallic Alloys

A. F. Usugaa, C. S. Praveenb,c and A. Comas-Vivesa,d,*

a Department of Chemistry, Universitat Autònoma de Barcelona, 08193 Cerdanyola del Vallès, Catalonia, Spain

b International School of Photonics, Cochin University of Science and Technology, University Road, South Kalamassery, Kalamassery, Ernakulam, Kerala, 682022, India

c Inter University Centre for Nano Materials and Devices, Cochin University of Science and Technology, University Road, South Kalamassery, Kalamassery, Ernakulam, Kerala, 682022, India

d Institute of Materials Chemistry, TU Wien, 1060 Vienna, Austria

E-mail: aleix.comas@tuwien.ac.at; aleix.comas@uab.cat

Table S1. Size of supercell of surface model for Ni-Ga-based alloys with their respective side view.

| System | supercell | Side view |
| --- | --- | --- |
| Ni(111) | 2x2x1 |  |
| Ni(211) | 2x3x1 |  |
| Ni3Ga(111) | 2x2x1 |  |
| Ni3Ga(211)Ni-step | 2x3x1 |  |
| Ni3Ga(211)Ga-step | 2x3x1 |  |
| Ni5Ga3(221) | 1x1x1 |  |
| Ni5Ga3(211)Ni-step | 1x1x1 |  |
| Ni5Ga3(211)Ga-step | 1x1x1 |  |

Table S2. Summary of the performance of different Graph Convolutional operators, this test was only performing a training of 100 epoch.

|  | Training set |  |  | Test set |  |
| --- | --- | --- | --- | --- | --- |
|  | MSE [eV] | R2 | Total time [min] | MSE [eV] | R2 |
| GCNConv | 0.03067 | 0.97588 | 1.8722 | 0.04894 | 0.95654 |
| GraphConv | 0.02649 | 0.97914 | 1.5295 | 0.07317 | 0.93536 |
| GATConv | 0.03463 | 0.97287 | 2.3889 | 0.12814 | 0.88759 |
| GraphSAGE | 0.02615 | 0.97940 | 1.5610 | 0.04869 | 0.95715 |

Table S3. Summary of hyperparameter for each ML-based model implemented.

| Algorithm | Parameters |
| --- | --- |
| GNN | - GraphSAGE Dim_output: 512 (Alloys dataset)/256 (Ni-Ga dataset) Agregation: 'mean' Normalize: False - Global_max_pool Dim_output: 512 (Alloys dataset)/256 (Ni-Ga dataset) - Dropout Ratio of dropout: 0.1 - Optimizer Algorithm: Adam Learning rate: 0.001 (Alloys dataset)/0.0005 (Ni-Ga dataset) Epoch: 1000 - Batch size Alloys dataset Training/validation/test set: 64 Ni-Ga dataset Training/validation/test set: 32 |
| GNNExplainer | Algorithm: GNNExplainer Epochs: 1000 Explanation_type: 'phenomenon' Node_mask_type: 'attributes' Edge_mask_type: 'object' Model_config: dict(mode='regression', task_level='graph', return_type='raw') |
| CatBoost | N_estimators: 1500 Learning_rate: 0.1 Depth: 9 Loss_function: 'LogCosh' Silent: True Min_data_in_leaf: 0 L2_leaf_reg: 0.2 |
| UMAP | N_components: 2 N_neighbors: 10 Min_dist: 0 |

Figure S1. UMAP-based 2D dimensionality reduction of pooled graph embeddings on the training set. Visualization of 2D reduced dimension with p-orbital occupancy of the main adsorbate bonding atom on the surface.

Figure S2. UMAP-based 2D dimensionality reduction of pooled graph embeddings on the training set. Visualization of 2D reduced dimension with average atomic radius of the surface atoms.

Figure S3. UMAP-based 2D dimensionality reduction of pooled graph embeddings on the training set. Visualization of 2D reduced dimension with the type of reaction (reaction 0 is for C* + 2O* formation).

Figure S4. UMAP-based 2D dimensionality reduction of pooled graph embeddings on the training set. Visualization of 2D reduced dimension with the average work function of the surface atoms.

Figure S5. UMAP-based 2D dimensionality reduction of pooled graph embeddings on the training set. Visualization of 2D reduced dimension with the step termination of the surface atoms (0 for flat, 1 Ni-termination, and 2 for Ga-termination).

Figure S6. UMAP-based 2D dimensionality reduction of pooled graph embeddings on the training set. Visualization of 2D reduced dimension with d-orbital occupancy of the surface atoms.

Figure S7. Violin plot showing the reaction energy for each reaction step alongside the atomic radius for the training set of the Ni-Ga dataset.