Supporting Information

A strategy to improve the performance of MnCe-MOFs/ZSM-5 for formaldehyde degradation at ambient temperature

Zi-su Yang 1, Qiong Huang 1, *, Xi Tong 1, Jia-xin Shan 1, Chen Wei 1, Jun-jie Mao 1, Bo Yang 1, Da-wei Li 1, Min-dong Chen 1, Tao Tao 2, Hong Yang 3, *, and Bing Li 4
1Jiangsu Collaborative Innovation Center of Atmospheric Environment and Equipment Technologies, Jiangsu Key Laboratory of Atmospheric Environmental Monitoring & Pollution Control, School of Environmental Science & Engineering, Nanjing University of Information Science & Technology, Nanjing 210044, China; 

2School of Chemistry and Materials Science, Nanjing University of Information Science & Technology, Nanjing 210044, China; 

3Department of Geography and Environmental Science, University of Reading, Whiteknights, Reading RG6 6AB, UK;
4Jiangsu Zhongchuang Qingyuan Technology Co., Ltd, Yancheng 224001, PR China

*Corresponding author 1: Dr. Qiong Huang

School of Environmental Science and Engineering, Nanjing University of Information Science & Technology, Nanjing 210044, China

Address: No. 219 Ningliu Road, Nanjing University of Information Science & Technology, School of Environmental Science and Engineering, 210044, Nanjing, China

E–mail: hqhaixia@163.com

Tel: +86 25 58731090     Fax: +86 25 58731090

*Corresponding author 2: Dr. Hong Yang

Department of Geography and Environmental Science, University of Reading, Whiteknights, Reading, RG6 6AB, UK

E–mail: hongyanghy@gmail.com (H. Y.)

Tel: +44 (0)1183787750

In order to explore the reaction mechanism of catalyzed oxidation of HCHO, the MnCe-MOFs-500/ZSM-5 catalyst with the best catalytic oxidation performance was placed in the environment of HCHO/N2 and HCHO/O2 at room temperature for in-situ infrared spectrum analysis (Fig. S1). The experimental results showed that the positions of vibration peaks in the in-situ infrared spectra of catalysts were similar, but the intensities were different under anaerobic and aerobic conditions. The adsorption peaks at wave numbers of 3710 cm-1 and 1660 cm-1 were caused by the bending vibration of H2O adsorbed on the catalyst surface and hydroxyl group on the surface. The peak at the wave number of 3660 cm-1 belongs to the stretching vibration peak ν (OH) of the structural hydroxyl group. In Fif. S1 (a), the strength of the vibration peak decreases gradually with time; in Fig. S1 (b), the strength of the vibration peak is basically unchanged, indicating that hydroxyl (OH) groups will be consumed in the catalytic oxidation process of HCHO. In the presence of O2, it can replenish the consumed groups. The wide peak at the wave number of 3480 cm-1 is the association peak formed by the superposition of hydrogen bond and H2O symmetric stretching and asymmetric stretching vibration, indicating that water will be produced during the reaction of catalyst and HCHO, and water will further participate in the adsorption and dissociation process of HCHO. The peaks at the wave number of 3240 cm-1 correspond to formate C-H stretching vibration peak ν (CH), while the peaks at the wave number of 2840cm-1 and 1060 cm-1 are attributed to the CH stretching vibration peak ν (CH) and CO stretching vibration peak ν (CO) associated with dioxymethylene (DOM). These species are intermediate products of HCHO oxidation process. 

Its peak strength gradually weakens in the HCHO/N2 environment, and gradually becomes stronger in the HCHO/O2 environment, indicating that the presence of O2 can produce reactive oxygen species on the catalyst surface, thus oxidizing and decomposing HCHO. The peak at 2340 cm-1 is the adsorption peak of CO2, indicating that the catalytic reaction process of HCHO will produce CO2. The peak at 1560cm-1 corresponds to COO asymmetric stretching vibration ν (COO), the peak at 1460 cm-1 corresponds to CH bending vibration δ (CH), and the peak at 1360 cm-1 corresponds to COO symmetric stretching vibration νs (COO).

[image: image1.png](a) HCHO/N,

3660

)

: 60m1n

Absorbance Intensity (a.

4000 3500

3710 3480 3240

3000

Wavenumber (cm'l)

2500

2000

1500

1000



[image: image2.png](b) HCHO/O,

Absorbance Intensity (a.u.)

4000

3660
3710 3480
ini 3240 2840

Omll:

3500

3000 2500 2000
Wavenumber (cm'l)

1500

1000



 

Fig. S1 The in situ FTIRs of MnCe-MOFs-500/ZSM-5 catalysts
