Supporting Information

Moisture-induced surface degradation mechanism of argyrodite Li6PS5Cl under dry-room conditions

Yoon-Seong Kim1, Jeong-Doo Yi2, Sihyeon Sung3, Dong-Hwa Seo1*

1 Department of Materials Science and Engineering, Korea Advanced Institute of Science and Technology (KAIST), 291, Daehak-ro, Yuseong-gu, Daejeon 34141, Republic of Korea

2 Korea Automotive Technology Institute (KATECH), 303, Pungse-ro, Pungse-myeon, Cheonan-si, Chungcheongnam-do 31214, Republic of Korea

3 Samsung SDI, 882, Dongtanwoncheon-ro, Yeongtong-gu, Suwon-si, Gyeonggi-do 16677, Republic of Korea

*Correspondence and requests for materials should be addressed to Dong-Hwa Seo (dseo@kaist.ac.kr)

Table of contents

- Supplementary Figure 1 | Difference in ionic conductivity between the pristine and 3-day dry room exposed Li6PS5Cl (LPSC).

- Supplementary Figure 2 | Difference in the X-ray diffraction (XRD) pattern between the pristine and the 7-day dry room exposed LPSC.

- Supplementary Figure 3 | X-ray photoelectron spectroscopy (XPS) analysis detection for initial surfaces.

- Supplementary Table 1 | Theoretical reaction energies (Ereaction) of three possible reaction equations based on bulk structures.

- Supplementary Table 2 | Lattice parameters of structures used in computational simulations.

- Supplementary Figure 4 | Structural definition for atomic layers of the LPSC surface.

- Supplementary Figure 5 | S-O substitution energy (Esub) values depending on the case of oxygen substitution.

- Supplementary Figure 6 | Bond elongation after the 2nd layer-substitution (LPSCO).

- Supplementary Figure 7 | Atomic definition for the oxygen and sulfur sites from the third to the fifth layers of the fully O-substituted LPSC at the first three layers (LPSCO123).

- Supplementary Figure 8 | Relative stability of the structures, where S-O exchange occurs between the oxygen at the third atomic layer and non-bonding sulfur or the broken P–S bonding site in the layers below, compared to the LPSCO123.

- Supplementary Figure 9 | Phase distribution of LPSC surface depending on the etching beam intensity.

- Supplementary Figure 10 | XPS depth analysis of LPSC5d.

- Supplementary Figure 11 | XPS depth analysis of the 3-minute etched LPSC25d.

Supplementary Figure 1 | Difference in ionic conductivity between the pristine and 3-day dry room exposed Li6PS5Cl (LPSC).

Supplementary Figure 2 | Difference in the XRD pattern between the pristine and the 7-day dry room exposed LPSC.

Supplementary Figure 3 | X-ray photoelectron spectroscopy (XPS) analysis detection for initial surfaces. Phase distributions of initial surfaces depending on the dry room exposure time, non-exposure (LPSC), 5-day exposure (LPSC5d), and 25-day exposure (LPSC25d), in a S 2p spectra and b P 2p spectra.

| Reaction equations | Ereaction [eV / formula unit] |
| --- | --- |
| (1) Li6PS5Cl + 6H2O → LiCl + Li3PO4 + 2LiOH + 5H2S | –6.222 |
| (2) 2LiOH + CO2 → Li2CO3 + H2O | –1.465 |
| (3) Li6PS5Cl + 4H2O + 2O2 → LiCl + Li3PO4 + Li2SO4 + 4H2S | –18.991 |

Supplementary Table 1 | Theoretical reaction energies (Ereaction) of three possible reaction equations based on bulk structures.

| Structure | Lattice parameters (Å) |  |  |
| --- | --- | --- | --- |
|  | a | b | c |
| LPSC-bulk | 10.255 | 10.255 | 10.255 |
| LPSC-slab | 10.255 | 10.255 | 44.389 |

Supplementary Table 2 | Lattice parameters of structures used in computational simulations.

Supplementary Figure 4 | Structural definition for atomic layers of the LPSC surface.

Supplementary Figure 5 | S-O substitution energy (Esub) values depending on the case of oxygen substitution. Esub values for a 1st layer-substituted and b 2nd layer-substituted LPSC structures.

Supplementary Figure 6 | Bond elongation after the 2nd layer-substitution (LPSCO).

Supplementary Figure 7 | Atomic definition for the oxygen and sulfur sites from the third to the fifth layers of the fully O-substituted LPSC at the first three layers (LPSCO123).

Supplementary Figure 8 | Relative stability of the structures, where S-O exchange occurs between the oxygen at the third atomic layer and the sulfur at the non-bonding site or the broken P–S bonding site in the layers below, compared to the LPSCO123.

Supplementary Figure 9 | Phase distribution of LPSC surface depending on the etching beam intensity. The distribution of decomposition products depending on the beam intensity in a S 2p spectra and b P 2p spectra.

Supplementary Figure 10 | XPS depth analysis of LPSC5d. The change in decomposition phase compositions of LPSC5d after 3 minutes of etching with the 0.5 kV beam in a S 2p spectra and b P 2p spectra.

Supplementary Figure 11 | XPS depth analysis of the 3-minute etched LPSC25d. The change in decomposition phase compositions of the 3-minute etched LPSC25d after an additional 40 minutes of etching with the 1.0 kV beam in a S 2p spectra and b P 2p spectra.