Supporting Information

Single-atom Pt Doped Nanoceria for Enhanced Cell Phagocytosis and Nanozyme Activities in Keratitis Immune Regulation

Jianguo Zhao1, #, Wanqing Lou2, #, Yixin Wang3, #, Lu Wang4, Xiaoqian Jin1, Chenyang Wang4, Jinjin Zhang5, Wenjuan Zhuang5, Jiayi Wei4, Dajun Lin4, Yishun Guo1, Yi Shao5, *, Zipei Jiang1, * and Bailiang Wang4, *

Figure S1. The fringe spacing of (a) CeO2 and (b) single-atom Pt/CeO2 processed by Digital Micrograph. According to the direction of vertical stripes, the average of five peaks is lattice fringe spacing.

Figure S2. XPS Ce3d spectra of CeO2 and single-atom Pt/CeO2 with different Pt doping ratios. The proportion of Ce3+ is marked on the right side of the corresponding image.

Figure S3. XPS O1d spectra of CeO2 and single-atom Pt/CeO2 at different doping ratios. The values on the right of figure correspond to OSur/(OAds+ OSur+ OLat).

Figure S4. XPS Pt4f spectra of single-atom Pt/CeO2 at different doping ratios.

Figure S5. (a) TEM and (b) HRTEM images of single-atom Pt/CeO2 with Pt doping at 1:7. (Scale bar = 5 nm, 2 nm in enlarged image).

Figure S6. The multienzyme-mimetic abilities of single-atom Pt/CeO2 at different Pt-doping ratios. (a) H2O2, (b) and (c) DPPH-scavenging activities of single-atom Pt/CeO2 nanozymes at different Pt doping ratios.

Figure S7. The diagram of bubbles produced by decomposition of H2O2 into O2 at the presence of CeO2 and single-atom Pt/CeO2.

Figure S8. DPPH• removal efficiency of single-atom Pt/CeO2 at different concentrations.

Figure S9. The cellular uptake of CeO2 and single-atom Pt/CeO2 by HCECs through fluorescence staining after 0.5 h and 12 h incubation. The green fluorescence represents the location of CeO2 and single-atom Pt/CeO2. A representative image of three biological replicates from each group is shown. (Scale bar = 50 µm)

Figure S10. Representative 3D fluorescent images of cellular phagocytosis to CeO2 and single-atom Pt/CeO2 by HCECs. (Scale bar = 50 µm)

Figure S11. Cell survival rate of HCECs after incubation with different concentrations of H2O2.

Figure S12. Biocompatibility experiments. Slit-lamp images and H&E staining observation of corneas after CeO2 and single-atom Pt/CeO2 drops treatments for 7 days. (Scale bar = 50 µm)

Figure S13. Corneal penetration of FITC labeled single-atom Pt/CeO2 on the eye surface of healthy mice. (Scale bar = 200 µm)