Supporting information

Enhanced Carrier Dynamics Resulted from Non-Volatile Chloride Additive for Improved Average Efficiency of PSCs

Zheng Zhang, Haimin Li*, Haohui Li, Bo An, Yuhao Wei, Jiao Liao, Xiangxue Lv, Xingchong Liu, Hanyu Wang

School of New Energy and Materials, Southwest Petroleum University, Chengdu 610500, P. R. China

*Corresponding author: Haimin Li, Email: lucialee@126.com (H. L.), Tel: (+86)28-83037409

Figure S1. SEM histogram of grain number of perovskite films different PbCl2 contents.

Figure S2. AFM diagram, 3D AFM diagram and RMS of PbI2 films with different PbCl2 contents.

Figure S3. SEM diagram of PbI2 films with different PbCl2 contents.

Figure S4. SEM cross-section of perovskite films with different PbCl2 contents.

Figure S5. Thickness diagram of target device with different molar concentration.

Figure S6. The statistical diagram of VOC, JSC, FF and PCE parameters of control devices with different molar concentrations.

Figure S7. The statistical diagram of VOC, JSC, FF and PCE parameters of target devices with different molar concentrations.

Figure S8. Full XPS spectra of control and target perovskite films

Figure S9. Ultraviolet-visible absorption spectra and Tauc-plots of perovskite films with different PbCl2 contents.

Figure S10. The statistical diagram of VOC, JSC, FF and PCE parameters of different PbCl2 contents devices under 1.4 mM process.

Figure S11. Hysteresis diagram of control and target optimal device.

Supplementary Table

Table S1. Parameter table for the preparation of perovskite films with different thicknesses

| Lead halide precursor concentration (mmol/mL) | Concentration of FAI (mg/mL) | Concentration of MACl (mg/mL) |
| --- | --- | --- |
| 1.2 | 50 | 5.0 |
| 1.3 | 60 | 6.0 |
| 1.4 | 75 | 7.5 |
| 1.5 | 90 | 9.0 |

Table S2. Fs-TA carrier kinetics plots fitting results chart at 790 nm wavelength.

| Samples | τ0 (ps) |  | τ1 (ps) | A1 | τ2 (ps) |  | A2 | τ3 (ps) |  | A3 | τave (ps) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0% PbCl2 |  | 0.33 | 88.9 | 0.32 |  | 236 | 0.20 |  | 950 | 0.48 | 840.8 |
| 5% PbCl2 |  | 0.37 | 6.56 | 0.43 |  | 819 | 0.21 |  | 841 | 0.36 | 828.5 |
| 10% PbCl2 |  | 0.46 | 693 | 0.20 |  | 8.23 | 0.30 |  | 1300 | 0.50 | 1190.1 |

Note: The fitting of TA carrier dynamics curve is consistent with the following formula:

y=y0+A1exptτ1+A2exptτ2+A3exptτ3

where A1, A2 and A3 are the relative amplitudes and τ1, τ2 and τ3 are the time constants. Average lifetime τave=a1τ1+a2τ2+a3τ3, where ai=AiτiAiτi.

Table S3. TRPL plots fitting results chart.

| Samples | A1 | τ1（ns） | A2 | τ2（ns） | τave（ns） |
| --- | --- | --- | --- | --- | --- |
| 0% PbCl2 | 0.37 | 61.27 | 0.63 | 325.56 | 188.17 |
| 5% PbCl2 | 0.28 | 114.54 | 0.72 | 838.90 | 571.92 |
| 10% PbCl2 | 0.85 | 20.25 | 0.15 | 144.07 | 19.71 |

Note: The fitting of TRPL plots conforms to the following equation:

y=y0+A1exptτ1+A2exptτ2

where A1 and A2 are the relative amplitudes and τ1 and τ2 are the time constants. Average lifetime τave=a1τ1+a2τ2, where ai=AiτiAiτi.

Table S4. EIS plots fitting results chart.

| Samples | Rs（Ω） | Rtr（Ω） | Ctr（F） | Rrec（Ω） | Crec（F） |
| --- | --- | --- | --- | --- | --- |
| Control | 2.92 | 1.46×104 | 2.94×10-8 | 8289 | 3.65×10-7 |
| Target | 1.76 | 1.14×105 | 5.49×10-7 | 9097 | 5.78×10-8 |

Table S5. Parameter table of optimal device hysteresis test results for control and target.

| Samples | Scan direction | JSC (mA/cm2) | VOC (V) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| Target | Forward | 24.79 | 1.15 | 80.59 | 23.15 |
|  | Reverse | 23.53 | 1.15 | 79.81 | 21.74 |
| Control | Forward | 23.79 | 1.12 | 78.08 | 20.88 |
|  | Reverse | 21.59 | 1.11 | 71.59 | 17.23 |