Table 1 Test results of main indicators of asphalt

| Evaluation indicators | High elasticity modifier | Virgin asphalt | H-asphalt |
| --- | --- | --- | --- |
| Penetration (25℃)/0.1mm | 10 | 65 | 40.5 |
| Ductility (15℃)/cm | — | ＞100 | 60.6 |
| Softening point/◦C | 128 | 52.5 | 78 |
| 60℃ Dynamic viscosity/Pa•s | — | 186.8 | 9700 |
| Density (15℃) g/cm3 | 0.98 | 1.033 | 1.042 |
| Mass loss after thin film oven test /% | — | -0.01 | -0.10 |
| Flash point/℃ | 236 | 270 | 275 |
| Morphology |  |  |  |