Supplementary Information

Cellulose Carbamate Synthesis and Dissolution from Wheat Straw: Influence of Biomass Origin and Inorganic Removal Compared to Softwood Dissolving Pulps

Ryen M. Fraziera, Mariana Lendewiga, Fernando Urdanetaa, Jorge Francoa, Jannatun Nayeema, Alfonso Domingueza, Ericka Fordb, Joel J. Pawlaka, Richard Vendittia, Orlando J. Rojasc,d,e, Ronalds Gonzaleza,*

a 	Department of Forest Biomaterials, North Carolina State University, Raleigh, NC 27695, USA.

b 	Department of Textile Engineering, Chemistry and Science, The Nonwovens Institute, North Carolina State University, Raleigh, NC 27695, USA.

c  	Bioproducts Institute, Department of Chemical & Biological Engineering, The University of British Columbia, Vancouver, BC Canada V6T 1Z3.

d	 Department of Wood Science, Faculty of Forestry, The University of British Columbia, 2900–2424 Main Mall Vancouver, BC Canada V6T 1Z4.

e 	Department of Chemistry, 2036 Main Mall. Vancouver, The University of British Columbia, Vancouver, BC Canada V6T 1Z1.

*Corresponding author, rwgonzal@ncsu.edu, Department of Forest Biomaterials, North Carolina State University, Raleigh, NC 27695, USA, phone number: 919-802-5219.

S.1 ZnO / sodium hydroxide solvent preparation

A 0.7% ZnO / 8% NaOH solution was prepared and left in a freezer overnight to cool to -10 to -5°C. To achieve this solution, first a 20% NaOH aqueous solution was mixed with the ZnO until transparent, then diluted with the remaining water to reach 8% NaOH.

Immediately after adding CC samples to the cold alkali, they were stirred using a vortex mixer for 1 minute, then placed in a freezer. After 30 minutes, the samples were stirred again for 1 minute on the vortex mixer, then placed into a freezer overnight. Agitation and freezing were repeated 24 hours later, for three more cycles, with 1 minute agitation time and 30-minute freezing time.

S.2 Pulp fiber analysis

Table S.1 Fiber quality analysis of softwood and WS DPs, including fiber length, width, and fines content

| DP | Length Weighted Fibers (mm) | Width Arithmetic (um) | Length Weighted % Fines | Arithmetic % Fines |
| --- | --- | --- | --- | --- |
| Softwood | 0.546 | 23.5 | 38 | 65.5 |
| WS PHK | 0.283 | 18.9 | 53.5 | 75.9 |
| WS PHK + EDTA | 0.263 | 17.4 | 60 | 80.2 |

Fig. S.1 Microscopic images of the a) softwood, b) WS, and c) WS + EDTA DPs prior to derivatization and dissolution. Epidermis cells are present in the WS pulps with and without EDTA

Table S.2 Experimental results of softwood and WS carbamates

| DP biomass | Pulping | Experiment (replicates) | Derivatization time (h) | Avg. DS | Soluble fraction (%) in %0.7 ZnO / 8% NaOH |
| --- | --- | --- | --- | --- | --- |
| Softwood | PHK | 1S(1, 2, 3) | 0 | 0.07 +/- 0.04 | 85.3 +/- 0.92 |
|  |  |  | 1 | 0.17 +/- 0.02 | 86.9 +/- 1.95 |
|  |  |  | 2 | 0.29 +/- 0.10 | 90.4 +/- 2.04 |
|  |  |  | 4 | 0.46 +/- 0.06 | 87.5 +/- 1.34 |
|  |  |  | 6 | 0.86 +/- 0.16 | 75.0 +/- 6.20 |
| WS | PHK | 1W(1, 2, 3) | 0 | 0.03 +/- 0.01 | 82.2 +/- 0.85 |
|  |  |  | 1 | 0.09 +/- 0.01 | 89.6 +/- 1.23 |
|  |  |  | 2 | 0.17 +/- 0.01 | 91.3 +/- 2.06 |
|  |  |  | 4 | 0.43 +/- 0.18 | 81.1 +/- 4.67 |
|  |  |  | 6 | 0.76 +/- 0.20 | 77.9 +/- 4.15 |
| WS | PHK + EDTA | 2W(1, 2, 3) | 0 | 0.04 +/- 0.02 | 82.9 +/- 2.12 |
|  |  |  | 1 | 0.16 +/- 0.05 | 88.3 +/- 1.12 |
|  |  |  | 2 | 0.27 +/- 0.08 | 89.1 +/- 0.21 |
|  |  |  | 4 | 0.53 +/- 0.13 | 80.1 +/- 1.66 |
|  |  |  | 6 | 0.64 +/- 0.20 | 76.0 +/- 1.46 |

Fig. S.2 FTIR Spectra of a) 1,3,5-Triazine-2,4,6-Triol (C3H3N3O3, Cyanuric Acid) and b) 1,3,5-Triazine (C3H3N3) (ChemicalBook, 2017a; ChemicalBook, 2017b)

a)

b)

S.3 References

ChemicalBook, 2017a. 1,3,5-Triazine(290-87-9) IR1. https://www.chemicalbook.com/SpectrumEN_108-80-5_IR1.htm

ChemicalBook, 2017b. Cyanuric acid(108-80-5) IR1. https://www.chemicalbook.com/SpectrumEN_290-87-9_IR1.htm