Supplementary Material

Conductive, superhydrophobic, and microwave-absorbing cotton fabric by dip-coating of aqueous silk nanofibers stabilized MWCNTs and octadecanoyl chain bonding

Ling Liua, Mingyuan Wua,b, Qingyun Wua,b, Jiuyi Liua,b, Jianjun Yanga,b, Jianan Zhang*a, b, c

a School of Chemistry and Chemical Engineering, Anhui University;

b Anhui Province High Performance Engineering Laboratory of Water-based Polymer Materials;

c Institute of Physical Science and Information Technology, Anhui University, Hefei 230601, China

Corresponding Author: Jianan Zhang, * E-mail: jianan@ahu.edu.cn.

ORCID, Jianan Zhang: 0000-0003-3195-9882.

Ling Liu: C19201060@stu.ahu.edu.cn;

MingYuan Wu: 93125@ahu.edu.cn

Qingyun Wu: wuqingyun@ahu.edu.cn;

Jiuyi Liu: 16060@ahu.edu.cn;

Jianjun Yang: 87006@ahu.edu.cn;

Address: 111 Jiulong, Hefei 230601, Anhui, P. R. China

Tel: +86 551 63861745; Fax: +86 551 63861745

1. The wetting behavior movies of MWCNTs-CF and C18-MWCNTs-CF

The hydrophilicity of CF was enhanced by the disposition of SNFs stabilized MWCNTs, and the water droplets were quickly absorbed so that the contact angle can’t be captured.

Movie S1. The wetting behavior movie of MWCNTs-CF.

The octadecanoyl chain-tethered C18-MWCNTs-CF was expected to enable the hydrophilic CF with superhydrophobic characteristics after the active sites of CF and SNFs were reacted with stearoyl chloride. Therefore, C18-MWCNTs-CF displayed superhydrophobicity with a WCA of about 154° due to the increased surface roughness induced by hydrophobic octadecanoyl chain.

Movie S2. The wetting behavior movie of C18-MWCNTs-CF.