Supplementary information

Green-Synthesized Iron Oxide-Chitosan Nanocomposite for Chromium and Nanoplastics Remediation

Shouvik Mahanty1,2, Gopala Krishna Darbha2,3*, Richard Paul4, Ramin Boroujerdi4, Eugenia Valsami-Jones5, Santanu Majumder4*

1Department of Atomic Energy, Saha Institute of Nuclear Physics, Sector 1, AF Block, Bidhannagar, Kolkata 700064, West Bengal, India

2Environmental Nanoscience Laboratory, Department of Earth Sciences, IISER Kolkata, Mohanpur, West Bengal, Pincode- 741246, India

3Center for Climate & Environmental Studies, IISER Kolkata, Mohanpur, West Bengal, Pincode- 741246, India

4Department of Life and Environmental Sciences, Bournemouth University (Talbot Campus), Fern Barrow, Poole BH12 5BB, UK

5School of Geography, Earth and Environmental Sciences, University of Birmingham, Edgbaston, Birmingham B15 2TT, UK

*Corresponding Authors

Dr. Gopala Krishna Darbha, Associate Professor, Indian Institute of Science Education and Research (IISER) Kolkata, Mohanpur, West Bengal, Pin- 741246, India

Email: gkdarbha@iiserkol.ac.in

Dr. Santanu Majumder, Department of Life and Environmental Sciences, Bournemouth University (Talbot Campus), Fern Barrow, Poole BH125BB, UK

Email: smajumder@bournemouth.ac.uk

Fig S1: Sampling location

Fig S2: SEM-EDX mapping of a) IO-NPs b) C – Chitosan c) IO-NPs+C

| Fitted models | Equation | Parameters and significance |
| --- | --- | --- |
| Kinetic models |  |  |
| Pseudo 1st order |  | qe = Equilibrium sorption capacity (mg/g) qt = Sorption capacity at time= t (mg/g) K1, K2 are respective rate constants c= resistance in mass transfer |
| Pseudo 2nd order |  |  |
| Isotherm models |  |  |
| Langmuir |  | Ci (mg/L)= Initial concentration Ce (mg/L) = equilibrium concentration, qe = sorption capacity at equilibrium (mg/g), qm = obtained maximum sorption capacity (mg/g) and KL, Kf are Langmuir (L/mg), Freundlich (mg/g) (L/mg)1/n |
| Freundlich | qe=KFCen |  |
| Thermodynamic equations |  |  |
| Gibbs free energy | ΔG= -RTlnKL | R is the universal gas constant (8.314 J K-1 mol-1); T is the absolute temperature (Kelvin) KL= Ca/Ce Ca= (Ce-Ci)/Ce ΔG= Gibbs free energy ΔS= entropy ΔH= enthalpy of system |
| Vent Hoff’s equation | lnKL= ΔS/R-ΔH/RT |  |

Table S1- Fitted kinetic, isotherm and thermodynamic models (1-6).

Fig. S3: a) Desorption of NPs and Cr ions in different concentration of NaOH d) adsorption efficiency of IO-NPs and IO-NPs+C for the adsorption of NPs and Cr ions. For all the experiments (p < 0.0001; two-way ANOVA and Tukey’s multiple comparisons test)

Fig S4: Comparative analysis of the Isotherm, Kinetics and Thermodynamics parameters for the adsorption of NPs and Cr ions by mycosynthesized IO-NPs and IO-NPs+C

Table S2: CCD for adsorption of NPs and Cr by IO-NPs+C.

| Sl No | Variables |  |  |  | Response 1 |  | Response 2 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Actual | Predicted | Actual | Predicted |
|  | A: adsorbent dose (mg/L) | B: temp (C) | C: pH | D: time (min) | % Cr removed |  | % NPs removed |  |
| 1 | 75 | 25 | 5.5 | 90 | 85.21 | 85.47841 | 93.12 | 93.15991 |
| 2 | 100 | 15 | 3 | 120 | 60.78 | 61.84763 | 63.21 | 62.57896 |
| 3 | 100 | 15 | 8 | 120 | 35.23 | 34.99773 | 36.14 | 36.81021 |
| 4 | 50 | 15 | 8 | 60 | 5.12 | 5.274534 | 13.22 | 12.85679 |
| 5 | 75 | 25 | 5.5 | 90 | 85.21 | 85.47841 | 93.12 | 93.15991 |
| 6 | 50 | 35 | 3 | 60 | 89.21 | 89.20703 | 91.22 | 91.33974 |
| 7 | 75 | 25 | 5.5 | 90 | 85.21 | 85.47841 | 93.12 | 93.15991 |
| 8 | 100 | 35 | 8 | 120 | 76.13 | 76.27533 | 78.15 | 77.64441 |
| 9 | 50 | 35 | 8 | 60 | 65.11 | 64.47213 | 69.86 | 69.88599 |
| 10 | 75 | 5 | 5.5 | 90 | 1.11 | 0.989908 | 2.23 | 2.611215 |
| 11 | 100 | 35 | 3 | 120 | 98.12 | 97.73023 | 99.11 | 100.2632 |
| 12 | 75 | 25 | 5.5 | 90 | 85.21 | 85.47841 | 93.12 | 93.15991 |
| 13 | 75 | 25 | 5.5 | 30 | 21.11 | 21.72496 | 28.23 | 28.25448 |
| 14 | 50 | 15 | 3 | 120 | 47.12 | 46.92858 | 45.53 | 45.55148 |
| 15 | 50 | 35 | 8 | 120 | 70.23 | 70.22128 | 71.26 | 71.60193 |
| 16 | 100 | 15 | 8 | 60 | 20.11 | 19.41358 | 22.23 | 21.83928 |
| 17 | 75 | 25 | 10.5 | 90 | 38.22 | 38.57551 | 41 | 40.89491 |
| 18 | 50 | 35 | 3 | 120 | 90.11 | 91.23618 | 91.23 | 91.01568 |
| 19 | 100 | 15 | 3 | 60 | 50.21 | 49.98348 | 49.2 | 49.64803 |
| 20 | 50 | 15 | 3 | 60 | 35.12 | 35.40443 | 37.56 | 37.46054 |
| 21 | 75 | 25 | 5.5 | 150 | 40.12 | 39.33826 | 43.11 | 42.90135 |
| 22 | 100 | 35 | 8 | 60 | 70.23 | 70.18618 | 70.32 | 71.08848 |
| 23 | 75 | 45 | 5.5 | 90 | 96.12 | 96.07011 | 97.89 | 97.32462 |
| 24 | 100 | 35 | 3 | 60 | 95.23 | 95.36108 | 96.12 | 95.74723 |
| 25 | 75 | 25 | 5.5 | 90 | 85.21 | 85.47841 | 93.12 | 93.15991 |
| 26 | 50 | 15 | 8 | 120 | 20.22 | 20.51868 | 23.22 | 22.98773 |
| 27 | 75 | 25 | 5.5 | 90 | 85.21 | 85.47841 | 93.12 | 93.15991 |
| 28 | 25 | 25 | 5.5 | 90 | 78.92 | 78.51846 | 80.12 | 80.41293 |
| 29 | 125 | 25 | 5.5 | 90 | 98.92 | 99.15156 | 99.12 | 98.6429 |
| 30 | 75 | 25 | 3 | 90 | 95.21 | 93.09698 | 98.12 | 97.8021 |

1. Final euation in terms of coded factor the removal of NPs and Cr by IO-NPs analysed in RSM interface:

%Cr Removed = +85.47+5.16  A+23.77  B-12.90  C+4.40  D-2.11  A  B -0.11  A  C +0.085  A  D +1.35  B C -2.37  B  D +0.93  C  D +0.84  A2 -9.24  B2 -5.28  C2 - 13.74  D2                                                                                                               (S 3)

%NPs Removed = +93.16 +4.56  A +23.68  B -11.81  C +3.66  D -1.94  A  B -0.80  A  C +1.21  A  D +0.79  B  C -2.10  B  D + 0.51  C  D - 0.91  A2 -10.80  B2 -7.16  C2 -14.40  D2                                                                                                       (S 4)

Where A is IO-NPs+C dose, B is temperature, C is pH, and D is time.

Table S3: ANOVA for the interacting factors of RSM for NPs and Cr by IO-NPs+C

| Adsorbent | Source | Sum of Squares | df | Mean Square | F Value | p-value Prob > F |
| --- | --- | --- | --- | --- | --- | --- |
| Cr | Model | 26302.48 | 14 | 1878.749 | 2797.979 | < 0.0001 |
|  | A-Adsorbent Concentration | 638.6017 | 1 | 638.6017 | 951.0554 | < 0.0001 |
|  | B-Temp | 13560.31 | 1 | 13560.31 | 20195.07 | < 0.0001 |
|  | C-pH | 3120.165 | 1 | 3120.165 | 4646.794 | < 0.0001 |
|  | D-time | 464.816 | 1 | 464.816 | 692.2403 | < 0.0001 |
|  | AB | 70.98063 | 1 | 70.98063 | 105.7099 | < 0.0001 |
|  | AC | 0.1936 | 1 | 0.1936 | 0.288324 | 0.5992 |
|  | AD | 0.1156 | 1 | 0.1156 | 0.172161 | 0.6841 |
|  | BC | 29.10603 | 1 | 29.10603 | 43.34696 | < 0.0001 |
|  | BD | 90.15503 | 1 | 90.15503 | 134.2659 | < 0.0001 |
|  | CD | 13.8384 | 1 | 13.8384 | 20.60922 | 0.0004 |
|  | A2 | 19.6619 | 1 | 19.6619 | 29.28204 | < 0.0001 |
|  | B2 | 2382.434 | 1 | 2382.434 | 3548.106 | < 0.0001 |
|  | C2 | 455.8179 | 1 | 455.8179 | 678.8395 | < 0.0001 |
|  | D2 | 5269.138 | 1 | 5269.138 | 7847.212 | < 0.0001 |
| NPs | Model | 26798.61 | 14 | 1914.187 | 5939.756 | < 0.0001 |
|  | A-Adsorbent Concentration | 498.4994 | 1 | 498.4994 | 1546.853 | < 0.0001 |
|  | B-Temp | 13455.92 | 1 | 13455.92 | 41753.98 | < 0.0001 |
|  | C-pH | 2614.695 | 1 | 2614.695 | 8113.449 | < 0.0001 |
|  | D-time | 321.7873 | 1 | 321.7873 | 998.5119 | < 0.0001 |
|  | AB | 60.5284 | 1 | 60.5284 | 187.8207 | < 0.0001 |
|  | AC | 10.27202 | 1 | 10.27202 | 31.87428 | < 0.0001 |
|  | AD | 23.4256 | 1 | 23.4256 | 72.69007 | < 0.0001 |
|  | BC | 9.9225 | 1 | 9.9225 | 30.7897 | < 0.0001 |
|  | BD | 70.81222 | 1 | 70.81222 | 219.7316 | < 0.0001 |
|  | CD | 4.1616 | 1 | 4.1616 | 12.91352 | 0.0027 |
|  | A2 | 23.0207 | 1 | 23.0207 | 71.43367 | < 0.0001 |
|  | B2 | 3255.635 | 1 | 3255.635 | 10102.3 | < 0.0001 |
|  | C2 | 839.755 | 1 | 839.755 | 2605.775 | < 0.0001 |
|  | D2 | 5786.323 | 1 | 5786.323 | 17955.07 | < 0.0001 |

Table S4: R2 and Adequate Precision for RSM model for NPs and Cr by IO-NPs+C

| IO-NPs from fungal isolates | Adsorbent | R2 | Adjusted R2 | Predicted R2 | Adequate Precision |
| --- | --- | --- | --- | --- | --- |
| Aspergillus iranicus (STSP9) | Cr | 0.999 | 0.999 | 0.998 | 169.41 |
|  | NPs | 0.999 | 0.999 | 0.998 | 243.26 |

Fig. S5: RSM optimization of Cr ions and NPs adsorption (a - b) on IO-NPs+C shows predicted % removal vs experimental % removal as calculated from RSM analysis.

Fig. S6: RSM optimization of Cr ions and NPs adsorption using desirability function.

Fig. S7: ANN modelling of NPs and Cr ions adsorption (a - b) on IO-NPs+C shows predicted % removal vs. experimental % removal as calculated from ANN analysis.

Table S5: R2 of ANN model for simultaneous NPs and Cr ion removal using IO-NPs+C

| Algorithm selected for hidden layer | Selected Functions |  |  | IO-NPs from fungal isolates | Correlation coefficient (R2) for heavy metal ion adsorption |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Output Layer | Transfer 1 | Transfer 2 |  | NP | Cr |
|  | Levenberg-Marquardt backpropagation | Trainlm | Poslin | Aspergillus iranicus (STSP9) | 0.963 | 0.988 |

2. COPR water quality

Table S6: General characteristics of COPR Cr-contaminated groundwater

| pH | 7.6 | Temperature (C) | 21.8 |
| --- | --- | --- | --- |
| ORP (mV) | -38.3 | EC (µs/cm2) | 1368 |
| TDS (mg/L) | 684 |  |  |
| Cr(total) (mg/L) | 12.68± 1.2 | Cr(VI) (mg/L) | 10.96± 1.01 |
| Borewell Depth | 40 ft |  |  |
| SO4 (mg/L) | 172 | NO3 (mg/L) | 5.26 |
| Total Alkalinity (mg/L) | 210 | Total Hardness (mg/L) | 170 |
| Other Metal/metalloid content (mg/L) |  |  |  |
| Na | 129.48 ± 1.2 | Mg | 52.68 ± 0.3 |
| K | 12.46 ± 0.1 | Mn | 0.018 ± 0.01 |
| Co | 0.015 ± 0.01 | Cu | 0.003 ± 0.001 |
| Zn | 0.037 ± 0.01 | As | 0.003 ± 0.001 |
| Ca | 81.54 ± 1.9 | Pb | 0.011 ± 0.001 |
| Fe | 0.015 ± 0.01 | Hg | 0.007 ± 0.001 |

References:

- Simonin, J. P., & Bouté, J. (2016). Intraparticle diffusion-adsorption model to describe liquid/solid adsorption kinetics. Revista mexicana de ingeniería química, 15(1), 161-173.

- Wamba, A. G., Lima, E. C., Ndi, S. K., Thue, P. S., Kayem, J. G., Rodembusch, F. S., & De Alencar, W. S. (2017). Synthesis of grafted natural pozzolan with 3-aminopropyltriethoxysilane: preparation, characterization, and application for removal of Brilliant Green 1 and Reactive Black 5 from aqueous solutions. Environmental Science and Pollution Research, 24, 21807-21820.

- Liu, Y., & Shen, L. (2008). A general rate law equation for biosorption. Biochemical Engineering Journal, 38(3), 390-394.

- Boparai, H. K., Joseph, M., & O’Carroll, D. M. (2011). Kinetics and thermodynamics of cadmium ion removal by adsorption onto nano zerovalent iron particles. Journal of hazardous materials, 186(1), 458-465.

- Ayawei, N., Ebelegi, A. N., & Wankasi, D. (2017). Modelling and interpretation of adsorption isotherms. Journal of chemistry, 2017(1), 3039817.

- Chen, X. (2015). Modeling of experimental adsorption isotherm data. information, 6(1), 14-22.