# Supporting Information

# Molecular Structure, Interactions and Antimicrobial Properties of Curcumin-PLGA Complexes – A DFT Study

Mahendiraprabu Ganesan, Selvarengan Paranthaman*

Department of Physics and International Research Centre, Kalasalingam Academy of Research and Education (Deemed to be University), Krishnankoil – 626 126, India

*Corresponding Author: Email. psrengan@hotmail.com

Chemical hardness (η) and Chemical potential (µ):

The chemical hardness (η) and chemical potential (µ) are calculated using the highest occupied molecular orbital (EHOMO) and the lowest unoccupied molecular orbital (ELUMO) energies. They are,

where I = ‒EHOMO and A = ‒ELUMO, where I and A are the ionization potential and electron affinity of the molecules respectively.

Fukui function:

The condensed Fukui functions are calculated using the NBO atomic charges:

f+ = q(N + 1) – q(N)

f- = q(N) – q(N – 1)

f0 = ½ [q(N + 1) – q(N – 1)]

were f+, f-, and f0 are the nucleophilic, electrophilic, and radical attacks, respectively.

Interaction energy:

The interaction energies were calculated using the following equation

Eint(AB) = E(AB) − E(A) − E(B)

where E(AB) is the energy of the complex, E(A) and E(B) are the energies of the isolated monomers A and B respectively.

Dual Descriptor(∆f):

The equation for Dual Descriptor(∆f) is:

∆f = f+ − f-

where ∆f is defined as the difference between the nucleophilic and electrophilic Fukui function. Two situations need to be considered: if ∆f > 0, then the site is favored for a nucleophilic attack, whereas if ∆f < 0, then the site may be favored for an electrophilic attack.

AIM analysis:

Earlier Rozas et al. have studied the strength of the H–bond interactions [1]. They have reported that the interactions may be classified as follows: (i) for strong H-bonds (2ρBCP) < 0, HBCP< 0 and covalent in nature, (ii) for medium H-bonds (2ρBCP) > 0, HBCP< 0 and partially covalent in nature and (iii) for weak H-bonds (2ρBCP) > 0 and HBCP> 0 and electrostatic in nature. The van der Waals interactions are characterized when the sum of van der Waal's radii of these atoms is lesser than the distance between interacting atoms. The relation between Laplacian and the energy of bond interactions were expressed by the viral theorem:

¼(2ρ(rBCP))  = 2G(rBCP) + Vρ(rBCP) = H(rBCP)

where ρ(rBCP) is the electron energy density, G(rBCP) is the electron kinetic energy density, Vρ (rBCP) is the electron potential energy density and H(rBCP) is the total electron density at BCP. Earlier, Espinosa [2] proposed the proportionality between H-bond energy (EHB) and electron potential energy density (VBCP) at H···O contact by the following equation, EHB = ½(VBCP) a.u.

RDG analysis:

The NCI index is based on the reduced density gradient (RDG or s(r)), which is a function of the electron density ρ(r) and its first derivative ∇ρ(r) [3, 4],

RDG= s(r)=12(3π2)1/3∇ρ(r)ρ(r)4/3

The NCI index is elucidating weak interactions in regions where QTAIM-defined BCPs are absent. Using plots of RDG against ρ(r), the NCI index can be efficiently applied to identify regions with noncovalent interactions as RDG approaches zero at low densities [5].

NBO analysis:

The stabilization energy (E(2)) associated with the delocalization donor (i) to acceptor (j) orbitals is determined by using follow equation:

E(2)=qiFij2Ej-Ei

Where qi is the donor orbital occupancy; Ej, Ei are diagonal elements (orbital energies) and F(i,j) off diagonal element, respectively associated with NBO Fock matrix.

Table S1 Calculated bond length value of Curcumin, LA and SSC using M06-2X/6-31+G* level of theory and compared with the available experimental data

| SSC | M06-2X | Expa | Deviation | Curcumin | M06-2X | Expc | Deviation |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C1–C2 | 1.512 | 1.495 | -0.017 | C7–O1 | 1.367 | 1.366 | -0.001 |
| C1‒H3 | 1.097 | 1.097 | 0.000 | C7=C11 | 1.406 | 1.417 | 0.011 |
| C1‒H4 | 1.098 | 1.097 | -0.001 | C7–C13 | 1.385 | 1.377 | -0.008 |
| C1‒O6 | 1.398 | 1.406 | 0.008 | C8–O2 | 1.367 | 1.366 | -0.001 |
| C2=O5 | 1.208 | 1.21 | 0.002 | C8=C12 | 1.406 | 1.417 | 0.011 |
| O6‒H7 | 0.973 | 0.956 | -0.017 | C8–C14 | 1.386 | 1.377 | -0.009 |
| C2–O8 | 1.339 | 1.349 | 0.010 | C9–C19 | 1.462 | 1.457 | -0.005 |
| O8–H9 | 0.974 | 0.989 | 0.015 | C10–C20 | 1.463 | 1.457 | -0.006 |
| LA | M06-2X | Expb | Deviation | C11–O3 | 1.353 | 1.364 | 0.011 |
| O1–H11 | 0.972 | 0.82 | -0.152 | C12–O4 | 1.354 | 1.364 | -0.010 |
| O2–H12 | 0.974 | 0.79 | -0.184 | C13=C9 | 1.408 | 1.410 | 0.002 |
| C4–01 | 1.404 | 1.425 | 0.021 | C14=C10 | 1.408 | 1.410 | 0.002 |
| C4–C5 | 1.525 | 1.521 | -0.004 | C15–C9 | 1.398 | 1.401 | 0.003 |
| C4–C6 | 1.518 | 1.519 | 0.001 | C15=C17 | 1.392 | 1.388 | -0.004 |
| C4–H7 | 1.101 | 0.96 | -0.005 | C16–C10 | 1.399 | 1.401 | 0.002 |
| C5–H8 | 1.094 | 0.98 | -0.114 | C16=C18 | 1.391 | 1.388 | -0.003 |
| C5–H9 | 1.092 | 0.96 | -0.132 | C17–C11 | 1.388 | 1.379 | -0.009 |
| C5–H10 | 1.093 | 1.02 | -0.073 | C18–C12 | 1.389 | 1.379 | -0.01 |
| C6–O2 | 1.34 | 1.32 | -0.02 | C19=C23 | 1.343 | 1.348 | 0.005 |
| C6–O3 | 1.209 | 1.208 | -0.001 | C20=C24 | 1.345 | 1.348 | 0.003 |
| C6–C4 | 1.518 | 1.519 | 0.001 | C21–O5 | 1.251 | 1.312 | 0.061 |
|  |  |  |  | C22–O6 | 1.328 | 1.316 | -0.008 |
|  |  |  |  | C21–C23 | 1.476 | 1.450 | -0.026 |
|  |  |  |  | C22–C24 | 1.457 | 1.450 | -0.007 |
|  |  |  |  | C21–C25 | 1.444 | 1.392 | -0.052 |
|  |  |  |  | C22=C25 | 1.374 | 1.403 | 0.029 |
|  |  |  |  | C26–O1 | 1.414 | 1.440 | 0.026 |
|  |  |  |  | C27–O2 | 1.415 | 1.440 | 0.025 |

Note: a Ref No:[6], b Ref No:[7], c Ref No: [8].

Table S2. Calculated condensed Fukui functions of Cur using M06-2X/6-31+G* level of theory.

|  | f+1 | f0 | f-1 | Δf |
| --- | --- | --- | --- | --- |
| O1 | -0.577 | -0.603 | -0.604 | -0.604 |
| O2 | -0.575 | -0.596 | -0.598 | -0.598 |
| O3 | -0.738 | -0.788 | -0.795 | -0.795 |
| O4 | -0.741 | -0.779 | -0.791 | -0.791 |
| O5 | -0.215 | -0.732 | -0.841 | -0.841 |
| O6 | -0.703 | -0.827 | -0.876 | -0.876 |
| C7 | 0.156 | 0.397 | 0.153 | 0.153 |
| C8 | 0.172 | 0.365 | 0.162 | 0.162 |
| C9 | 0.628 | 0.354 | 0.553 | 0.553 |
| C10 | 0.743 | 0.554 | 0.726 | 0.726 |
| C11 | -0.264 | 0.158 | -0.307 | -0.307 |
| C12 | -0.213 | -0.015 | -0.248 | -0.248 |
| C13 | 0.195 | -0.583 | 0.259 | 0.259 |
| C14 | 0.138 | -0.468 | 0.159 | 0.159 |
| C15 | -0.419 | -0.271 | -0.562 | -0.562 |
| C16 | -0.442 | -0.353 | -0.557 | -0.557 |
| C17 | -0.222 | -0.269 | -0.184 | -0.184 |
| C18 | -0.239 | -0.266 | -0.197 | -0.197 |
| C19 | -0.748 | -0.081 | -0.761 | -0.761 |
| C20 | -0.642 | -0.349 | -0.800 | -0.800 |
| C21 | -0.584 | 0.538 | -0.422 | -0.422 |
| C22 | 0.038 | 0.563 | 0.107 | 0.107 |
| C23 | 0.367 | -0.414 | 0.242 | 0.242 |
| C24 | -0.234 | -0.218 | -0.175 | -0.175 |
| C25 | 0.728 | -0.453 | 0.505 | 0.505 |
| C26 | -0.255 | -0.293 | -0.257 | -0.257 |
| C27 | -0.259 | -0.294 | -0.260 | -0.260 |
| H28 | 0.576 | 0.564 | 0.552 | 0.552 |
| H29 | 0.573 | 0.563 | 0.552 | 0.552 |
| H30 | 0.592 | 0.650 | 0.644 | 0.644 |
| H31 | 0.262 | 0.255 | 0.240 | 0.240 |
| H32 | 0.260 | 0.252 | 0.239 | 0.239 |
| H33 | 0.247 | 0.241 | 0.233 | 0.233 |
| H34 | 0.241 | 0.237 | 0.231 | 0.231 |
| H35 | 0.284 | 0.262 | 0.233 | 0.233 |
| H36 | 0.279 | 0.262 | 0.237 | 0.237 |
| H37 | 0.248 | 0.266 | 0.239 | 0.239 |
| H38 | 0.270 | 0.261 | 0.235 | 0.235 |
| H39 | 0.274 | 0.224 | 0.180 | 0.180 |
| H40 | 0.249 | 0.228 | 0.192 | 0.192 |
| H41 | 0.294 | 0.238 | 0.195 | 0.195 |
| H42 | 0.201 | 0.200 | 0.197 | 0.197 |
| H43 | 0.200 | 0.200 | 0.198 | 0.198 |
| H44 | 0.229 | 0.209 | 0.187 | 0.187 |
| H45 | 0.202 | 0.200 | 0.198 | 0.198 |
| H46 | 0.199 | 0.199 | 0.196 | 0.196 |
| H47 | 0.226 | 0.209 | 0.190 | 0.190 |

Table S3. Natural bond orbital (NBO) charges (in e) of Cur and Cur-complexes calculated at M06-2X/6-31+G* level of theory.

| Cur | q | Cur-SSC | q | Cur-AAT | q | Cur-LA | q | Cur-PLGA | q |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O1 | -0.577 | O1 | -0.576 | O1 | -0.577 | O1 | -0.576 | O1 | -0.577 |
| O2 | -0.577 | O2 | -0.577 | O2 | -0.575 | O2 | -0.576 | O2 | -0.576 |
| O3 | -0.712 | O3 | -0.710 | O3 | -0.710 | O3 | -0.710 | O3 | -0.712 |
| O4 | -0.712 | O4 | -0.710 | O4 | -0.709 | O4 | -0.711 | O4 | -0.709 |
| O5 | -0.676 | O5 | -0.667 | O5 | -0.754 | O5 | -0.718 | O5 | -0.673 |
| O6 | -0.729 | O6 | -0.725 | O6 | -0.720 | O6 | -0.720 | O6 | -0.728 |
| C7 | 0.256 | C7 | 0.256 | C7 | 0.262 | C7 | 0.256 | C7 | 0.253 |
| C8 | 0.258 | C8 | 0.255 | C8 | 0.257 | C8 | 0.255 | C8 | 0.248 |
| C9 | -0.112 | C9 | -0.115 | C9 | -0.118 | C9 | -0.109 | C9 | -0.103 |
| C10 | -0.109 | C10 | -0.120 | C10 | -0.122 | C10 | 0.033 | C10 | -0.128 |
| C11 | 0.301 | C11 | 0.303 | C11 | 0.312 | C11 | 0.305 | C11 | 0.302 |
| C12 | 0.299 | C12 | 0.304 | C12 | 0.306 | C12 | 0.301 | C12 | 0.299 |
| C13 | -0.276 | C13 | -0.273 | C13 | -0.264 | C13 | -0.278 | C13 | -0.280 |
| C14 | -0.278 | C14 | -0.273 | C14 | -0.273 | C14 | -0.327 | C14 | -0.284 |
| C15 | -0.212 | C15 | -0.215 | C15 | -0.211 | C15 | -0.213 | C15 | -0.218 |
| C16 | -0.214 | C16 | -0.210 | C16 | -0.209 | C16 | -0.265 | C16 | -0.209 |
| C17 | -0.282 | C17 | -0.281 | C17 | -0.286 | C17 | -0.282 | C17 | -0.281 |
| C18 | -0.280 | C18 | -0.281 | C18 | -0.280 | C18 | -0.281 | C18 | -0.284 |
| C19 | -0.138 | C19 | -0.139 | C19 | -0.094 | C19 | -0.123 | C19 | -0.129 |
| C20 | -0.154 | C20 | -0.131 | C20 | -0.128 | C20 | -0.160 | C20 | -0.163 |
| C21 | 0.498 | C21 | 0.489 | C21 | 0.510 | C21 | 0.546 | C21 | 0.500 |
| C22 | 0.430 | C22 | 0.426 | C22 | 0.442 | C22 | 0.436 | C22 | 0.409 |
| C23 | -0.320 | C23 | -0.336 | C23 | -0.342 | C23 | -0.345 | C23 | -0.329 |
| C24 | -0.293 | C24 | -0.315 | C24 | -0.310 | C24 | -0.314 | C24 | -0.303 |
| C25 | -0.462 | C25 | -0.474 | C25 | -0.460 | C25 | -0.474 | C25 | -0.455 |
| C26 | -0.327 | C26 | -0.328 | C26 | -0.334 | C26 | -0.328 | C26 | -0.327 |
| C27 | -0.327 | C27 | -0.328 | C27 | -0.328 | C27 | -0.328 | C27 | -0.327 |
| H28 | 0.528 | H28 | 0.529 | H28 | 0.531 | H28 | 0.529 | H28 | 0.528 |
| H29 | 0.528 | H29 | 0.529 | H29 | 0.529 | H29 | 0.529 | H29 | 0.529 |
| H30 | 0.557 | H30 | 0.555 | H30 | 0.557 | H30 | 0.563 | H30 | 0.557 |
| H31 | 0.250 | H31 | 0.252 | H31 | 0.257 | H31 | 0.258 | H31 | 0.248 |
| H32 | 0.249 | H32 | 0.252 | H32 | 0.250 | H32 | 0.250 | H32 | 0.252 |
| H33 | 0.247 | H33 | 0.245 | H33 | 0.244 | H33 | 0.246 | H33 | 0.269 |
| H34 | 0.246 | H34 | 0.244 | H34 | 0.246 | H34 | 0.246 | H34 | 0.261 |
| H35 | 0.263 | H35 | 0.263 | H35 | 0.262 | H35 | 0.263 | H35 | 0.263 |
| H36 | 0.263 | H36 | 0.263 | H36 | 0.264 | H36 | 0.263 | H36 | 0.268 |
| H37 | 0.259 | H37 | 0.265 | H37 | 0.227 | H37 | 0.255 | H37 | 0.257 |
| H38 | 0.257 | H38 | 0.262 | H38 | 0.257 | H38 | 0.257 | H38 | 0.259 |
| H39 | 0.234 | H39 | 0.236 | H39 | 0.240 | H39 | 0.236 | H39 | 0.234 |
| H40 | 0.241 | H40 | 0.242 | H40 | 0.243 | H40 | 0.241 | H40 | 0.256 |
| H41 | 0.249 | H41 | 0.254 | H41 | 0.254 | H41 | 0.251 | H41 | 0.245 |
| H42 | 0.217 | H42 | 0.217 | H42 | 0.226 | H42 | 0.217 | H42 | 0.216 |
| H43 | 0.217 | H43 | 0.218 | H43 | 0.233 | H43 | 0.220 | H43 | 0.216 |
| H44 | 0.242 | H44 | 0.242 | H44 | 0.236 | H44 | 0.241 | H44 | 0.241 |
| H45 | 0.217 | H45 | 0.216 | H45 | 0.217 | H45 | 0.217 | H45 | 0.218 |
| H46 | 0.217 | H46 | 0.219 | H46 | 0.217 | H46 | 0.217 | H46 | 0.216 |
| H47 | 0.242 | H47 | 0.242 | H47 | 0.243 | H47 | 0.242 | H47 | 0.243 |
|  |  | C48 | -0.207 | C48 | -0.232 | O48 | -0.787 | O48 | -0.554 |
|  |  | C49 | 0.798 | C49 | 0.791 | O49 | -0.744 | O49 | -0.733 |
|  |  | H50 | 0.249 | H50 | 0.252 | O50 | -0.615 | O50 | -0.785 |
|  |  | H51 | 0.237 | H51 | 0.256 | C51 | -0.011 | O51 | -0.600 |
|  |  | O52 | -0.613 | O52 | -0.620 | C52 | -0.709 | O52 | -0.628 |
|  |  | O53 | -0.736 | O53 | -0.823 | C53 | 0.813 | C53 | -0.025 |
|  |  | H54 | 0.527 | H54 | 0.550 | H54 | 0.236 | C54 | -0.722 |
|  |  | O55 | -0.774 | O55 | -0.741 | H55 | 0.251 | C55 | 0.827 |
|  |  | H56 | 0.519 | H56 | 0.547 | H56 | 0.247 | C56 | 0.822 |
|  |  |  |  |  |  | H57 | 0.256 | C57 | -0.194 |
|  |  |  |  |  |  | H58 | 0.537 | H58 | 0.273 |
|  |  |  |  |  |  | H59 | 0.521 | H59 | 0.253 |
|  |  |  |  |  |  |  |  | H60 | 0.270 |
|  |  |  |  |  |  |  |  | H61 | 0.265 |
|  |  |  |  |  |  |  |  | H62 | 0.234 |
|  |  |  |  |  |  |  |  | H63 | 0.245 |
|  |  |  |  |  |  |  |  | H64 | 0.533 |
|  |  |  |  |  |  |  |  | H65 | 0.528 |

References

1. 	Rozas I, Alkorta I, Elguero J (2000) Behavior of Ylides Containing N, O, and C Atoms as Hydrogen Bond Acceptors. J Am Chem Soc 122:11154–11161. https://doi.org/10.1021/ja0017864

2. 	Espinosa E, Molins E, Lecomte C (1998) Hydrogen bond strengths revealed by topological analyses of experimentally observed electron densities. Chem Phys Lett 285:170–173. https://doi.org/10.1016/S0009-2614(98)00036-0

3. 	Contreras-García J, Calatayud M, Piquemal J-P, Recio JM (2012) Ionic interactions: Comparative topological approach. Comput Theor Chem 998:193–201

4. 	Wu P, Chaudret R, Hu X, Yang W (2013) Noncovalent interaction analysis in fluctuating environments. J Chem Theory Comput 9:2226–2234

5. 	Contreras-García J, Johnson ER, Keinan S, et al (2011) NCIPLOT: a program for plotting noncovalent interaction regions. J Chem Theory Comput 7:625–632

6. 	Blom CE, Bauder A (1982) Structure of glycolic acid determined by microwave spectroscopy. J Am Chem Soc 104:2993–2996

7. 	Borba A, Gómez-Zavaglia A, Lapinski L, Fausto R (2004) Rotational isomers of lactic acid: First experimental observation of higher energy forms. Phys Chem Chem Phys 6:2101–2108. https://doi.org/10.1039/b316642b

8. 	Kolev TM, Velcheva EA, Stamboliyska BA, Spiteller M (2005) DFT and experimental studies of the structure and vibrational spectra of curcumin. Int J Quantum Chem 102:1069–1079. https://doi.org/10.1002/qua.20469