Tables

Table 1 – Control factors levels description.

| Process parameters | Number of levels | Description |
| --- | --- | --- |
| Welding current (kA) | 7 | 6, 7, 8, 9, 10, 11, 12 |
| Welding time (cycle) | 4 | 8, 12, 16, 20 |
| Electrode force (kgf) | 2 | 226, 343 |

Table 2 – Chemical composition and mechanical properties of the base material.

| Chemical composition (%) |  |  |  | Yield Strength (MPa) | Ultimate Tensile Strength (MPa) |
| --- | --- | --- | --- | --- | --- |
| C (max.) | Mn (max.) | P (max.) | S (max.) |  |  |
| 0.12 | 0.60 | 0.05 | 0.05 | 140 (min.) | 280 (min.) |

Table 3 – Interpretation of correlation coefficients. Adapted from (Hinkle et al., 2003).

| Correlation coefficient | Interpretation |
| --- | --- |
| 0.91 a 1.00 | Very high correlation |
| 0.71 a 0.90 | High correlation |
| 0.51 a 0.70 | Moderate correlation |
| 0.31 a 0.50 | Low correlation |
| 0.00 a 0.30 | Negligible correlation |

Table 4 – Summary of statistical analysis.

| Analysed responses | Control factors influence |  |  | Radj2 | Correlation classification | RSE | RSE (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cwel | Twel | Fele |  |  |  |  |
| ECtotal | ↑ | ↑ | - | 0.97 | Very high | 0.23 Wh | 6.05% |
| dnugget | ↑ | ↑ | ↓ | 0.67 | Moderate | 0.33 mm | 5.95% |
| EEmachine | ↑ | ↑ | - | 0.55 | Moderate | 1.08% | 4.11% |
| EEtotal | ↓ | ↓ | - | 0.92 | Very high | 0.14 mm/Wh | 8.70% |

Table 5 – Proposed expulsion indicator (Exmaterial) for each sample.

|  | Electrode force (kgf) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 226 |  |  |  |  | 343 |  |  |  |
| Welding current (kA) | Welding time (cycles) |  |  |  |  | Welding time (cycles) |  |  |  |
|  | 8 | 12 | 16 | 20 |  | 8 | 12 | 16 | 20 |
| 6 | 0% | 1% | 1% | 1% |  | 2% | 1% | 1% | 2% |
|  | 0% | 2% | 1% | 1% |  | 2% | 1% | 1% | 2% |
|  | 1% | 0% | 2% | 1% |  | 2% | 0% | 0% | 1% |
| 7 | 0% | 1% | 1% | 1% |  | 0% | 2% | 0% | 1% |
|  | 1% | 2% | 1% | 1% |  | 1% | 2% | 0% | 0% |
|  | 2% | 1% | 1% | 1% |  | 0% | 1% | 1% | 1% |
| 8 | 6% | 8% | 5% | 1% |  | 1% | 1% | 1% | 1% |
|  | 10% | 9% | 9% | 11% |  | 1% | 1% | 1% | 1% |
|  | 10% | 8% | 2% | 1% |  | 1% | 1% | 0% | 1% |
| 9 | 7% | 6% | 12% | 7% |  | 2% | 2% | 1% | 9% |
|  | 9% | 6% | 12% | 8% |  | 1% | 1% | 2% | 1% |
|  | 11% | 12% | 9% | 9% |  | 1% | 10% | 1% | 8% |
| 10 | 7% | 7% | 11% | 7% |  | 2% | 12% | 8% | 12% |
|  | 7% | 12% | 12% | 10% |  | 11% | 8% | 13% | 7% |
|  | 13% | 7% | 9% | 11% |  | 9% | 14% | 10% | 10% |
| 11 | 4% | 6% | 5% | 6% |  | 1% | 9% | 10% | 7% |
|  | 5% | 5% | 11% | 9% |  | 0% | 6% | 5% | 6% |
|  | 12% | 5% | 11% | 4% |  | 1% | 8% | 10% | 8% |
| 12 | 8% | 6% | 8% | 12% |  | 9% | 7% | 8% | 13% |
|  | 8% | 4% | 10% | 6% |  | 5% | 7% | 7% | 12% |
|  | 8% | 12% | 11% | 6% |  | 10% | 10% | 8% | 7% |

Table 6 – Definition of the energy label for the weldability lobe considering Fele= 226 kgf.

| Weldability lobe (Fele= 226 kgf) |  | ECtotal (Wh) range | EEtotal (mm/Wh) range | Energy label |
| --- | --- | --- | --- | --- |
| Cwel (kA) | Twel (cycles) |  |  |  |
| 8 | 20 | > 4.0 and ≤ 4.5 | ≥ 1.2 and < 1.4 | M |

Table 7 – Definition of the energy label for the weldability lobe considering Fele= 343 kgf.

| Weldability lobe (Fele= 343 kgf) |  |  | ECtotal (Wh) range | EEtotal (mm/Wh) range | Energy label |
| --- | --- | --- | --- | --- | --- |
| Cwel (kA) | Twel (cycles) |  |  |  |  |
| 8 | 8 | ≤ 2.0 |  | ≥ 2.4 | A |
| 9 | 8 | > 2.0 and ≤ 2.5 |  | ≥ 2.4 | B |
| 8 | 9 | > 2.0 and ≤ 2.5 |  | ≥ 2.2 and < 2.4 | C |
| 9 | 9 |  |  |  |  |
| 11 | 8 |  |  |  |  |
| 8 | 10 | > 2.0 and ≤ 2.5 |  | ≥ 2.0 and < 2.2 | D |
| 9 | 10 | > 2.5 and ≤ 3.0 |  | ≥ 2.0 and < 2.2 | E |
| 11 | 9 |  |  |  |  |
| 8 | 11 | > 2.5 and ≤ 3.0 |  | ≥ 1.8 and < 2.0 | F |
| 8 | 12 |  |  |  |  |
| 9 | 11 |  |  |  |  |
| 8 | 13 | > 2.5 and ≤ 3.0 |  | ≥ 1.6 and < 1.8 | H |
| 11 | 10 | > 3.0 and ≤ 3.5 |  | ≥ 1.8 and < 2.0 | G |
| 11 | 11 | > 3.0 and ≤ 3.5 |  | ≥ 1.6 and < 1.8 | I |
| 9 | 12 |  |  |  |  |
| 8 | 14 |  |  |  |  |
| 9 | 13 |  |  |  |  |
| 8 | 15 | > 3.0 and ≤ 3.5 |  | ≥ 1.4 and < 1.6 | J |
| 9 | 14 |  |  |  |  |
| 8 | 16 | > 3.5 and ≤ 4.0 |  | ≥ 1.4 and < 1.6 | K |
| 8 | 17 |  |  |  |  |
| 9 | 15 |  |  |  |  |
| 9 | 16 |  |  |  |  |
| 8 | 18 | > 3.5 and ≤ 4.0 |  | ≥ 1.2 and < 1.4 | L |
| 8 | 19 | > 4.0 and ≤ 4.5 |  | ≥ 1.2 and < 1.4 | M |
| 8 | 20 |  |  |  |  |