Multimodal sensing platform based on MnO2 nanozyme and carbon dots for colorimetric and fluorescent detection of peroxynitrite

Man Dua, Shuang Houa, Xinyue Yanga, Yue Zhanga,*, Haijun Lva, Yaran Zhoua, Shuang Zongb,**, Haiwen Songc,***

aCollege of Chemical and Pharmaceutical Engineering, Hebei University of Science and Technology, Shijiazhuang 050018, P. R. China;

bDepartment of Chemical and Environmental Engineering, Hebei Chemical & Pharmaceutical College, Shijiazhuang 050026, P.R. China.

cHebei Lansheng Biotechnology Co., LTD., Shijiazhuang 052260, P. R. China.

*Corresponding author

**Corresponding author

***Corresponding author

E-mail addresses: yuezhang@hebust.edu.cn (Yue Zhang), ynszong@hebcpc.edu.cn (Shuang Zong), haiwen1230@yeah.net (Haiwen Song)

Contents

Table S1. Comparison of fluorescent probes for ONOO-.	1

Preparation of peroxynitrite (ONOO-)	4

Fig. S1 XRD pattern of CDs.	5

Fig. S2 TEM images of MnO2 NSs.	5

Fig. S3 TEM images of CDs.	6

Fig. S4 Fluorescence decay curves of CDs solution in the presence and absence of oxTMB solution.	7

Fig. S5 Fluorescence decay curves of CDs solution in the presence and absence of ONOO- solution.	7

Table S2. The kinetic parameters for oxidase-like activity of MnO2 NSs and other nanozymes.	8

Fig. S6 Cytotoxicity assays of CDs at different concentrations for HUVEC cells.	9

References	10

Table S1. Comparison of fluorescent probes for ONOO-.

| No. | Probes | Structure | λex/λem (nm) | Linear range | LOD | Application |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | K-ONOO |  | 405/570,678 | 0-15 μM | 212 nM | Cells Zebrafish imaging | [1] |  |
| 2 | GOl-ONOO |  | 420/600 | 8-40 μM | 250 nM | Cells | [2] |  |
| 3 | DCM-ONOO |  | 520/685 | 0-20 μM | 96 nM | Cells Mouse imaging | [3] |  |
| 4 | MAR |  | 323/408 | 0-15 μM | 6.97 nM | Cells | [4] |  |
| 5 | WND-1 |  | 420/527 | 0-100 μM | 930 nM | Cells Zebrafish imaging | [5] |  |
| 6 | MULTI-ONOO- |  | 410/706 | 0-20 μM | 11.6 nM | Cells Mouse imaging | [6] |  |
| 7 | NIR-VO |  | 540/686 | 0-50 μM | 1.44 nM | Cells Zebrafish imaging Mouse imaging | [7] |  |
| 8 | TR-ONOO- |  | 390/490 | 0-100 μM | 520 nM | Cells | [8] |  |
| 9 | GYP |  | 457/656 | 0-15 μM | 270 nM | Cells Mouse imaging | [9]] |  |
| 10 | - |  | 380/545，435 | 0-20 μM | 320 nM | Cells Zebrafish imaging | [10] |  |
| 11 | TCPB |  | 362/460 | 0-14 μM | 1590 nM | Cells Mouse imaging | [11] |  |
| 12 | MeOTPE-NO2 |  | 380/505 | 0-200 μM | 35.1 nM | Cells Mouse imaging | [12] |  |
| 13 | NAP-ONOO |  | 460/560 | 0-100 μM | - | Cells Mouse imaging Zebrafish imaging | [13] |  |
| 14 | HN-ONOO |  | 360/542 | 0-125 μM | 1117 nM | Cells Mouse imaging | [14] |  |
| 15 | AcA-MO |  | 650/739 | 0-1 μM | 17.5 nM | Cells Zebrafish imaging Mouse imaging | [15] |  |
| 16 | PC-CDs | - | 365/450,645 | 0-100 μM | 500 nM | Serum samples | [16] |  |
| 17 | CDs | - | 488/560 | 0-7 μM 7.5-10 μM | 200 nM | Cells Mouse imaging | [17]] |  |
| 18 | C-dots-TPP | - | 420/575 | 0.2-1 μM | 13.5 nM | Cells | [[18]] |  |
| 19 | PN-CDs | - | 340/406 | 1-60 μM | 380 nM | Cells | [19] |  |
| 20 | Trp-CD | - | 370/457 | 2.5-25 μM | 1500 nM | Serum samples | [20] |  |
| 21 | CSU-FT | - | 405/706 | 0-20 μM | 11.7 nM | Cells Mouse imaging | [21] |  |
| 22 | Rhb-ONOO | - | 580/628 | 0-1 μM | 33 nM | Cells Mouse imaging | [22] |  |
| 23 | TMB+MnO2 NSs CDs TMB+MnO2 NSs+CDs | - | 350/446 360/480 | 1-70 μM 0.3-55 μM 0.3-45 μM | 28.73 nM 25.47 nM 40.17 nM | Test strip Smartphone software Serum samples Cells | This work |  |

Preparation of peroxynitrite (ONOO-)

According to the literature [23], ONOO- were prepared with slight modifications. Hydrochloric acid (0.7 M) and hydrogen peroxide (0.6 M) were sequentially added to a reaction flask pre-cooled to 0 °C, followed by continuous stirring for 30 min. Subsequently, a mixed solution of sodium hydroxide (1.5 M) and sodium nitrite (0.6 M) was slowly added into the aforementioned reaction flask, and a pale yellow peroxynitrite (ONOO-) solution was immediately generated. After the preparation was completed, the obtained ONOO- solution was transferred to a container and stored in a refrigerator at -18 °C away from light for subsequent experimental use.

Fig. S1 XRD pattern of CDs.

Fig. S2 TEM images of MnO2 NSs.

Fig. S3 TEM images of CDs.

Fig. S4 Fluorescence decay curves of CDs solution in the presence and absence of oxTMB solution.

Fig. S5 Fluorescence decay curves of CDs solution in the presence and absence of ONOO- solution.

Table S2. The kinetic parameters for oxidase-like activity of MnO2 NSs and other nanozymes.

| Nanozymes | Substrate | Km (mM) | Vmax (10-7 M/s) | Refs |
| --- | --- | --- | --- | --- |
| MnO2 nanozyme | TMB | 0.298 | 1.37 | [24] |
| Mn3O4 NFs | TMB | 13.2 | 0.135 | [25] |
| OV-Mn3O4 NFs | TMB | 1.66 | 0.397 | [25] |
| MnO2@ZIF-67 | TMB | 2.325 | 0.5875 | [26] |
| MnO2@ZIF-67@MAA | TMB | 1.722 | 0.393 | [26] |
| MnO2 NS | TMB | 0.0198 | 5.534 | [27] |
| Pt/MnO2/GO | TMB | 0.41 | 7.12 | [28] |
| MnO2 NFs | TMB | 0.121 | 0.665 | [29] |
| CoNCN | TMB | 0.53 | 3.24 | [30] |
| AgNPs@COF-TD | TMB | 0.26 | 0.298 | [31] |
| MnO2 NSs | TMB | 0.3293 | 2.5058 | This work |

Fig. S6 Cytotoxicity assays of CDs at different concentrations for HUVEC cells.

References

- Kang H, Shu W, Yu J, Gao MX, Han RB, Jing J, Zhang RB, Zhang XL (2022) A near-infrared fluorescent probe for ratiometric imaging peroxynitrite in Parkinson's disease model. Sens Actuators B Chem 359:131393. https://doi.org/10.1016/j.snb.2022.131393

- Li JS, Tang J, Yang XP, Xie PY, Liu JF, Zhang D, Ye Y (2022) A novel aggregation-induced emission fluorescent probe to visualize peroxynitrite levels during Golgi stress. Sens Actuators B Chem 358:131513. https://doi.org/10.1016/j.snb.2022.131513

- Luo XZ, Cheng ZY, Wang R, Yu FB (2021) Indication of dynamic peroxynitrite fluctuations in the rat epilepsy model with a near-infrared two-photon fluorescent probe. Anal chem 93:2490-2499. https://doi.org/10.1021/acs.analchem.0c04529

- Jiang HQ, Shi LL, Wang WX, Yang Y, Fang M, Zhu WJ, Li C (2025) A bifunctional AIEgen fluorescent probe for detection viscosity and ONOO- in living cells. J Mol Struct 1329:141381. https://doi.org/10.1016/j.molstruc.2025.141381

- Liu YY, Ma YY, Lin WY (2022) Construction of a bi-functional ratiometric fluorescent probe for detection of endoplasmic reticulum viscosity and ONOO- in cells and zebrafish. Sens Actuators B Chem 373:132742. https://doi.org/10.1016/j.snb.2022.132742

- Xu WZ, Yang QM, Zeng JQ, Tan LB, Zhou LY, Peng LP, Zhou YZ, Xie C, Luo K, Zhang Z (2022) A biomarker (ONOO-)-activated multicolor fluorescent probe for early detection and assessment of arthritis. Sens Actuators B Chem 359:131565. https://doi.org/10.1016/j.snb.2022.131565

- Zhan JT, Huang HW, Quan W, Lin WY (2025) Innovative two-dimensional fluorescent probe of viscosity and ONOO- for high-throughput screening of antioxidant drugs and its application in epilepsy. Sens Actuators B Chem 440:137887. https://doi.org/10.1016/j.snb.2025.137887

- Yan HL, Xu XJ, Li JS, Xie PY, Cao WB, Yang XP, Ye Y (2023) A novel fluorescence-on fluorescent probe for ONOO- detection in HeLa cells. J Photochem Photobiol A 440:114638. https://doi.org/10.1016/j.jphotochem.2023.114638

- Lu GY, Fan HE, Wang KD, Tian GN, Chen CY, Wang Y, Wang L, Fan XJ (2024) A novel fluorescent probe for the detection of peroxynitrite and its application in mice epileptic brain model. Talanta 267:125157. https://doi.org/10.1016/j.talanta.2023.125157

- Zeng XD, Chen X, Chen J, Ma MS, Jin H, Yu SH, Liu ZG (2023) A simple highly selective ratiometric fluorescent probe for detection of peroxynitrite and its bioimaging applications. Dyes Pigm 210:110993. https://doi.org/10.1016/j.dyepig.2022.110993

- Zhang ZC, Li CC, Niu JT, Luo HT, Wang FY, Tan Y, Wang CF, Wu XH, Liu XY, Zhang XL, Kang YF (2026) A NIR dual-channel fluorescent probe for detecting viscosity and ONOO- in vitro and vivo. Spectrochim Acta Part A 344:126760. https://doi.org/10.1016/j.saa.2025.126760

- Yan M, Yu MM, Wang ZK, Yu FB, Fang WW (2025) An ɑ-ketoamide-based fluorescent probe via aggregation induced emission for ONOO- detection in vivo. Talanta 293:128064. https://doi.org/10.1016/j.talanta.2025.128064

- Fan CL, Ma KF, Chi WJ, LiMeng YW, Dong QX, Gao YA, Zeng CK, Meng WS, Shu W, Zeng CY (2025) An innovative fluorescent probe for monitoring of ONOO- in multiple liver-injury models. Talanta 283:127194. https://doi.org/10.1016/j.talanta.2024.127194

- Wei LC, Zhang P, Yu T, Ren NX, Chen J, Yang FT, Shu W (2024) A highly sensitive and specific fluorescent probe for detecting ONOO- in liver-injured cells and tissues. Microchem J 205:111209. https://doi.org/10.1016/j.microc.2024.111209

- Zhu YX, Liu CY, Rong XD, Zhu YX, Wen HY, Zheng M, Sheng WL, Huang SY, Zhu BC (2025) A novel acridine-based mitochondria-targeted near-infrared fluorescent probe for the detection of HOCl/ONOO- in vivo. Sens Actuators B Chem 442:138143. https://doi.org/10.1016/j.snb.2025.138143

- Shao JJ, Sun S, Zhan D, Pan LP, Min GZ, Li XB, Huang KL, Chen W, Yang LK, Liu XY, Lin NB (2022) Phycocyanin-carbon dots nanoprobe for the ratiometric fluorescence determination of peroxynitrite. Spectrochim Acta Part A 275:121177. https://doi.org/10.1016/j.saa.2022.121177

- Liu HF, Liu JB, Zhang S, Chen Y, Zhang JL, Sun YQ, Zheng ZY, Hu S, Li ZH, Tang WX (2023) Spying on the peroxynitrite fluctuation during hearing loss enabled by rationally designed fluorescent carbon dots. Chem Eng J 452:139024. https://doi.org/10.1016/j.cej.2022.139024

- Wu XX, Sun S, Wang YH, Zhu JL, Jiang K, Leng YM, Shu QH, Lin HW (2017) A fluorescent carbon-dots-based mitochondria-targetable nanoprobe for peroxynitrite sensing in living cells. Biosens Bioelectron 90:501-507. https://doi.org/10.1016/j.bios.2016.10.060

- Gong YQ, Yu B, Yang W, Zhang XL (2016) Phosphorus, and nitrogen co-doped carbon dots as a fluorescent probe for real-time measurement of reactive oxygen and nitrogen species inside macrophages. Biosens Bioelectron 79:822-828. https://doi.org/10.1016/j.bios.2016.01.022

- Simões EFC, Esteves da Silva JCG, Leitão JMM (2014) Carbon dots from tryptophan doped glucose for peroxynitrite sensing. Anal Chim Acta 852:174-180. https://doi.org/10.1016/j.aca.2014.08.050

- Xu WZ, Tan LB, Zeng JQ, Yang QM, Zhou YZ, Zhou LY (2022) Molecular engineering for construction of a novel ONOO-- activated multicolor fluorescent nanoprobe for early diagnosis and assessing treatment of arthritis in vivo. Biosens Bioelectron 209:114242. https://doi.org/10.1016/j.bios.2022.114242

- Ou PH, Ran HY, Ye XP, Wang JY, Pang ML, Zhao LL, Chen MZ, Li X, Ma YP, Wang P, Chen J, Luo Q, Peng YB (2023) A robust high selectivity fluorescence turn-on nanoprobe for peroxynitrite detection in inflammatory cells and mice. Spectrochim Acta Part A 291:122381. https://doi.org/10.1016/j.saa.2023.122381

- Peng T, Yang D (2010) HKGreen-3: a rhodol-based fluorescent probe for peroxynitrite. Org Lett 12:4932-4935. https://doi.org/10.1021/ol102182j

- Liang N, Ge XY, Zhao Y, Xia L, Song ZL, Kong RM, Qu FL (2023) Promoting sensitive colorimetric detection of hydroquinone and Hg2+ via ZIF-8 dispersion enhanced oxidase-mimicking activity of MnO2 nanozyme. J Hazard Mater 454:131455. https://doi.org/10.1016/j.jhazmat.2023.131455

- Lu WH, Chen J, Kong LS, Zhu F, Feng ZY, Zhan JH (2021) Oxygen vacancies modulation Mn3O4 nanozyme with enhanced oxidase-mimicking performance for l-cysteine detection. Sens Actuators B Chem 333:129560. https://doi.org/10.1016/j.snb.2021.129560

- Cui YH, Zhao N, Wang SH, Yan HY, Han DD (2025) Colorimetric detection of tetracycline by enhancing peroxidase-like activity of polymerized MnO2@ZIF-67 nanocomposites. Biosens Bioelectron 287:117726. https://doi.org/10.1016/j.bios.2025.117726

- Zhang YY, Zhao TF, Zhao B, Sun B, Zhang XH, Gu YW, Zhang QF, Li M (2024) Development of MnO2 nanosheets nanozyme-based colorimetric and photothermal dual-signal platform for monitoring alkaline phosphatase activity. Microchem J 207:111656. https://doi.org/10.1016/j.microc.2024.111656

- Yi ZH, Ren YS, Li Y, Li YN, Long F, Zhu AN (2023) Rational design of three-in-one Pt/MnO2/GO hybrid nanozyme with enhanced catalytic performance for colorimetric detection of ascorbic acid and cysteine. Talanta 265:124839. https://doi.org/10.1016/j.talanta.2023.124839

- Yue XY, Hao CX, Fu L, Wu CY, Bai YH (2025) Smartphone-assisted colorimetric sensing hydrogels based on MnO2 NFs nanozyme for highly sensitive and rapid detection of tert-butylhydroquinone in edible oils. Food Chem 492:145264. https://doi.org/10.1016/j.foodchem.2025.145264

- Li Y, Lu YW, Zhang XD, Cao HY, Huang YM (2022) Cobalt-embedded nitrogen-doped carbon nanosheets with enhanced oxidase-like activity for detecting perfluorooctane sulfonate. Microchem J 181:107814. https://doi.org/10.1016/j.microc.2022.107814

- Jia ZX, Shi DP, Wang JB, Lin XC (2024) Covalent organic frameworks surface-anchored with silver nanoparticles for colorimetric detection of dopamine based on its oxidase-mimicking activity. Microchem J 200:110428. https://doi.org/10.1016/j.microc.2024.110428