Quantitative evaluation of encrustations in double-J ureteral stents with micro-computed tomography and semantic segmentation

Shaokai Zheng1*, Pedro Amado1, Bernhard Kiss2, Fabian Stangl2, Andreas Haeberlin3, Daniel Sidler4, Dominik Obrist1, Fiona Burkhard2, and Francesco Clavica1

1 ARTORG Center for Biomedical Engineering Research, University of Bern, 3010 Bern, CH; 2 Department of Urology, Inselspital, Bern University Hospital, University of Bern, 3010 Bern, CH; 3 Department of Cardiology, Inselspital, Bern University Hospital, University of Bern, 3010 Bern, CH; 4 Department of Nephrology and Hypertension, Inselspital, Bern University Hospital, University of Bern, 3010 Bern, CH. *Email: shaokai.zheng@outlook.com

Supplementary Material S2.

This supplementary material provides accompanying tables for Figure 2 in the main text.

|  | Stone patients |  |  | Transplant patients |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | <42 d (n = 10) | ≥42 d (n = 4) | p* value | <28 d (n = 4) | ≥28 d (n = 5) | p value |
| Renal | 0.084 (0.035-0.28) | 3.5 (2.5-7.3) | 0.004 | 0.14 (0.087-0.18) | 0.41 (0.075-0.66) | 0.6 |
| Proximal | 0.015 (0.0091-0.43) | 3.8 (0.71-13) | 0.054 | 0.016 (0.0066-0.28) | 0.015 (0.0040-0.024) | 0.6 |
| Distal | 0.026 (0.0094-0.036) | 0.16 (0.087-0.45) | 0.014 | 0.017 (0.0050-2.87) | 0.0015 (0.0014-0.46) | 0.4 |
| Bladder | 0.064 (0.030-0.36) | 0.66 (0.14-1.2) | 0.1 | 0.38 (0.22-0.70) | 0.080 (0.044-0.29) | 0.2 |
| Data are given in median (IQR); d = days. *P values are corrected using the Bonferroni-Holm method. |  |  |  |  |  |  |

Table S2.1.  Accompanying data for Figure 2a-b. Comparisons of EVR over indwelling times in each patient group.

|  | Stone patients (n = 10) | Transplant patients (n = 8) | p value |
| --- | --- | --- | --- |
| Renal | 0.084 (0.035-0.28) | 0.14 (0.075-0.36) | 0.6 |
| Proximal | 0.015 (0.0091-0.43) | 0.011 (0.0044-0.035) | 0.3 |
| Distal | 0.026 (0.0094-0.036) | 0.0050 (0.0014-0.94) | 0.2 |
| Bladder | 0.064 (0.030-0.36) | 0.26 (0.085-0.52) | 0.3 |
| Data are given in median (IQR). |  |  |  |

Table S2.2.  Accompanying data for Figure 2c. Comparisons of EVR between stone and transplant patients with stent indwelling time <42 days.

|  | Stone patients (n = 14) | Transplant patients (n = 9) | p value |
| --- | --- | --- | --- |
| Renal | 0.28 (0.10-0.52) | 0.29 (0.18-0.45) | 0.8 |
| Proximal | 0.19 (0.091-0.64) | 0.015(0.0064-0.068) | 0.013 |
| Distal | 0.057 (0.022-0.069) | 0.013 (0.0044-0.17) | 0.3 |
| Bladder | 0.20 (0.031-0.46) | 0.17 (0.14-0.68) | 0.4 |
| Data are given in median (IQR). |  |  |  |

Table S2.3.  Accompanying data for Figure 2d. Comparisons of ERL of each stent section between patient groups.