Supplementary Materials for

Interfacial excess charge dynamics as a quantitative descriptor for deciphering lithium dendrite growth

Xuezhong Li 1, 3, †, Genmin Lai 2, †, Wei Deng 1, 3, *, Zhifang Wei 4, Jianwei Li 2, Chi Fang 2, Taisen Zuo 5, 6, He Cheng 5, 6, Phakkhananan Pakawanit 7, Suihan Cui 2, Bao Qiu 4, Xufeng Zhou 4, Jiaxin Zheng 2, *, Yongbing Tang 1, 3, *

1. Advanced Energy Storage Technology Research Center, Shenzhen Institutes of Advanced Technology, Chinese Academy of Sciences, Shenzhen, Guangdong 518055, China

2. School of Advanced Materials, Peking University, Shenzhen Graduate School, Shenzhen, Guangdong 518055, China

3. University of Chinese Academy of Sciences (UCAS), Beijing, 100049, China

4. Ningbo Institute of Materials Technology and Engineering, Chinese Academy of Sciences, Ningbo 315201, PR China

5. Spallation Neutron Source Science Center, Dongguan, Guangdong 518055, China

6. Institute of High Energy Physics, Chinese Academy of Sciences, Beijing, China.

7. Synchrotron Light Research Institute, Nakhon Ratchasima, 30000, Thailand

† These authors contribute equally.

∗ Correspondence: w.deng@siat.ac.cn, zhengjx@pkusz.edu.cn, tangyb@siat.ac.cn

Supplementary Table 1. The formula of employed electrolytes.

| Label | Formula of electrolyte |
| --- | --- |
| A | 1.0 M LiPF6 in DMC/FEC (vol. 1/1) |
| B | 1.0 M LiDFOB+0.7M LiBF4 in DEC/FEC (vol. 1/2) |
| C | 1.0 M LiFSI in DOL/DME (vol. 1/1) |
| D | 1.0 M LiFSI in DME |
| E | 1.0 M LiFSI in CPME |
| F | 1.0 M LiFSI in DEE |
| G | 4.0 M LiFSI in DME |
| H | 4.0 M LiFSI in CPME |
| I | 4.0 M LiFSI in DEE |
| J | 8.0 M LiFSI in DME |
| K | LiFSI/DME/TTE (mol. 1/1.2/3) |
| L | 8.0 M LiFSI in DMC/TTE (mol. 1/1) |

Supplementary Note 1

Machine learning model details. To achieve accurate prediction of atomic charge for large-scale systems, we trained the QMTP model for the interfaces of Li metal with LiFSI, DEE mixed solution and LiFSI, DME mixed solution. The QMTP model includes two modules, the charge module as well as the energy and force module.1 To fully leverage the advantages of QMTP and improve the simulation efficiency, we only used the charge module in this work. The charge module obtains the electronegativity V(ni) based on the local atomic environment and then outputs the charge value for each atom using the charge equilibration scheme2. The model parameters levmaxQ was set as 12 and the rcQ was chosen to be 5.0 for atomic charge fitting. The training datasets are derived from AIMD simulations sampling and active learning sampling strategy3. The CP2K4,5 based on density functional theory (DFT) was used to generate the training and testing datasets. The wave function was extended to the Gaussian DZVP basis set (DZVP-MOLOPT-SR-GTH) by using the Gaussian and plane waves (GPW) methods with the Goedecker-Teter-Hutter (GTH)6 pseudopotentials. The Grimme's D3 method was employed to account for dispersion effects7. The plane wave cut-off was set to 800 Ry for the auxiliary basis set. The Г-centered k-point sampling grid of 2 × 2 × 1 and 4 × 4 × 1 were set for interface between Li metal and LiFSI, DEE mixed solution as well as LiFSI, DME mixed solution, respectively. Details on models training and testing are provided in Supplementary Table 2.

Supplementary Table 2. Mean absolute errors (MAE) of charge for the machine learning models.

| System | State | Datasets | Charge (me) |
| --- | --- | --- | --- |
| Interface between Li metal and LiFSI, DEE mixed solution | train | 620 | 4.121 |
|  | test | 173 | 4.112 |
| Interface between Li metal and LiFSI, DME mixed solution7 | train | 3678 | 8.278 |
|  | test | 740 | 7.278 |

Supplementary Note 2

For interfacial charge distribution factors (f) calculation.

As proposed in the main text, the interfacial charge distribution factor (f) is defined as the exchange current density normalized by the net surface charge. For the excess charge on electrode, the term σexcess can be calculated using Expression S3, where Cdl corresponds to the double layer capacitance.

|  | σexcess=(EPZC-Eplating)*Cdl | S3 |
| --- | --- | --- |

In the case of excess countercharge arising from cation screening, σscreening can be evaluated using Expression S4, where it is expressed as the function of electrolyte concentration (c0). Here, γ and m represent the magnitude and scaling behavior of the concentration-dependent contribution, respectively.

|  | σscreening= γ*c0m | S4 |
| --- | --- | --- |

Based on the relationships described in Expression S3-4, the overall relationship of the interfacial charge distribution factor can be generalized in Expression S5.

|  | f=J0(EPZC-Eplating)*Cdl-γ*c0m | S5 |
| --- | --- | --- |

However, due to the inaccessibility of explicit values for γ and m across different electrolyte, system-specific simplifications are introduced to enable practical evaluation of f under distinct regimes.

For DE/WSE, given the relatively low electrolyte concentration (typically ~1.0 M), the contribution of σscreening is considered negligible. Expression S5 can therefore be simplified to Expression S6.

|  | f=J0(EPZC-Eplating)*Cdl | S6 |
| --- | --- | --- |

By assuming Cdl remains constant for the fixed coin cell configuration and electrodes, and the parameters of J0, EPZC and Eplatingare experimentally accessible, the distribution factor (f) can be quantitatively compared across DE/WSE.

For HCE/LHCE, in these high-concentration electrolytes, the influence of electrode excess charge is significantly reduced due to enhanced cation–anion interactions. Thus, Expression S5 can be reduced to Expression S7, where the term σexcess (associated with electrode excess charge) is omitted.

|  | f=J0-γ*c0m | S7 |
| --- | --- | --- |

Under this assumption, the distribution factor is primarily governed by the exchange current density (J0) and the concentration-dependent term σscreening, facilitating direct comparative analysis.

For HWSE, both electrode excess charge and cation screening effects are significant. To enable quantitative comparison, we assume the distribution factor (f) for electrolyte D is unity (equals to 1.0), and usually the Cdl for the Li symmetric cell is approximately 20 μF. By further assuming the scaling factor m = 1 in Expression S5, by using the distribution factor (f) of electrolyte D and Cdl, the γ is calculated as 12.3. Then Expression S5 can be simplified to Expression S8. Substituting experimentally determined values for J0, EPZC, Eplatingand c0into Expression S8 allows for quantitative comparison of distribution factor variations within HWSE.

|  | f=J0(EPZC-Eplating)*20.0-12.3*c0 | S8 |
| --- | --- | --- |

Supplementary Note 3

Details about the exchange current density calculation.

Since the applied voltage during potentiostatic plating reflects the combined effects of cell polarization, charge transfer resistance and interfacial impedance, the PEIS measurement is immediately performed after the plating step to isolate the voltage contribution specifically associated with charge transfer. The exchange current density (J0) was calculated based on impedance data obtained from PEIS. The EIS data were deconvoluted using the distribution of relaxation times (DRT) method to separate the contributions of cell resistance (Rs), SEI resistance (RSEI) for 0.5-10 Hz and charge transfer resistance (Rct) for 100-1000 Hz. At the end of the potentiostatic step, the voltage (ηct) accounting for the Rct were used to calculate (J0) using the classical small-overpotential approximation in Equation S1 and Expression S2:

|  | J0=iRTηctF*A | S1 |
| --- | --- | --- |
|  | ηct=η*Rct-RsRSEI-Rs | S2 |

where i is the current density at the end of the potentiostatic step, η is the overpotentials applied over the cells (20 mV in this work), Rs, Rct and RSEI are obtained from PEIS results, and A is the electrode area, F denotes the Faraday constant, R is the universal gas constant, and T is the temperature (298 K).

Supplementary Note 4

For the calculation of variations of ECSA during potentiostatic Li plating.

According to the Cottrell equation (Equation S9), the time-dependent current density (i) in the diffusion-limited regime is expressed as:

|  | i=nFD1/2cAπt | S9 |
| --- | --- | --- |

where n is the number of electrons transferred, F is the Faraday constant, D is the diffusion coefficient of electrolyte, c is the initial concentration of electrolyte, A is the ECSA of electrode, and t is time. Under potentiostatic electroplating conditions, the current in the diffusion-limited regime is inversely proportional to t.

To evaluate ECSA variation associated with dendrite growth, current-time curve in the diffusion-limited region is analyzed, as illustrated in Supplementary Figure 1. Let the inflection point be defined at (t1, it1), and the endpoint at (t3, it3). Assuming the ECSA at t1 is A1, and that ECSA evolves over time (An) according to the linear growth function defined in Expression S10:

|  | An=A1*1+k1*(tn-t1) | S10 |
| --- | --- | --- |

where k1 represents the rate of ECSA variation, corresponding to dendrite growth rate assigned in main text. Substituting Expression S10 into the Cottrell equation  (Equation S9) gives the instantaneous current (itn) at time tn as Expression S11:

|  | itn=nFπ*D112*c1*A1t1*1+k1*(tn-t1) | S11 |
| --- | --- | --- |

To compare k1 across different electrolytes while eliminating the influence of D and c, we refer to Equation S9 and define the current–time behavior at two characteristic points for different electrolyte as the initial points, e.g., (t1, it1) and (t2, it2). Taking the ratio of these two points leads to Expression S12 and S13.

|  | it1=nFπ*D112*c1*A1t1 | S12 |
| --- | --- | --- |
|  | it2=nFπ*D212*c2*A2t2 | S13 |

Then we observe that the contribution of D and c can be replaced by the variation of current density and time across different electrolyte at the initial point as Expression S14, enabling the normalized comparison k1 of between electrolytes.

|  | it1*t1it2*t2=D112*c1*A1D212*c2*A2 | S14 |
| --- | --- | --- |

The goal is to relate the slope of the rising segment in the current-time curve to the assumed growth rate of ECSA. Herein by using Expression S11 for different points in different electrolytes, as shown in Supplementary Figure 1 (t1, it1) and (t3, it3) for one electrolyte, and (t2, it2) and (t4, it4) for another one, we can obtain the Expression S15.

|  | ∆it4-t2∆it3-t1=D212*c2*A2D112*c1*A1*k2*∆t4-2t2+1t4-1t2k1*∆t3-1t3+1t3-1t1 | S15 |
| --- | --- | --- |

Substituting Expression S14 into Expression S15 yields Expression S16:

|  | ∆it4-t2∆it3-t1*it1*t4it2*t3=k2*∆t4-2*t4+t2-t4k1*∆t3-1*t3+t1-t3 | S16 |
| --- | --- | --- |

Herein, we define A, B and C as Expression S17-19.

|  | Slope2*it1Slope1*it2=A and Slope2Slope1=∆it4-t2∆t4-2∆it3-t1∆t3-1 | S17 |
| --- | --- | --- |
|  | t2-t4∆t4-2*t4=B | S18 |
|  | t1-t3∆t3-1*t3=C | S19 |

Assuming one electrolyte as the baseline (e.g., setting k1 = 1), the relative ECSA growth rate k2 for another electrolyte can then be calculated via Expression S20-21.

|  | k2=A*1+C-B | S20 |
| --- | --- | --- |
|  | k2=Slope2*it1Slope1*it2*1+t1-t3∆t3-1*t3-t2-t4∆t4-2*t4 | S21 |

Thus, by measuring the onset points and endpoint of each electrolyte, the quantitative comparison of different electrolytes on ECSA variation rates during potentiostatic electroplating can be achieved.

Supplementary Figure 1. Electrochemical characterization of electrolyte A (1.0 M LiPF6 in DMC/FEC (vol. 1/1)): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 2. Electrochemical characterization of electrolyte B (1.0 M LiDFOB+0.7M LiBF4 in DEC/FEC (vol. 1/2)): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 3. Electrochemical characterization of electrolyte C (1.0 M LiFSI in DOL/DME (vol. 1/1)): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 4. Electrochemical characterization of electrolyte D (1.0 M LiFSI in DME): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 5. Electrochemical characterization of electrolyte E (1.0 M LiFSI in CPME): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 6. Electrochemical characterization of electrolyte F (1.0 M LiFSI in DEE): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 7. Electrochemical characterization of electrolyte G (4.0 M LiFSI in DME): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 8. Electrochemical characterization of electrolyte H (4.0 M LiFSI in CPME): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 9. Electrochemical characterization of electrolyte I (4.0 M LiFSI in DEE): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 10. Electrochemical characterization of electrolyte J (8.0 M LiFSI in DME): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 11. Electrochemical characterization of electrolyte K (LiFSI/DME/TTE (mol. 1/1.2/3)): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 12. Electrochemical characterization of electrolyte L (8.0 M LiFSI in DMC/TTE (mol. 1/1)): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Figure 13. Electrochemical characterization of LHWSE (LiFSI/DEE/TTE (mol. 1/1/4)): (a) average CE for Li plating/stripping determined using the modified Aurbach method; (b) the curves for Eplating and (c) the curves for EPZC from single-frequency impedance spectroscopy; (d) current-time profile during potentiostatic Li plating; (e) PEIS curve recorded immediately after Li plating during potentiostatic control experiment; (f) calculated average exchange current density derived from (d, e) and the detailed was discussed in Supplementary Note 2.

Supplementary Table 3. The measured CEs, Eplating and EPZC, along with their corresponding average values and standard deviations, are summarized for the various electrolytes as presented in the supplementary figures above.

| Electrolyte | CEs |  |  | Average CEs | STD CEs | Eplating (vs. Li+/Li) |  |  | Average Eplating | STD Eplating | EPZC (vs. SHE) |  |  | Average EPZC | STD EPZC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A | 97.08 | 97.32 | 97.15 | 97.18 | 0.12 | -0.0421 | -0.046 | -0.0486 | -0.0456 | 0.003 | -1.985 | -1.985 | -1.99 | -1.987 | 0.003 |
| B | 97.95 | 97.47 | 97.59 | 97.67 | 0.25 | -0.0344 | -0.0465 | -0.0546 | -0.0452 | 0.010 | -2.021 | -2.035 | -2.04 | -2.032 | 0.010 |
| C | 98.23 | 98.37 | 97.74 | 98.11 | 0.33 | -0.0195 | -0.0195 | -0.0269 | -0.0220 | 0.004 | -2.185 | -2.19 | -2.185 | -2.187 | 0.003 |
| D | 98.44 | 98.32 | 98.59 | 98.45 | 0.14 | -0.0174 | -0.0174 | -0.0233 | -0.0194 | 0.003 | -2.25 | -2.23 | -2.23 | -2.237 | 0.012 |
| E | 99.01 | 98.89 | 98.76 | 98.89 | 0.13 | -0.0317 | -0.0339 | -0.0378 | -0.0345 | 0.003 | -2.26 | -2.255 | -2.27 | -2.262 | 0.008 |
| F | 98.94 | 99.18 | 99.12 | 99.08 | 0.12 | -0.0161 | -0.0195 | -0.02 | -0.0185 | 0.002 | / | -2.245 | -2.25 | -2.248 | 0.004 |
| G | 98.81 | 98.45 | 98.65 | 98.64 | 0.18 | -0.0282 | -0.033 | -0.0421 | -0.0344 | 0.007 | -2.08 | -2.075 | -2.085 | -2.080 | 0.005 |
| H | 98.78 | 99.07 | 98.67 | 98.84 | 0.21 | -0.0421 | -0.0438 | -0.0441 | -0.0433 | 0.001 | -1.885 | -1.87 | -1.87 | -1.875 | 0.009 |
| I | 99.32 | 99.29 | 99.12 | 99.24 | 0.11 | -0.0381 | -0.04 | -0.0438 | -0.0406 | 0.003 | -1.85 | -1.86 | -1.86 | -1.857 | 0.006 |
| J | 99.33 | 99.26 | 99.37 | 99.32 | 0.06 | -0.0716 | -0.0756 | -0.0794 | -0.0755 | 0.004 | -1.855 | -1.85 | -1.84 | -1.848 | 0.008 |
| K | 99.294 | 99.57 | 99.32 | 99.39 | 0.15 | -0.0375 | -0.0375 | -0.0443 | -0.0398 | 0.004 | / | -1.795 | -1.8 | -1.798 | 0.004 |
| L | 99.58 | 99.47 | 99.46 | 99.50 | 0.07 | -0.0375 | -0.0388 | -0.0434 | -0.0399 | 0.003 | -1.745 | -1.755 | -1.748 | -1.749 | 0.005 |
| LHWSE | 99.62 | 99.57 | 99.55 | 99.58 | 0.04 | -0.037 | -0.0356 | -0.0388 | -0.0371 | 0.002 | -1.79 | -1.79 | -1.795 | -1.792 | 0.003 |

Supplementary Table 4. Detailed parameters for calculating ECSA in Figure 3b, c.

| Label | Formula of electrolyte | t1 | i1 | t3 | i3 | t2 | i2 | t4 | i4 | kx/kbase |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| base | 75 mV with 0.5 h under potentiostatic control | 999 | 0.58473 | 1800 | 0.6156 | 999 | 0.5847 | 1800 | 0.6156 | 1.000 |
| base-1 | 100 mV with 0.5 h under potentiostatic control | 999 | 0.58473 | 1800 | 0.6156 | 1273 | 3.785 | 1800 | 4.52 | 4.953 |
| base-2 | 125 mV with 0.5 h under potentiostatic control | 999 | 0.58473 | 1800 | 0.6156 | 993 | 7.36 | 1800 | 13.7 | 16.244 |
| base-3 | 100 mV with 1.0 h under potentiostatic control | 999 | 0.58473 | 1800 | 0.6156 | 2215 | 4.15 | 3600 | 6.5 | 5.892 |
| base+FEC | 100 mV with 0.5 h under potentiostatic control, electrolyte with 5% FEC as additives | 999 | 0.58473 | 1800 | 0.6156 | 1273 | 3.4 | 1800 | 3.85 | 3.376 |

Supplementary Note 5

The formula of base electrolyte is 1.0 M LiPF6 in DMC/EMC (vol. 1/1) for Li symmetrical cells, and the The formula of base+FEC electrolyte is 1.0 M LiPF6 in DMC/EMC (vol. 1/1) with additional 5% wt. FEC solvent. In this section, the cell with base electrolyte with potentiostatic control set as 75 mV and 0.5 h is selected as baseline for calculating the growth rate of ECSA. Thus, the (t1, it1) and (t3, it3) points of cell was used as the parameter of kbase for the calculations in Supplementary Table 4.

Supplementary Table 5. Detailed parameters for calculating growth rate of ECSA and exchange current densities for different electrolytes.

| Label | t1 | i1 | t3 | i3 | t2 | i2 | t4 | i4 | kx/kbase | ave. k | Rs | Rct | Rct+RSEI | J0 | ave. J0 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| D/baseline | 2810 | 3.966 | 5410 | 6.240 | 2810 | 3.966 | 5410 | 6.240 | 1.000 | 0.938 | / |  |  |  |  |
| D | 2810 | 3.966 | 5410 | 6.240 | 3093 | 1.250 | 5505 | 1.719 | 0.705 |  | 2.000 | 10.288 | 12.615 | 3.36 | 4.93 |
|  | 2810 | 3.966 | 5410 | 6.240 | 1465 | 1.129 | 5505 | 2.053 | 0.919 |  | 1.950 | 7.685 | 9.283 | 4.27 |  |
|  | 2810 | 3.966 | 5410 | 6.240 | 3240 | 2.260 | 5505 | 3.535 | 1.129 |  | 1.500 | 6.055 | 7.171 | 7.15 |  |
| A | 2810 | 3.966 | 5410 | 6.240 | 2940 | 0.777 | 5450 | 1.528 | 1.744 | 1.930 | 1.350 | 8.886 | 10.678 | 2.78 | 2.62 |
|  | 2810 | 3.966 | 5410 | 6.240 | 1250 | 0.433 | 5450 | 1.282 | 2.115 |  | 1.700 | 8.807 | 10.575 | 2.45 |  |
| B | 2810 | 3.966 | 5410 | 6.240 | 1750 | 0.942 | 5450 | 2.120 | 1.532 | 1.561 | 1.400 | 6.402 | 7.623 | 4.26 | 3.88 |
|  | 2810 | 3.966 | 5410 | 6.240 | 2750 | 0.938 | 5450 | 1.826 | 1.589 |  | 1.650 | 8.531 | 10.235 | 3.49 |  |
| C | 2810 | 3.966 | 5410 | 6.240 | 1950 | 1.297 | 5450 | 2.378 | 1.08 | 1.199 | 1.600 | 6.515 | 7.926 | 4.93 | 4.77 |
|  | 2810 | 3.966 | 5410 | 6.240 | 1650 | 1.318 | 5450 | 2.602 | 1.163 |  | 1.200 | 7.293 | 8.723 | 4.78 |  |
|  | 2810 | 3.966 | 5410 | 6.240 | 3450 | 1.489 | 5450 | 2.378 | 1.354 |  | 1.400 | 8.064 | 10.065 | 4.61 |  |
| E | 2810 | 3.966 | 5410 | 6.240 | 4250 | 2.115 | 5450 | 2.270 | 0.482 | 0.401 | 9.500 | 18.859 | 21.186 | 6.60 | 6.60 |
|  | 2810 | 3.966 | 5410 | 6.240 | 4450 | 2.195 | 5450 | 2.348 | 0.439 |  | 8.700 | 18.175 | 20.707 | 6.59 |  |
| F | 2810 | 3.966 | 5410 | 6.240 | 3030 | 3.971 | 5450 | 4.902 | 0.316 | 0.297 | 1.500 | 4.510 | 5.282 | 11.05 | 9.33 |
|  | 2810 | 3.966 | 5410 | 6.240 | 3750 | 3.325 | 5450 | 3.926 | 0.277 |  | 1.500 | 5.618 | 6.625 | 8.11 |  |
|  | 2810 | 3.966 | 5410 | 6.240 | 3650 | 3.314 | 5450 | 3.684 | 0.281 |  | 1.350 | 3.944 | 4.842 | 8.83 |  |
| G | 2810 | 3.966 | 5410 | 6.240 | 3832 | 3.131 | 5510 | 3.750 | 0.534 | 0.462 | 1.700 | 4.406 | 5.167 | 9.20 | 8.84 |
|  | 2810 | 3.966 | 5410 | 6.240 | 3710 | 3.221 | 5410 | 3.887 | 0.552 |  | 2.200 | 3.657 | 4.297 | 14.72 |  |
|  | 2810 | 3.966 | 5410 | 6.240 | 4010 | 2.366 | 5410 | 2.673 | 0.420 |  | 2.430 | 6.391 | 8.213 | 7.12 |  |
|  | 2810 | 3.966 | 5410 | 6.240 | 4810 | 1.753 | 5410 | 1.832 | 0.341 |  | 2.700 | 8.311 | 10.338 | 4.34 |  |
| H | 2810 | 3.966 | 5410 | 6.240 | 1550 | 1.347 | 5450 | 1.867 | 0.449 | 0.412 | 9.000 | 21.561 | 25.064 | 4.78 | 5.47 |
|  | 2810 | 3.966 | 5410 | 6.240 | 3650 | 1.925 | 5450 | 2.211 | 0.374 |  | 9.000 | 18.657 | 20.946 | 6.16 |  |
| I | 2810 | 3.966 | 5410 | 6.240 | 4105 | 2.834 | 5512 | 3.086 | 0.287 | 0.233 | 2.050 | 6.772 | 8.080 | 6.78 | 6.58 |
|  | 2810 | 3.966 | 5410 | 6.240 | 3210 | 2.824 | 5410 | 3.069 | 0.179 |  | 2.700 | 14.179 | 18.552 | 6.37 |  |
| J | 2810 | 3.966 | 5410 | 6.240 | 5085 | 1.258 | 5510 | 1.313 | 0.467 | 0.349 | 6.000 | 18.472 | 22.240 | 3.01 | 2.57 |
|  | 2810 | 3.966 | 5410 | 6.240 | 4710 | 1.261 | 5410 | 1.338 | 0.396 |  | 3.700 | 12.808 | 16.053 | 3.03 |  |
|  | 2810 | 3.966 | 5410 | 6.240 | 5010 | 0.647 | 5410 | 0.657 | 0.186 |  | 3.500 | 11.850 | 14.920 | 1.68 |  |
| K | 2810 | 3.966 | 5410 | 6.240 | 4810 | 1.840 | 5410 | 1.909 | 0.283 | 0.243 | / |  |  |  |  |
|  | 2810 | 3.966 | 5410 | 6.240 | 2915 | 1.888 | 5510 | 2.067 | 0.166 |  | 2.800 | 7.315 | 9.361 | 5.50 | 5.90 |
|  | 2810 | 3.966 | 5410 | 6.240 | 4602 | 1.684 | 5172 | 1.743 | 0.279 |  | 2.600 | 6.168 | 10.041 | 6.30 |  |
| L | 2810 | 3.966 | 5410 | 6.240 | 4062 | 1.256 | 5511 | 1.278 | 0.055 | 0.211 | 8.000 | 13.724 | 23.089 | 6.62 | 6.23 |
|  | 2810 | 3.966 | 5410 | 6.240 | 4916 | 1.044 | 5511 | 1.089 | 0.329 |  | 7.600 | 16.840 | 29.437 | 4.46 |  |
|  | 2810 | 3.966 | 5410 | 6.240 | 4510 | 1.291 | 5410 | 1.355 | 0.250 |  | 8.000 | 13.193 | 22.694 | 7.61 |  |
| LHWSE | 2810 | 3.966 | 5410 | 6.240 | 4810 | 2.875 | 5410 | 2.947 | 0.188 | 0.180 | 4.700 | 24.019 | 33.870 | 5.38 | 6.54 |
|  | 2810 | 3.966 | 5410 | 6.240 | 5110 | 4.889 | 5410 | 4.944 | 0.169 |  | 4.000 | 14.570 | 17.440 | 7.69 |  |

Supplementary Table 6. The quantitative comparison of detailed parameters of different electrolytes: CEs, Eplating, EPZC, J0, distribution factor and kx. The comparison of distribution factor between electrolytes are categorized three groups: electrolytes A-F, electrolytes G-I and electrolytes J-L.

| Label | Formula of electrolyte | CE (%) | Epzc (V vs. SHE) | Eplating (V vs. Li+/Li) | J0 (mA/cm2) | Distribution factor (f) | kx/kbaseline |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A | 1.0 M LiPF6 in DMC/FEC (vol. 1/1) | 97.18 | -2.032 | -0.0456 | 2.62 | 0.415 | 1.930 |
| B | 1.0 M LiDFOB+0.7M LiBF4 in DEC/FEC (vol. 1/2) | 97.67 | -1.987 | -0.0452 | 3.88 | 0.581 | 1.561 |
| C | 1.0 M LiFSI in DOL/DME (vol. 1/1) | 98.11 | -2.187 | -0.0220 | 4.77 | 0.910 | 1.199 |
| D | 1.0 M LiFSI in DME | 98.45 | -2.237 | -0.0194 | 4.93 | 1.000 | 0.938 |
| E | 1.0 M LiFSI in CPME | 99.10 | -2.248 | -0.0185 | 6.60 | 1.349 | 0.401 |
| F | 1.0 M LiFSI in DEE | 99.21 | -2.262 | -0.0345 | 9.33 | 1.917 | 0.297 |
| G | 4.0 M LiFSI in DME | 98.64 | -2.080 | -0.0344 | 8.84 | 1.000 | 0.462 |
| H | 4.0 M LiFSI in CPME | 98.84 | -1.875 | -0.0433 | 5.47 | 3.788 | 0.412 |
| I | 4.0 M LiFSI in DEE | 99.24 | -1.877 | -0.0406 | 6.58 | 4.125 | 0.233 |
| J | 8.0 M LiFSI in DME | 99.32 | -1.848 | -0.0755 | 2.57 | 1.000 | 0.349 |
| K | LiFSI/DME/TTE (mol. 1/1.2/3) | 99.39 | -1.798 | -0.0398 | 5.90 | 2.294 | 0.243 |
| L | 8.0 M LiFSI in DMC/TTE (mol. 1/1) | 99.50 | -1.749 | -0.0399 | 6.23 | 2.420 | 0.211 |
| LHWSE | LiFSI/DEE/TTE (mol. 1/1/4) | 99.58 | -1.792 | -0.0371 | 6.54 | 2.527 | 0.180 |

Supplementary Figure 14. Snapshots and radial distribution functions near the electrolyte/electrode interface for electrolyte D (a), electrolyte F (b) and electrolyte J (c) were obtained from CMD simulations.

Supplementary Figure 15. Phase-field simulations were conducted to investigate dendrite growth morphology, composition field and electrical field under varying nucleation conditions, with nucleation site numbers of 1, 3, 5, 7, 9, 11, 13 and 15 under uniform and random nucleation behavior.

Supplementary Figure 16. Phase-field simulations were conducted to investigate dendrite growth under varying nucleation conditions, with nucleation site numbers of 5, 7, and 11. Two nucleation behaviors, namely uniform and random spatial distributions, were considered. Simulations were carried out at time intervals of 0, 10, 20, 40, 60, and 80 s to track the evolution of dendrite growth morphology.

Supplementary Figure 17. The SANS data for the Li deposit in LHWSE under the areal Li plating capacity of 6.0 mAh cm-2, and the related slope for the curve showing the fractal character.

Supplementary Table 7. The detailed parameters and mass of each part of Li/NCM811 pouch cell.

| Components | Cell parameters | Values |
| --- | --- | --- |
| Cathode | Cathode type | NCM811 |
|  | Cathode areal loading (mg/cm2) | 26.0 |
|  | Ratio of active cathode material (%) | 96 |
|  | Areal capacity of cathode (mAh/cm2) | 5.0 |
|  | Electrode size (cm2) | 6.2*7.2 |
|  | Number of electrode sheets | 15 |
|  | Thickness of Al foil (μm) | 10 |
|  | Total mass of cathode electrode (g) | 36.602 |
| LMA | Thickness of LMA (μm) | 20 |
|  | Total mass of LMA (g) | 1.517 |
| Electrolyte | Injection ratio (g/Ah) | 1.00 |
|  | Total mass of electrolyte (g) | 6.50 |
| Separator | Thickness of separator (μm) | 12.0 |
|  | Total mass of separator (g) | 1.644 |
| Packing Al | Total mass of packing Al (g) | 0.982 |
| Tabs | Total mass of tabs (g) | 0.324 |
| Pouch cell | N/P ratio | 0.80 |
|  | Charge/discharge rate (C) | 0.1C/0.1C |
|  | Capacity (Ah) | 6.48 |
|  | Energy (Wh) | 24.50 |
|  | Mass of cell (g) | 47.569 |
|  | Energy density (Wh/kg) | 515 |

Supplementary Figure 18. Digital photograph of LMB pouch cell for showing its mass.

Supplementary Figure 19. Cycling performances of 1.2 Ah Li/NCM pouch cells by using LHWSE under stack pressure of 100 kPa.

Supplementary Figure 20. (a) The charge and discharge profiles the pouch cell with LHWSE in Fig.4f for 10th to 50th cycles. Cell flatness distribution of Li/NCM811 pouch cells with LHWSE (b) and electrolyte A (c) after cycling.

Reference:

1	Lai, G. et al. Unraveling charge effects on interface reactions and dendrite growth in lithium metal anode. npj Computational Materials 11, 121 (2025).

2	Rappe, A. K. & Goddard III, W. A. Charge equilibration for molecular dynamics simulations. The Journal of Physical Chemistry 95, 3358-3363 (1991).

3	Novikov, I. S., Gubaev, K., Podryabinkin, E. V. & Shapeev, A. V. The MLIP package: moment tensor potentials with MPI and active learning. Machine Learning: Science and Technology 2, 025002 (2020).

4	Kühne, T. D. et al. CP2K: An electronic structure and molecular dynamics software package-Quickstep: Efficient and accurate electronic structure calculations. The Journal of Chemical Physics 152 (2020).

5	Hutter, J., Iannuzzi, M., Schiffmann, F. & VandeVondele, J. cp2k: atomistic simulations of condensed matter systems. Wiley Interdisciplinary Reviews: Computational Molecular Science 4, 15-25 (2014).

6	Goedecker, S., Teter, M. & Hutter, J. Separable dual-space Gaussian pseudopotentials. Physical Review B 54, 1703 (1996).

7	Grimme, S., Antony, J., Ehrlich, S. & Krieg, H. A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu. The Journal of Chemical Physics 132 (2010).