# Supplementary Information

Sunlight-Catalysed Green Synthesis of Copper Nanoparticles Using Green Tea Extract

# UV–Vis Spectroscopy Raw Data (Absorbance vs Wavelength)

# FTIR Spectroscopy Raw Data (Wavenumber vs Intensity)

# XRD Patterns (2θ vs Intensity)

# SEM Micrographs (Representative Images)

# Zeta Potential Measurements

# Antimicrobial Assay Results (Zone of Inhibition, mm)

Antimicrobial Assay Data Table:

| Concentration (µg/mL) | E. coli (mm) | S. aureus (mm) |
| --- | --- | --- |
| 25 | - | - |
| 50 | - | - |
| 100 | 15.2 | 13.7 |