Supplementary Materials

Solid-state optical properties of self-assembling amyloid-like peptides with different charged states at the terminal ends

Chiara Schiattarella,‡a Carlo Diaferia‡b, Enrico Gallo,c Bartolomeo Della Ventura,d Giancarlo Morelli,b Luigi Vitagliano,e Raffaele Velotta*d and Antonella Accardo*b

aInstitute of Applied Sciences and Intelligent Systems, CNR, Via P. Castellino 111, Naples, 80131, Italy.

bDepartment of Pharmacy and Research Centre on Bioactive Peptides (CIRPeB), University of Naples “Federico II”, Via Mezzocannone 16, Naples, 80134, Italy.

Email: antonella.accardo@unina.it

cIRCCS SDN, Via Gianturco 113, Naples, 80143, Italy;

dDepartment of Physics “Ettore Pancini”, University of Naples “Federico II”, Via Cintia 26, Naples, 80125, Italy. Email:rvelotta@unina.it

eInstitute of Biostructures and Bioimaging (IBB), CNR, Via Mezzocannone 16, 80134, Naples, Italy.

Figure S1: Fluorescence microscopy images of: a) H+-F6-O-, b) Ac-F6-O-, c) H+-F6-Amide and d) Ac-F6-Amide. All the samples are prepared by deposition of peptide solution (5.0 mg·mL-1) in HFIP on a clean coverslip glass and slowly dried at room temperature. On the left, images in the bright field, in the center and on the right PL images in the DAPI (4’,6-diamidino-2-phenylindole; λexc = 359 nm, λem = 461 nm) and GFP (Green Fluorescent protein λexc = 488 nm, λem = 507 nm) spectral regions. The scale bar = 50 μm.

Figure S2: Normalized fluorescence spectra of peptide films H+-F6-O- (a), Ac-F6-O- (b) and H+-F6-Am (c) versus the excitation wavelength in the range between 330 and 430 nm

Figure S3: (a) Excitation spectra of the F6 setting λem= 400 nm (solid lines) and λem = 450 nm (dash-dotted lines) at 100 mg/mL concentration. (b) Fluorescence spectra of the F6 at λexc = 257 nm.

Figure S4: a) Schematic representation of the Aβ-peptide variants with charged/uncharged termini. b) Selected micrograph acquired on the Aβ-peptide solution (5 mg/mL) deposited on stub and air-dried (scale bar 100 μm). c) Fluorescence emission spectra of ThT, Aβ-peptide and the mix of ThT and the peptide.