SUPPORTING INFORMATION

Machine learning-assisted large-scale identical-location electron microscopy quantifies electrocatalyst degradation

Ana Rebeka Kamšek1,2,*, Francisco Ruiz-Zepeda1,3, Domen Tabernik4, Jan Vidergar1,2, Anja Logar1,5, Ambrož Kregar6, Danijel Skočaj4, Goran Dražić1, Nejc Hodnik1,3,5,*

1 Department of Materials Chemistry, National Institute of Chemistry, Hajdrihova 19, 1000 Ljubljana, Slovenia

2 Faculty of Chemistry and Chemical Technology, University of Ljubljana, Večna pot 113, 1000 Ljubljana, Slovenia

3 Institute of Metals and Technology, Lepi pot 11, 1000 Ljubljana, Slovenia

4 Faculty of Computer and Information Science, University of Ljubljana, Večna pot 113, 1000 Ljubljana, Slovenia

5 University of Nova Gorica, Vipavska 13, 5000 Nova Gorica, Slovenia

6 Faculty of Mechanical Engineering, University of Ljubljana, Aškerčeva 6, 1000 Ljubljana, Slovenia

Corresponding authors: ana.rebeka.kamsek@ki.si, nejc.hodnik@ki.si

SI 1. Structural characterization of the investigated Pt-Co/C sample

SI 2. Analyzing the activation and degradation datasets by mechanism

SI 3. Cyclic voltammograms for activation and degradation

SI 4. TF-RDE and EDX investigations of the Pt-Co/C sample

SI 5. Analyzing datasets with automated particle detection and association

SI 6. Modeling metal dissolution and carbon corrosion on model nanoparticles

SI 1. Structural characterization of the investigated Pt-Co/C sample

Supplementary Fig. 1. STEM images. BF- (top) and HAADF-STEM (bottom) images of the Pt-Co/C electrocatalyst in its initial state at various magnifications.

Supplementary Fig. 2. X-ray diffraction. Background-subtracted XRD pattern with Miller indices for the Fm-3m Pt-Co crystal phase. The star markers denote the Co signal.

SI 2. Analyzing the activation and degradation datasets by mechanism

Supplementary Table 1. Average values and standard deviations of equivalent sphere diameters and circularities of Pt-Co nanoparticles, determined for each mechanism during potential cycling activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 4 M HClO4).

|  | diameter, before [nm] | circularity, before [] | diameter, after [nm] | circularity, after [] | number of events |
| --- | --- | --- | --- | --- | --- |
| dissolution | 3.99 ± 0.84 | 0.87 ± 0.03 | 3.40 ± 0.89 | 0.88 ± 0.02 | 106 |
| no changes | 3.75 ± 0.82 | 0.87 ± 0.02 | 3.71 ± 0.82 | 0.87 ± 0.02 | 46 |
| detachment | 2.80 ± 0.77 | 0.81 ± 0.12 |  |  | 24 |
| attachment |  |  | 2.63 ± 1.02 | 0.81 ± 0.12 | 13 |
| agglomeration | 3.96 ± 0.76 | 0.87 ± 0.02 | 5.02 ± 1.63 | 0.79 ± 0.12 | 11 |
| deposition | 3.24 ± 1.00 | 0.87 ± 0.02 | 3.60 ± 1.01 | 0.88 ± 0.02 | 9 |

Supplementary Table 2. Average values and standard deviations of equivalent sphere diameters and circularities of Pt-Co nanoparticles, determined for each mechanism during potential cycling activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 0.1 M HClO4), followed by degradation (5000 cycles, 0.4–1.2 VRHE, 1 V/s, 0.1 M HClO4).

|  | diameter, before [nm] | circularity, before [] | diameter, after [nm] | circularity, after [] | number of events |
| --- | --- | --- | --- | --- | --- |
| dissolution | 3.67 ± 0.79 | 0.88 ± 0.02 | 3.02 ± 1.03 | 0.87 ± 0.02 | 235 |
| no changes | 3.82 ± 0.87 | 0.88 ± 0.01 | 3.81 ± 0.87 | 0.87 ± 0.02 | 214 |
| detachment | 2.59 ± 0.59 | 0.84 ± 0.11 |  |  | 131 |
| deposition | 3.51 ± 0.92 | 0.88 ± 0.02 | 3.91 ± 0.96 | 0.87 ± 0.02 | 58 |
| attachment |  |  | 2.41 ± 0.75 | 0.65 ± 0.15 | 38 |
| agglomeration | 4.07 ± 0.75 | 0.88 ± 0.01 | 4.43 ± 1.78 | 0.83 ± 0.08 | 12 |
| Ostwald ripening | 3.62 ± 0.43 | 0.89 ± 0.01 | 3.96 ± 0.49 | 0.88 ± 0.01 | 5 |
| complete Ostwald ripening | 3.29 ± 2.35 | 0.89 ± 0.01 | 3.81 ± 2.03 | 0.84 ± 0.05 | 3 |

SI 3. Cyclic voltammograms for activation and degradation

Supplementary Fig. 3. Cyclic voltammetry results, collected with a modified floating electrode setup. The first and last cycles of the (a, c) potential cycling activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 0.1 M HClO4) and (b, d) degradation (5000 cycles, 0.4–1.2 VRHE, 1 V/s, 0.1 M HClO4) of the Pt-Co/C.

SI 4. TF-RDE and EDX investigations of the Pt-Co/C sample

Supplementary Fig. 4. RDE and EDX investigation of the Pt-Co/C electrocatalyst. a, Specific activity (SA), ECSA, and mass activity (MA) of the Pt-Co/C after activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 600 rpm, 0.1 M HClO4) and degradation (5000 cycles, 0.4–1.2 VRHE, 1 V/s, 600 rpm, 0.1 M HClO4), measured with a rotating disk electrode. b, Ex situ EDX-STEM elemental analysis of the Pt-Co/C in the initial state, after activation, and after degradation. Adapted from 1. Attribution 4.0 International (CC BY 4.0).

SI 5. Analyzing datasets with automated particle detection and association

Supplementary Note 1: Details on automated particle detection using a neural network

Automatic particle detection was implemented using a Center-direction Regression Network (CeDiRNet) designed for point-based object detection.2 The network consists of a two-stage architecture, regressing dense center-directions with a ConvNeXt backbone and a Feature Pyramid Network in the first stage, and a point localization from dense center-direction maps in the second stage.

CeDiRNet performs dense, per-pixel regression of vectors pointing to the nearest object center, enabling robust localization by leveraging a broad spatial context around each center rather than relying on a single-pixel prediction. The mathematically well-defined appearance of the regressed center-directions renders the localization stage independent of domain-specific image features, allowing the use of a generic pre-trained model trained entirely on synthetic data.

The architecture was implemented in PyTorch 1.9, with CUDA 11.1, using Python 3.8. Code and datasets will be made publicly available at https://github.com/vicoslab/CeDiRNet-STEM.

- Attribute extension for particle radius and circularity

The first stage of CeDiRNet was further extended to regress particle radius and circularity as a dense map prediction following a similar extension for orientations in CeDiRNet-3DoF.3 Both attributes were associated with the corresponding center location of the particle, regressing the associated values within 15 pixels of the center during training, while reading the values at the detected particle center during inference.

Circularity value was regressed directly, with values ranging from 0 and 1, while radius was transformed into a logarithmic value to reduce the range of values for regression. Both radius and circularity were trained using L1 together with center-directions, weighing the radius and circularity loss with a factor of 0.5 and applying an additional uncertainty weighting between them and the center-directions loss.4

- Input and learning details

For input, pairs of BF- and HAADF-STEM images were resized to 512x512 pixels, merged into two-channel images, and normalized according to the ImageNet standard. The dense regression network was trained on a single NVIDIA A100 40GB GPU using 23 pairs of images for 100 epochs using the Adam optimizer with a batch size of 4 and a learning rate of 10-4 with polynomial decay using an exponent of 0.9. During training, images were augmented using random horizontal and vertical flips and color jittering with a factor of 0.3, each applied with a probability of 0.5.

The regression stage weights were initialized from an ImageNet pre-trained ConvNeXt-base model, whereas the localization stage employed a generic network from ref. 2, learned on 16x NVIDIA A100 40GB GPUs using 512x512 pixel synthetic images for 200 epochs with a batch size of 786 and 5000 unique synthetic samples per epoch without any further training on STEM images.

Supplementary Table 3. Average values and standard deviations of equivalent sphere diameters and circularities of Pt-Co nanoparticles (automated detection, manual association) were determined for each mechanism during potential cycling activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 4 M HClO4).

|  | diameter, before [nm] | circularity, before [] | diameter, after [nm] | circularity, after [] | number of events |
| --- | --- | --- | --- | --- | --- |
| dissolution | 3.88 ± 0.84 | 0.83 ± 0.03 | 3.30 ± 0.83 | 0.84 ± 0.03 | 88 |
| no changes | 3.97 ± 0.85 | 0.83 ± 0.04 | 3.96 ± 0.86 | 0.83 ± 0.03 | 47 |
| deposition | 2.58 ± 0.82 | 0.86 ± 0.04 | 3.10 ± 0.76 | 0.84 ± 0.03 | 18 |
| detachment | 2.47 ± 0.62 | 0.84 ± 0.03 |  |  | 12 |
| attachment |  |  | 1.99 ± 0.73 | 0.87 ± 0.06 | 9 |
| Ostwald ripening | 3.56 ± 0.19 | 0.84 ± 0.00 | 4.14 ± 0.17 | 0.83 ± 0.01 | 2 |
| complete Ostwald ripening | 3.51 ± 0.10 | 0.83 ± 0.00 | 3.59 ± 0.00 | 0.86 ± 0.00 | 1 |

Supplementary Fig. 5. Degradation events for Pt-Co nanoparticles during activation (automated detection, manual association). Scatter plots with histograms showing circularities and equivalent sphere diameters before (red) and after (blue) activation for all events and individual degradation mechanisms (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 4 M HClO4).

Supplementary Table 4. Average values and standard deviations of equivalent sphere diameters and circularities of Pt-Co nanoparticles (automated detection, manual association) determined for each mechanism during potential cycling activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 0.1 M HClO4), followed by degradation (5000 cycles, 0.4–1.2 VRHE, 1 V/s, 0.1 M HClO4).

|  | diameter, before [nm] | circularity, before [] | diameter, after [nm] | circularity, after [] | number of events |
| --- | --- | --- | --- | --- | --- |
| dissolution | 3.77 ± 1.05 | 0.85 ± 0.02 | 3.13 ± 1.02 | 0.85 ± 0.02 | 206 |
| no changes | 3.75 ± 1.04 | 0.85 ± 0.02 | 3.74 ± 1.05 | 0.86 ± 0.02 | 118 |
| detachment | 2.41 ± 0.80 | 0.86 ± 0.04 |  |  | 86 |
| deposition | 3.44 ± 0.89 | 0.85 ± 0.02 | 3.97 ± 0.93 | 0.85 ± 0.02 | 76 |
| attachment |  |  | 2.41 ± 0.78 | 0.91 ± 0.02 | 20 |
| Ostwald ripening | 3.86 ± 1.31 | 0.86 ± 0.03 | 4.41 ± 1.43 | 0.85 ± 0.02 | 7 |
| agglomeration | 3.56 ± 0.35 | 0.84 ± 0.01 | 3.89 ± 0.34 | 0.83 ± 0.01 | 4 |
| reshaping | 2.03 ± 0.00 | 0.86 ± 0.00 | 1.16 ± 0.00 | 0.76 ± 0.00 | 1 |

Supplementary Fig. 6. Degradation events for Pt-Co nanoparticles during potential cycling activation, followed by degradation (automated detection, manual association). Scatter plots with histograms showing circularities and equivalent sphere diameters before (red) and after (blue) activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 0.1 M HClO4) and degradation (5000 cycles, 0.4–1.2 VRHE, 1 V/s, 0.1 M HClO4) for all events and individual degradation mechanisms.

Supplementary Table 5. Average values and standard deviations of equivalent sphere diameters and circularities of Pt-Co nanoparticles (manual segmentation, automated association) were determined for each mechanism during potential cycling activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 4 M HClO4).

|  | diameter, before [nm] | circularity, before [] | diameter, after [nm] | circularity, after [] | number of events |
| --- | --- | --- | --- | --- | --- |
| dissolution | 3.98 ± 0.84 | 0.87 ± 0.03 | 3.38 ± 0.89 | 0.87 ± 0.02 | 96 |
| no changes | 3.81 ± 0.82 | 0.87 ± 0.02 | 3.77 ± 0.81 | 0.87 ± 0.02 | 46 |
| detachment | 2.90 ± 0.87 | 0.88 ± 0.02 |  |  | 19 |
| deposition | 3.20 ± 0.81 | 0.86 ± 0.02 | 3.85 ± 1.29 | 0.85 ± 0.08 | 9 |
| agglomeration | 3.86 ± 0.81 | 0.88 ± 0.02 | 4.52 ± 1.97 | 0.80 ± 0.12 | 8 |
| attachment |  |  | 2.95 ± 0.94 | 0.89 ± 0.02 | 8 |
| complete Ostwald ripening | 3.83 ± 0.95 | 0.86 ± 0.02 | 3.95 ± 0.72 | 0.89 ± 0.01 | 2 |
| Ostwald ripening | 4.74 ± 0.78 | 0.88 ± 0.02 | 5.35 ± 0.67 | 0.84 ± 0.01 | 2 |

Supplementary Fig. 7. Degradation events for Pt-Co nanoparticles during activation (manual segmentation, automated association). Scatter plots with histograms showing circularities and equivalent sphere diameters before (red) and after (blue) activation for all events and individual degradation mechanisms (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 4 M HClO4).

Supplementary Table 6. Average values and standard deviations of equivalent sphere diameters and circularities of Pt-Co nanoparticles (manual segmentation, automated association) determined for each mechanism during potential cycling activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 0.1 M HClO4), followed by degradation (5000 cycles, 0.4–1.2 VRHE, 1 V/s, 0.1 M HClO4).

|  | diameter, before [nm] | circularity, before [] | diameter, after [nm] | circularity, after [] | number of events |
| --- | --- | --- | --- | --- | --- |
| dissolution | 3.70 ± 0.79 | 0.88 ± 0.02 | 3.03 ± 1.00 | 0.87 ± 0.02 | 201 |
| no changes | 3.75 ± 0.87 | 0.88 ± 0.01 | 3.76 ± 0.87 | 0.87 ± 0.02 | 190 |
| detachment | 2.73 ± 0.67 | 0.88 ± 0.03 |  |  | 112 |
| deposition | 3.48 ± 0.93 | 0.88 ± 0.02 | 4.12 ± 1.18 | 0.87 ± 0.04 | 62 |
| attachment |  |  | 2.52 ± 1.06 | 0.87 ± 0.03 | 24 |
| agglomeration | 3.88 ± 0.94 | 0.88 ± 0.01 | 3.86 ± 0.92 | 0.86 ± 0.04 | 23 |
| Ostwald ripening | 4.32 ± 1.18 | 0.89 ± 0.01 | 4.82 ± 1.41 | 0.85 ± 0.05 | 7 |
| complete Ostwald ripening | 3.86 ± 0.81 | 0.81 ± 0.02 | 3.68 ± 0.73 | 0.88 ± 0.01 | 5 |

Supplementary Fig. 8. Degradation events for Pt-Co nanoparticles during potential cycling activation, followed by degradation (manual segmentation, automated association). Scatter plots with histograms showing circularities and equivalent sphere diameters before (red) and after (blue) activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 0.1 M HClO4) and degradation (5000 cycles, 0.4–1.2 VRHE, 1 V/s, 0.1 M HClO4) for all events and individual degradation mechanisms.

Supplementary Table 7. Average values and standard deviations of equivalent sphere diameters and circularities of Pt-Co nanoparticles (automated detection, automated association) were determined for each mechanism during potential cycling activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 4 M HClO4).

|  | diameter, before [nm] | circularity, before [] | diameter, after [nm] | circularity, after [] | number of events |
| --- | --- | --- | --- | --- | --- |
| dissolution | 3.89 ± 0.83 | 0.84 ± 0.03 | 3.28 ± 0.83 | 0.84 ± 0.03 | 94 |
| no changes | 3.99 ± 0.83 | 0.83 ± 0.04 | 3.98 ± 0.83 | 0.83 ± 0.03 | 45 |
| deposition | 2.78 ± 0.95 | 0.85 ± 0.03 | 3.36 ± 0.99 | 0.83 ± 0.03 | 16 |
| detachment | 2.42 ± 0.59 | 0.84 ± 0.04 |  |  | 15 |
| attachment |  |  | 2.47 ± 0.93 | 0.87 ± 0.04 | 14 |
| Ostwald ripening | 3.71 ± 0.50 | 0.85 ± 0.01 | 4.04 ± 0.54 | 0.84 ± 0.02 | 8 |
| agglomeration | 3.58 ± 0.19 | 0.84 ± 0.02 | 3.46 ± 0.00 | 0.83 ± 0.00 | 1 |

Supplementary Fig. 9. Degradation events for Pt-Co nanoparticles during activation (automated detection, automated association). Scatter plots with histograms showing circularities and equivalent sphere diameters before (red) and after (blue) activation for all events and individual degradation mechanisms (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 4 M HClO4).

Supplementary Table 8. Average values and standard deviations of equivalent sphere diameters and circularities of Pt-Co nanoparticles (automated detection, automated association) determined for each mechanism during potential cycling activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 0.1 M HClO4), followed by degradation (5000 cycles, 0.4–1.2 VRHE, 1 V/s, 0.1 M HClO4).

|  | diameter, before [nm] | circularity, before [] | diameter, after [nm] | circularity, after [] | number of events |
| --- | --- | --- | --- | --- | --- |
| dissolution | 3.80 ± 1.08 | 0.85 ± 0.02 | 3.17 ± 0.98 | 0.85 ± 0.02 | 182 |
| no changes | 3.70 ± 1.06 | 0.85 ± 0.02 | 3.68 ± 1.07 | 0.86 ± 0.02 | 110 |
| detachment | 2.69 ± 0.91 | 0.86 ± 0.03 |  |  | 100 |
| deposition | 3.34 ± 0.89 | 0.85 ± 0.03 | 3.82 ± 0.91 | 0.85 ± 0.02 | 66 |
| attachment |  |  | 3.26 ± 1.48 | 0.86 ± 0.02 | 19 |
| agglomeration | 3.74 ± 0.86 | 0.85 ± 0.02 | 4.38 ± 1.02 | 0.84 ± 0.02 | 13 |
| Ostwald ripening | 3.80 ± 0.81 | 0.85 ± 0.01 | 4.13 ± 0.82 | 0.85 ± 0.02 | 7 |
| complete Ostwald ripening | 4.16 ± 1.21 | 0.84 ± 0.02 | 4.24 ± 0.86 | 0.85 ± 0.02 | 3 |
| reshaping | 2.03 ± 0.00 | 0.86 ± 0.00 | 1.16 ± 0.00 | 0.75 ± 0.00 | 1 |

Supplementary Fig. 10. Degradation events for Pt-Co nanoparticles during potential cycling activation, followed by degradation (automated detection, automated association). Scatter plots with histograms showing circularities and equivalent sphere diameters before (red) and after (blue) activation (200 cycles, 0.05–1.2 VRHE, 300 mV/s, 0.1 M HClO4) and degradation (5000 cycles, 0.4–1.2 VRHE, 1 V/s, 0.1 M HClO4) for all events and individual degradation mechanisms.

SI 6. Modeling metal dissolution and carbon corrosion on model nanoparticles

Supplementary Note 2: Details on theoretical modeling of particle evolution during activation

The mathematical model of metal dissolution and carbon corrosion describes morphological development of the catalyst as a consequence of electrochemical reactions taking place on the surface of catalyst particles and the adjacent carbon surface. The model aims to describe the changes in sizes (ri) and positions (xi) of a limited set of particles, observed with STEM.

- Particle size

The change of particle sizes was modelled by describing the electrochemical processes of catalyst dissolution and redeposition. To simplify the modelling, it was assumed that the catalyst particle surface is always formed of Pt, a reasonable first approximation given that the small analyzed nanoparticles contain approximately 65 at.% of Pt.1 This allows for the use of well-established electrochemical processes on the Pt surface. Pt dissolution and redeposition lead to a direct change in particle size.

PtDD:    Pt⇌Pt2++2e-;		EDD = 1.155 V RHE					(1)

Crucially, the equilibrium electric potential of a catalyst particle is affected by its size via the Kelvin term: EDDr=EDD-12FσPtMPtρPtr, where r is the particle radius, σPt surface tension, MPt molar mass, ρPt density, and F Faraday constant.

The Kelvin term lowers the equilibrium potential of smaller particles more than larger particles, leading to faster dissolution and potential transfer of Pt from smaller towards larger particles.5 Dissolution and redeposition of Pt were modelled as a Butler-Volmer reaction, describing the time derivative of particles:6

dridt=-MPtρPtkDise2αDDFUt-EDDriRT-kDepcPt2+,icPt2+,refe-21-αDDFUt-EDDriRT ,			(2)

where kDis and kDep are reaction rate constants of dissolution and deposition, αDD is the charge transfer coefficient, and R is the gas constant. The dynamics is primarily driven by the changes in electric potential Ut, but is also significantly affected by temperature T and the concentrations of Pt2+ ions in the vicinity of the i-th particle cPt2+,i.

To describe the dynamics of these concentrations, we assigned each particle a control volume Vi, defined by a Voronoi diagram, attributed to the particle positions  xi.7 The change of Pt2+ ions concentration due to dissolution and redeposition is thus calculated as

dcPt2+,idtDD =1ViρPtMPtdridt .									(3)

The transfer of Pt2+ ions between neighboring Voronoi volumes is controlled by diffusion

dcPt2+,idtdif =1Vij,nghDPt2+SijdijcPt2+,j-cPt2+,i						(4)

where DPt2+ is Pt2+ ion diffusivity, Sij the contact surface between i-th and j-th Voronoi volumes, and dij the distance between i-th and j-th particle, with summation taken over neighbouring Voronoi volumes. The loss of Pt due to diffusion into the electrolyte is described similarly:

dcPt2+,idtloss =1Vij,extDPt2+SijdijcPt2+,el-cPt2+,i						(5)

with Sij and dij describing the contact surface and distance to the exterior of the Voronoi diagram.

- Detachment and agglomeration

Detachment and agglomeration of catalyst particles are described in the model as a result of corrosion of carbon support around the particles, which is in turn caused by oxidation processes on Pt and the carbon surface.8 The corrosion is initiated by the formation of hydroxide and oxide groups at different equilibrium potentials:

C1:    C*+H2O⇌C-OH+H++e-;			EC1=0.29 V RHE

C2:    C-OH⇌C=O+H++e-;				EC2=0.80 V RHE		(6)

Pt1:  Pt*+H2O⇌Pt-OH+H++e-, 			EPt1=0.79 V RHE

Pt2:  Pt-OH⇌Pt=O+H++e-; 				EPt2=0.80 V RHE

The dynamics of these processes on the i-th particle are described by Butler-Volmer equations.6

rC1,i=kC1(aH2OΘC,ieαC1F(U(t)-EC1)/RT-aH+ΘCOH,ie-(1-αC1)F(U(t)-EC1)/RT),

rC2,i=kC2(ΘCOH,ieαC2F(U(t)-EC2)/RT-aH+ΘCO,ie-(1-αC2)F(U(t)-EC2)/RT),				(7)

rPt1,i=kPt1(aH2OΘPteαPt1F(U(t)-EPt1(ri)-rOxΘOx)/RT-krevaH+ΘPtOH,ie-(1-αPt1)F(U(t)-EPt1(ri))/RT),

rPt2,i=kPt2(ΘPtOH,ieαPt2F(U(t)-EPt2(ri)-rOxΘOx)/RT-krevaH+ΘPtO,ie-(1-αPt2)F(U(t)-EPt2(ri))/RT).

Reaction rates are determined by reaction rate constants kj, equilibrium potentials Ej, and charge transfer coefficients αj for each of the reactions (j = C1, C2, Pt1, Pt2), as well as by relative surface coverages of i-th particle with PtOH groups (ΘPtOH,i),  PtO groups (ΘPtO,i), and unoxidised surface Pt* (ΘPt,i), and relative coverage of its surrounding carbon support with COH groups (ΘCOH,i),  CO groups (ΘCO,i), and unoxidised surface C* (ΘC,i). aH2O and aH+ denote water and proton activity and rOx describes the interaction between Pt surface oxides, with ΘOx=ΘPtOH+ΘPtO. As for the case of Pt dissolution, the equilibrium potential of Pt oxidation is affected by particle size via the Kelvin term

EPt1r=EPt1+12FrσPtOHMPtOHρPtOH -σPtMPtρPt ,							(8)

EPt2r=EPt2+12FrσPtOMPtOρPtO -σPtOHMPtOHρPtOH .

with σ, M and ρ referring to surface tension, molar mass, and density of the species.

Surface coverages of oxide groups ΘCOH,i, ΘCO,i, ΘPtOH,i and ΘPtO,i determine the rates of carbon corrosion via two electrochemical reactions. Carbon hydroxide groups COH can react either with water or with Pt hydroxide PtOH, via reactions

C3:    C-OH+H2O→C*+CO2+3H++3e-;  		EC2=0.96 V RHE

PtC: Pt-OH+C-OH→C*+Pt*+CO2+2H++2e-; 	EPtC=0.62 V RHE		(9)

with reaction rates

rPtC,i=kPtCΘCOH,iΘPtOH,ie2αPtCF(U(t)-EPtC)/RT,						(10)

rC3,i=kC3aH2OΘCOH,ie3αC3F(U(t)-EC3)/RT.

The dynamics of oxide surface growth is determined by reaction rates rPt1,i, rPt2,i, rC1,i, rC2,i, and surface density of defect sites ΓPt and ΓC  on Pt and carbon surface, respectively.6,9

dΘPtOH,idt=FΓPtrPt1,i-rPt2,i-drirPtC,i,

dΘPtOdt=FΓPtrPt2,i,										(11)

dΘCOH,idt=FΓCrC1,i-rC2,i-rC3,i-rPtC,i,

dΘCO,idt=FΓCrC2,i.

Furthermore, carbon corrosion rates rPtC,i and rC3,i determine how the contact surface between the catalyst particle and carbon support changes over time. In the model, the contact surface of the i-th particle was described by the contact angle φC,i resulting in the contact surface

SC,i=2πri2(1-cosφC,i). 									(12)

Assuming that carbon corrosion takes place up to the distance d from the particle, the rate of change of contact angle can be written as

dφC,idt=-3d + 2ri2d2 + 3 d ri + 3 ri2ρCMCrPtC,i+rC3,i 							(13)

where ρC and MC are the density and molar mass of carbon.

Carbon corrosion can lead to the detachment and agglomeration of particles even before the contact angle SC,i reduces to zero, provided that the attractive forces between particles are sufficiently strong. The agglomeration process was modelled by comparing the attraction forces between particles with the adhesion force between particles and the carbon support.

It was assumed in the model that the i-th and j-th particles are attracted by the Casimir force10

Fcas,ij=αcasπ3rirj720Lij3 ri + rj1 -Lij2ri + rj + Lij61ri +1rj 						(14)

which depends on the particle radii ri and rj, and the distance between particle surfaces Lij.

The total attraction force on the i-th particle is therefore

Fattr,i=jFcas,ijrj-rirj-ri.									(15)

The adhesion force Fadh,i on the particle is exactly opposite the attraction force, as long as attraction is not too strong. The limiting force Fadh,max,i⁡that can be produced by adhesion is assumed to be directly proportional to the contact surface, Fadh,max,i=αadhSC,i. The total force on the i-th particle is therefore

Fi= Fattr,i1-min Fattr,i,Fadh,L,i Fattr,i .  								(16)

The movement of particles due to force Fi was modelled under the assumption of strong drag, resulting in velocity being proportional to the force, changing the particle position xi as

dxidt=vi=βFi	.										(17)

In total, 10 variables are modelled for each particle: particle size ri, 3 coordinates of position xi, Pt2+ ion concentration cPt2+,i, oxide coverages ΘPtOH,i, ΘPtO,i, ΘCOH,i, ΘCO,i and contact angle φC,i.

Calibration of the model, aimed at achieving the best fit between experimental data and model results, was performed by adjusting the values of the following model parameters: reaction rate constants kC1, kC2, kC3,kPt1,kPt2,kPtC,kPtDD, Pt2+ ion diffusivity DPt2+, Pt2+ ion concentration in the electrolyte cPt2+,el, and relative strenghts of Casimir (αcas) and adhesion force (αadh).

The values of other parameters were adopted from the literature. The values of all model parameters are listed in Supplementary Table 9.

Supplementary Table 9. List of parameters used in the model. The values of parameters are accompanied by a short description and the source.

| Parameter | Value | Units | Description | Source |
| --- | --- | --- | --- | --- |
| EC1 | 0.2 | V | Equilibrium potential for reaction C1 | Ref. 11 |
| EPt1 | 0.7 | V | Equilibrium potential for reaction Pt1 | Ref. 11 |
| EC2 | 0.8 | V | Equilibrium potential for reaction C2 | Ref. 11 |
| EPt2 | 0.8 | V | Equilibrium potential for reaction Pt2 | Ref. 11 |
| EC3 | 0.95 | V | Equilibrium potential for reaction C3 | Ref. 11 |
| EPtC | 0.65 | V | Equilibrium potential for reaction PtC | Ref. 11 |
| EPtDis | 1.188 | V | Equilibrium potential for Pt dissolution | Ref. 12 |
| αC1 | 0.5 | - | Charge transfer coefficient for reaction C1 | assumed |
| αPt1 | 0.5 | - | Charge transfer coefficient for reaction Pt1 | assumed |
| αC2 | 0.5 | - | Charge transfer coefficient for reaction C2 | assumed |
| αPt2 | 0.5 | - | Charge transfer coefficient for reaction Pt2 | assumed |
| αC3 | 0.5 | - | Charge transfer coefficient for reaction C3 | assumed |
| αPtC | 0.5 | - | Charge transfer coefficient for reaction PtC | assumed |
| αPtDis | 0.5 | - | Charge transfer coefficient for Pt dissolution | assumed |
| kC1 | 3.01×10-9 | mol/m2s | Reaction rate constant for reaction C1 | fitted |
| kPt1 | 4.77×10-5 | mol/m2s | Reaction rate constant for reaction Pt1 | fitted |
| kC2 | 8.79×10-7 | mol/m2s | Reaction rate constant for reaction C2 | fitted |
| kPt2 | 1.45×10-5 | mol/m2s | Reaction rate constant for reaction Pt2 | fitted |
| kC3 | 1.43×10-13 | mol/m2s | Reaction rate constant for reaction C3 | fitted |
| kPtC | 2.19×10-11 | mol/m2s | Reaction rate constant for reaction PtC | fitted |
| kDis | 5.92×10-9 | mol/m2s | Reaction rate constant for Pt dissolution | fitted |
| kDep | 2.08×10-9 | mol/m2s | Reaction rate constant for Pt deposition | fitted |
| ΓPt | 2.15 | As/m2 | Pt oxidation surface area | Ref. 8 |
| ΓC | 4.6 | As/m2 | Carbon oxidation surface area | Ref. 8 |
| d | 1 | nm | Carbon corrosion depth | Ref. 8 |
| DPt2+ | 2.11×10-14 | m2/s | Diffusivity of Pt2+ | fitted |
| cPt2+,ref | 1 | mol/l | Reference Pt2+concentration | Ref. 12 |
| cPt2+,el | 4.93×10-3 | mol/l | Pt2+concentration in electrolyte | fitted |
| rOx | 30 | kJ/mol | Pt oxide interaction | Ref. 12 |
| krev | 0.3 | - | Pt oxidation reversibility | Ref. 13 |
| αCas | 10-27 | Nm2 | Casimir force strength | assumed |
| αAdh | 109 | N/m2 | Adhesion force strength | fitted |
| β | 0.05 | m/Ns | Drag coefficient | assumed |
| ρPt | 21090 | kg/m3 | Pt density | Ref. 12 |
| ρPtOH | 14170 | kg/m3 | Pt-OH density | Ref. 8 |
| ρPtO | 14100 | kg/m3 | Pt=O density | Ref. 12 |
| ρC | 2000 | kg/m3 | Carbon density | - |
| σPt | 2.73 | J/m2 | Pt surface tension | Ref. 12 |
| σPtOH | 1.34 | J/m2 | Pt-OH surface tension | Ref. 8 |
| σPtO | 1 | J/m2 | Pt=O surface tension | Ref. 12 |
| MPt | 195 | g/mol | Pt molar mass | Ref. 12 |
| MPtOH | 212 | g/mol | Pt-OH molar mass | Ref. 8 |
| MPtO | 211 | g/mol | Pt=O molar mass | Ref. 12 |
| MC | 12 | g/mol | Carbon molar mass | - |
| MH2O | 18 | g/mol | Water molar mass | - |

The geometric parameters of the 11 model nanoparticles before and after simulated potential cycling conditions are listed in Supplementary Table 10.

Supplementary Table 10. Radii, contact angles, and contact surfaces for all analyzed model nanoparticles.

| particle id | radius, before [nm] | angle, before [rad] | surface, before [nm2] | radius, after [nm] | angle, after [rad] | surface, after [nm2] | surface change [nm2] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.99 | 1.57 | 24.83 | 1.86 | 0.08 | 0.08 | 24.75 |
| 2 | 1.40 | 1.57 | 12.29 | 0.99 | 0.01 | 0.00 | 12.29 |
| 3 | 1.61 | 1.57 | 16.21 | 1.38 | 0.01 | 0.00 | 16.21 |
| 4 | 1.99 | 1.57 | 24.90 | 1.86 | 0.08 | 0.08 | 24.82 |
| 5 | 1.85 | 1.57 | 21.49 | 1.70 | 0.03 | 0.01 | 21.48 |
| 6 | 1.85 | 1.57 | 21.55 | 1.70 | 0.03 | 0.01 | 21.55 |
| 7 | 2.77 | 1.57 | 48.11 | 2.70 | 0.39 | 3.38 | 44.72 |
| 8 | 2.19 | 1.57 | 30.25 | 2.09 | 0.18 | 0.43 | 29.81 |
| 9 | 1.82 | 1.57 | 20.87 | 1.67 | 0.03 | 0.01 | 20.86 |
| 10 | 1.21 | 1.57 | 9.25 | 0.00 | 0.13 | 0.00 | 9.25 |
| 11 | 1.77 | 1.57 | 19.73 | 1.61 | 0.02 | 0.00 | 19.73 |

References

(1)	Moriau, L. J.; Hrnjić, A.; Pavlišič, A.; Kamšek, A. R.; Petek, U.; Ruiz-Zepeda, F.; Šala, M.; Pavko, L.; Šelih, V. S.; Bele, M.; Jovanovič, P.; Gatalo, M.; Hodnik, N. Resolving the Nanoparticles’ Structure-Property Relationships at the Atomic Level: A Study of Pt-Based Electrocatalysts. iScience 2021, 24 (2), 102102. https://doi.org/10.1016/j.isci.2021.102102.

(2)	Tabernik, D.; Muhovič, J.; Skočaj, D. Dense Center-Direction Regression for Object Counting and Localization with Point Supervision. Pattern Recognit 2024, 153. https://doi.org/10.1016/j.patcog.2024.110540.

(3)	Tabernik, D.; Muhovič, J.; Urbas, M.; Skočaj, D. Center Direction Network for Grasping Point Localization on Cloths. IEEE Robot Autom Lett 2024, 9 (10), 8913–8920. https://doi.org/10.1109/LRA.2024.3455802.

(4)	Kendall, A.; Gal, Y.; Cipolla, R. Multi-Task Learning Using Uncertainty to Weigh Losses for Scene Geometry and Semantics. In Proceedings of the IEEE Conference on Computer Vision and Pattern Recognition (CVPR); 2018; pp 7482–7491.

(5)	Plieth, W. J. Electrochemical Properties of Small Clusters of Metal Atoms and Their Role in Surface Enhanced Raman Scattering. J Phys Chem 1982, 86, 3166–3170. https://doi.org/https://doi.org/10.1021/j100213a020.

(6)	Kregar, A.; Gatalo, M.; Maselj, N.; Hodnik, N.; Katrašnik, T. Temperature Dependent Model of Carbon Supported Platinum Fuel Cell Catalyst Degradation. J Power Sources 2021, 514. https://doi.org/10.1016/j.jpowsour.2021.230542.

(7)	Voronoi, G. Nouvelles Applications Des Parametres Continus La Th Orie Des Formes Quadratiques. Sur Quelques Proprietes Des Formes Quadratiques Positives Parfaites. Journal für die reine und angewandte Mathematik 1908, No. 133, 97–102. https://doi.org/https://doi.org/10.1515/crll.1908.133.97.

(8)	Kregar, A.; Tavčar, G.; Kravos, A.; Katrašnik, T. Predictive System-Level Modeling Framework for Transient Operation and Cathode Platinum Degradation of High Temperature Proton Exchange Membrane Fuel Cells. Appl Energy 2020, 263, 114547. https://doi.org/10.1016/j.apenergy.2020.114547.

(9)	Kregar, A.; Kravos, A.; Katrašnik, T. Methodology for Evaluation of Contributions of Ostwald Ripening and Particle Agglomeration to Growth of Catalyst Particles in PEM Fuel Cells. Fuel Cells 2020, 20 (4), 487–498. https://doi.org/10.1002/fuce.201900208.

(10)	Teo, L. P. Casimir Effect between Two Spheres at Small Separations. Physical Review D - Particles, Fields, Gravitation and Cosmology 2012, 85 (4). https://doi.org/10.1103/PhysRevD.85.045027.

(11)	Pandy, A.; Yang, Z.; Gummalla, M.; Atrazhev, V. V.; Kuzminyh, N. Yu.; Sultanov, V. I.; Burlatsky, S. A Carbon Corrosion Model to Evaluate the Effect of Steady State and Transient Operation of a Polymer Electrolyte Membrane Fuel Cell. J. Electrochem. Soc. 2013, 160 (9), F972–F979. https://doi.org/10.1149/2.036309jes.

(12)	Bi, W.; Gray, G. E.; Fuller, T. F. PEM Fuel Cell PtC Dissolution and Deposition in Nafion Electrolyte. Electrochemical and Solid-State Letters 2007, 10 (5), 101–104. https://doi.org/10.1149/1.2712796.

(13)	Darling, R. M.; Meyers, J. P. Kinetic Model of Platinum Dissolution in PEMFCs. J Electrochem Soc 2003, 150 (11), A1523. https://doi.org/10.1149/1.1613669.