Supplementary Information

# Layered Polymeric Carbon Nitride as a Green Support for Cellulase Immobilization: Improved Stability, Activity, and Reusability

# Nuri Gulescia*, Orhan Altanb, Ali Toprakc, Mustafa Serkan Yalcind, Ramazan Bilgine, Deniz Yildirimf*

a Department of Occupational Health and Safety, Faculty of Health Sciences, University of Gumushane, Gumushane, Turkiye

b Department of Chemistry and Chemical Processing Technologies, Vocational School of Technical Science, University of Mersin, Mersin, Turkiye

c Department of Chemistry and Chemical Processing Technologies, Vocational School of Acigol, University of Nevsehir Haci Bektas Veli, Nevsehir, Turkiye

d Department of Chemistry and Chemical Processing Technologies, Vocational School of Technical Science, University of Mersin, Mersin, Turkiye

e Department of Chemistry, Faculty of Sciences & Letters, University of Cukurova, Adana, Turkiye

f Department of Chemical Engineering, Faculty of Engineering, University of Cukurova, Adana, Turkiye

Methods

Instrumental analysis

The Attenuated Total Reflectance (ATR) method was used to perform FT-IR analysis of bare PCN support and immobilized cellulase preparations. Spectra were collected over the 400-4000 cm-1 range using a Perkin Elmer Spectrum 100 FT–IR spectrometer equipped with a sampling module (ZnSe/diamond) and single reflection detector at room temperature. Recording was done 32 scans at 4 cm-1 resolution for each spectrum. The background spectra were obtained as a control using the same acquisition parameters for each sample measurement.

The surface morphology of supports before and after cellulase immobilization was investigated by scanning electron microscopy (SEM, Quanta 650 Field Emission SEM). Samples were sputtered with a layer of gold to minimize charging effects. SEM was operated at 10 kV and the images of samples were recorded at different magnifications (10000x-100000x). The morphology of immobilized enzymes was also evaluated by transmission electron microscopy (TEM) (JEOL JEM-2100PLUS) operated at an acceleration voltage of 200kV.

Cellulase assay

The cellulase activity was measured according to Miller with slight modification [30]. Briefly, 50 μL of free cellulase (1 mg/mL in pH 5.0 acetate buffer) or 5 mg of immobilized cellulase preparation was added to 250 μL of cellulose solution (1.0 mg/mL in pH 5.0 acetate buffer) in a test tube at 30 °C. The mixture was gently shaken for 30 min reaction time, and then, 300 μL of DNS solution was added onto the reaction mixture. Then, the samples were kept in the boiling water for 10 min and cooled in an ice bath. Subsequently, 3.4 mL of distilled water was added onto the samples. The released amount of reducing sugar was spectrophotometrically determined at 540 nm. A blank reaction containing no free or immobilized cellulase was run in parallel. The cellulase activity is defined as the amount of enzyme that releases 1 μmol reducing sugar in the assay conditions.

(A)

(B)

(C)

(D)

Fig. S1. Lineweaver-Burk plots of free cellulase (A), PCN@cellulase (B), PCN@cellulase/Glu (C), and PCN/Glu@cellulase (D).