Table 1 Rietveld refinement results and lattice parameters for 5.0 mol% Bi3+ single-doped and 5.0 mol% Er3+/x mol% Bi3+ (x = 0, 1.0, and 5.0) co-doped YNbO4 powder phosphors.

| Formula | Y1-xBixNbO4 | Y0.95-xEr0.05BixNbO4 |  |  |
| --- | --- | --- | --- | --- |
|  | x = 0.05 | x = 0 | x = 0.01 | x = 0.05 |
| Radiation type | CuKα1 radiation with λ = 1.5406 Å |  |  |  |
| 2θ range | 10-70° |  |  |  |
| Symmetry | Monoclinic system |  |  |  |
| Space group | C2/c (15) |  |  |  |
| Cell parameters | a =7.629Å b = 10.965 Å c = 5.307Å α = γ = 90° β = 138.467° V = 294.402 Å3 | a = 7.616Å b = 10.946Å c = 5.296 Å α = γ = 90° β = 138.408° V = 293.129 Å3 | a = 7.624Å b = 10.956 Å c = 5.302Å α = γ = 90° β = 138.435° V = 293.837 Å3 | a = 7.632 Å b = 10.969 Å c = 5.309 Å α = γ = 90° β = 138.460° V = 294.772 Å3 |
| Reliability factors | χ2 = 1.549 Rwp = 22.66 % Rp = 15.46 % | χ2 = 1.496 Rwp = 22.48 %, Rp = 15.37% | χ2 = 1.488 Rwp = 22.83% Rp = 15.62% | χ2 = 1.539 Rwp = 22.93 % Rp = 15.87 % |

Table 2 Relative (Ωλ) and real (Ωλ) J-O parameters of Er3+ ions in YNbO4: Er3+/x mol% Bi3+ (x = 0, 1.0, 3.0 and 5.0) phosphors.

| x /mol% Ω()λ / 10-21 cm2 | 0 | 1.0 | 3.0 | 5.0 |
| --- | --- | --- | --- | --- |
| Ω2 | 1.26 | 2.17 | 2.37 | 2.92 |
| Ω2 | 5.29 | 4.71 | 4.09 | 3.98 |
| Ω4 | 4.35 | 7.68 | 9.11 | 11.78 |
| Ω4 | 1.83 | 1.66 | 1.57 | 1.61 |
| Ω6 | 1.40 | 2.81 | 3.63 | 4.58 |
| Ω6 | 5.90 | 6.10 | 6.27 | 6.25 |

Table 3 Experimental and theoretical values of AH/AS for YNbO4: Er3+/x mol% Bi3+ (x = 0, 1.0, 3.0 and 5.0) phosphors

| x /mol% |  | 0 | 1.0 | 3.0 | 5.0 |
| --- | --- | --- | --- | --- | --- |
| AH/AS | Experimental | 10.66 | 9.72 | 8.07 | 7.53 |
|  | Theoretical | 13.17 | 11.40 | 9.80 | 9.66 |