Tables

Table (1): Two-way ANOVA test results.

| Measurement | Parameter | Sum of squares (II) | df | Mean square | f-value | p-value |
| --- | --- | --- | --- | --- | --- | --- |
| Translucency (TP) | Material | 479.58 | 2 | 239.79 | 6622.20 | <0.001* |
|  | Thermocycling | 24.55 | 1 | 24.55 | 1106.66 | <0.001* |
|  | Material* Thermocycling | 1.30 | 2 | 0.65 | 29.31 | <0.001* |
| Surface roughness (Ra) | Material | 0.00 | 2 | 0.00 | 0.802 | 0.471ns |
|  | Thermocycling | 0.00 | 1 | 0.00 | 1.267 | 0.282ns |

*Significant (p<0.05).

Table (2): Summary statistics and simple main effects comparisons for translucency values.

| Material Thermocycling | Translucency (TP) (Mean±SD) |  |  | f-value | p-value |
| --- | --- | --- | --- | --- | --- |
|  | CEREC Tessera | Initial LiSi | Amber mill |  |  |
| Non aged | 14.71±0.19B | 11.39±0.15C | 19.24±0.21A | 3446.23 | <0.001* |
| Aged | 16.41±0.15B | 12.43±0.07C | 21.09±0.22A | 4128.94 | <0.001* |
| f-value | 322.36 | 128.55 | 376.87 |  |  |
| p-value | <0.001* | <0.001* | <0.001* |  |  |

Values with different superscripts within the same horizontal row  are significantly different *Significant (p<0.05)

Table (3): Summary statistics and main effects comparisons for color change.

| Parameter |  | Color change (ΔE) (Mean±SD) | f-value | p-value |
| --- | --- | --- | --- | --- |
| Material | CEREC Tessera | 1.80±0.10C | 230.23 | <0.001* |
|  | Initial LiSi | 2.24±0.12B |  |  |
|  | Amber mill | 3.10±0.13A |  |  |

Values with different superscripts within the same vertical column are significantly different *Significant (p<0.05).

Table (4): Summary statistics and main effects comparisons for surface roughness.

| Parameter |  | Surface roughness (Ra) (Mean±SD) | f-value | p-value |
| --- | --- | --- | --- | --- |
| Material | CEREC Tessera | 0.2537±0.0014 | 0.802 | 0.471 ns |
|  | Initial LiSi | 0.2534±0.0013 |  |  |
|  | Amber mill | 0.2537±0.0011 |  |  |
| Thermocycling | Non aged | 0.2537±0.0008 | 1.267 | 0.282 ns |
|  | Aged | 0.2545±0.0020 |  |  |

*Significant (p<0.05).