Metal-embedded nitrogen-doped carbon nanocages from ZIF-67 for efficient ciprofloxacin degradation via peroxymonosulfate activation
Huanxuan Li 1*, Xueheng Wei 1, Chen Liu 1, Xing Gao 2, Ning Li 1, Chen Xu 1, Jingang Huang 1, Xiuyan Liu 1, Shaodan Xu 1* 
1 College of Materials and Environmental Engineering, Hangzhou Dianzi University, Hangzhou 310018, PR China.

2 China Aerospace Planning and Design Group Co., Ltd. Zhejiang Branch, Hangzhou 310000, China

*Corresponding authors. E-mail addresses: hxlee@hdu.edu.cn (H. Li), xusd@hdu.edu.cn (S. Xu).

Text S1. EPR measurement
The electron paramagnetic resonance (EPR) measurement was carried out on a Bruker spectrometer (A300) to detect Reactive oxygen species (ROS) during the PMS activation using DMPO (SO4•−, ·OH, and O2•−) and TEMP (1O2) as the spin-trapping agents. The reaction solutions (10 μl) were sampled into quartz capillary tubes. The instrumental parameters were as follows: microwave frequency at 9.44 GHz, sweep width of 100 G, modulation amplitude of 1.00 G, 30 for receiver gain, modulation frequency at 100 kHz, 40.96 ms for time constant, and 80 ms for conversion time.

[image: image1.emf]0 10 20 30 40 50 60 70 80 90

2θ/(°)

ZIF-67(Co)

Intensity


Fig. S1. XRD patterns of ZIF-67(Co).
[image: image2.emf]0 10 20 30 40 50 60

0.0

0.2

0.4

0.6

0.8

1.0

Reaction time

/

min

C

/

C

0

 

ZIF-67(FeCo)-800/PMS

 

CoFe

2

O

4

/PMS

 

CoFe

2

O

4

-2/PMS

 

Fe

0

/PMS

 

 

Fe

3

O

4

/PMS

CIP

[image: image3.emf]10 20 30 40 50 60 70

¨

¨

¨

ª

ª

ª

CoFe

2

O

4

ª

ª

ª

ª

ª

ª

ª

ª

ª

CoFe

2

O

4

 (PDF#22-1086)

Fe

3

O

4

 (PDF#19-0629)

Co (PDF#15-0806)

Co

¨

ZIF-67(FeCo)-800

CoFe

2

O

4

-2

2θ/(°)

Intensity

0

100

200

300

400

500

600

700

800

900

1000

0

100

200

300

400

500

600

700

800

900

1000


Fig. S2. (a) The comparison degradation of CIP by PMS activated with different catalysts; (b) The comparison XRD of CoFe2O4-2 and ZIF-67(FeCo)-800. Experiment condition: PMS = 1.0 mmol·L–1, catalyst = 50 mg·L–1, CIP = 10 mg·L–1, CoFe2O4-2 was prepared from a mixture of Fe3O4 nanoparticles (50 nm) and cobalt(II) oxide with an Fe/Co molar ratio of 2:1 calcined at 800°C for 2 h under nitrogen atmosphere. 
[image: image4.emf]240 280 320 360 400 440 480 520 560 600

0.0

0.2

0.4

0.6

0.8

Absorbance

Wavelenth

/

nm

 0 min

 2 min

 5 min

 10 min

 15 min

 20 min

  30 min 

 45 min

 60 min

 90 min 

 120 min

CIP

[image: image5.emf]240 280 320 360 400 440 480 520 560 600

0.0

0.4

0.8

1.2

1.6

2.0

2.4

2.8

3.2

3.6

Absorbance

Wavelenth

/

nm

 0 min

 2 min

 4 min

 6 min

 8 min

 10 min

  15 min 

 20min

 30 min

OG


[image: image6.png]10 min 15 min 20 min




Fig. S3. UV-Vis spectra of CIP (a) and OG (b) over time, and the change of color of the OG (c) in the ZIF-67(FeCo)-800PMS system. Experiment condition: PMS = 1.0 mmol·L–1; CIP = 10 mg·L–1; OG = 0.2 mmol·L–1; catalysts = 50 mg·L–1; initial pH unadjusted.
[image: image7.emf]1400 1200 1000 800 600 400 200 0

Used ZIF-67(FeCo)-800 

Co 2p

Fe 2p

ZIF-67(FeCo)-800 

Binding energy/eV

C 1s

O 1s

Survey

Intensity


Fig. S4. Survey spectra of fresh and used ZIF-67(FeCo)-800.

[image: image8.emf]545 540 535 530 525

 

Raw   

 

Fit

      

O

defective 

   

 

 

O

absorbed

        

O

lattice 

   

 

O 1s

Binding energy

/

eV

Intensity

-60000

-50000

-40000

-30000

-20000

-10000

0

10000

20000

30000

40000

50000

60000

70000

80000

90000

100000

-250000

-200000

-150000

-100000

-50000

0

50000

100000

150000

Used ZIF-67(FeCo)-800

ZIF-67(FeCo)-800


Fig. S5. XPS analysis for O 1s spectra of fresh and used ZIF-67(FeCo)-800.

[image: image9.emf]298 296 294 292 290 288 286 284 282 280

 

Raw      

 

Fit

      

 sp

2

C

 

  

 

C-N/C-O     

 

 C=O

 

C 1s

Binding energy/eV

Intensity

-30000

-20000

-10000

0

10000

20000

30000

40000

-100000

-50000

0

50000

Used ZIF-67(FeCo)-800

ZIF-67(FeCo)-800


Fig. S6. XPS analysis for C 1s spectra of fresh and used ZIF-67(FeCo)-800.

[image: image10.emf]10 20 30 40 50 60 70

Used ZIF-67(FeCo)-800

Fresh ZIF-67(FeCo)-800

2θ/(°)

Intensity

0

100

200

300

400

500

600

700

800

900

1000

0

100

200

300

400

500

600

700

800

900

1000


Fig. S7. XRD patterns of fresh and used ZIF-67(FeCo)-800

[image: image11.emf]0.0 0.2 0.4 0.6 0.8 1.0 1.2 1.4 1.6

-0.3

-0.2

-0.1

0.0

0.1

0.2

0.3

0.4

0.5

Current

 

Potential/(V 

vs

.Pt/AgCl)

ZIF-67(Co)-800

ZIF-67(Fe)-800

ZIF-67(FeCo)-800

[image: image12.emf]0 -100 -200 -300 -400 -500

0

-100

-200

-300

-400

-500

ZIF-67(Co)-800

ZIF-67(Fe)-800

ZIF-67(FeCo)-800

-Z

²

 

Z'

/

ohm


Fig. S8. Cyclic voltammetry curve (CV) (a) and electrochemical impedance spectroscopy (EIS) (b) analysis of as-prepared samples.
[image: image13.emf]0

2

4

6

8

10

ZIF-67(Co)-800

ZIF-67(FeCo)-800

8.76

0.93

5.8

ZIF-67(Fe)-800

4.6

Concentration/(mg·L

–1

)

 Leaching iron

 Leaching cobalt


Fig. S9. The concentrations of leaching metal ions under different systems. Reaction conditions: PMS = 1.0 mmol·L–1; CIP = 10 mg·L–1; catalysts = 50 mg·L–1; initial pH =7.0, T = 25 ℃.
[image: image14.emf]0 10 20 30 40 50 60

0.0

0.2

0.4

0.6

0.8

1.0

Reaction time

/

min

C

/

C

0

OG


Fig. S10. Filtrate test for OG removal. Reaction conditions: PMS = 1.0 mmol·L–1; OG = 0.2 mmol·L–1; initial pH unadjusted; T = 25 ℃. Noted that: filtrate test was conducted after the completion of the first reaction (PMS = 1.0 mmol·L–1; OG = 0.2 mmol·L–1; ZIF-67(FeCo)-800 = 50 mg·L–1) cycle, the catalyst was separated for discarding, while the filtrate was collected and re-added with 1.0 ml of 20 mmol·L–1 OG and 0.5 ml of 200 mmol·L–1 PMS to initiate the reaction. Samples were taken at intervals to determine the concentrations of OG. 
Table S1 Summary of catalytic degradation of contaminant with various carbon-based catalysts.

	Type of catalysts
	Reaction conditions
	Performance
	References

	Co@NCNTs
	CIP=20 mg·L–1, Catalyst=0.1 g·L–1, PMS= 1.0 mmol·L–1, initial pH=7, T=25℃
	50 min, 100%
	[1]

	N-BC/CoSx
	CIP=10 mg·L–1, Catalyst=0.2 g·L–1, PMS= 2.0 mmol·L–1
	60 min, 100%
	[2]

	FeN/C
	Bisphenol F =10 mg·L–1, Catalyst=0.05 g·L–1, PMS= 1.0 mmol·L–1
	90 min, 97.1%
	[3]

	Fe3C@NCNT
	phenol = 20 mg·L–1, Catalyst=0.2 g·L–1, PMS= 2.0 g·L–1
	20 min, 100%
	[4]

	Co-S@NC
	DIN =10 mg·L–1, Catalyst=0.1 g·L–1, PMS= 0.65 mmol·L–1
	90 min, 100%
	[5]

	CS-Co
	TMP =5 mg·L–1, Catalyst=0.1 g·L–1, PMS= 0.5 mmol·L–1
	60 min, 96.5%
	[6]

	ZIF-67(Co)-800
	CIP=10 mg·L–1, Catalyst=0.05 g·L–1, PMS= 1.0 mmol·L–1
	150 min, 100%
	This study

	ZIF-67(FeCo)-800
	CIP=10 mg·L–1, Catalyst=0.05 g·L–1, PMS= 1.0 mmol·L–1
	150 min, 93.4%
	This study


References

[1] J. Qin, J. Cao, J. Huang, Y. Sun, J. Zhang, M. Huang, Cobalt nanoparticles embedded in carbon nanotubes with high specific surface area activate peroxymonosulfate to degrade ciprofloxacin. Diam. Relat. Mate. 144 (2024) 110975.

[2] R. Wang, Z. He, W. Wang, J. Bu, D. Wang, G. Zeng, Y. Yang, Rational design of cobalt sulfide anchored on nitrogen-doped carbon derived from cyanobacteria waste enables efficient activation of peroxymonosulfate for organic pollutants oxidation. Chemosphere, 314 (2023) 137733.

[3] S. Wu, H. Liu, C. Yang, X. Li, Y. Lin, K. Yin, J. Sun, Q. Teng, C. Du, Y. Zhong, High- performance porous carbon catalysts doped by iron and nitrogen for degradation of bisphenol F via peroxymonosulfate activation, Chem. Eng. J. 392 (2020) 123683.

[4] C. Wang,J. Kang, P. Liang, H.Zhang, H.Sun,M.O. Tade, S. Wang, Ferric carbidenanocrystals encapsulated in nitrogen-doped carbon nanotubes as an outstandingenvironmental catalyst, Environ.Sci.: Nano 4 (1) (2017) 170-179.
[5]W. Du, Q. Zhang, Y. Shang, W. Wang, Q. Li, Q. Yue, B. Gao, X. Xu, Sulfate saturated biosorbent-derived Co-S@NC nanoarchitecture as an efficient catalyst for peroxymonosulfate activation, Appl. Catal. B 262 (2020) 118302.

[6] Y. Liu, H. Guo, Y. Zhang, X. Cheng, P. Zhou, J. Deng, J. Wang, W. Li, Highly efficient removal of trimethoprim based on peroxymonosulfate activation by carbonized resin with Co doping: Performance, mechanism and degradation pathway, Chem. Eng. J. 356 (2019) 717-726.

(b)





(a)





(a)





(b)





(c)





(b)





(a)








