Table 1. Copolymerization of ethylene with metal carbonyls using palladium complexesa

aA mixture of the catalyst (10 μmol) and Mx(CO)y in toluene (10 mL) was stirred in a glass tube under an ethylene atmosphere (3.0 MPa) for 3 h in a 50 mL autoclave. bYields of isolated product after precipitation with methanol (80 mL). cMolecular weights determined by size-exclusion chromatography using polystyrene standards corrected by universal calibration. dCO incorporation ratio (i. r.) in mol% determined by 1H NMR analysis. eThe I/A ratio was determined by 1H NMR analysis. I/A = Isolated carbonyls/Alternating carbonyls. gFe2(CO)9 was added outside the glass tube along with toluene (1.0 mL). fEthylene containing about 0.3 mol% CO was used. Dip = 2,6-diisopropylphenyl; Lut = 2,6-lutidine.