Supporting Information

Regulating the Microcrystalline Structure of Anthracite via Thermal Treatment Strategies for Enhanced Sodium Ion Storage Performance

Yulong Zhanga, Deping Xiong a*, Yandong Xieb*, Qu Wanga, Zuyong Fenga

AUTHOR ADDRESS

aSchool of Physics and Optoelectronic Engineering, Guangdong University of Technology, Guangzhou 510006, China.

bSchool of Materials Engineering, Lanzhou Institute of Technology, Lanzhou 730050, China.

* Corresponding author.

E-mail address: depingxiong@gdut.edu.cn.  yandongxie35@foxmail.com.

Formula 1

2dsinθ=mλ#（1）where, d denotes the interplanar spacing,  θ represents the angle between the planes, m indicates the diffraction order, and λ signifies the wavelength of the X-rays.

Table S1 Analysis results of pore size and volume by BJH method of ASC600-1400、ASC700-1400、ASC800-1400.

| Sample(name) | Vtot(cm3 g-1) | Dave(nm) | SBET(m2 g-1) | D10(nm) | D50(nm) | D90(nm) | D99(nm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ASC600-1400 | 0.0331 | 7.3635 | 17.9762 | 3.0310 | 16.3927 | 96.0928 | 117.4859 |
| ASC700-1400 | 0.0274 | 8.6299 | 12.7001 | 3.3439 | 22.3226 | 98.1777 | 118.5173 |
| ASC800-1400 | 0.0260 | 8.3165 | 12.5052 | 3.4853 | 19.1212 | 97.4836 | 119.791 |

Table S2 Contributions of corresponding oxygen-containing functional groups to the fitted O1S spectra of ASC700-1400.

| Sample | Contains oxygen functional content (peak area) | C=O (%) | C-O (%) |
| --- | --- | --- | --- |
| ASC700-1400 | 203347.51 | 96.41 | 87.3 |

Table S3 Contributions of corresponding carbon -containing functional groups to the fitted C1S spectra of ASC700-1400.

| Sample | Contains carbon functional content (peak area) | C=O (%) | C-O (%) | C-C(%) |
| --- | --- | --- | --- | --- |
| ASC700-1400 | 332399.14 | 33.64 | 44.48 | 56.55 |

Fig S1 ACS600-1400、ACS700-1400、ACS800-1400 Platform capacity share.

Fig S2 ACS600-1400、ACS700-1400、ACS800-1400 Intercalation capacity ratio.

Fig S3 Contribution percentages of diffusion-controlled and capacitive processes at different scan rates of ASC700-1400.

Fig S4 CV curves displaying the capacitive contribution (yellow area) to the total current at 1 mV s−1 of ASC700-1400.

Fig S5 GITT curves of the ASC600-1400 during the discharge/charge process.

Fig S6 GITT curves of the ASC700-1400 during the discharge/charge process.

Fig S7 GITT curves of the ASC800-1400 during the discharge/charge process.