Supporting Information

Fabrication of vacancy-independent and intrinsically stable ferroelectric HfO2 through valence-complementary codoping

Shutaro Asanuma*, Hiroyuki Ota, Yukinori Morita, Shogo Hatayama, and Shinji Migita

S. Asanuma, H.Ota, Y. Morita, S. Hatayama, S. Migita

Semiconductor Frontier Research Center, National Institute of Advanced Industrial Science and Technology (AIST), Tsukuba Central 2, 1-1-1 Umezono, Tsukuba, Ibaraki 305-8568, Japan

S. Asanuma, S. Hatayama

NEC-AIST Quantum Technology Cooperative Research Laboratory, National Institute of Advanced Industrial Science and Technology (AIST), Tsukuba Central 2, 1-1-1 Umezono, Tsukuba, Ibaraki 305-8568, Japan

*Corresponding author. e-mail: shutaro-asanuma@aist.go.jp

1. The compositional analysis using X-ray Photoelectron Spectroscopy (XPS)

To investigate the cause of TaN layer delamination induced by annealing in Ar + O2 (21%), XPS measurements were performed. The analyzed sample with Y0.06Nb0.06Hf0.88O2 (YNHO) (45 nm)/TaN (10 nm)/n-Si structures are identical to the sample annealed at 600 °C for 10-min and naturally cooled, as shown in Figure 2b and 2c of the main text. Since these films were not specifically fabricated for XPS measurements, the combination of the YNHO layer and the TaN electrode layer was not ideal for compositional analysis. For instance, the atomic numbers of Hf and Ta differ by only one, and their 4f7/2 and 4f5/2 peak positions are very close. Consequently, near the YNHO/TaN interface, the Hf and Ta spectra overlap, making precise separation challenging.[1]

Given these limitations, the present XPS analysis focused solely on confirming oxygen incorporation into the TaN layer during annealing in Ar + O2 (21%). A detailed investigation of the electronic states in YNHO will be conducted in future work using a structure optimized for XPS measurements. The XPS system employed is described in the Methods section of the main text.

Figure S1a shows XPS spectra obtained from a sample annealed at 600 °C for 10-min in N2, measured through repeated cycles of Ar ion sputtering to remove a few nanometers of the surface followed by XPS acquisition. From top to bottom, the spectra correspond to the surface through to the 10th cycle, the 11th to 20th cycles, the 21st to 30th cycles, and the 31st to 40th cycles, respectively. The spectra represent progressively deeper regions along the direction indicated by the solid arrows in the figure. Up to cycle 20, only Hf 4f peaks from YNHO are observed. In cycles 21–23, minor peaks corresponding to Ta2Ox emerge near the interface. However, since Hf peaks are also present in this spectrum, it is presumed that Ar sputtering has caused intermixing at the YNHO/TaN interface layer. From cycle 24 onward, TaN peaks dominate, and no Ta2Ox peaks are detected.[2,3]

Figure S1b shows XPS spectra from a sample annealed at 600 °C for 10-min in Ar + O2 (21%), measured using the same procedure. Up to cycle 18, only Hf 4f peaks from YNHO are observed. From cycle 19, Ta2Ox peaks begin to appear, and between cycles 21–30, these peaks are more intense than those of TaN. After cycle 31, TaN peaks become dominant, although Ta2Ox peaks persist through cycle 40.[2,3]

These results indicate that annealing in Ar + O2 (21%) at 600 °C for 10-min led to significant oxygen incorporation into the lower TaN layer, resulting in the formation of TaOxNy. This likely caused an increase in the volume of the bottom electrode, leading to its delamination from the substrate.

Figure S1. XPS depth profiling of Y0.06Nb0.06Hf0.88O2 (45 nm)/TaN (10 nm)/n-Si structures annealed at 600 °C for 10-min. a) Spectra from the sample annealed in N2. From top to bottom are XPS spectra measured after Ar sputtering cycles 1–10 , 11–20, 21–30 and 31–40. Within each figure, the spectra correspond to progressively deeper positions along the direction indicated by the arrows. Up to cycle 20 only Hf 4f peaks from the YNHO layer are observed; weak Ta2Ox peaks appear at cycles 21–23, and TaN peaks dominate thereafter. b) Spectra from the sample annealed in Ar + O2 (21%). Up to cycle 18 only Hf 4f peaks are seen; Ta2Ox peaks emerge from cycle 19, become more intense than TaN peaks between cycles 21–30, and although TaN peaks dominate beyond cycle 31, Ta2Ox persists through cycle 40. These profiles demonstrate significant oxygen incorporation into the TaN electrode under Ar + O2 annealing, leading to TaOxNy formation and likely causing electrode delamination.

2. Transmission Electron Microscopy Images

In the main text, we primarily presented TEM images optimized for analyzing the crystal structure. However, numerous additional TEM images were acquired beyond those shown in the main figure. Since these images also provide valuable insights into the properties of YNHO films, they are presented here at larger sizes for clarity.

Figure S2a–h shows ABF-STEM (Figure S2a, S2c, S2e, S2g) and HAADF-STEM (Figure S2b, S2d, S2f, S2h) images of the same sample shown in Figure 2a–d of the main text. Figure S2e and S2f correspond to high-magnification regions within the red box in Figure S2c; and Figure S2g and S2h correspond to the red box in Figure S2e. As noted in the main text, Figure S2e and S2f reveal domains without lattice distortions extending over areas larger than 40 nm × 40 nm. Figure S2g is the original image of Figure 1c.

Figure S3a–h present ABF-STEM (Figure S3a, S3c, S3e, S3g) and HAADF-STEM (Figure S3b, S3d, S3f, S3h) images of the same sample shown in Figure 2e and 2f of the main text. The red circle in Figure S3a indicates the region irradiated by the electron beam during the electron diffraction measurement shown in Figure 1g. The TEM images in Figure S3a–d demonstrate the formation of an exceptionally flat interface between the YNHO layer and the TaN electrode, indicating the creation of a high-quality capacitor structure. Figure S3g is the original image of Figure 1e.

Figure S4a–e show ABF-STEM (Figure S4a, S4c), HAADF-STEM (Figure S4b, S4d), and Energy Dispersive X-ray Spectroscopy (EDX) (Figure S4e) images from another cell on the same wafer as the samples used in Figure 3a–d of the main text. Similar to Figure S3, these TEM images reveal extremely flat YNHO and TaN electrode layers. Furthermore, Figure S4e shows the presence of oxygen at the Si substrate surface and on the top surface of the upper TaN electrode, suggesting the persistence of a native oxide layer. Although the deposition and processing steps described in the Methods included procedures to remove the native oxide, it is presumed that complete removal was not achieved.

Figure S2. Expanded STEM images of YNHO films. a–h) Annular bright-field scanning TEM (ABF-STEM; a, c, e, g) and high-angle annular dark-field STEM (HAADF-STEM; b, d, f, h) images of the same sample presented in Figure 2a–d of the main text. Panels (e) and (f) are high-magnification views of the region marked by the red box in Figure S2c; and panels (g) and (h) correspond to the red box in Figure S2e. As noted in the main text, (e) and (f) reveal undistorted lattice domains extending over areas larger than 40 nm × 40 nm. g) This image is the original image of Figure 1c.

Figure S3. Interface morphology and electron-beam irradiation site in TaN/YNHO/TaN capacitors. a–h) ABF-STEM (a, c, e, g) and HAADF-STEM (b, d, f, h) images of the sample shown in Figure 1e–f of the main text. The red circle in (a) indicates the region subjected to electron-diffraction analysis (Figure 1g). Panels (a)–(d) demonstrate the formation of an exceptionally flat interface between the YNHO layer and the TaN electrode, confirming a high-quality capacitor structure. g) This image is the original image of Figure 1e.

Figure S4. Cross-sectional STEM and EDX mapping of TaN/YNHO/TaN capacitors. a–d) ABF-STEM (a, c) and HAADF-STEM (b, d) images from another device on the same wafer as the samples used in Figure 3a–d of the main text, showing extremely flat interfaces between the YNHO film and TaN electrodes. e) Energy-dispersive X-ray spectroscopy (EDX) elemental map of the same region, revealing residual oxygen at the Si substrate surface and on the top of the upper TaN electrode, indicative of a persistent native oxide layer despite pre-processing oxide-removal steps.

3. Electron Diffraction Simulation

The crystallographic data used for the electron diffraction simulations in Figure 1h of the main text are as follows:

I4mm

Lattice parameters: a = 3.59 Å, c = 5.12 Å

Atomic positions:

| Wyckoff | Element | x | y | z |
| --- | --- | --- | --- | --- |
| 2a | Hf(Y,Nb) | 0 | 0 | 0 |
| 4b | O | 0.5 | 0 | 0.24 |

P4mm

Lattice parameters: a = 3.59 Å, c = 5.12 Å

Atomic positions:

| Wyckoff | Element | x | y | z |
| --- | --- | --- | --- | --- |
| 1a | Hf(Y,Nb) | 0 | 0 | 0 |
| 1b | Hf(Y,Nb) | 0.5 | 0.5 | 0.51 |
| 2c | O | 0.5 | 0 | 0.24 |
| 2c | O | 0.5 | 0 | 0.74 |

These atomic positions were determined under the condition that there exist viewing directions in which the structure appears as shown in Figure 1d and 1f. Here, the oxygen positions were set to 0.24 and 0.74 as provisional values for the simulation, considering slight deviations from 0.25 and 0.75. These are provisional values and do not represent precise experimental determinations. Similarly, the value of 0.51 for the Hf(Y,Nb) atom at the Wyckoff position 1b in P4mm is also a provisional value, intended only to indicate a displacement from the body-centered position.

4. X-ray Diffraction Profile Fitting

The X-ray diffraction (XRD) profile shown in Figure 2e of the main text was fitted using the following procedure.

The raw XRD data are provided in Supplementary Data. The fitting was performed over the 2θ range of 58°–62°. The fitting function consisted of the sum of two Lorentzian functions and a background term, expressed as:

P2θ=h11+2θ-2θ12σ12+h21+2θ-2θ22σ22+b

where P(2θ) is the X-ray intensity, hi, 2θi, and σi represent the intensity, peak position, and full width at half maximum (FWHM) of the i-th peak, respectively, and b denotes the background level. Parameter optimization was carried out using the least-squares method, and calculations were performed with the Solver add-in in Microsoft Excel. As a result of the fitting, the parameters were determined as follows:
h1 = 10.33, θ1 = 30.17, σ1 = 0.28, h2 = 4.02, θ2 = 29.98, σ2 = 0.28, b = 6.90

The above values are rounded to two decimal places. Furthermore, because particle size is considered independent of particle orientation, σ1 was set equal to σ2.

Using these peak positions, the interplanar spacings d were calculated as:

d103 = 1.540592sin29.98 ≈1.54152

d211 = 1.540592sin30.17 ≈1.53272

For a tetragonal system, if the lattice constants along the a- and c-axes are denoted as “a” and “c”, respectively, the interplanar spacing dhkl for Miller index (h,k,l) can be expressed as:

1dhkl2 = h2+k2a2+l2c2

Substituting the values for the (103) and (211) planes give:

1d1032 = 1a2+9c2 ≈0.42082

1d2112 = 5a2+1c2 ≈0.42567

Solving these equations yields the lattice constants a ≈ 3.59 Å, c ≈ 5.12 Å.

5. Details of endurance and leakage current measurements

Figure S5a shows the pulse sequence for ferroelectric properties—including P–E hysteresis loops, I–V curves, positive-up-negative-down (PUND) measurements, and endurance characteristics. Specifically, a predetermined number of wave pulses for electrical stress were first applied, followed by measurements of P–E hysteresis, and PUND measurements. This cycle of stress application and measurement was then repeated until 109 or 1010 cycles. A 6 V, 100 kHz square wave (50 % duty cycle) was used for electrical stress application, and a 6 V, 1 kHz triangular wave was used for the P–E hysteresis and PUND measurements.

As described in the main text, leakage current measurements were also performed. For the leakage current measurements, the leakage current measurement function of the ferroelectric tester was used instead of an instrument capable of measuring extremely small currents; therefore, the lower detection limit of the measurable current is 1 nA. The leakage current was measured by applying a stepwise voltage waveform and observing the response current at each voltage level. The voltage steps were 0.5 V, ranging from −5 V to +5 V. For the same sample used in Figure 3a–d, each voltage level was applied for 1000 ms, and the initial 100 ms, during which displacement current flows, was excluded from the calculation of the average current. The waveform of the applied stepwise voltage and the measurement results before and after the endurance measurements are shown in Figure S5b and S5c, respectively. Figure S5d shows the data from Figure S5b and S5c replotted with the electric field on the horizontal axis and the leakage current on the vertical axis. At 2.77 MV cm−1, the leakage current density is approximately 2 × 10−3 A cm−2, and the leakage current values show almost no change before and after 1010 cycles voltage application. Similarly, leakage current measurements were also performed on the sample used in Figure 3e–h. For this sample, each voltage level was applied for 50 ms, and the initial 10 ms was excluded from the calculation of the average current. The waveform and the results before and after the endurance measurements are shown in Figure S5e and S5f, respectively. As can be seen from the figure, the leakage current of this sample was buried in noise, making it impossible to determine the exact value. The difference in noise levels between Figure S5b,c and Figure S5e,f is due to the difference in measurement ranges: the former has a range of 500 nA, whereas the latter has a range of 50 nA, resulting in different signal amplification factors. This noise is presumed to be due to the leakage current being below the measurement limit of the instrument, which is 1 nA. As supporting evidence for this assumption, Figure S5g shows the leakage current measurement results for a different cell on the same wafer as the sample used in Figure 3e–h. In the region where the applied voltage is low and the leakage current is small, the leakage current is buried in noise (0–5s, 15–20s); however, as the applied voltage increases and the leakage current exceeds 1 nA, it becomes detectable (8–13s). From these results, it is inferred that the leakage current of the sample in Figure S5e and S5f is below 10−5 A cm−2 when an electric field of 2.77 MV cm−1 is applied.

The leakage current value of 2 × 10−3 A cm−2 at 2.77 MV cm−1 for the sample in Figure S5b–d is slightly higher compared to previously reported HfO2-based ferroelectric materials.[4–7] In contrast, the leakage current value of below 10−5 A cm−2 at 2.77  MV cm−1 for the sample in Figure S5e and S5f is comparable to the leakage current values of other HfO2-based ferroelectrics.[4–7] It is known that the leakage current in HfO2 is influenced by currents flowing along grain boundaries.[8] Therefore, the difference in leakage current values between Figure S5b–d and S5e,f is presumed to arise from differences in grain boundary length and other factors caused by the annealing conditions. However, further investigation is required to clarify the details. The issues regarding the annealing conditions are also discussed in the following section.

Figure S5. Pulse scheme and leakage-current behavior of YNHO capacitors. a) Schematic of the measurement cycle: a series of 6 V, 100 kHz square-wave stress pulses (50 % duty) is applied, followed by P–E hysteresis and PUND measurements using a 6 V, 1 kHz triangular waveform; this cycle is repeated up to 109 or 1010 stress pulses. b) Applied stepwise voltage waveform (−5 V to +5 V in 0.5 V steps; 1000 ms per step, first 100 ms excluded) used to measure leakage current before endurance cycling for the sample in Figure 3a–d. c) Leakage-current measurement of the same device after 1010 cycles. d) Replot of (b) and (c) data as leakage-current density versus electric field. e) Applied stepwise voltage waveform (−5 V to +5 V in 0.5 V steps; 50 ms per step, first 10 ms excluded) used to measure leakage current before endurance cycling for the sample in Figure 3e–h. f) Leakage-current measurement of the same device after 109 cycles. g) Verification of leakage current in a different cell on the same wafer: in the low-voltage regions (0–5 s, 15–20 s), only noise is observed because the current is below the detection limit of 1 nA, whereas in the high-voltage region (8–13 s), the leakage current exceeds 1 nA and becomes detectable.

6. “Slanted hysteresis” and “Sheered hysteresis”

As described in the main text, the shapes of the P–E and PUND hysteresis curves indicate that polarization reversal does not occur abruptly near the coercive field (Ec), but instead progresses gradually after the polarity of the applied voltage is reversed, with the switching current continuing to flow. This type of hysteresis behavior, often referred to as “slanted hysteresis” or “sheared hysteresis,” is commonly observed when a ferroelectric material is connected in series with a dielectric layer or when a distribution of Ec exists.[9–11] In structures where ferroelectric and dielectric regions are arranged in series, a higher dielectric fraction leads to a more gradual polarization change in response to the applied voltage.

Comparing Figure 3c and 3g, the total polarization change (2Pᵣ) is 23 μC cm−2 in Figure 3c and 31 μC cm−2 in Figure 3g. This difference indicates that the hysteresis loop in Figure 3c is more slanted, suggesting a higher dielectric content. These results can be interpreted as evidence that longer annealing times promote crystallization of initially amorphous YNHO, increasing the fraction of the ferroelectric phase. This interpretation is also consistent with the observation that a longer annealing time results in a larger 2Pᵣ value. Similar to the discussion on leakage current in the previous section, it was found that the shape of the P–E hysteresis also changes depending on the annealing time. In the future, it will be necessary to advance studies to optimize the annealing conditions of YNHO according to the intended applications.

However, these findings do not exclude the possibility of a coercive field (Ec) distribution. Since YNHO is a material in which local inhomogeneity is intentionally introduced, an Eₑ distribution may exist. This issue remains to be clarified in future investigations.

Supporting Information References

1. S. Hofmann, Atomic mixing, surface roughness and information depth in high-resolution AES depth profiling of a GaAs/AlAs superlattice structure, Surf. Interface Anal. 1994, 21, 673–678. https://doi.org/10.1002/sia.740210912

2. W. Dai, Y. Shi, Effect of bias voltage on microstructure and properties of Tantalum Nitride coatings deposited by RF magnetron sputtering, Coatings 2021, 11, 911. https://doi.org/10.3390/coatings11080911

3. J.-C. Chang, J. Birch, G. K. Gueorguiev, B. Bakhit, G. Greczynski, F. Eriksson, P. Sandström, L. Hultman, C.-L. Hsiao, Domain epitaxial growth of Ta3N5 film on c-plane sapphire substrate, Surf. Coat. Technol. 2022, 443, 123581. https://doi.org/10.1016/j.surfcoat.2022.128581

4. H. Ryu, K. Xu, J. Kim, S. Kang, J. Guo, W. Zhu. Exploring new metal electrodes for ferroelectric aluminum-doped hafnium oxide, IEEE Trans. Electron Devices 2019, 66, 5, 2359–2364. https://doi.org/10.1109/TED.2019.2907070

5. T. Song, R. Bachelet, G. Saint-Girons, R. Solanas, I. Fina, F. Sánchez, Epitaxial Ferroelectric La-Doped Hf0.5Zr0.5O2 Thin Films, ACS Appl. Electron. Mater. 2020, 2, 10, 3221–3232. https://doi.org/10.1021/acsaelm.0c00560

6. H. A. Hsain, Y. Lee, M. Materano, T. Mittmann, A. Payne, T. Mikolajick, U. Schroeder, G. N. Parsons, J. L. Jones Many routes to ferroelectric HfO2: A review of current deposition methods, J. Vac. Sci. Technol. A 2022, 40, 010803. https://doi.org/10.1116/6.0001317

7. S. Kim, S.-H. Lee, I. H. Jo, T. J. Park, J. H. Kim, Reduced leakage current in atomic-layer-deposited HfO2 thin films deposited at low temperature by in-situ defect passivation, Appl. Surf. Sci. 2024, 645, 158790. https://doi.org/10.1016/j.apsusc.2023.158790

8. K. McKenna, A. Shluger, V. Iglesias, M. Porti, M. Nafría, M. Lanza, G. Bersuker, Grain boundary mediated leakage current in polycrystalline HfO2 films, Microelectron. Eng. 2011, 88, 1272–1275. https://doi.org/10.1016/j.mee.2011.03.024

9. U. Robels, J. H. Calderwood, G. Arlt, Shift and deformation of the hysteresis curve of ferroelectrics by defects: an electrostatic model, J. Appl. Phys. 1995, 77, 4002–4008. https://doi.org/10.1063/1.359511

10. A. K. Tagantsev, M. Landivar, E. Colla, N. Setter, Identification of passive layer in ferroelectric thin films from their switching parameters, J. Appl. Phys. 1995, 78, 2623–2630. https://doi.org/10.1063/1.360122

11. M. Mai, C. Zhu, G. Liu, X. Ma, Effect of dielectric layer on ferroelectric responses of P(VDF-TrFE) thin films, Phys. Lett. A 2018, 382, 2372–2375. https://doi.org/10.1016/j.physleta.2018.05.049