Table captain

Table 1: Calculated HOMO energy (EH), LUMO energy (EL), HOMO-LUMO energy gap (Eg), Fermi level energy (EF) and work function (ϕ), Electronegativity χ, Chemical potential μ,  Chemical softness S, Electrophilicity index ω, electron donating capability (ω-.), electron accepting capability (ω+) of Zr@V2O5.  All data are in eV.

Table-2: Some standard thermodynamical parameters of Zr@V2O5 in gas phase.

Table 3, QTAIM topological parameters for electron density ρ(r), Laplacian of electron density ∇2ρ(r), kinetic electron density G(r), potential electron density V(r), eigenvalues of Hessian matrix (λ), and bond ellipticity index (ε) at the BCPs (3,-1) of Zr@V2O5 in gas phase.

Table 4. Zones of inhibition (mm) values against the Salmonella typhi and Lactobacillus acidophilus for V2O5

Table 5. Zones of inhibition (mm) values against the Salmonella typhi and Lactobacillus acidophilus for Zr doped V2O5 nanoparticles

Table 1: Calculated HOMO energy (EH), LUMO energy (EL), HOMO-LUMO energy gap (Eg), Fermi level energy (EF) and work function (ϕ), Electronegativity χ, Chemical potential μ,     Chemical softness S, Electrophilicity index ω, electron donating capability (ω-.), electron accepting capability (ω+) of Zr@V2O5.  All data are in eV.

| Parameters | V2O5 | Zr@V2O5 |  |
| --- | --- | --- | --- |
| HOMO(eV) | -8.83 | -5.6 |  |
| LUMO(eV) | -6.19 | -3.2 |  |
| Ionization potential (IP) | 8.83 | 5.6 |  |
| Electron affinity (EA) | 6.19 | 3.2 |  |
| Energy gap Eg (eV) | 2.6 | 2.3 |  |
| Fermi level EF (eV) | -7.51 | -4.4 |  |
| Work function ϕ (eV) | 7.51 | 4.4 |  |
| Electronegativity χ | 7.51 | 4.4 |  |
| Chemical potential μ | -7.51 | -4.4 |  |
| Chemical hardness η | 1.32 | 1.2 |  |
| Chemical softness S | 0.38 | 0.4 |  |
| Electrophilicity index ω | 21.3 | 8.3 |  |
| electronic charge | 5.69 | 3.8 |  |
| electron donating capability (ω-.) | 25.3 | 10.7 |  |
| electron accepting capability (ω+) | 17.8 | 6.2 |  |

Table-2: Some standard thermo dynamical parameters of Zr@V2O5 in gas phase.

| Parameters | Zr@V2O5 |
| --- | --- |
| Thermal energy (kcal/mol) | 16.393 |
| Specific heat (CV) (cal/mol-K) | 29.449 |
| Entropy (S) (cal/mol-K) | 101.502 |
| ZPVE (kcal/mol) | 10.495 |
| Gibbs free energy (G) (kcal/mol) | -39.640 |

Table 3, QTAIM topological parameters for electron density ρ(r), Laplacian of electron density ∇2ρ(r), kinetic electron density G(r), potential electron density V(r), eigenvalues of Hessian matrix (λ), and bond ellipticity index (ε) at the BCPs (3,-1) of Zr@V2O5 in gas phase.

| System | Bond | ρ(r) | ∆2 ρ(r) | G (r) | V(r) | V(r) /G(r) | λ1 | λ2 | λ3 | ε | Ent (kJ/mol) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Zr@V2O5 | 2O…6O | 0.010 | 0.038 | 0.0078 | -0.0060 | 0.7692 | 0.049 | -0.003 | -0.007 | 0.146 | 7.9 |
|  | 3O…Zr | 0.009 | 0.020 | 0.0049 | -0.0047 | 0.9592 | 0.034 | -0.007 | -0.006 | 0.212 | 6.2 |

Table 4. Zones of inhibition (mm) values against the Salmonella typhi and Lactobacillus acidophilus for V2O5

| Compound | Organisms | Concentration(µg/mL) |  |  | (D) Antibiotic (1mg/ml) |
| --- | --- | --- | --- | --- | --- |
|  |  | 50 (A) | 75 (B) | 100 (C) |  |
| V2O5 | Salmonella typhi | 7 | 7 | 7 | 11 |
|  | Lactobacillus acidophilus | 6 | 7 | 8 | 21 |

Table 5. Zones of inhibition (mm) values against the Salmonella typhi and Lactobacillus acidophilus for Zr doped V2O5 nanoparticles

| Compound | Organisms | Concentration(µg/mL) |  |  | (D) Antibiotic (1mg/ml) |
| --- | --- | --- | --- | --- | --- |
|  |  | 50 (A) | 75 (B) | 100 (C) |  |
| Zr doped V2O5 | Salmonella typhi | 9 | 10 | 11 | 12 |
|  | Lactobacillus acidophilus | 8 | 10 | 11 | 21 |