Data-driven lithium-ion battery capacity estimation from voltage relaxation

Jiangong Zhu a, b, Yuan Huang a,b, Michael Knapp b *, Xinhua Liu c, Yixiu Wang a, d, R. Bhushan Gopaluni d, Yankai Cao d, Michael Heere b,e, Martin J. Mühlbauer b, Liuda Mereacre b , Haifeng Dai a *, Anatoliy Senyshyn e, Xuezhe Wei a, Helmut Ehrenberg b

a Clean Energy Automotive Engineering Center, School of Automotive Engineering, Tongji University, 201804 Shanghai, China

b Institute for Applied Materials (IAM), Karlsruhe Institute of Technology (KIT), 76344 Eggenstein-Leopoldshafen, Germany

c School of Transportation Science and Engineering, 100083, Beihang University, Beijing, China

d Department of Chemical and Biological Engineering, University of British Columbia, BC V6T 1Z3, Canada

e Heinz Maier-Leibnitz Zentrum (MLZ), Technische Universität München, Lichtenbergstr. 1, 85748 Garching b. München, Germany

Table S1 Specifications of NCA and NCM energy

| Sample name | NCA battery | NCM battery |
| --- | --- | --- |
| Battery type | 18650 |  |
| Anode material | Graphite/Si |  |
| Cathode material | Li0.86Ni0.86Co0.11Al0.03O2 (NCA) | Li0.84(Ni0.83Co0.11Mn0.07)O2 (NCM) |
| Electrolyte | Solution of lithium hexafluorophosphate (LiPF6) |  |
| Nominal voltage | 3.6 V |  |
| Cutoff voltage | 2.65 V - 4.2 V | 2.5 V - 4.2 V |
| Nominal capacity | 3.5 Ah |  |
| Battery mass | 45.0 g |  |

Table S2 Statistical features extracted from one voltage relaxation curve, xi is the battery terminal voltage, i=1,…,n, n is the number of samples in one relaxation curve

| Maxima (MAX) | xmax=maxxi |
| --- | --- |
| Mean (MEAN) | x=1ni=1nxi |
| Minima (MIN) | xmin=minxi |
| Variance (VAR) | μ2=1ni=1nxi-x2 |
| Skewness (SKE) | μ3=1ni=1nx-xμ23 |
| Excess Kurtosis (KUR) | μ4=1ni=1nx-xμ24-3 |

Table S3 Hyperparameters in ElasticNet, XGBoost, Support Vector Regression (SVR), and Deep Neural Network (DNN)

| ElasticNet |  | XGBoost |  | SVR |  | DNN |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| alphas | {0.001+(20-0.001)/19*i¦i=0..19} | learning_rate | 0.8 | kernels | [‘poly’, ‘rbf’, ‘linear’] | Layer type | Number of neurons | Activation function |
| l1_ratio | {0.001+(20-0.001)/19*i¦i=0..19} | N_estimators | 6 | epsilons | [0.01, 0.1, 1, 5, 10, 20] | Dense | 32 | ‘sigmoid’ |
| cv | 5 | Max_depth | 6 | Cs | [0.01, 0.1, 1, 5, 10, 20] | Dropout | 0.1 |  |
|  |  | Objective | reg:squarederror | gammas | [‘scale’, ‘auto’] | Dense | 32 | ‘sigmoid’ |
|  |  | Lambda | 1 | cv | 5 | Dropout | 0.1 |  |
|  |  | alpha | 0 |  |  | Dense | 16 | ‘sigmoid’ |
|  |  | subsample | 1 |  |  | Dropout | 0.1 |  |
|  |  |  |  |  |  | Dense | 16 | ‘sigmoid’ |
|  |  |  |  |  |  | Dropout | 0.1 |  |
|  |  |  |  |  |  | Dense | 8 | ‘sigmoid’ |
|  |  |  |  |  |  | Dropout | 0.1 |  |
|  |  |  |  |  |  | Dense | 1 | ‘softplus’ |

Table S4 Correlation matrix between extracted features

|  | VAR | SKE | MAX | MIN | MEAN | KUR |
| --- | --- | --- | --- | --- | --- | --- |
| VAR | 1 | -0.456 | -0.503 | -0.812 | -0.714 | -0.290 |
| SKE | -0.456 | 1 | 0.217 | 0.355 | 0.237 | 0.957 |
| MAX | -0.504 | 0.217 | 1 | 0.902 | 0.950 | 0.206 |
| MIN | -0.813 | 0.355 | 0.902 | 1 | 0.985 | 0.268 |
| MEAN | -0.714 | 0.238 | 0.950 | 0.985 | 1 | 0.177 |
| KUR | -0.290 | 0.957 | 0.206 | 0.268 | 0.177 | 1 |

Fig.S1 Test results of estimated capacity versus real capacity for ElasticNet and SVR models. NCA_test (a), NCM_test1 (b), and NCM_test2 (c) of ElasticNet method. NCA_test (d), NCM_test1 (e), and NCM_test2 (f) of SVR method.

Fig.S2 DNN method structure