Supplementary Materials

The following Supplementary Information accompanies the article “FTIR analysis of experimental adhesives: Investigating spectral reproducibility, chemometric approaches, and archaeological applications.” It provides additional data and figures that complement the main text. The Supplementary Information includes detailed file-naming conventions for FTIR spectra files available for download (Table S1); extended reference library comparisons (Figures S1-S7); examples of spectra from inclusions (Figure S8); and an expanded peak table for Group 1 with associated band assignments and interpretations (Table S2). Full spectral files are provided as downloadable CSV files in the ULiège Dataverse repository at https://doi.org/10.58119/ULG/BVGFPW.

1. Dateset file naming conventions

| Dataset | Convention | Example |
| --- | --- | --- |
| KBr/LN-MCT-B (Agilent): Exp. 91 Raw data | A (Agilent), Experiment #, sample #, point #, description, resolution (cm-1), analyst | a exp 91 01 point 1 reddish surface |
| KBr/LN-MCT-B (Agilent): Exp. 91 KKT data | A (Agilent), Experiment #, sample #, point #, description, resolution (cm-1), analyst, processing | a exp 91 01 point 1 reddish surface 2cm sm KKT |
| ZnSe/TE-MCT-A (Bruker): Exp. 91 Raw data | B (Bruker), Experiment #, sample #, point #, description, resolution (cm-1), analyst | b exp 91 03 point 1 yellow surface 2cm ll |
| ZnSe/TE-MCT-A (Bruker): Exp. 91 KKT data | B (Bruker), Experiment #, sample #, point #, description, resolution (cm-1), analyst, processing | b exp 91 03 point 1 yellow surface 2cm ll KKT |
| Validation set: Exp. 121 Raw data | Experiment #, sample #, point #, description, resolution (cm-1), analyst | exp 121 214 point 1 light yellow spot 2cm ll |
| Validation set: Exp. 121 KKT data | Experiment #, sample #, point #, description, resolution (cm-1), analyst | exp 121 214 point 1 light yellow spot 2cm ll KKT |
| Orientation test: Exp. 91 Raw data | Experiment #, sample #, point #, description, orientation #, resolution (cm-1), analyst | exp 91 11 point 1 vegetal fiber orientation 1 2cm ll |
| Orientation test: Exp 91 KKT data | Experiment #, sample #, point #, description, orientation #, resolution (cm-1), analyst, processing | exp 91 11 point 1 vegetal fiber orientation 1 2cm ll KKT |

Table S1. Table describing the naming conventions used for the files within the datasets generated for this project. Data files can be found in the ULiège Dataverse respository at https://doi.org/10.58119/ULG/BVGFPW.

Reference library comparisons

Figure S1. Comparison of sample 91-04 to pure beeswax (PK62200) from the INFRA-ART spectral library. PK62200 was collected in transmission mode, presenting a higher resolution than 91-04, but providing a highly consistent match between the two.

Figure S2. Comparison of sample 91-05 to Arabic gum, also known as Acacia gum, (PK63300) from the INFRA-ART spectral library. PK63300 was recorded in transmission mode, presenting a higher resolution than 91-05, but providing a strong match between the two. The interference of the flint substrate can also be observed due to the thin and translucent nature of the sample.

Figure S3. Comparison of sample 91-23 to modern tree resin (Pistacia lentiscus) from the Kimmel library. There are minor similarities present but significant differences, suggesting this is a tree resin of a different species as well as a likely admixture.

Figure S4. Comparison of sample 91-29 to a modern tree resin (Pistacia lenstiscus) in the Kimmel spectral library. There are some shared similarities, but this match is not strong, suggesting that this is a tree resin of a different species as well as a possible admixture.

Figure S5. Comparison of sample 91-29 to colophony (also known as rosin), a resin derived from pine trees and other coniferous plants, in the INFRA-ART spectral library sourced from Kremer Pigments. There are some shared similarities, but this match is not strong suggesting that sample 91-29 corresponds with a tree resin of a different species, as well as a possible admixture.

Figure S6. Comparison of sample 91-32 to rosin (Kaplan Art Craft Dark, no. 7), also known as colophony, which is a resin derived from pine trees and other coniferous plants, in the University of Minnesota Archaeological Materials Infrared Spectra Library. There are strong similarities suggesting a likely match.

Figure S7. Comparison of sample 91-14 to pure beeswax (PK62200) in the INFRA-ART spectral library. There are significant peak matches between the two, though overlapping signals suggest 91-14 is a possible admixture.

Figure S8. Example spectra from inclusions in samples 91-01 (top), 91-11 (middle) and 91-11 (bottom) collected with the KBr/LN-MCT-B instrument, illustrating the high noise levels and irregular features observed compared to the rest of the dataset.

Expanded Peak Table

| Group 1 |  |  |  |
| --- | --- | --- | --- |
| Wavenumber (cm⁻¹) – KBr/LN-MCT-B | Wavenumber (cm⁻¹) – ZnSe/TE-MCT-A | Assignment | Notes |
| - | 3380 | O–H (±N–H) stretch | Broad phenolic/alcoholic O–H; moisture/adsorbed water may contribute |
| 2980 | 2945 | CH₃ asym. stretch. | Aliphatic methyl groups in terpenoid resin acids |
| 2920 | 2920 | CH₂ asym. stretch | Aliphatic chain backbone |
| 2890 | 2870 | CH stretch, aromatic overlap | Methyl groups in aromatic-substituted resins; weak aromatic effect |
| 2855 | 2855 | CH₂ sym. stretch | Long-chain aliphatic CH₂ moieties; wax/resin components |
| 1867 | - | Overtone / combination band | Weak; possibly combination/overtone from oxidation or resin aging |
| 1843 | - | Overtone / combination band | Similar as above; likely minor overtone contributions |
| 1791 | - | Overtone / combination band | Very weak; perhaps ester carbonyl overtone or conjugated carbonyl stretch from oxidation |
| 1733 | 1733 | C=O stretch | Ester / carboxylic acid carbonyl; strong carbonyl fingerprint |
| - | 1726 | C=O stretch | Weak shoulder; indicative of mixed carbonyl species |
| 1715 | 1715 | C=O stretch | Carboxylic acid carbonyl; diagnostic in resin aging |
| 1695 | 1695 | C=O stretch | Possibly carbonyls in conjugated or hydrogen-bonded contexts |
| 1683 | 1684 | ν(C–O–C) / conjugated ester | Weak ester or ether link; possible conjugation |
| 1669 | 1669 | O–H-associated / H-bonded carbonyl shift. | Weak; shift indicates hydrogen bonding or macromolecular structure |
| 1662 | 1662 | δ(CH₂) / exocyclic -C=C-H bending. | Weak; possible unsaturation or exocyclic double bond |
| 1652 | 1655 | C=C stretch / weak amide I overlap | Could also reflect proteins (if present) or unsaturated terpenoid double bonds |
| 1646 | 1648 | C=C stretch / H-bonded O–H | Very weak; likely conjugated double bonds or H-bonded carbonyl interactions |
| 1635 | 1636 | C=C / possibly aromatic / H-O-H bending overlap | Very weak; water bending component possible where residue is thin |
| 1606 | 1604 | Aromatic C=C stretch | Phenolic ring vibrations; key aromatic signature |
| - | 1590 | Aromatic C=C shoulder | Weak; substitution or partial conjugation effects |
| - | 1580 | Aromatic C=C shoulder | Very weak; aromatic substitution effects |
| 1575 | 1572 | Aromatic/skeletal | Very weak aromatic skeletal vibration |
| 1568 | 1568 | Aromatic/skeletal | Very weak aromatic skeletal vibration |
| 1539 | 1535 | Aromatic/skeletal | Very weak aromatic skeletal vibration |
| 1516 | 1517 | C=C (phenolic/aromatic) | Diagnostic phenolic band for conifer resins |
| 1506 | 1504 | Aromatic/phenolic | Minor phenolic contribution |
| 1496 | 1493 | Aromatic/phenolic | Weak aromatic band; substitution-dependent |
| 1488 | 1482 | Aromatic/phenolic (shoulder) | Shoulder in phenolic region; low intensity |
| 1471 | 1471 | CH₂ scissoring / ring deformation | Weak shoulder; aliphatic framework and/or ring deformation |
| 1464 | 1464 | CH₂ scissoring | Aliphatic hydrocarbons (resin/wax) |
| 1456 | 1453 | CH₂ deformation (±CH₃ bend overlap) | Chain deformation; can overlap CH₃ bending |
| 1435 | 1435 | CH₂/CH₃ bending | Aliphatic hydrocarbon; waxy component indicator |
| 1418 | 1420 | CH₂ bending | Weak shoulder reflecting local chain environment |
| 1386 | 1383 | CH₃ bending | Methyl deformation; branching in terpenoids/waxes |
| 1338 | 1332 | Skeletal / C–H wag | Very weak skeletal vibration of aliphatic/aromatic systems |
| 1327 | 1322 | Skeletal / C–H wag | Very weak; minor skeletal mode |
| 1273 | 1276 | C–O stretch | Strong acidic C–O; oxidized terpenoid resin acids |
| 1238 | 1238 | C–O stretch | Medium C–O in esters/acids |
| 1208 | 1211 | C–O | Weak C–O from resin-derived linkages |
| 1169 | 1169 | C–O–C / C–C | Terpenoid esters/resin-acid region |
| 1126 | 1124 | C–O–C / C–C | Esters/terpenoid backbone vibrations typical of conifer resins |
| 1035 | 1035 | Si–O stretch; ± carbohydrate C–O | Strong band; can include substrate silicate plus residue C–O |
| 982 | 982 | C–H deformation / ring or lattice mode | Weak; low-frequency deformation; possible phosphate/carbohydrate overtones |
| 967 | 962 | C–H deformation / ring or lattice mode | Weak minor deformation |
| - | 870 | Aromatic OOP bend. | Weak; substituted aromatic ring OOP bending |
| 854 | 850 | Aromatic OOP | Very weak |
| 833 | 834 | N–O stretch (alt: silicate overtone) | Weak; possible nitrate contamination; silicate overtone also possible |
| - | 825 | Aromatic OOP / weak overtone | Very weak overtone/combination in ring region |
| 822 | 820 | Aromatic OOP / skeletal | Weak aromatic OOP or skeletal vibration |
| - | 804 | Aromatic/Si–O related (very weak) | Very weak ring or silicate-related feature |
| - | 790 | Aromatic/Si–O related (very weak) | Very weak ring or silicate-related feature |
| 776 | 776 | Si–O bend | Silicate/clay band; substrate influence when residues are thin or caused by admixtures |
| 745 | 742 | CH₂ rocking / ring deformation | Very weak, long-chain CH₂ rocking and/or aromatic ring deformation |
| 718 | - | CH₂ rocking | Long-chain aliphatic rocking (waxes/resins) |
| 679 | - | SO₄²⁻ ν₄ bending (gypsum/bassanite from ochre/sand contaminants) | Sulfate bending typical of hydrated Ca-sulfates, present in ochre or sand fillers |
| 667 | - | SO₄²⁻ ν₄ bending (gypsum) | Distinct ν₄ at 664–669 cm⁻¹, matches ochre/sand mineral traces |
| 647 | - | SO₄²⁻ ν₄ broad band / Fe-O | Broadened sulfate from clay or sand; possible hematite/goethite |
| 632 | - | OH libration (apatite) or sulfate overprint | 630–632 cm⁻¹ classic for hydroxyapatite OH libration, but more likely sulfate |
| 616 | - | SO₄²⁻ ν₄ | Ochre-derived sulfates |
| 599 | - | SO₄²⁻ ν₄ or PO₄³⁻ ν₄ | Could be gypsum or clay/apatite phosphate |
| 590 | - | Fe–O stretch (hematite/goethite in ochre) | Hematite bands |
| 580 | - | Fe–O stretch | Hematite/goethite range |
| 575 | - | PO₄³⁻ ν₄ bending | Possible apatite/soil phosphate |
| 566 | - | PO₄³⁻ ν₄ bending lower component | Possible apatitic phosphate |
| 558 | - | PO₄³⁻ ν₄ or Fe–O | Low-side PO₄ shoulder; Fe-oxide possible |
| 545 | - | Fe–O (hematite/goethite) | Iron oxide in ochre |
| 535 | - | Fe–O or clay lattice | Silicate/iron lattice bands from clay additives |

Table S2. Expanded peak table for Group 1 with associated molecular band assignments. This table lists all shared peaks detected within the defined group; additional peaks may be present within individual samples. Weak peaks may arise from instrument artifacts or substrate contributions. “OOP” indicates out-of-plane vibrations. Full peak lists for all other groups, including minor peaks and shoulders, are provided as CSV spectra files at [link]. Only major peaks are summarized in the main manuscript for clarity. Molecular band assignments draw on a wide range of published FTIR reference data (e.g. Edwards 1996; Edwards and Falk 1997; Socrates 2001; Schiegl and Conard 2006; Vahur et al. 2011; Cinta-Pinzaru et al. 2012; Bruni and Guglielmi 2014; Chukanov 2014; Helwig et al. 2014; Duce et al. 2015; Beltran et al. 2016; Monnier et al. 2017; Martin-Ramos et al. 2018; Shaw 2022; Schmidt and Koch 2024).

References

Beltran, V., Salvado, N., Buti, S., Pradell, T. (2016). Ageing of resin from Pinus species assessed by infrared spectroscopy. Anal. Bioanal. Chem., 408, 4073-4082. DOI 10.1007/s00216-016-9496-x

Bruni, S., and Guglielmi, V. (2014). Identification of archaeological triterpenic resins by the non-separative techniques FTIR and 13C NMR: The case of Pistacia resin (mastic) in comparison with frankincense. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 121, 613-622. http://dx.doi.org/10.1016/j.saa.2013.10.098

Chukanov, N. V. (2014). Infrared Spectra of Mineral Species: Extended Library. Springer Science+Business Media, Dordrecht.

Cinta-Pinzaru, S., Pop, D., and Nemeth, L. (2012). FT-Raman and FT-Infrared investigations of archaeological artefacts from Foeni Neolithic site (Banat, Romania). Studia Universitatis Babes-Bolyai, Geologia, 53 (1), 31-37.

Duce, C., Orsini, S., Spepi, A, Colombini, M.P., Rine, M.R., Ribechini, E. (2015). Thermal degradation chemistry of archaeological pine pitch containing beeswax as an additive. Journal of Analytical and Applied Pyrolysis, 111, 254-264.  http://dx.doi.org/10.1016/j.jaap.2014.10.020

Edwards, H.G.M., and Falk, M.J. (1997). Fourier Transform Raman Spectroscopic study of ancient resins: a feasibility study of application to archaeological artefacts. Journal of Raman Spectroscopy, 28, 211-218.

Edwards, H.G.M., et al. (1996). Farwell, DW., and Daffner, L. 1996. Fourier-transform Raman spectroscopic study of natural waxes and resins

Helwig, K., Monahan, V., Poulin, J., Andrews, T.D. (2014). Ancient projectile weapons from ice patches in northwestern Canada: Identification of resin and compound resin-ochre hafting adhesives. Journal of Archaeological Science, 41, 655-665. http://dx.doi.org/10.1016/j.jas.2013.09.010

Martin-Ramos, P., Fernandez-Coppel, I.A., Ruiz-Potosme, N.M., and Martin-Gil, J. (2018). Potential of ATR-FTIR spectroscopy for the classification of natural resins. Biology, Medicine, Engineering and Science Reports, 4(1): 03-06. DOI : 10.5530/bems.4.1.2

Monnier, G., Frahm, E., Luo, B., Missal, K. (2017a). Developing FTIR microspectroscopy for analysis of plant residues on stone tools. Journal of Archaeological Science, 78, 158-178. http://dx.doi.org/10.1016/j.jas.2016.12.004

Schiegl, S. and Conard, N.J. (2006). The Middle Stone Age sediments at Sibudu: results from FTIR spectroscopy and microscopic analyses. Southern African Humanities, 18 (1): 149-172.

Schmidt, P., and Koch, T.J. (2024). The molecular composition of birch tar and its infrared spectrum. Archaeological and Anthropological Sciences, 16:193. https://doi.org/10.1007/s12520-024-02102-5

Shaw, C.L. (2022). An evaluation of the infrared 630 cm-1 OH libration band in bone mineral as evidence of fire in the archaeological record. Journal of Archaeological Science: Reports, 46, 103655. https://doi.org/10.1016/j.jasrep.2022.103655

Socrates, G. (2001). Infrared and Raman Characteristic Group Frequencies: Tables and Charts. West Sussex: Wiley.

Vahur, S., Kriiska, A., Leito, I. (2011). Investigation of the adhesive residue on the flint insert and the adhesive lump found from the Pulli early Mesolithic settlement site (Estonia) by Micro-ATR-FT-IR spectroscopy. Estonian Journal of Archaeology, 15, 1, 3-17. https:// doi:10.3176/arch.2011.1.01