Supporting Information

Optimizing a Dynamic Infrared Emitter by Tailoring Titanium Carbide MXene Surface Chemistry

Neda Daliran a, c, Ali Reza Oveisi b*, Zhiming Wang a, c*

a Institute of Fundamental and Frontier Sciences University of Electronic Science and Technology of China, Chengdu 611731, P. R. China

b Department of Organic Chemistry, Faculty of Chemistry, Lorestan University, Khorramabad, 68151-44316, Iran

c Shimmer Center, Tianfu Jiangxi Laboratory, Chengdu 641419, China

Email Addresses: zhmwang@uestc.edu.cn & oveisi.a@lu.ac.ir

In figures S1 and S2, the emissivity plot of the VO2-tungstan (W) composite /SiO2/Ti3C2Tx MXene thermal emitter for two different VO2-W and SiO2 thicknesses across the temperature range of 298-332 K is provided.

Figure S1: Average emissivity of the thermal emitter VO2-W/SiO2/Ti3C2Tx with different surface terminations for two different VO2-W thicknesses. (a): VO2-W/SiO2/Ti3C2, (b): VO2-W/SiO2/Ti3C2F2, (c):  VO2-W/SiO2/Ti3C2O2, (d) VO2-W/SiO2/Ti3C2(OH)2.

Figure S2: Average emissivity of the thermal emitter VO2-W/SiO2/Ti3C2Tx with different surface terminations for two different SiO2 thicknesses. (a): VO2-W/SiO2/Ti3C2, (b): VO2-W/SiO2/Ti3C2F2, (c):  VO2-W/SiO2/Ti3C2O2, (d) VO2-W/SiO2/Ti3C2(OH)2.

Table S1. Thermal properties of the involved materials in the structure.

| Materials | Thermal Conductivity (W/m. K) | density(Kg/m3) | Specific Heat Capacity (J/kg. K) |
| --- | --- | --- | --- |
| Ti3C2Tx MXene | Ref. 1 | 4210 2 | Ref. 3 |
| SiO2 | 29 | 3990 | 765 |
| VO2 | Ref. 4 | Ref. 5 | Ref. 6 |
| Tungsten | 175 | 19250 | 132.51 |
| Glass | 1.22 | 2380 | 700 |

References

1	Wang, M., Liu, Y., Zhang, H., Wu, Y. & Pan, L. Thermal conductivities of Ti3C2Tx MXenes and their interfacial thermal performance in MXene/epoxy composites – a molecular dynamics simulation. International Journal of Heat and Mass Transfer 194, 123027, (2022).

2	https://www.americanelements.com/titanium-carbide-ti3c2tx-12363-89-2.

3	Srivatsa, S. et al. Temperature Evolution of Composition, Thermal, Electrical and Magnetic Properties of Ti3C2Tx-MXene. Materials 17, 2199 (2024).

4	Hamaoui, G. et al. Thermophysical characterisation of VO2 thin films hysteresis and its application in thermal rectification. Scientific Reports 9, 8728, (2019).

5	Lu, Y., Chen, L. l. & Liu, Z. w. in IOP Conference Series: Materials Science and Engineering.  012130 (IOP Publishing).

6	Popuri, S. et al. Structurally Restricted Phase Transitions in VO2(B) and Their Impact on Transport Properties. The Journal of Physical Chemistry C 119, 25085-25092, doi:10.1021/acs.jpcc.5b07826 (2015).