Supporting Materials

# Novel Conditioner for Efficient Dewaterability and Modification of Oily Sludge with High Water Content

Biming Liua,*, Yue Tengb,*, Wenbin Songa, Haixia Wuc

a School of Environmental Sciences and Engineering, Nanjing Tech University, Nanjing 211800, China

b College of Civil Engineering, Nanjing Tech University, Nanjing 211800, China

c College of Urban Construction, Nanjing Tech University, Nanjing 211800, China

Correspondence to: Biming Liu (E-mail: bimingliu@tsinghua.edu.cn), Yue Teng (E-mail: sunadnmoon19960203@163.com)

# Table S1. Industrial analysis of OS.

| Industrial analysis | OS/(%) |
| --- | --- |
| Mad | 79.30 |
| Aad | 8.74 |
| Vad | 10.39 |
| FCad | 1.57 |

# Table S2. The form and relative content of C in OS and OSAD.

| Samples | Peak | Binding energy /eV | Full width at half maxima (FWHM)/eV | Area | Percentage /% |
| --- | --- | --- | --- | --- | --- |
| OS | sp2-C | 284.73 | 0.98 | 95173.54 | 72.36 |
|  | C-O | 285.04 | 1.53 | 34733.01 | 26.41 |
|  | C=O | 286.68 | 1.91 | 1612.47 | 1.23 |
| OSAD | sp2-C | 284.77 | 0.99 | 75156.52 | 70.65 |
|  | C-O | 285.10 | 1.56 | 29295.32 | 27.54 |
|  | C=O | 287.11 | 2.50 | 1928.64 | 1.82 |

# Table S3. The form and relative content of O in OS and OSAD.

| Samples | Peak | Binding energy /eV | Full width at half maxima (FWHM) /eV | Area | Percentage/% |
| --- | --- | --- | --- | --- | --- |
| OS | Quinone | 532.15 | 1.21 | 12839.29 | 68.68 |
|  | Phenolic -OH and ether C-O-C | 532.35 | 2.43 | 5856.37 | 31.32 |
| OSAD | Quinone | 531.79 | 2.04 | 7818.71 | 57.63 |
|  | Phenolic -OH and ether C-O-C | 532.14 | 1.56 | 5749.32 | 42.37 |

# Table S4. The form and relative content of S element in OS and OSAD.

| Samples | Peak | Binding energy /eV | Full width at half maxima (FWHM)/eV | Area | Percentage /% |
| --- | --- | --- | --- | --- | --- |
| OS | Sulfate Sulfur | 170.70 | 1.25 | 52.27 | 3.14 |
|  | Sulfonate (sulfone) | 169.16 | 2.01 | 361.79 | 21.77 |
|  | Sulfide (sulfoxide) | 167.36 | 2.18 | 96.00 | 5.78 |
|  | Aromatic sulfur (thiophene) | 164.69 | 1.68 | 421.40 | 25.36 |
|  | Aliphatic Sulfur | 163.72 | 1.00 | 449.15 | 27.03 |
|  | Mercaptan | 162.87 | 0.96 | 281.24 | 16.92 |
| OSAD | Sulfate Sulfur | 169.89 | 1.47 | 236.92 | 15.21 |
|  | Sulfonate (sulfone) | 168.99 | 1.17 | 247.72 | 15.91 |
|  | Sulfide (sulfoxide) | 167.86 | 1.52 | 151.04 | 9.70 |
|  | Aromatic sulfur (thiophene) | 164.68 | 1.69 | 249.59 | 16.03 |
|  | Aliphatic Sulfur | 163.78 | 1.08 | 367.69 | 23.61 |
|  | Mercaptan | 162.88 | 1.16 | 304.36 | 19.54 |

# Table S5. Atomic ratio (at.%) of OS, OSAD at optimum dosage of conditioner.

| Samples | C (at.%) | O (at.%) | N (at.%) | S (at.%) | Cl (at.%) |
| --- | --- | --- | --- | --- | --- |
| OS | 94.74 | 4.51 | 0.28 | 0.44 | 0.03 |
| OSAD | 94.71 | 3.89 | 0.79 | 0.60 | 0.01 |