Supporting Information for

Control of the macroscopic shape of assemblies formed from microparticles based on host–guest interaction

Takahiro Itami1, Akihito Hashidzume1*, Yuri Kamon1, Hiroyasu Yamaguchi1, and Akira Harada2*

1Graduate School of Science, Osaka University, 1-1 Machikaneyama-cho, Toyonaka, Osaka 560-0043, Japan

2The Institute of Scientific and Industrial Research, Osaka University, 8-1 Mihogaoka, Ibaraki, Osaka 567-0047, Japan

*Corresponding author.

E-mail address: hashidzume@chem.sci.osaka-u.ac.jp (AHashidzume), harada@chem.sci.osaka-u.ac.jp (AHarada).

Table S1 | Results of the interaction of βCD(x)-SAP with Ad(y)-SAP microparticlesa.

|  | y / mol% |  |  |  |
| --- | --- | --- | --- | --- |
| x / mol% | 5.2 | 7.1 | 10.7 | 15.1 |
| 16.2 | – | – | – | – |
| 22.3 | – | – | – | – |
| 26.7 | + | + | + | + |

a. “+” and “–” denote assembly formation and no assembly formation, respectively.

| (a) |  |
| --- | --- |
| (b) |  |

Figure S1 | 1H FGMAS NMR spectra for βCD-NH2, Ad-NH2•HCl, unmodified SAP, βCD(x)-SAP, and Ad(y)-SAP.

| (a) |  |
| --- | --- |
| (b) |  |

Figure S2 | ATR FT/IR spectra for βCD-NH2, Ad-NH2•HCl, unmodified SAP, βCD(x)-SAP, and Ad(y)-SAP.

Figure S3 | A typical example of optical micrograms for βCD(26.7)-SAP (a) and Ad(15.1)-SAP microparticles (b).

Figure S4 | Examples for colloidal aggregates constructed using a Tunable Diffusion Limited Aggregation software46,47.  Df = 1.75 (a, c, e, and g) and 2.05 (b, d, f, and h) formed from 15 (a and b), 30 (c and d), 100 (e and f), and 200 particles (g and h).