Supplementary Material

Supplementary Fig.1. Comparison between the total lenses produced and the resulting ophthalmic waste in 2023.

Supplementary Fig.2. Particle size distribution of lens-grinding waste before and after undergoing ultrasound treatment obtained using laser diffraction. Each curve represents a different measurement for the specified condition.

Supplementary Table 1. Particle size distribution parameters (span and characteristic diameters) of lens-grinding waste, determined by laser diffraction using the Fraunhofer approximation. Values represent the average of multiple measurements.

|  | # D[3,2]µm | # D[4,3]µm | # d[0.9]µm | # d[0.5]µm | # d[0.1]µm | # span |
| --- | --- | --- | --- | --- | --- | --- |
| # Lens-grinding waste | # 9.14 (±0.48) | # 70.52 (±7.94) | # 153.03 (±20.65) | # 33.38 (±3.16) | # 4.02 (±0.33) | # 4.45 # (±0.18) |
| # Lens-grinding waste after submitting to ultrasounds | # 7.119 (±0.008) | # 53.260 (±0.897) | # 118.286 (±0.953) | # 23.530 (±0.121) | # 2.730 (±0.008) | # 4.911 (±0.018) |

Supplementary Table 2. Quantification of heavy metals in ophthalmic waste by atomic absorption spectroscopy.

| # Sample | # mg Cu/g | # mg Cd/g | # mg Cr/g | # mg Pb/g |
| --- | --- | --- | --- | --- |
| # Ophthalmic waste | # 0.0069 | # ≤0.0001 | # 0.0063 | # 0.0116 |

Supplementary Table 3. Elemental analysis by EDS of ophthalmic residues of edging lenses.

| Element | Normalized Content (wt. %) | Error (wt. %) |
| --- | --- | --- |
| Carbon | 59.17 | 16.27 |
| Nitrogen | 9.13 | 4.53 |
| Oxygen | 11.66 | 4.26 |
| Silicon | 0.36 | 0.12 |
| Sulfur | 19.68 | 1.49 |

Supplementary Fig. 3. Differential scanning calorimetry characterisation of lens-grinding waste.

Supplementary Fig. 4. TGA characterisation of lens-grinding waste.

Supplementary Fig. 5. FTIR characterisation of lens waste.

Supplementary Fig. 6. GC-MS chromatogram of the ophthalmic lens wastewater obtained in the final stage of 187 eyeglass lens grinding.

Supplementary Table 4. Compounds identified by GC-MS in ophthalmic wastewater.

| # Retention time | # Name of Compound | # MW in g/mol | # Formula | # % Similarity |
| --- | --- | --- | --- | --- |
| # 4.252 | # Formyl pyruvyl urea | # 158.11 | # C5H6N2O4 | # 64 |
| # 5.340 | # 4-methyl-2-pentanol | # 102.17 | # C6H14O | # 59 |
| # 7.471 | # 2,4-dimethyl-3-hexene | # 112.21 | # C8H16 | # 43 |
| # 8.365 | # Trans-2-pentenal | # 84.12 | # C5H8O | # 64 |
| # 8.657 | # Diisoamyl ether | # 158.28 | # C10H22O | # 64 |
| # 9.087 | # 1-Methyl-2-propylcyclohexane | # 140.27 | # C10H20 | # 80 |
| # 9.222 | # 3,3,4-trimethyl-hexane | # 128.25 | # C9H20 | # 53 |
| # 9.379 | # 3-ethyl-3-heptanol | # 144.25 | # C9H20O | # 38 |
| # 22.176 | # Heptadecyl pentafluoropropionate | # 402.49 | # C20H35F5O2 | # 76 |
| # 22.447 | # 2-(methoxymethyl)-1,1,3,3-tetramethyl-1,3-disilacyclohexane | # 216.47 | # C10H23OSi2 | # 72 |
| # 22.782 | # Sulfurous acid, butyl octadecyl ester | # 390.7 | # C22H46O3S | # 83 |
| # 22.887 | # Nonahexacontanoic acid | # 999.83 | # C69H138O2 | # 76 |
| # 22.960 | # Nonahexacontanoic acid | # 999.83 | # C69H138O2 | # 64 |
| # 24.057 | # HAHNFETT # Phytol acetate | # --- # 338.57 | # --- # C69H138O2 | # 81 # 72 |
| # 24.358 | # Heptadecyl heptafluorobutyrate | # 452.5 | # C21H35F7O2 | # 76 |

Supplementary Fig. 7. GS-MS chromatogram represents the analysis of the solid ophthalmic waste in the final stage of 187 eyeglass lens grinding.

Supplementary Table 5. Compounds identified by GC-MS in solid ophthalmic waste.

| # Retention time | # Name of Compound | # MW in g/mol | # Formula | # % Similarity |
| --- | --- | --- | --- | --- |
| # 5.349 | # 2-Hexanol | # 102.17 | # C6H14O | # 59 |
| # 7.761 | # Styrene | # 104.15 | # C8H8 | # 95 |
| # 8.368 | # 3,4-Dihydropyran | # 84.12 | # C5H8O | # 59 |
| # 9.088 | # Sulfurous acid, cyclohexylmethyl pentadecyl ester | # 388.60 | # C22H44O3S | # 64 |
| # 15.880 | # Octanoic acid-tert bytyl ester | # 200.32 | # C12H24O2 | # 37 |
| # 17.512 | # meso-2,3-Diisobutyl-2,3-dimethylsuccinic acid dinitrile | # --- | # --- | # 72 |
| # 17.570 | # 2,6-di-t-butyl-4-methylene-2,5-cyclohexadiene-1-one | # 218.33 | # C15H22O | # 99 |
| # 17.664 | # meso-2,3-Diisobutyl-2,3-dimethylsuccinic acid dinitrile | # 219.37 | # C13H24N2 | # 72 |
| # 17.957 | # 2,6-bis(1,1-dimethylethyl)-4-methyl-phenol | # 220.35 | # C16H24O | # 97 |
| # 19.651 | # 2H-Imidazole-2-thione, 1,3-dihydro-1-methyl- | # 114.17 | # C4H6N2S | # 50 |
| # 19.783 | # 6,6-Dimethylcycloocta-2,4-dienone | # 150.22 | # C10H14O | # 43 |
| # 21.301 | # 2,4-diphenyl-4-methyl-1-pentene | # 236.35 | # C17H18 | # 96 |
| # 21.436 | # Cis-para-methane | # 140.27 | # C10H20 | # 30 |
| # 21.655 | # Diallyl terephthalate | # 260.29 | # C14H14O4 | # 74 |
| # 21.725 | # 2,4-Diphenyl-4-methyl-2(E)-pentene | # 236.35 | # C18H20 | # 97 |
| # 21.984 | # N-(Anilinocarbothioyl)valine | # --- | # --- | # 46 |
| # 22.111 | # 2-(2H-benzotriazol-2-yl)-4-(1,1,3,3-tetramethylbutyl)phenol (ultraviolet absorvent UV-329) | # 323.43 | # C20H25N3O | # 86 |
| # 22.438 | # 1,1,2,2-tetramethyl-1,2-digermacyclopentane | # 247.50 | # C7H18Ge2 | # 56 |
| # 22.954 | # Dibutyl phthalate | # 278.34 | # C16H22O4 | # 93 |
| # 24.056 | # 11,13-Dimethyl-12-tetradecen-1-ol acetate # 9-Decen-1-ol, trifluoroacetate | # 282.46 # 252.27 | # C18H34O2 # C12H19F3O2 | # 74 # 68 |
| # 24.662 | # 3-(2,5-Dimethyl-1H-pyrrole-3-yl)-1,3-dihydro-indol-2-one | # --- | # --- | # 90 |
| # 25.968 | # Bisphenol A | # 228.29 | # C15H16O2 | # 98 |

E

D

C

B

A

Supplementary Fig. 8. 1H DOSY NMR of ophthalmic wastewater obtained in the final stage of 187 eyeglass lens grinding.

Supplementary Table 6. The measurement of ophthalmic wastewater was done at 25ºC in deuterated chloroform. a 1H DOSY NMR experiment. b Hydrodynamic radius calculated via the Stokes-Einstein equation D = kBT/6πƞrH (kB, Boltzmann constant; T, absolute temperature; ƞ, viscosity of CDCl3 at 298 K); * Molecular weights above 1000 g/mol suggest aggregation in solution.

| Compound | Diffusion coefficient (10-10 m2/s) a | Hydrodynamic radius (nm)b | Molecular weight (g/mol) |
| --- | --- | --- | --- |
| A | 8.8 | 1.58 × 10-9 | 173 |
| B | 9.1 | 7.94 × 10-10 | 413 |
| C | 9.17 | 6.76 × 10-10 | 944 |
| D | 9.7 | 1.99 × 10-10 | 18296* |
| E | 10.01 | 9.77 × 10-11 | 129031* |

Supplementary Fig. 9. 19F NMR of ophthalmic wastewater obtained in the final stage of 187 eyeglass lens grinding.

Supplementary Fig. 10. 1H DOSY NMR of solid ophthalmic waste obtained in the final stage of 187 eyeglass lens grinding.

Supplementary Table 7. The measurement of solid ophthalmic waste was done at 25ºC in deuterated chloroform. a 1H DOSY NMR experiment. b Hydrodynamic radius calculated via the Stokes-Einstein equation D = kBT/6πƞrH (kB, Boltzmann constant; T, absolute temperature; ƞ, viscosity of CDCl3 at 298 K); * Molecular weights above 1000 g/mol suggest aggregation in solution.

| # Compound | # Diffusion coefficient (10-10 m2/s) a | # Hydrodynamic radius (nm) b | # Molecular weight (g/mol) |
| --- | --- | --- | --- |
| # F | # 8.8 | # 1.58 × 10-9 | # 246 |
| # G | # 9.06 | # 8.71 × 10-10 | # 550 |
| # H | # 9.13 | # 7.41 × 10-10 | # 773 |
| # I | # 9.8 | # 1.58 × 10-10 | # 33991* |
| # J | # 9.9 | # 1.26 × 10-10 | # 64703* |

J

I

H

G

F

Supplementary Fig. 11. 19F NMR of solid ophthalmic waste obtained in the final stage of 187 eyeglass lens grinding.

A

B

Supplementary Fig. 12. Optic industry wastewater supernatant obtained in the final stage of eyeglass lens grinding (A) and solids from ophthalmic spectacle lens wastewater (B).