Supplementary Information

Polar nematic state in an iron-based superconductor LaFeAsO1-xHx

Sachiko Maki1, Jun-ichi Yamaura1,*, Soshi Iimura1, Hitoshi Abe2,3,4, Hajime Sagayama2, Reiji Kumai2, Youichi Murakami1,2, Satoru Matsuichi1, Hideo Hosono1

1Materials Research Center for Element Strategy, Tokyo Institute of Technology, Yokohama, Kanagawa 226-8503, Japan

2Institute of Materials Structure Science, High Energy Accelerator Research Organization (KEK), Tsukuba, Ibaraki 305-0801, Japan

3Department of Materials Structure Science, School of High Energy Accelerator Science, SOKENDAI, Tsukuba, Ibaraki 305-0801, Japan

4Graduate School of Science and Technology, Ibaraki University, Mito, Ibaraki 310-8512, Japan

Contents

Page	Title

2	Character of XRD profile in the polar structure

3	Fourier-filtered EXAFS oscillations and amplitudes

3−4	Beat and difference profile of Fourier-filtered EXAFS amplitudes

Character of XRD profile in the polar structure

The crystal structure of PP2 was determined to be the polar structure by XRD measurement in the literature18. We summarise the essential point for detecting the loss of inversion symmetry. The 220T reflection in the tetragonal phase with non-polar space group P4/mmm splits into two reflections in the orthorhombic phase. Figure S1 shows the powder XRD profiles (solid lines) and their deconvolutions (dashed lines) estimated by using pseudo-Voigt functions for x = 0 and 0.51 in the orthorhombic phases. For x = 0 the 400O and 040O reflections (blue dashed lines) have the equivalent structure factor with the non-polar structure (space group Cmme), where the slight difference of their intensities comes from the angle-dependent Lorentz-polarization factor. In contrast, for x = 0.51 the 040O and 004O reflections (magenta dashed lines) have the inequivalent structure factor with the polar structure (space group Aem2). The formation of polar axis along the c-axis raises the imaginary part component in the structure factor only for the 004O reflection. As a result, the intensity of 004O reflection is lower than that of 040O reflection, as shown in Fig. S1b (see the detail in Supplementary Information of Ref. [18]).

Fig. S1 XRD profiles split from the 220T reflection for x = 0 (PP1) and x = 0.51 (PP2). The observed profiles and their deconvolutions are represented by the respective solid and dashed lines for x = 0 (a) and 0.51 (b). The tetragonal c-axis is transformed into the orthorhombic a-axis only for x = 0.51.

Fourier-filtered EXAFS oscillations and amplitudes

Fig. S2 Fourier-filtered EXAFS oscillations and amplitudes at 30, 30, 17, 17 K for x = 0.51, 0.45, 0.42, 0.37, respectively. The blue solid and black solid lines show the lowest temperature and 250 K data, respectively.

Beat and difference profile of Fourier-filtered EXAFS amplitudes

EXAFS is expressed as the following formula:

χq=jNjFj(q)exp⁡(-2q2σj2)qrj2sin⁡(2qrj+∅j(q)), 		(1)

where Nj, Fj(q), σj2, rj, and j(q) are the coordination number, the scattering amplitude, the mean square displacement, the bond distance, and the phase shift, respectively. In the high temperature region, the uniform As−Fe distance gives Nj = 4 and rj = RHT, thus, eq. (1) equals

χq=4F(q)exp⁡(-2q2σHT2)qRRT2sin⁡(2qRHT+∅(q)).			(2)

In the low temperature region, the As−Fe distance splits in two with rj ≈ RHT + ΔR/2, RHT−ΔR/2, thus, eq. (1) approximates

χq≈2Fqexp-2q2σLT2qRHT2sin2qRHT+q∆R+∅q+sin2qRHT-q∆R+∅q      =4Fqexp-2q2σLT2qRHT2sin2qRHT+∅qcosq∆R,		(3)

where rj2 is approximated by RHT2 with RHT >> ΔR (RHT = 2.439 Å, ΔR ≈ 0.07 Å). The oscillation involves the beat with the condition of qΔR = π/2.

Here, we analyse EXAFS amplitude with the beat and introduce a phenomenological formula χdif(q) = k2χ(q)(T)−s0k2χ(s1q)(250 K), which is estimated by subtracting the amplitude at 250 K from the objective amplitude with the scale factors of s0 and s1. The former and latter factors correct the temperature variations of the mean square displacement and the bond distance, respectively. The difference amplitudes χdif(q) for x = 0.51, 0.45, 0.42, and 0.37 are shown in Fig. S3. We evaluate the kink position qbeat as the peaks in the wavenumber derivatives of χdif(q). The qbeat values at lowest temperature are qbeat ~ 11.2, 11.0, 11.6, and 11.3 Å-1 for x = 0.51, 0.45, 0.42, and 0.37, respectively.

Fig. S3 Difference profiles of Fourier-filtered EXAFS amplitudes. The beats at the lowest temperatures are located at qbeat ~ 11.2, 11.0, 11.6, and 11.3 Å-1, indicated by the arrows, for x = 0.51, 0.45, 0.42, and 0.37, respectively.