Supplementary Material

This table provides detailed analytical results for all microplastic particles identified in sediment samples collected from Regions A, B, and C of Tripoli Port. Each entry includes the sample code and observed particle color, the polymer type identified through Fourier Transform Infrared (FTIR) spectroscopy, the spectral match percentage with reference polymer standards, and the reference library used for identification. The dataset captures the full diversity of polymer compositions, colors, and match confidence levels, enabling precise source attribution and material characterization. While the main text summarizes polymer and color distributions at an aggregate level, this table offers a complete record of the underlying data for transparency, reproducibility, and future comparative studies.

Supplementary Table. FTIR analysis data of microplastic samples from Tripoli Port beach sediments

| Sample Code & Color | Identified Polymer Type | Match % | Reference Library Used |
| --- | --- | --- | --- |
| A1 Blue | Polyethylene (PE) | 85.85 | HR Nicolet Sampler Library |
| A1 White | Polyethylene (PE) | 86.96 | HR Nicolet Sampler Library |
| A2 White | Polypropylene (PP), Atactic | 62.55 | Hummel Polymer Sample Library |
| A3 Sky | Polypropylene (PP), Atactic | 68.49 | Hummel Polymer Sample Library |
| A3 White | Polyethylene (PE) | 91.52 | HR Nicolet Sampler Library |
| A4 Blue | Polyethylene (PE), Low Density | 76.14 | Aldrich Condensed Phase Sample Library |
| A5 White 1 | Polyethylene (PE) | 85.69 | HR Nicolet Sampler Library |
| A5 White 2 | Polyethylene (PE) | 91.76 | HR Nicolet Sampler Library |
| A6 Blue | Polypropylene (PP), Atactic | 69.25 | Hummel Polymer Sample Library |
| A6 Green | Polypropylene (PP), Atactic | 77.80 | Hummel Polymer Sample Library |
| A7 White | Polyethylene (PE) | 91.47 | HR Nicolet Sampler Library |
| A8 Blue | Polyethylene (PE), Low Density | 76.10 | Aldrich Condensed Phase Sample Library |
| A8 White | Polypropylene (PP), Atactic | 76.32 | Hummel Polymer Sample Library |
| A9 Red | Styrene–Butadiene Block Polymer | 72.37 | HR Nicolet Sampler Library |
| A10 White | Polystyrene (PS), Atactic | 66.89 | Hummel Polymer Sample Library |
| B1 Blue | Poly (Ethylene:Propylene:Diene) | 42.64 | Hummel Polymer Sample Library |
| B2 Yellow | Polypropylene (PP), Atactic | 54.94 | Hummel Polymer Sample Library |
| B3 White | Polyethylene (PE) | 89.88 | HR Nicolet Sampler Library |
| B3 Green | Polystyrene (PS), Atactic | 68.39 | Hummel Polymer Sample Library |
| B4 Blue | Polyethylene (PE) | 84.68 | HR Nicolet Sampler Library |
| B5 Blue | Polyethylene (PE), Low Density | 74.90 | Aldrich Condensed Phase Sample Library |
| B6 White | Polystyrene (PS), Atactic | 67.73 | Hummel Polymer Sample Library |
| B7 Violet | Polyethylene (PE) | 90.37 | HR Nicolet Sampler Library |
| B8 Blue | Polypropylene (PP), Atactic | 48.87 | Hummel Polymer Sample Library |
| B9 White 1 | Polypropylene (PP), Atactic | 53.77 | Hummel Polymer Sample Library |
| B9 Blue | Polyethylene (PE) | 86.45 | HR Nicolet Sampler Library |
| B9 White 2 | Polyethylene (PE) | 86.45 | HR Nicolet Sampler Library |
| B10 White | Polypropylene (PP), Atactic | 80.28 | Hummel Polymer Sample Library |
| B10 Green | Polystyrene (PS), Atactic | 68.34 | Hummel Polymer Sample Library |
| C1 Green | Polypropylene (PP), Atactic | 66.01 | Hummel Polymer Sample Library |
| C2 Blue | Poly (Ethylene:Propylene:Diene) | 65.94 | Hummel Polymer Sample Library |
| C2 Red | Styrene–Butadiene Block Polymer | 72.79 | HR Nicolet Sampler Library |
| C2 White | Polypropylene (PP), Atactic | 69.25 | Hummel Polymer Sample Library |
| C3 White Filmy | Polyethylene (PE) | 88.69 | HR Nicolet Sampler Library |
| C3 White | Polyethylene (PE) | 86.83 | HR Nicolet Sampler Library |
| C4 White | Polystyrene (PS), Atactic | 74.32 | Hummel Polymer Sample Library |
| C5 Blue | Polyethylene (PE) | 86.13 | HR Nicolet Sampler Library |
| C5 Green | PP + Poly (Ethylene:Propylene) | 65.46 | HR Nicolet Sampler Library |
| C6 White | Polyethylene (PE) | 85.20 | HR Nicolet Sampler Library |
| C7 White | Polypropylene (PP), Atactic | 74.86 | Hummel Polymer Sample Library |
| C8 Black | Cellophane | 35.02 | Hummel Polymer Sample Library |
| C8 Blue | Polyethylene (PE) | 87.09 | HR Nicolet Sampler Library |
| C9 Blue | Polystyrene (PS), Atactic | 63.61 | Hummel Polymer Sample Library |
| C10 Green | Polyvinyl Chloride (PVC) | 68.11 | Hummel Polymer Sample Library |

Supplementary Figure. Image form lab

The supplementary material provides the complete dataset and supporting evidence underlying the findings presented in this study. Detailed Fourier Transform Infrared (FTIR) spectroscopy results for all microplastic particles collected from Regions A, B, and C of Tripoli Port are included. Each entry records the sample code, observed particle color, polymer type identified, spectral match percentage, and the reference library used for verification.

Additionally, supplementary figures show the raw FTIR spectra obtained for individual samples across all regions, providing visual confirmation of spectral matches with reference polymers. These figures illustrate the diversity of polymer compositions identified, ranging from dominant polymers such as polyethylene (PE), polypropylene (PP), and polystyrene (PS) to less common materials like polyvinyl chloride (PVC), cellophane, and styrene–butadiene block polymers.

Together, these supplementary tables and figures serve as a permanent record of the analytical process, enabling future researchers to perform comparative assessments and meta-analyses. They also enhance the credibility of the results by documenting the full diversity of polymer types and spectral characteristics encountered in the study area